Fig. 1S The upper part shows the XRPD monitoring (every 9 min. from the bottom to the top) of the solvent depletion of the network of 1 after treatment with amyl acetate. The lower part reports the corresponding variation of the cells parameters with time, obtained by Rietveld analysis of the profiles. The decrease of c  is accompained by an increase of a,  as expected since the two axes are constrained through the relationship  2|a|2 + |c|2 = 4Lr2 , with Lr (the rhombic edge) almost constant and equal to 2 × (Cu…Cu), ca. 22.1 Å.

Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002