Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

2-D soft ferromagnet based on [WV(CN)8]3- and CuII with TC of 34 K

Robert Podgajny, Tomasz Korzeniak,  Maria Bałanda,  Tadeusz Wasiutyński, William Errington, Terence J.Kemp, Nathaniel W.Alcock and Barbara Sieklucka*

Supplementary material

Contents

- Figure S1. Structure of [Cu(tetren)]2+ cation in 1.

- Figure S2. Atom numbering scheme of (NC)7W-CN-Cu(NC)4 structural motif of 2: W1-C1 = 2.165(7), W1-C2 = 2.178(9), W1-C3 = 2.146(9), W1-C4 = 2.177(11) , W1-C5 = 2.138(8), C1-N1 = 1.160(11), C2-N2 = 1.121(11), C3-N3 = 1.141(12), C4-N4 = 1.125(17), C5-N5 = 1.159(12), Cu1-N1 = 2.115(7), Cu1-N2B = 1.992(8), Cu1-N3B = 1.971(8) Å; W-C-N = 176-178.5, Cu1-N1-C1 = 174(2), Cu1-N2B-C2B = 169.3(7), Cu1-N3B-C3B = 169.4(8)o. Symmetry transformation used to generate equivalent atoms: B –x+1/2, -y+1/2, z+1/2.

- Table S1. IR spectra of {(tetrenH5)0.8CuII4[WV(CN)8]47.2H2O}n (1), tetren·5HCl (2), [Cu(tetren)](ClO4)2 (3) and tetren (4).

- Figure S3. IR spectra of {(tetrenH5)0.8CuII4[WV(CN)8]47.2H2O}n (1), tetren·5HCl (2), [Cu(tetren)](ClO4)2 (3), and tetren (4) in 400-1800 cm-1 range.

- Figure S4. IR spectra of {(tetrenH5)0.8CuII4[WV(CN)8]47.2H2O}n (1), tetren·5HCl (2), [Cu(tetren)](ClO4)2 (3), and tetren (4) in 1800-4000 cm-1 range.

Figure S1. Structure of [Cu(tetren)]2+ cation in 1.

Figure S2. Atom numbering scheme of (NC)7W-CN-Cu(NC)4 structural motif of 2: W1-C1 = 2.165(7), W1-C2 = 2.178(9), W1-C3 = 2.146(9), W1-C4 = 2.177(11) , W1-C5 = 2.138(8), C1-N1 = 1.160(11), C2-N2 = 1.121(11), C3-N3 = 1.141(12), C4-N4 = 1.125(17), C5-N5 = 1.159(12), Cu1-N1 = 2.115(7), Cu1-N2B = 1.992(8), Cu1-N3B = 1.971(8) Å; W-C-N = 176-178.5, Cu1-N1-C1 = 174(2), Cu1-N2B-C2B = 169.3(7), Cu1-N3B-C3B = 169.4(8)o. Symmetry transformation used to generate equivalent atoms: B –x+1/2, -y+1/2, z+1/2.

Table. S1. IR spectra of {(tetrenH5)0.8CuII4[WV(CN)8]47.2H2O}n (1)*,  tetren·5HCl (2)*, [Cu(tetren)](ClO4)2 (3)* and tetren (4)**(in cm-1)

| *in KBr pellet; **in film; Bruker IFS 47. {(tetrenH5)0.8CuII4 WV(CN)8]42H2O}n | tetren·5HCl | [Cu(tetren)](ClO4)2 | tetren | # Interpretation | # Reference |
| --- | --- | --- | --- | --- | --- |
| 3620s(sh,br) |  |  |  |  (O–H) isolated | 1 |
| 3437s(br) | 3431s | 3425s(sh) | 3356s |  (N–H) secondary | 1,2,3 |
|  | 3218s(sh), 144s(sh) | 3349s, 3281s, 3142m | 3281s |  (N–H) primary | 1,2,3 |
| 3023m, 2848m | 2986–2822vs(br) | 2954s, 2892 | 2935vs, 2816vs(sh) |  (C–H) | 1 |
| 2732m(br) | 2691–2383vs(br) |  |  |  (N+–H) | 1 |
| 2204s, 2164m, 2148m(sh) |  |  |  |  (CN) bridging  (CN) terminal | 4 5 |
| 1618s | 1611s,1601s, 1535s | 1628s(sh), 1584s | 1599s |  (N–H) | 1,3 |
| 1501w, 1452m | 1493s, 1479s | 1469s | 1461s |  (CH2) in plane | 1,3 |
| 1344w, 1237w, 983m | 1357s, 1335m, 1291s, 1100w, 1059s, 998m, 969s | 1391w, 1362w, 1313w, 1281w | 1348m, 1304m, 1128s, 1070m, 1015m | (C–N), (C–C) skeletal stretching,  (C–H) | 1,3 |
|  |  | 1096vs(br), 1017w, 990m |  | (Cl–O) | 3 |
| 812m, 793m | 817s | 881w, 849m, 820w | 908s, 846s, 777s (br) |  (N–H) out of plane | 1 |
|  |  | 625vs |  |  (Cl–O) | 3 |
| 498s |  |  |  |  (W–C) | 5 |
|  |  | 583m, 549m, 529m, 456m |  |  (Cu–N) | 2 |

- M. Szafran (ed.), Spectroscopic methods in determination of the structure of organic compounds. Tables and exercises. (in polish), Warszawa PWN 1988.

- Z. Lu, C. Duan, Y. Tian, Z. Wu, Y. You, Z. Zhou, T. Mak,  Polyhedron 1997, 16, 909.

- R. Parker, L. Spiccia, B. Moubaraki, K. Murray, B. Skelton, A. White, Inorg. Chim. Acta 2000, 300, 922.

- This work.

- W. P. Griffith, J. Chem. Soc., Dalton Trans. 1975, 2489.

Fig. S3. IR spectra of {(tetrenH5)0.8CuII4[WV(CN)8]47.2H2O}n (1), tetren·5HCl (2), [Cu(tetren)](ClO4)2 (3), and tetren (4) in 400-1800 cm-1 range.

Fig. S4. IR spectra of {(tetrenH5)0.8CuII4[WV(CN)8]47.2H2O}n (1), tetren·5HCl (2), [Cu(tetren)](ClO4)2 (3), and tetren (4) in 1800-4000 cm-1 range.