Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

| Potential Parameters |  |  |  |
| --- | --- | --- | --- |
| Ion | Charges (e) |  | Core-shell interaction (eVÅ-2) |
|  | Core | Shell |  |
| F | +1.380 | -2.380 | 101.200000 |
| Oxygen of carbonate group (O) | +0.587 | -1.632 | 507.400000 |
| Oxygen of water (Ow) | +1.250 | -2.050 | 209.449602 |
| Ca | +2.000 |  |  |
| Carbon of carbonate group (C) | +1.135 |  |  |
| Hydrogen of water (Hw) | +0.400 |  |  |
| Doubly-bonded oxygen of methanoic acid (OD) | -0.380 |  |  |
| Hydroxy oxygen of methanoic acid (OH) | -0.380 |  |  |
| Carbon of methanoic acid (CD) | +0.310 |  |  |
| Hydroxy hydrogen of methanoic acid (HO) | +0.350 |  |  |
| Hydrogen attached to carbon of methaonoic acid (HC) | +0.100 |  |  |
|  | Buckingham Potential |  |  |
| Ion pair | A (eV) |  (Å) | C (eVÅ6) |
| Ca – O | 1550.0 | 0.29700 | 0.0 |
| Ca – F | 1272.8 | 0.2997 | 0.0 |
| Ca – Ow | 1186.6 | 0.29700 | 0.0 |
| Hw – O | 396.3 | 0.23000 | 0.0 |
| Hw – Ow | 396.3 | 0.25000 | 10.0 |
| O – O | 16372.0 | 0.21300 | 3.47 |
| F – F | 99731833.99084 | 0.12013 | 17.02423 |
| O – Ow | 12533.6 | 0.21300 | 12.09 |
| Ca – OH | 563.64 | 0.29700 | 0.0 |
| F – Ow | 79785220.99 | 0.12013 | 26.78752 |
| F – Hw | 715.339 | 0.2500 | 10.00 |
| Ca – OD | 563.64 | 0.29700 | 0.0 |
| OH – O | 37898119 | 0.12013 | 11.309 |
| OD – O | 37898119 | 0.12013 | 11.309 |
| OH – F | 37898119 | 0.12013 | 25.1 |
| OD – F | 37898119 | 0.12013 | 25.1 |
| Ow –OH | 4797.6 | 0.213 | 30.2 |
| Ow – OD | 4797.6 | 0.213 | 30.2 |
| Ow – HO | 396.3 | 0.25 | 0.0 |
| Ow – HC | 396.3 | 0.25 | 0.0 |
| Ow – CD | 895 | 0.26 | 0.0 |
|  | Lennard-Jones Potential |  |  |
|  | A (eVÅ12) |  | B (eVÅ6) |
| Ow – Ow | 39344.98 |  | 42.15 |
| HC – O | 2915.25 |  | 4.222 |
| HO – O | 2915.25 |  | 4.222 |
| CD – O | 3315.91 |  | 19.846 |
| OD – Hw | 1908.1 |  | 5.55 |
| OH – Hw | 1908.1 |  | 5.55 |
| HC – F | 2915.25 |  | 9.3784 |
| HO – F | 2915.25 |  | 9.3784 |
| CD – F | 3315.91 |  | 44.012 |
|  | Morse Potential |  |  |
|  | D (eV) |  (Å-1) | r0 (Å) |
| C – O | 4.710000 | 3.80000 | 1.18000 |
| Hw – Ow | 6.203713 | 2.22003 | 0.92376 |
| CD – HC | 4.66 | 1.77 | 1.10 |
| OH – HO | 4.08 | 2.28 | 0.96 |
| CD – OH | 4.29 | 2.00 | 1.37 |
| CD – OD | 6.22 | 2.06 | 1.23 |
|  | Three-body Potential |  |  |
|  | k (eV rad-2) |  |  |
| Ocore – C – Ocore | 1.69000 |  | 120.000000 |
| H – Owshell – H | 4.19978 |  | 108.693195 |
| OH – HO – CD | 4.29 |  | 112.000000 |
| CD – HC – OH | 4.72 |  | 110.000000 |
| CD – OD – HC | 4.72 |  | 120.000000 |
| CD – OD – OH | 12.45 |  | 123.000000 |
|  | Four-body Potential |  |  |
|  | k (eV rad-2) |  |  |
| C – Ocore – Ocore – Ocore | 0.11290 |  | 180.0 |
|  | Intermolecular Coulombic interaction (%) |  |  |
| Hw – Ow | 50 |  |  |
| Hw – Hw | 50 |  |  |