Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

Delayed lanthanide luminescence sensing of aromatic carboxylates using heptadentate tri-amide Tb(III) cyclen complexes: the recognition of salicylic acid  in water

Thorfinnur Gunnlaugsson,*a Andrew J. Harte,a Joseph P. Leonard,a and Mark Nieuwenhuyzenb

a Department of Chemistry, Trinity College Dublin , Dublin 2, Ireland. Fax: 00 353 1 671 2826; Tel: 00 353 1 608 3459; E-mail: gunnlaut@tcd.ie

b School of Chemistry, Queen’s University of Belfast, Belfast BT9 5AG, Northern Ireland. Fax: 00 44 2890 665297; Tel: 00 44 2890 274242; E-mail: woody.m@qub.ac.uk

# Supplementary information

## Synthesis of Tb.1, Tb.2, Eu.1 and Eu.2

General synthesis of 2-(4,10-Bis-methylcarbamoylmethyl-1,4,7,10tetraaza-cyclododec-1-yl)-N-methyl-acetamide Ln(III) [Ln.1]

88.2mg, (0.23mmol) of 2-(4,7-Bis-methylcarbamoylmethyl-1,4,7,10 tetraaza-cyclododec-1-yl)-N-methyl-acetamide and 0.26mmol of Ln (III) Triflouromethane sulphonate was added to a 25ml single necked RBF which contained 10ml of freshly dried acetonitrile. The solution was freeze thawed three times, placed under an argon atmosphere and left stirring at 82C for 24 hrs.  The resulting solution was cooled to room temperature and then dropped slowly onto 100ml of dry Diethyl ether. The diethyl ether was poured off to leave of 2-(4,10-Bis-methylcarbamoylmethyl-1,4,7,10tetraaza-cyclododec-1-yl)-N-methyl-acetamide Ln(III) Yields > 95% achieved in all complexes. Characterisation shows that all complexes contain triflate counter anions and at least two water molecules.

2-(4,10-Bis-methylcarbamoylmethyl-1, 4,7,10tetraaza-cyclododec-1-yl)-N-methyl-acetamide Tb (III) [Tb.1]

Calculated for C20H35N7O12F9S3Tb.(H20)2(CH2Cl2)2: C, 22.07; H, 3.62; N, 8.19, Found: C, 21.61; H, 3.59; N, 7.85; Calculated for C19H36N7O9F6S2Tb:[MH+ peak] m/z = 843.1174, found: 843.1171; Calculated for C18H36N7O6F3STb:[MH+ peak] m/z = 694.1653, found: 694.1674; H(MeOD, 400 MHz) 121.87, 107.11, 78.35, 71.89, 68.58, 39.94, 14.52, 7.75, 6.28, 4.26, 1.96, 1.78, 1.49, 1.07, - 7.21  ;    F (MeOD, 376 MHz) – 85.54; Mass Spec (MeCN, ES+) m/z Expected :544.4, Found: 272.3 (M+H/2), 843.1(M[Triflate]2+H), 694.16 (M[Triflate]+H) ; IR max(cm-1)  3435, 3137, 2960, 2924, 1637, 1420, 1259, 1169, 1087, 1030, 994, 974, 798, 639, 574, 519.

2-(4,10-Bis-methylcarbamoylmethyl-1, 4,7,10tetraaza-cyclododec-1-yl)-N-methyl-acetamide Eu (III) [Eu.1]

Calculated for C20H35N7O12F9S3Eu.(H20)2(CH2Cl2)2: C, 22.19; H, 3.64 ; N, 8.24 , Found: C, 22.29; H, 3.74; N, 8.38; Calculated for C17H36N7O3Eu:[MH+ peak] m/z = 539.2092, found: 539.2087; Calculated for C18H36N7O6F3SEu:[MH+ peak] m/z = 688.1612, found: 688.1548; Calculated for C19H36N7O9F6S2Eu:[MH+ peak] m/z = 837.1133, found: 837.1181;  H(MeOD, 400 MHz) 27.04, 14.96, 11.44, 5.20, 3.68, 2.76, 2.41, 1.55, -0.09, -1.84, -4.93, -7.35, -10.77, - 12.31, -16.66 ;    F(MeOD, 376 MHz) – 80.45; Mass Spec (MeCN, ES+) m/z Expected :539.2, Found: 539.2(M+H), 668.1 (M[Triflate] +H), 837.1 (M[Triflate]2+H); IR max(cm-1)   3455, 3386, 3297, 3143, 3000, 2933, 2885, 1639, 1587, 1465, 1419, 1288, 1245, 1160, 1091, 1027, 725, 638, 576, 516.

General synthesis of 2-(4,10-Bis-dimethylcarbamoylmethyl-1,4,7,10tetraaza-cyclododec-1-yl)-N,N-dimethyl-acetamide Ln(III) [Ln.2]

94.7mg, (0.22mmol) of 2-(4,10-Bis-dimethylcarbamoylmethyl-1,4,7,10tetraaza-cyclododec-1-yl)-N,N-dimethyl-acetamide and 0.25mmol of Ln (III) Triflouromethane sulphonate was added to a 25ml single necked RBF which contained 10ml of freshly dried acetonitrile. The solution was freeze thawed three times, placed under an argon atmosphere and left stirring at 82C for 24 hrs.  The resulting solution was cooled to room temperature and then dropped slowly onto 100ml of dry Diethyl ether. The diethyl ether was poured off to leave of 2-(4,10-Bis-dimethylcarbamoylmethyl-1,4,7,10 tetraaza-cyclododec-1-yl)-N,N-dimethyl-acetamide Ln(III) as an oil . Yields > 95% achieved in all complexes. Characterisation shows that all complexes contain triflate counter anions and at least two water molecules.

2-(4,10-Bis-dimethylcarbamoylmethyl-1,4,7,10tetraaza-cyclododec-1-yl)-N,N-dimethyl-acetamide Tb(III) [Tb.2]

Calculated for C23H41N7O12F9S3Tb.(H20)2(CHCl3)2: C, 22.95; H, 3.62; N, 7.49, Found: C, 22.23; H, 3.71; N, 7.36; Calculated for C22H42N7O6F3STb:[MH+ peak] m/z = 736.2123, found: 736.2148; H(CD3OCD3, 400 MHz)  ;  39.92, 32.70, 9.00, 3.95, 3.02, 1.02  F (CD3OCD3, 376 MHz) – 78.74; Mass Spec (MeCN, ES+) m/z Expected : 586.5, Found: 884.15 (M[Triflate]2+H), 736.21  (M[Triflate]+H) ; IR max(cm-1)  3434, 2957, 2927, 2856, 1625, 1508, 1465, 1438, 1412, 1279, 1256, 1171, 1084, 1171, 1084, 1030, 960, 824, 761, 640, 574, 518.

2-(4,10-Bis-dimethylcarbamoylmethyl-1,4,7,10tetraaza-cyclododec-1-yl)-N,N-dimethyl-acetamide Eu(III) [Eu.2]

Calculated for C23H41N7O12F9S3Eu.(H20)2(CHCl3)2: C, 23.07; H, 3.64; N, 7.53, Found: C, 22.67; H, 3.74; N, 7.55; Calculated for C21H42N7O6F3SEu:[MH+ peak] m/z = 730.2082, found: 730.2045 ; H(CD3OCD3, 400 MHz)  13.91, 3.24, 2.60, 2.06, 1.30, 0.89, 0.01, -1.32, -4.95, -8.95, -12.87, -17.65;    F (CD3OCD3, 376 MHz) – 78.74; Mass Spec (MeCN, ES+) m/z Expected :579.56, Found: 878.15 (M[Triflate]2+H), 730.20  (M[Triflate]+H) ; IR max(cm-1)  3434, 2982, 2927, 2884, 1625, 1508, 1459, 1438, 1413, 1280, 1258, 1173, 1084, 1031, 960, 824, 762,  641, 573, 518.

Figure S1. The changes in the Tb(III) emission upon addition of salicylic acid. Inserted is the changes in –log[6] as a function of Tb(III) emission at 549 nm.

[6] = dsfsaff.45mM 0.4mM

[6] = 0M

Table S1. Tb(III) excited state lifetimes and q values for Tb.1 and Tb.2

| Complex | t (ms) & k | t (ms) & k |
| --- | --- | --- |
| Tb.1 | No Ligand | Ligand (3) |
| H2O | 869.065 s, 1.151 | 1626.118s, 0.615 |
| D2O | 1386.333 s, 0.721 | 1895.347s, 0.527 |
| Tb.2 | No Ligand | Ligand (3) |
| H2O | 720.137 s, 1.389 | 1593.083s, 0.628 |
| D2O | 1080.445 s, 0.926 | 1795.929s, 0.557 |

Determination of q Values:

[q 0.5] :  qTb(III) = 5 [(1/H2O-1/D2O) – 0.06]

| Complex | q | q |
| --- | --- | --- |
| Tb.1 | No Ligand | Ligand (3) |
|  | 1.85 | 0.14 |
| Tb.2 | No Ligand | Ligand (3) |
|  | 2.015 | 0.06 |