Supplementary information:

## Experimental details

Table 1 Summary of Crystal and Structure Refinement Data for 2

Table 2 Atomic coordinates (  104) and equivalent isotropic displacement parameters (Å2  103) for 2.

Figure. S1 ORTEP view with non-H atomic numbering scheme for 2. Ellipsoids are at the 30% probability level. Selected bond lengths [Å] and angles [].

Figure S2 The side view of 1-D cation chain for 2.

Figure S3 Temperature dependence of the molar magnetic susceptibility of 2. The solid line represents the best fit by Baker equation in high temperature range.

Experimental details:

Synthesis of [FBzPy]2[Ni(mnt)2] (1).

This compound was prepared by the direct combination of 1:2:2 mol equiv of NiCl2.6H2O, Na2mnt and [FBzPy]Cl in H2O. A red precipitate given was filtered off, washed by water and dried under vacuum. Yield: 92% (Found: C, 53.45; H, 3.08; N, 11.68. Calc. for C32H22F2N6NiS4: C, 53.72; H, 3.10; N, 11.75%.). IR spectra data (cm-1): (CN) 2193.4vs, (C=C) of mnt2- 1483.7vs.

Synthesis of [FBzPy][Ni(mnt)2] (2).

A MeCN solution (10 cm3) of I2 (150 mg, 0.59 mmol) was slowly added to a MeCN solution (20cm3) of [FBzPy]2[Ni(mnt)2] (715 mg, 1.0 mmol), and stirred for 15 min. MeOH (90 cm3) was then added, and the mixture allowed to stand overnight. The microcrystals formed were filtered off, washed with MeOH and dried in vacuum. Yield: 84%. (Found: C, 45.79; H, 2.11; N, 13.35. Calc. for C20H11FN5NiS4: C, 45.56; H, 2.10; N, 13.28%). IR(cm-1): (CN) 2202.3vs, (C=C) of mnt2- 1454.1m. Good shaped single crystals suitable for X-ray analysis were obtained by dispersing Et2O into MeCN solution of 2 about a week.

Table1 Summary of Crystal and Structure Refinement Data for 2

| Empirical formula Empirical formula | C20H11FN5NiS4 |
| --- | --- |
| Fw | 527.29 |
| Temp/K | 293(2) |
| Wavelength/Å | 0.71073 |
| Space group | P21/c |
| a / Å | 12.1500(4) |
| b / Å | 25.9523(6) |
| c / Å | 7.3397(3) |
|  /  | 101.74 |
| V / Å3 | 2265.95(13) |
| ## Z | 4 |
| Density (calc)/ Mg/m3 | 1.546 |
| Abs coeff. / mm-1 | 1.251 |
| F(000) | 1068 |
|  range for data collection | 1.57 to 25.05 |
| Index ranges | -14  h  12, -19  k  30, -8  l  8 |
| Reflns collected | 7854 |
| Independent reflns | 4013 [Rint = 0.0436] |
| Refinement method on F2 | Full-matrix least-squares |
| Data / restraints / params | 4013 / 0 / 281 |
| Goodness-of-fit on F2 | 1.046 |
| Final R indices [I>2(I)] | R1 = 0.0619, wR2 = 0.1535 |
| R indices (all data) | R1 = 0.0994, wR2 = 0.1804 |
| Extinction coefficient | 0.0021(5) |
| Largest diff peak and hole, e Å-3 | 0.879 and -0.659 |

Table 2.  Atomic coordinates (  104) and equivalent isotropic displacement parameters (Å2  103) for 2. U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

Atom	x	y	z	U(eq)

Ni(1)	2721(1)	2789(1)	5234(1)	56(1)

S(2)	3848(1)	2156(1)	6060(2)	63(1)

S(1)	1338(1)	2282(1)	4207(2)	64(1)

S(3)	1635(1)	3435(1)	4347(2)	65(1)

S(4)	4127(1)	3277(1)	6287(2)	67(1)

N(1)	608(5)	909(2)	3597(9)	101(2)

N(2)	4001(5)	745(2)	6003(8)	99(2)

N(3)	1685(5)	4853(2)	3920(9)	104(2)

N(4)	5112(6)	4593(2)	6636(10)	114(2)

C(1)	1199(5)	1244(2)	4036(8)	71(2)

C(2)	1917(4)	1683(2)	4572(7)	58(1)

C(3)	3015(4)	1628(2)	5413(7)	55(1)

C(4)	3552(5)	1135(2)	5717(8)	70(2)

C(5)	2067(5)	4462(2)	4367(9)	77(2)

C(6)	2519(5)	3956(2)	4894(7)	60(1)

C(7)	3618(4)	3886(2)	5758(7)	62(1)

C(8)	4410(5)	4295(2)	6241(9)	80(2)

F(1)	-2428(4)	3281(1)	9921(5)	108(1)

C(14)	-2278(5)	1124(2)	10485(8)	81(2)

C(15)	-2310(4)	1706(2)	10263(7)	62(1)

C(16)	-3289(5)	1956(3)	9475(8)	76(2)

C(19)	-1396(5)	2531(2)	10794(8)	75(2)

C(20)	-1365(5)	1998(2)	10908(8)	76(2)

C(18)	-2384(5)	2756(2)	10016(8)	73(2)

C(17)	-3338(5)	2486(3)	9347(8)	81(2)

N(5)	-2247(4)	852(2)	8727(6)	67(1)

C(11)	-2188(10)	354(3)	5503(11)	113(3)

C(10)	-1220(9)	550(3)	6588(16)	123(3)

C(12)	-3169(7)	414(3)	6109(12)	101(2)

C(13)	-3187(5)	661(2)	7697(11)	89(2)

C(9)	-1274(6)	793(3)	8204(11)	92(2)

Fig. S1 ORTEP view with non-H atomic numbering scheme for 2. Ellipsoids are at the 30% probability level. Selected bond lengths [Å] and angles []: Ni(1)-S(1) 2.1454(14), Ni(1)-S(2) 2.1441(14), Ni(1)-S(3) 2.1516(14), Ni(1)-S(4) 2.1412(15), S(2)-Ni(1)-S(1) 92.27(6), S(4)-Ni(1)-S(3) 92.46(6), S(2)-Ni(1)-S(3) 177.83(7).

Fig. S2 The side view of 1-D cation chain for 2.

Fig. S3 Temperature dependence of the molar magnetic susceptibility of 2.