# Electronic supplementary information

## Polymer nanosphere lithography: fabrication of an ordered trigonal polymeric nanostructure

Dong Kee Yi, and Dong-Yu Kim*

Center for Frontier Materials, Department of Materials Science and Engineering, Kwang Ju Institute of Science and Technology, 1 Oryong Puk-Ku, Kwang-Ju, 500-712, Republic of Korea. Tel: +82-062-970-2335; *E-mail: kimdy@kjist.ac.kr

## Contents

- Properties of the colloids used in this experiment.                2

- AFM image of trigonal nanostructures after Ar+ ion etching.       3

- Detailed explanations of figure 2.                              4

- Scheme of conventional nanosphere lithography.                 5

Gel Permeation Chromatography analysis revealed that soluble parts of polymer had Mn =

118,000, and the PDI value was 1.39. Compared with homo PS, the colloids showed an aliphatic

C=C stretch peak at 1637 cm-1 because it contains divinylbenzene (DVB) as the cross-linker:

monoreacted or nonreacted free DVB could be the origin of the C=C peak. The Tg of the

colloids was determined to be 123 oC from a second scan of differential scanning calorimetry.

1. Properties of the colloids used in this experiment.

2. AFM image of trigonal nanostructures after Ar+ ion etching.

Wide view of Fig. 2(b).

3. Detailed explanations of figure 2.

4. Scheme of conventional nanosphere lithography.

# Text boxes

### Corresponding SEM image