Supplementary data

A Novel Left-handed Double Helicate Constructed from Tartaric Acid Bridged Molybdenum(VI) and Gadolinium(III) Atoms

Chuan-De Wu, Can-Zhong Lu,* Xiang Lin, Ding-Ming Wu, Shao-Fang Lu, Hong-Hui Zhuang and Jin-Shun Huang

The State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, the Chinese Academy of Sciences, Fuzhou, Fujian 350002, P. R. China (E-mail: czlu@ms.fjirsm.ac.cn)

Table S1. Crystal data and structure refinement for [NH4][Mo2O4Gd(H2O)6(L-C4H2O6)2]·4H2O (1)

|  | 1 |
| --- | --- |
| Formula | C8H28GdMo2NO26 |
| Formula weight | 903.44 |
| Crystal size (mm3) | 0.20  0.12  0.06 |
| Crystal color | Colorless |
| Crystal system | Hexagonal |
| Space group | P6522 |
| Unit cell dimensions | a = 15.298(1) Å |
|  | c = 18.661(1) Å |
| Volume (Å3) | 3782.2(1) |
| Z | 6 |
| Calculated density (g·cm-3) | 2.380 |
| F(000) | 2634 |
| Temperature (K) | 293(2) |
| Wavelength (Å) | 0.71073 |
| Absorption coefficient (mm-1) | 3.692 |
| θ for data collection (o) | 2.66 to 25.09 |
| Limiting indices | -18≤h≤18, -18≤k≤18, -9≤l≤22 |
| Reflections collected | 11499 |
| Unique reflections (R(int)) | 2253 [R(int) = 0.0382] |
| Refinement method | Full-matrix least-squares on F2 |
| Absorption correction | SADABS |
| Data / restraints / parameters | 2253 / 0 / 187 |
| Goodness-of-fit on F2 | 1.087 |
| Final R indices [I > 2σ(I)] | R1 = 0.0257, wR2 = 0.0597 |
| R indices (all data) | R1 = 0.0333, wR2 = 0.0629 |
| Largest diff. peak and hole (e·Å3) | 0.513 and -0.409 |

R1 = (|Fo|  |Fc|) / |Fo|, wR2 = [w(Fo2  Fc2)2 / w(Fo2)2]0.5.

Table S2.  Atomic coordinates (x 104) and equivalent isotropic displacement parameters (Å2x 103) for 1.

| Atom x y z U(eq) | Atom x y z U(eq) |
| --- | --- |
| Gd 2724(1) -4552(1) 2500 25(1) Mo 1268(1) -7204(1) -214(1) 30(1) O(1) 1708(3) -6062(4) 655(2) 36(1) O(2) 2967(3) -5036(3) 1360(2) 36(1) O(3) 2707(3) -6675(3) -73(2) 31(1) O(4) 2979(3) -7123(3) 1385(2) 34(1) O(5) 5035(3) -6212(4) 174(2) 43(1) O(6) 4194(3) -7599(3) 827(2) 37(1) O(7) 709(4) -8157(4) 393(2) 46(1) O(8) 1242(4) -7803(4) -985(2) 50(1) O(9) 4453(4) -3955(5) 2752(3) 70(2) | O(10) 2916(6) -5982(5) 2675(3) 87(2) O(11) 3655(5) -3086(4) 1735(3) 79(2) O(101) 5625(7) -5028(7) -998(4) 114(3) O(102) 7160(20) -1422(10) 4167 147(11) O(103) 6280(13) -2984(14) 3773(7) 113(6) O(104) 329(11) -9836(6) -833 250(20) N(1) 2197(5) -7803(5) 3333 51(2) C(1) 2599(5) -5661(4) 850(3) 29(1) C(2) 3272(5) -5945(5) 452(3) 26(1) C(3) 3745(5) -6353(5) 979(3) 28(1) C(4) 4381(5) 6748(6) 618(3) 35(2) |

Table S3. Selected bond lengths [Å] for 1.

| Bond distances | Bond distances | Bond distances |
| --- | --- | --- |
| Gd-O(2) 2.343(4) Gd-O(2)#1 2.343(4) Gd-O(10) 2.372(5) Gd-O(10)#1 2.372(5) Gd-O(9) 2.374(5) Gd-O(9)#1 2.374(5) Gd-O(11)#1 2.430(5) Gd-O(11) 2.430(5) | Mo-O(8) 1.695(4) Mo-O(7) 1.701(4) Mo-O(4)#2 1.944(4) Mo-O(3) 1.946(4) Mo-O(6)#2 2.205(4) Mo-O(1) 2.227(4) O(1)-C(1) 1.238(7) O(2)-C(1) 1.264(7) | O(3)-C(2) 1.410(7) O(4)-C(3) 1.397(7) O(5)-C(4) 1.241(7) O(6)-C(4) 1.247(8) C(1)-C(2) 1.499(8) C(2)-C(3) 1.527(8) C(3)-C(4) 1.535(9) |

Table S4. Selected angles [º] for 1

| Atom1-atom2-atom3 angles | Atom1-atom2-atom3 angles | Atom1-atom2-atom3 angles |
| --- | --- | --- |
| O(2)-Gd-O(2)#1 148.2(2) O(2)-Gd-O(10) 73.80(17) O(2)#1-Gd-O(10) 80.88(17) O(2)-Gd-O(10)#1 80.88(17) O(2)#1-Gd-O(10)#1 73.80(17) O(10)-Gd-O(10)#1 73.9(4) O(2)-Gd-O(9) 88.82(17) O(2)#1-Gd-O(9) 101.70(16) O(10)-Gd-O(9) 72.5(3) O(10)#1-Gd-O(9) 146.4(2) O(2)-Gd-O(9)#1 101.70(16) O(2)#1-Gd-O(9)#1 88.82(17) O(10)-Gd-O(9)#1 146.4(2) O(10)#1-Gd-O(9)#1 72.5(3) O(9)-Gd-O(9)#1 141.1(3) O(2)-Gd-O(11)#1 142.39(16) O(2)#1-Gd-O(11)#1 69.25(16) O(10)-Gd-O(11)#1 129.1(2) O(10)#1-Gd-O(11)#1 130.30(19) O(9)-Gd-O(11)#1 74.5(2) | O(9)#1-Gd-O(11)#1 74.7(2) O(2)-Gd-O(11) 69.25(16) O(2)#1-Gd-O(11) 142.4(2) O(10)-Gd-O(11) 130.3(2) O(10)#1-Gd-O(11) 129.1(2) O(9)-Gd-O(11) 74.7(2) O(9)#1-Gd-O(11) 74.5(2) O(11)#1-Gd-O(11) 73.9(3) O(8)-Mo-O(7) 103.7(2) O(8)-Mo-O(4)#2 104.3(2) O(7)-Mo-O(4)#2 93.5(2) O(8)-Mo-O(3) 93.2(2) O(7)-Mo-O(3) 104.3(2) O(4)#2-Mo-O(3) 151.3(2) O(8)-Mo-O(6)#2 88.5(2) O(7)-Mo-O(6)#2 165.2(2) O(4)#2-Mo-O(6)#2 74.96(16) O(3)-Mo-O(6)#2 83.14(16) O(8)-Mo-O(1) 163.4(2) O(7)-Mo-O(1) 90.7(2) | O(4)#2-Mo-O(1) 82.68(16) O(3)-Mo-O(1) 74.93(15) O(6)#2-Mo-O(1) 78.69(16) C(1)-O(1)-Mo 115.4(4) C(1)-O(2)-Gd 147.3(4) C(2)-O(3)-Mo 122.8(3) C(3)-O(4)-Mo#3 123.1(4) C(4)-O(6)-Mo#3 116.4(4) O(1)-C(1)-O(2) 124.0(6) O(1)-C(1)-C(2) 117.2(5) O(2)-C(1)-C(2) 118.8(6) O(3)-C(2)-C(1) 109.6(5) O(3)-C(2)-C(3) 110.7(5) C(1)-C(2)-C(3) 109.5(5) O(4)-C(3)-C(2) 109.0(5) O(4)-C(3)-C(4) 109.6(5) C(2)-C(3)-C(4) 113.6(5) O(5)-C(4)-O(6) 126.0(6) O(5)-C(4)-C(3) 119.5(6) O(6)-C(4)-C(3) 114.4(6) |

Symmetry transformations used to generate equivalent atoms: #1: -x+y+1, y,-z+1/2; #2: x-y-1, x-1, z-1/6; #3: y+1, -x+y, z+1/6

Table S5. Anisotropic displacement parameters (Å2 x 103) for 1.

_______________________________________________________________________

U11      U22        U33      U23        U13      U12

_______________________________________________________________________

Gd      27(1)      24(1)      25(1)       0          4(1)      12(1)

Mo      31(1)      33(1)      25(1)      -1(1)      -3(1)      15(1)

O(1)     36(3)      49(3)      29(2)      -9(2)      -3(2)      26(2)

O(2)     45(3)      32(3)      31(2)      -5(2)       0(2)      20(2)

O(3)     32(2)      46(3)      22(2)     -10(2)      -9(2)      25(2)

O(4)     41(3)      41(3)      27(2)      14(2)       8(2)      26(2)

O(5)     35(3)      60(3)      40(3)      14(2)      12(2)      28(3)

O(6)     45(3)      41(3)      38(2)      12(2)       8(2)      32(2)

O(7)     50(3)      42(3)      44(3)      16(2)       3(2)      20(3)

O(8)     49(3)      57(3)      37(3)     -16(2)      -8(2)      21(3)

O(9)     39(3)     102(5)      57(3)      12(3)       0(3)      27(3)

O(10)   140(6)      96(5)      77(4)      53(4)      70(4)      98(5)

O(11)   115(5)      43(3)      94(4)      31(3)      77(4)      50(4)

O(101)  172(9)     135(7)      80(5)      10(5)       9(5)     109(7)

O(102)  150(20)    240(20)     19(7)      27(12)      0       77(11)

O(103)  135(15)    139(15)     62(8)      55(9)       2(8)     66(12)

O(104)   25(9)      10(6)     710(70)     39(18)      0        12(5)

N(1)     43(4)      43(4)      59(5)     -14(2)      14(2)      16(4)

C(1)     39(4)      31(4)      22(3)       2(3)      -2(3)      22(3)

C(2)     29(3)      28(3)      24(3)       4(3)       1(3)      17(3)

C(3)     31(4)      34(4)      22(3)       1(2)      -4(2)      19(3)

C(4)     32(4)      51(5)      29(3)       4(3)      -6(3)      26(3)

_______________________________________________________________________

Table S6. Selected Hydrogen Bonds Lengths (Å) for 1

| D d(D..A) A | D d(D..A) A |
| --- | --- |
| O9 2.932 O6i O9 2.772 O101ii O9 3.094 O101iii O9 3.081 O103 O10 2.995 O101iii O10 3.003 O4 O10 2.723 N1 O11 2.725 O5iv O101 2.994 O101v | O101 2.950 O103vi O101 3.064 O9iii O101 2.694 O5 O102 2.930 O8vii O103 2.852 O3ii O103 2.175 O103viii O104 3.140 O104ix N1 2.720 O10viii N1 2.772 O7x |

Symmetry transformations used to generate equivalent atoms: i: -x+1, -x+y+1, -z+1/3; ii: -x+1, -y-1, z+1/2; iii: -y, -x, -z+1/6; iv: y+1, -x+y+1, z+1/6; v: y+1, x-1, -z-1/3; vi: -x+1, -y-1, z-1/2; vii: -y, x-y-1, z+2/3; viii: y+1, x-1, -z+2/3; ix: x-y-1, x-1, z-1/6; x: -x+y+1, y, -z+1/2

Figures:

Figure S1. Thermogravimetric analyses (TGA) for 1 between 30 and 800oC

Figure S2. Powder X-ray diffraction patterns for before (top), after (middle) the removal of the water molecules and aqua ligands as well as after the solids of the evacuated samples were immersed in water (bottom) for 1.

Figure S3. ORTEP representation of the symmetry expanded local structure for 1 (30% probability ellipsoids).

Figure S4. The χMT and χM vs. T plots for 1.