# Supplementary data

A Building Block Approach to the Synthesis of Organic-Inorganic Oxide Materials:

The Hydrothermal Synthesis and Network Structure of [{Ni4(tpypyz)3}{Mo5O15(O3PCH2CH2PO3)}2]•23H2O (tpypyz = tetra-2-pyridylpyrazine).

Eric Burkholder, Vladimir Golub, Charles J. O'Connor and Jon Zubieta

Table 1.  Crystal data and structure refinement for 123H2O.

# Identification code 	MoNiP6R

Empirical formula 	C38N9H51Mo5Ni2O32.5P2

# Formula weight 	1812.94

Temperature 	90(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 24.6741(13) Å	= 90°.

b = 15.4148(8) Å	= 90°.

c = 30.8125(16) Å	 = 90°.

Volume	11719.4(11) Å3

# Z	8

Density (calculated)	2.053 Mg/m3

Absorption coefficient	1.820 mm-1

# F(000)	7174

Crystal size	0.50 x 0.10 x 0.02 mm3

Theta range for data collection	1.32 to 33.00°.

Index ranges	-36<=h<=36,

-23<=k<=23,

-47<=l<=46

Reflections collected	152194

Independent reflections	21129 [R(int) = 0.0834]

Completeness to theta = 33.00°	95.6 %

Max. and min. transmission	0.9645 and 0.4631

Refinement method	Full-matrix least-squares on F2

# Data / restraints / parameters	21129 / 0 / 870

Goodness-of-fit on F2	1.117

# Final R indices [I>2sigma(I)]	R1 = 0.0720, wR2 = 0.1179

R indices (all data)	R1 = 0.1249, wR2 = 0.1379

Largest diff. peak and hole	1.166 and -0.881 e.Å-3

Table 2.  Atomic coordinates ( x104) and equivalent isotropic displacement parameters (Å2x103) for 123H2O.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________

Mo(1)	7116(1)	5428(1)	2177(1)	14(1)

Mo(2)	8378(1)	4618(1)	2123(1)	13(1)

Mo(3)	8594(1)	4213(1)	954(1)	16(1)

Mo(4)	7339(1)	4047(1)	530(1)	17(1)

Mo(5)	6463(1)	4897(1)	1244(1)	18(1)

Ni(1)	8189(1)	2645(1)	2437(1)	12(1)

Ni(2)	9297(1)	908(1)	4203(1)	14(1)

P(1)	7760(1)	5741(1)	1228(1)	14(1)

P(2)	7429(1)	3462(1)	1598(1)	12(1)

O(1)	7790(1)	5432(2)	1710(1)	13(1)

O(2)	8310(2)	5596(2)	1025(1)	17(1)

O(3)	7307(2)	5272(2)	979(1)	15(1)

O(4)	7868(1)	3345(2)	1943(1)	13(1)

O(5)	7714(1)	3709(2)	1170(1)	13(1)

O(6)	7018(1)	4151(2)	1745(1)	14(1)

O(7)	8644(2)	3817(2)	2465(1)	17(1)

O(8)	7716(2)	4825(2)	2434(1)	16(1)

O(9)	8752(2)	5500(2)	2264(1)	20(1)

O(10)	6631(2)	5055(2)	2522(1)	21(1)

O(11)	7227(2)	6490(2)	2338(1)	17(1)

O(12)	6694(2)	5697(2)	1681(1)	17(1)

O(13)	5922(2)	4431(3)	1496(1)	26(1)

O(14)	6171(2)	5603(2)	883(1)	26(1)

O(15)	6682(2)	3974(2)	879(1)	19(1)

O(16)	7104(2)	4679(3)	115(1)	26(1)

O(17)	7313(2)	3022(2)	326(1)	26(1)

O(18)	8107(2)	4279(2)	480(1)	19(1)

O(19)	9157(2)	4679(3)	740(1)	23(1)

O(20)	8769(2)	3136(2)	936(1)	20(1)

O(21)	8670(2)	4365(2)	1582(1)	17(1)

O(86)	1111(9)	2088(11)	2361(6)	42(5)

O(87A)	1139(16)	1440(30)	1553(9)	120(18)

O(87B)	1361(15)	1018(18)	1740(12)	55(12)

O(88A)	6864(8)	209(14)	3837(10)	188(16)

O(88B)	7120(30)	-210(30)	3428(12)	140(30)

O(89)	9739(9)	4827(14)	3682(7)	29(5)

O(90)	9799(2)	2669(3)	598(1)	34(1)

O(91)	5359(2)	5956(3)	296(2)	42(1)

O(92)	9439(2)	3462(3)	3130(2)	44(1)

O(93)	9286(2)	6404(3)	1603(2)	55(2)

O(94)	5515(2)	3048(4)	1998(2)	51(1)

O(95)	4434(3)	5006(4)	457(2)	67(2)

O(96A)	866(4)	2569(9)	844(4)	74(5)

O(96B)	804(7)	2099(15)	1086(9)	49(7)

O(97A)	7821(16)	575(17)	3365(7)	17(11)

O(97B)	7550(40)	510(20)	3397(9)	89(17)

O(98A)	1480(20)	1460(40)	437(8)	178(18)

O(98B)	1390(9)	1090(20)	519(10)	77(10)

O(99)	9119(5)	4718(8)	3699(3)	120(4)

N(1)	7632(2)	2988(3)	2910(1)	14(1)

N(2)	8535(2)	2149(3)	2972(1)	12(1)

N(3)	8883(2)	2060(3)	2181(1)	14(1)

N(4)	9599(2)	118(3)	3710(1)	16(1)

N(5)	8962(2)	1431(3)	3670(1)	14(1)

N(6)	8794(2)	1859(3)	4474(1)	15(1)

N(7)	9943(2)	1771(3)	4263(1)	17(1)

N(8)	9685(2)	432(3)	4726(1)	13(1)

N(9)	8770(2)	-59(3)	4399(1)	15(1)

C(1)	7136(2)	3296(3)	2839(2)	20(1)

C(2)	6757(3)	3368(4)	3166(2)	30(1)

C(3)	6879(2)	3081(4)	3579(2)	28(1)

C(4)	7393(2)	2751(4)	3657(2)	25(1)

C(5)	7765(2)	2727(3)	3321(2)	18(1)

C(6)	8307(2)	2329(3)	3353(2)	15(1)

C(7)	8963(2)	1634(3)	2919(2)	13(1)

C(8)	9199(2)	1669(3)	2480(2)	16(1)

C(9)	9712(2)	1356(4)	2379(2)	22(1)

C(10)	9872(3)	1372(4)	1944(2)	29(1)

C(11)	9531(2)	1711(4)	1635(2)	23(1)

C(12)	9046(2)	2073(3)	1765(2)	18(1)

C(13)	9851(2)	-640(4)	3772(2)	22(1)

C(14)	9954(3)	-1216(4)	3434(2)	29(1)

C(15)	9770(2)	-1022(4)	3023(2)	26(1)

C(16)	9501(2)	-236(3)	2957(2)	18(1)

C(17)	9437(2)	324(3)	3307(2)	15(1)

C(18)	9129(2)	1148(3)	3283(2)	14(1)

C(19)	8597(2)	2071(3)	3726(2)	15(1)

C(20)	8568(2)	2403(3)	4177(2)	16(1)

C(21)	8377(2)	3208(4)	4286(2)	19(1)

C(22)	8380(2)	3444(4)	4727(2)	21(1)

C(23)	8565(2)	2870(4)	5032(2)	23(1)

C(24)	8778(2)	2089(4)	4889(2)	21(1)

C(25)	9985(2)	2531(4)	4055(2)	24(1)

C(26)	10323(3)	3191(4)	4192(2)	30(1)

C(27)	10628(2)	3060(4)	4563(2)	24(1)

C(28)	10595(2)	2270(3)	4781(2)	21(1)

C(29)	10263(2)	1631(3)	4615(2)	16(1)

C(30)	10171(2)	769(3)	4822(2)	13(1)

C(31)	9488(2)	-304(3)	4897(2)	13(1)

C(32)	8920(2)	-474(3)	4772(2)	15(1)

C(33)	8549(2)	-922(3)	5021(2)	18(1)

C(34)	8017(2)	-1003(4)	4873(2)	24(1)

C(35)	7879(2)	-624(4)	4487(2)	26(1)

C(36)	8260(2)	-144(4)	4261(2)	21(1)

C(37)	7568(2)	6852(3)	1231(2)	15(1)

C(38)	7078(2)	2456(3)	1513(2)	14(1)

________________________________________________________________________

Table 3.  Bond lengths [Å] and angles [°] for 123H2O.

_____________________________________________________

Mo(1)-O(10) 	1.701(4)

Mo(1)-O(11) 	1.733(3)

Mo(1)-O(12) 	1.895(4)

Mo(1)-O(8) 	1.920(4)

Mo(1)-O(1) 	2.198(3)

Mo(1)-O(6) 	2.388(3)

Mo(2)-O(9) 	1.699(4)

Mo(2)-O(7) 	1.750(3)

Mo(2)-O(21) 	1.857(4)

Mo(2)-O(8) 	1.919(4)

Mo(2)-O(1) 	2.302(3)

Mo(2)-O(4) 	2.396(3)

Mo(3)-O(19) 	1.697(4)

Mo(3)-O(20) 	1.717(3)

Mo(3)-O(18) 	1.894(4)

Mo(3)-O(21) 	1.957(4)

Mo(3)-O(2) 	2.254(3)

Mo(3)-O(5) 	2.399(4)

Mo(4)-O(17) 	1.703(4)

Mo(4)-O(16) 	1.710(4)

Mo(4)-O(18) 	1.933(4)

Mo(4)-O(15) 	1.948(4)

Mo(4)-O(5) 	2.238(3)

Mo(4)-O(3) 	2.342(3)

Mo(5)-O(13) 	1.704(4)

Mo(5)-O(14) 	1.713(4)

Mo(5)-O(15) 	1.891(4)

Mo(5)-O(12) 	1.913(4)

Mo(5)-O(3) 	2.309(4)

Mo(5)-O(6) 	2.362(3)

Ni(1)-N(2) 	2.007(4)

Ni(1)-O(4) 	2.027(3)

Ni(1)-N(1) 	2.074(4)

Ni(1)-O(11)#1 	2.077(4)

Ni(1)-N(3) 	2.089(4)

Ni(1)-O(7) 	2.128(4)

Ni(2)-N(5) 	2.007(4)

Ni(2)-N(8) 	2.015(4)

Ni(2)-N(9) 	2.068(4)

Ni(2)-N(4) 	2.083(4)

Ni(2)-N(7) 	2.086(5)

Ni(2)-N(6) 	2.096(4)

P(1)-O(2) 	1.510(4)

P(1)-O(3) 	1.537(4)

P(1)-O(1) 	1.562(3)

P(1)-C(37) 	1.776(5)

P(2)-O(4) 	1.528(4)

P(2)-O(6) 	1.536(4)

P(2)-O(5) 	1.544(3)

P(2)-C(38) 	1.795(5)

O(11)-Ni(1)#2 	2.077(4)

N(1)-C(1) 	1.331(7)

N(1)-C(5) 	1.367(6)

N(2)-C(7) 	1.330(6)

N(2)-C(6) 	1.331(6)

N(3)-C(12) 	1.344(6)

N(3)-C(8) 	1.350(6)

N(4)-C(13) 	1.338(6)

N(4)-C(17) 	1.344(6)

N(5)-C(18) 	1.336(6)

N(5)-C(19) 	1.347(6)

N(6)-C(24) 	1.327(6)

N(6)-C(20) 	1.361(6)

N(7)-C(25) 	1.339(6)

N(7)-C(29) 	1.357(7)

N(8)-C(30) 	1.340(6)

N(8)-C(31) 	1.341(6)

N(9)-C(36) 	1.334(7)

N(9)-C(32) 	1.366(6)

C(1)-C(2) 	1.377(8)

C(2)-C(3) 	1.381(8)

C(3)-C(4) 	1.387(8)

C(4)-C(5) 	1.387(7)

C(5)-C(6) 	1.475(7)

C(6)-C(19) 	1.411(7)

C(7)-C(18) 	1.410(7)

C(7)-C(8) 	1.474(7)

C(8)-C(9) 	1.389(8)

C(9)-C(10) 	1.397(8)

C(10)-C(11) 	1.376(8)

C(11)-C(12) 	1.379(8)

C(13)-C(14) 	1.391(8)

C(14)-C(15) 	1.377(8)

C(15)-C(16) 	1.397(7)

C(16)-C(17) 	1.390(7)

C(17)-C(18) 	1.483(7)

C(19)-C(20) 	1.482(7)

C(20)-C(21) 	1.369(7)

C(21)-C(22) 	1.407(7)

C(22)-C(23) 	1.368(8)

C(23)-C(24) 	1.384(8)

C(25)-C(26) 	1.382(8)

C(26)-C(27) 	1.382(8)

C(27)-C(28) 	1.392(7)

C(28)-C(29) 	1.379(7)

C(29)-C(30) 	1.491(7)

C(30)-C(31)#3 	1.406(7)

C(31)-C(30)#3 	1.406(7)

C(31)-C(32) 	1.478(7)

C(32)-C(33) 	1.380(7)

C(33)-C(34) 	1.393(8)

C(34)-C(35) 	1.368(8)

C(35)-C(36) 	1.384(8)

C(37)-C(38)#2 	1.545(7)

C(38)-C(37)#1 	1.545(7)

O(10)-Mo(1)-O(11)	104.54(18)

O(10)-Mo(1)-O(12)	101.09(18)

O(11)-Mo(1)-O(12)	96.30(16)

O(10)-Mo(1)-O(8)	96.99(17)

O(11)-Mo(1)-O(8)	102.58(16)

O(12)-Mo(1)-O(8)	149.59(15)

O(10)-Mo(1)-O(1)	160.44(15)

O(11)-Mo(1)-O(1)	93.71(15)

O(12)-Mo(1)-O(1)	83.53(14)

O(8)-Mo(1)-O(1)	71.77(14)

O(10)-Mo(1)-O(6)	89.96(15)

O(11)-Mo(1)-O(6)	162.60(14)

O(12)-Mo(1)-O(6)	71.07(13)

O(8)-Mo(1)-O(6)	84.79(13)

O(1)-Mo(1)-O(6)	73.42(12)

O(9)-Mo(2)-O(7)	102.00(17)

O(9)-Mo(2)-O(21)	100.77(17)

O(7)-Mo(2)-O(21)	104.30(16)

O(9)-Mo(2)-O(8)	101.67(17)

O(7)-Mo(2)-O(8)	97.79(16)

O(21)-Mo(2)-O(8)	144.27(16)

O(9)-Mo(2)-O(1)	92.72(15)

O(7)-Mo(2)-O(1)	162.36(15)

O(21)-Mo(2)-O(1)	82.10(14)

O(8)-Mo(2)-O(1)	69.42(13)

O(9)-Mo(2)-O(4)	177.99(16)

O(7)-Mo(2)-O(4)	75.99(14)

O(21)-Mo(2)-O(4)	79.79(14)

O(8)-Mo(2)-O(4)	78.76(13)

O(1)-Mo(2)-O(4)	89.27(12)

O(19)-Mo(3)-O(20)	100.98(19)

O(19)-Mo(3)-O(18)	101.37(17)

O(20)-Mo(3)-O(18)	100.77(17)

O(19)-Mo(3)-O(21)	104.77(17)

O(20)-Mo(3)-O(21)	97.08(16)

O(18)-Mo(3)-O(21)	144.72(16)

O(19)-Mo(3)-O(2)	83.76(16)

O(20)-Mo(3)-O(2)	174.86(16)

O(18)-Mo(3)-O(2)	80.06(14)

O(21)-Mo(3)-O(2)	79.68(14)

O(19)-Mo(3)-O(5)	170.10(15)

O(20)-Mo(3)-O(5)	85.63(15)

O(18)-Mo(3)-O(5)	69.92(14)

O(21)-Mo(3)-O(5)	81.48(13)

O(2)-Mo(3)-O(5)	89.92(12)

O(17)-Mo(4)-O(16)	103.80(19)

O(17)-Mo(4)-O(18)	100.33(18)

O(16)-Mo(4)-O(18)	99.60(18)

O(17)-Mo(4)-O(15)	96.80(18)

O(16)-Mo(4)-O(15)	99.49(18)

O(18)-Mo(4)-O(15)	150.42(15)

O(17)-Mo(4)-O(5)	97.16(16)

O(16)-Mo(4)-O(5)	158.78(16)

O(18)-Mo(4)-O(5)	73.06(14)

O(15)-Mo(4)-O(5)	81.05(14)

O(17)-Mo(4)-O(3)	164.90(16)

O(16)-Mo(4)-O(3)	88.40(16)

O(18)-Mo(4)-O(3)	86.10(14)

O(15)-Mo(4)-O(3)	72.08(14)

O(5)-Mo(4)-O(3)	71.47(12)

O(13)-Mo(5)-O(14)	103.6(2)

O(13)-Mo(5)-O(15)	100.28(18)

O(14)-Mo(5)-O(15)	102.33(17)

O(13)-Mo(5)-O(12)	100.60(18)

O(14)-Mo(5)-O(12)	99.86(17)

O(15)-Mo(5)-O(12)	144.84(16)

O(13)-Mo(5)-O(3)	166.66(16)

O(14)-Mo(5)-O(3)	89.48(17)

O(15)-Mo(5)-O(3)	73.82(14)

O(12)-Mo(5)-O(3)	79.49(14)

O(13)-Mo(5)-O(6)	87.14(16)

O(14)-Mo(5)-O(6)	167.48(17)

O(15)-Mo(5)-O(6)	81.74(14)

O(12)-Mo(5)-O(6)	71.40(13)

O(3)-Mo(5)-O(6)	80.22(12)

N(2)-Ni(1)-O(4)	170.21(15)

N(2)-Ni(1)-N(1)	78.58(17)

O(4)-Ni(1)-N(1)	97.69(15)

N(2)-Ni(1)-O(11)#1	90.30(15)

O(4)-Ni(1)-O(11)#1	98.77(14)

N(1)-Ni(1)-O(11)#1	89.70(16)

N(2)-Ni(1)-N(3)	78.31(17)

O(4)-Ni(1)-N(3)	105.39(15)

N(1)-Ni(1)-N(3)	156.83(16)

O(11)#1-Ni(1)-N(3)	88.79(15)

N(2)-Ni(1)-O(7)	93.74(15)

O(4)-Ni(1)-O(7)	77.55(14)

N(1)-Ni(1)-O(7)	95.99(15)

O(11)#1-Ni(1)-O(7)	173.57(14)

N(3)-Ni(1)-O(7)	87.14(15)

N(5)-Ni(2)-N(8)	175.64(18)

N(5)-Ni(2)-N(9)	105.66(17)

N(8)-Ni(2)-N(9)	78.60(17)

N(5)-Ni(2)-N(4)	77.68(17)

N(8)-Ni(2)-N(4)	101.55(17)

N(9)-Ni(2)-N(4)	90.98(17)

N(5)-Ni(2)-N(7)	97.57(17)

N(8)-Ni(2)-N(7)	78.28(17)

N(9)-Ni(2)-N(7)	156.12(17)

N(4)-Ni(2)-N(7)	99.44(17)

N(5)-Ni(2)-N(6)	78.56(17)

N(8)-Ni(2)-N(6)	102.50(17)

N(9)-Ni(2)-N(6)	90.89(17)

N(4)-Ni(2)-N(6)	155.77(17)

N(7)-Ni(2)-N(6)	88.30(17)

O(2)-P(1)-O(3)	112.2(2)

O(2)-P(1)-O(1)	107.8(2)

O(3)-P(1)-O(1)	111.41(19)

O(2)-P(1)-C(37)	112.6(2)

O(3)-P(1)-C(37)	105.2(2)

O(1)-P(1)-C(37)	107.6(2)

O(4)-P(2)-O(6)	110.26(19)

O(4)-P(2)-O(5)	107.4(2)

O(6)-P(2)-O(5)	112.45(19)

O(4)-P(2)-C(38)	110.0(2)

O(6)-P(2)-C(38)	108.8(2)

O(5)-P(2)-C(38)	107.9(2)

P(1)-O(1)-Mo(1)	126.0(2)

P(1)-O(1)-Mo(2)	136.2(2)

Mo(1)-O(1)-Mo(2)	96.55(12)

P(1)-O(2)-Mo(3)	117.4(2)

P(1)-O(3)-Mo(5)	126.7(2)

P(1)-O(3)-Mo(4)	130.5(2)

Mo(5)-O(3)-Mo(4)	92.11(12)

P(2)-O(4)-Ni(1)	149.5(2)

P(2)-O(4)-Mo(2)	115.90(18)

Ni(1)-O(4)-Mo(2)	93.26(13)

P(2)-O(5)-Mo(4)	128.5(2)

P(2)-O(5)-Mo(3)	136.79(19)

Mo(4)-O(5)-Mo(3)	93.13(12)

P(2)-O(6)-Mo(5)	121.79(19)

P(2)-O(6)-Mo(1)	131.8(2)

Mo(5)-O(6)-Mo(1)	91.27(11)

Mo(2)-O(7)-Ni(1)	112.17(18)

Mo(2)-O(8)-Mo(1)	122.11(18)

Mo(1)-O(11)-Ni(1)#2	140.7(2)

Mo(1)-O(12)-Mo(5)	126.14(18)

Mo(5)-O(15)-Mo(4)	121.48(19)

Mo(3)-O(18)-Mo(4)	123.36(18)

Mo(2)-O(21)-Mo(3)	151.1(2)

C(1)-N(1)-C(5)	118.6(5)

C(1)-N(1)-Ni(1)	125.8(4)

C(5)-N(1)-Ni(1)	114.5(3)

C(7)-N(2)-C(6)	124.6(4)

C(7)-N(2)-Ni(1)	117.6(3)

C(6)-N(2)-Ni(1)	117.7(3)

C(12)-N(3)-C(8)	118.9(5)

C(12)-N(3)-Ni(1)	126.9(4)

C(8)-N(3)-Ni(1)	114.1(3)

C(13)-N(4)-C(17)	118.4(5)

C(13)-N(4)-Ni(2)	125.1(4)

C(17)-N(4)-Ni(2)	115.4(3)

C(18)-N(5)-C(19)	124.0(4)

C(18)-N(5)-Ni(2)	118.2(3)

C(19)-N(5)-Ni(2)	117.7(3)

C(24)-N(6)-C(20)	118.2(5)

C(24)-N(6)-Ni(2)	126.1(4)

C(20)-N(6)-Ni(2)	113.8(3)

C(25)-N(7)-C(29)	118.5(5)

C(25)-N(7)-Ni(2)	125.0(4)

C(29)-N(7)-Ni(2)	114.5(3)

C(30)-N(8)-C(31)	124.5(4)

C(30)-N(8)-Ni(2)	117.4(3)

C(31)-N(8)-Ni(2)	116.7(3)

C(36)-N(9)-C(32)	118.5(5)

C(36)-N(9)-Ni(2)	124.8(4)

C(32)-N(9)-Ni(2)	114.4(3)

N(1)-C(1)-C(2)	122.2(5)

C(1)-C(2)-C(3)	120.0(6)

C(2)-C(3)-C(4)	118.4(6)

C(5)-C(4)-C(3)	119.1(5)

N(1)-C(5)-C(4)	121.6(5)

N(1)-C(5)-C(6)	113.8(5)

C(4)-C(5)-C(6)	124.2(5)

N(2)-C(6)-C(19)	116.5(5)

N(2)-C(6)-C(5)	114.3(4)

C(19)-C(6)-C(5)	129.1(5)

N(2)-C(7)-C(18)	116.7(4)

N(2)-C(7)-C(8)	113.9(4)

C(18)-C(7)-C(8)	129.4(5)

N(3)-C(8)-C(9)	122.0(5)

N(3)-C(8)-C(7)	114.4(5)

C(9)-C(8)-C(7)	123.6(5)

C(8)-C(9)-C(10)	117.8(5)

C(11)-C(10)-C(9)	119.9(6)

C(10)-C(11)-C(12)	118.9(5)

N(3)-C(12)-C(11)	122.1(5)

N(4)-C(13)-C(14)	122.4(5)

C(15)-C(14)-C(13)	119.4(5)

C(14)-C(15)-C(16)	118.5(5)

C(17)-C(16)-C(15)	118.7(5)

N(4)-C(17)-C(16)	122.5(5)

N(4)-C(17)-C(18)	113.7(4)

C(16)-C(17)-C(18)	123.4(4)

N(5)-C(18)-C(7)	116.6(4)

N(5)-C(18)-C(17)	113.1(4)

C(7)-C(18)-C(17)	130.1(4)

N(5)-C(19)-C(6)	116.2(4)

N(5)-C(19)-C(20)	113.9(4)

C(6)-C(19)-C(20)	130.0(5)

N(6)-C(20)-C(21)	122.2(5)

N(6)-C(20)-C(19)	113.5(4)

C(21)-C(20)-C(19)	124.0(5)

C(20)-C(21)-C(22)	118.0(5)

C(23)-C(22)-C(21)	119.9(5)

C(22)-C(23)-C(24)	118.1(5)

N(6)-C(24)-C(23)	123.3(5)

N(7)-C(25)-C(26)	123.0(5)

C(25)-C(26)-C(27)	118.2(5)

C(26)-C(27)-C(28)	119.7(5)

C(29)-C(28)-C(27)	118.7(5)

N(7)-C(29)-C(28)	121.9(5)

N(7)-C(29)-C(30)	113.2(4)

C(28)-C(29)-C(30)	124.6(5)

N(8)-C(30)-C(31)#3	118.2(4)

N(8)-C(30)-C(29)	112.8(4)

C(31)#3-C(30)-C(29)	128.9(5)

N(8)-C(31)-C(30)#3	117.2(4)

N(8)-C(31)-C(32)	113.0(4)

C(30)#3-C(31)-C(32)	129.6(5)

N(9)-C(32)-C(33)	121.5(5)

N(9)-C(32)-C(31)	113.2(4)

C(33)-C(32)-C(31)	125.0(5)

C(32)-C(33)-C(34)	119.2(5)

C(35)-C(34)-C(33)	118.7(5)

C(34)-C(35)-C(36)	119.8(5)

N(9)-C(36)-C(35)	122.1(5)

C(38)#2-C(37)-P(1)	115.7(3)

C(37)#1-C(38)-P(2)	109.3(3)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+3/2,y-1/2,z    #2 -x+3/2,y+1/2,z    #3 -x+2,-y,-z+1

Table 4.  Anisotropic displacement parameters (Å2x103) for 123H2O.  The anisotropic displacement factor exponent takes the form:  -22[ h2a*2U11 + ...  + 2 h k a* b* U12]

________________________________________________________________________

U11	U22 	U33	U23	U13	U12

________________________________________________________________________

Mo(1)	19(1) 	9(1)	15(1) 	1(1)	2(1) 	1(1)

Mo(2)	17(1) 	10(1)	12(1) 	1(1)	-1(1) 	-1(1)

Mo(3)	23(1) 	13(1)	12(1) 	3(1)	4(1) 	4(1)

Mo(4)	29(1) 	11(1)	12(1) 	1(1)	-4(1) 	0(1)

Mo(5)	20(1) 	13(1)	21(1) 	-1(1)	-5(1) 	1(1)

Ni(1)	17(1) 	10(1)	10(1) 	1(1)	-2(1) 	0(1)

Ni(2)	15(1) 	15(1)	11(1) 	1(1)	-2(1) 	2(1)

P(1)	21(1) 	8(1)	12(1) 	1(1)	0(1) 	1(1)

P(2)	17(1) 	8(1)	11(1) 	0(1)	-2(1) 	-1(1)

O(1)	17(2) 	11(2)	11(2) 	1(1)	-1(1) 	1(1)

O(2)	23(2) 	13(2)	17(2) 	4(1)	4(2) 	2(2)

O(3)	23(2) 	8(2)	14(2) 	-1(1)	-2(2) 	1(1)

O(4)	16(2) 	11(2)	12(2) 	1(1)	-3(1) 	1(1)

O(5)	18(2) 	11(2)	9(2) 	1(1)	-2(1) 	0(1)

O(6)	17(2) 	9(2)	16(2) 	0(1)	-4(1) 	2(1)

O(7)	21(2) 	16(2)	13(2) 	1(1)	-3(2) 	-2(2)

O(8)	25(2) 	12(2)	10(2) 	-1(1)	0(2) 	-1(2)

O(9)	24(2) 	16(2)	19(2) 	2(2)	-1(2) 	-6(2)

O(10)	25(2) 	15(2)	23(2) 	3(2)	6(2) 	3(2)

O(11)	23(2) 	12(2)	15(2) 	0(1)	0(2) 	2(1)

O(12)	23(2) 	8(2)	20(2) 	-2(1)	1(2) 	3(1)

O(13)	24(2) 	23(2)	32(2) 	-2(2)	-5(2) 	-1(2)

O(14)	32(2) 	18(2)	29(2) 	2(2)	-8(2) 	6(2)

O(15)	27(2) 	14(2)	16(2) 	-1(1)	-7(2) 	0(2)

O(16)	36(2) 	24(2)	18(2) 	5(2)	-7(2) 	3(2)

O(17)	46(3) 	13(2)	19(2) 	-3(2)	-4(2) 	-4(2)

O(18)	30(2) 	13(2)	13(2) 	4(1)	3(2) 	3(2)

O(19)	24(2) 	28(2)	18(2) 	10(2)	9(2) 	3(2)

O(20)	28(2) 	15(2)	15(2) 	2(1)	4(2) 	9(2)

O(21)	17(2) 	17(2)	18(2) 	2(1)	0(2) 	3(1)

O(86)	61(14) 	23(9)	43(11) 	25(8)	19(10) 	15(9)

O(87A)	160(30) 	150(30)	50(15) 	-1(19)	22(18) 	-110(30)

O(87B)	90(20) 	44(16)	32(17) 	18(11)	39(15) 	1(15)

O(88A)	129(17) 	132(18)	300(40) 	120(20)	69(18) 	38(13)

O(88B)	240(70) 	120(40)	50(20) 	30(20)	0(30) 	120(40)

O(89)	31(13) 	31(12)	25(11) 	-2(9)	0(9) 	5(10)

O(90)	35(3) 	40(3)	27(2) 	-1(2)	7(2) 	3(2)

O(91)	45(3) 	37(3)	44(3) 	2(2)	-22(2) 	-2(2)

O(92)	42(3) 	52(3)	37(3) 	12(2)	-17(2) 	-17(3)

O(93)	54(4) 	38(3)	74(4) 	15(3)	27(3) 	-2(3)

O(94)	52(3) 	55(3)	45(3) 	16(3)	5(3) 	-7(3)

O(95)	90(5) 	68(4)	42(3) 	-3(3)	-6(3) 	-37(4)

O(96A)	59(6) 	96(10)	69(9) 	-17(7)	-20(5) 	0(6)

O(96B)	26(10) 	59(14)	62(16) 	23(11)	2(9) 	6(9)

O(97A)	23(17) 	18(12)	10(11) 	5(6)	-7(8) 	-14(8)

O(97B)	140(50) 	68(13)	58(11) 	1(10)	-39(17) 	28(19)

O(98A)	210(30) 	290(40)	41(9) 	36(19)	59(15) 	170(30)

O(98B)	39(11) 	123(19)	70(16) 	-49(14)	31(10) 	-18(12)

O(99)	137(10) 	166(11)	56(6) 	-28(7)	-4(6) 	61(9)

N(1)	20(2) 	13(2)	11(2) 	2(2)	-1(2) 	3(2)

N(2)	15(2) 	11(2)	11(2) 	1(1)	-4(2) 	1(2)

N(3)	20(2) 	12(2)	11(2) 	2(2)	-1(2) 	-3(2)

N(4)	16(2) 	15(2)	17(2) 	1(2)	0(2) 	5(2)

N(5)	17(2) 	11(2)	12(2) 	1(2)	-2(2) 	2(2)

N(6)	17(2) 	16(2)	13(2) 	-1(2)	2(2) 	1(2)

N(7)	18(2) 	14(2)	18(2) 	3(2)	1(2) 	3(2)

N(8)	13(2) 	15(2)	10(2) 	2(2)	-1(2) 	3(2)

N(9)	13(2) 	15(2)	17(2) 	1(2)	-3(2) 	-1(2)

C(1)	19(3) 	21(3)	21(3) 	5(2)	-3(2) 	5(2)

C(2)	21(3) 	38(4)	30(3) 	8(3)	1(3) 	9(3)

C(3)	19(3) 	43(4)	21(3) 	6(3)	-1(2) 	10(3)

C(4)	21(3) 	37(3)	17(3) 	3(2)	3(2) 	7(3)

C(5)	21(3) 	18(2)	14(2) 	0(2)	-4(2) 	3(2)

C(6)	18(3) 	11(2)	15(2) 	0(2)	0(2) 	3(2)

C(7)	17(3) 	12(2)	11(2) 	2(2)	-2(2) 	-1(2)

C(8)	21(3) 	15(2)	11(2) 	-1(2)	-5(2) 	1(2)

C(9)	23(3) 	22(3)	21(3) 	4(2)	4(2) 	1(2)

C(10)	30(3) 	29(3)	26(3) 	1(3)	10(3) 	5(3)

C(11)	34(3) 	21(3)	14(2) 	-1(2)	7(2) 	0(2)

C(12)	24(3) 	17(2)	13(2) 	-1(2)	2(2) 	-7(2)

C(13)	24(3) 	21(3)	19(3) 	3(2)	-6(2) 	6(2)

C(14)	40(4) 	23(3)	25(3) 	-2(2)	2(3) 	16(3)

C(15)	29(3) 	25(3)	24(3) 	-5(2)	0(2) 	9(3)

C(16)	18(3) 	22(3)	15(2) 	-1(2)	-1(2) 	7(2)

C(17)	13(2) 	17(2)	15(2) 	3(2)	-2(2) 	4(2)

C(18)	18(3) 	15(2)	8(2) 	-1(2)	-1(2) 	3(2)

C(19)	18(3) 	14(2)	12(2) 	4(2)	1(2) 	2(2)

C(20)	16(3) 	20(2)	10(2) 	2(2)	-1(2) 	3(2)

C(21)	22(3) 	24(3)	12(2) 	-1(2)	-3(2) 	9(2)

C(22)	20(3) 	22(3)	21(3) 	-6(2)	3(2) 	7(2)

C(23)	27(3) 	31(3)	10(2) 	-8(2)	1(2) 	6(3)

C(24)	23(3) 	26(3)	14(2) 	2(2)	-2(2) 	-1(2)

C(25)	34(3) 	19(3)	18(3) 	10(2)	1(2) 	-1(2)

C(26)	34(4) 	23(3)	34(3) 	11(3)	5(3) 	1(3)

C(27)	25(3) 	17(3)	29(3) 	3(2)	1(2) 	-8(2)

C(28)	21(3) 	20(3)	20(3) 	0(2)	-2(2) 	-1(2)

C(29)	16(3) 	18(2)	13(2) 	1(2)	4(2) 	0(2)

C(30)	15(2) 	14(2)	9(2) 	-1(2)	-2(2) 	5(2)

C(31)	14(2) 	16(2)	8(2) 	1(2)	-2(2) 	-1(2)

C(32)	13(2) 	17(2)	14(2) 	-1(2)	-4(2) 	-2(2)

C(33)	19(3) 	17(2)	17(2) 	-4(2)	2(2) 	-2(2)

C(34)	21(3) 	23(3)	27(3) 	-1(2)	-4(2) 	-7(2)

C(35)	18(3) 	34(3)	27(3) 	-5(2)	-9(2) 	-7(2)

C(36)	20(3) 	24(3)	20(3) 	-2(2)	-9(2) 	-2(2)

C(37)	22(3) 	5(2)	18(2) 	3(2)	-4(2) 	1(2)

C(38)	13(2) 	10(2)	19(2) 	0(2)	0(2) 	-2(2)

________________________________________________________________________

Table 5.  Hydrogen coordinates ( x104) and isotropic displacement parameters (Å2x103)

for 123H2O.

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(1)	7039	3471	2554	24

H(2)	6412	3615	3107	35

H(3)	6617	3110	3805	33

H(4)	7488	2544	3937	30

H(9)	9946	1139	2598	26

H(10)	10217	1150	1863	34

H(11)	9627	1696	1336	27

H(12)	8821	2340	1553	21

H(13)	9965	-791	4057	26

H(14)	10148	-1737	3486	35

H(15)	9826	-1415	2789	31

H(16)	9363	-88	2679	22

H(21)	8247	3596	4070	23

H(22)	8253	3999	4813	25

H(23)	8549	3004	5332	27

H(24)	8919	1698	5099	25

H(25)	9773	2619	3801	28

H(26)	10345	3722	4036	36

H(27)	10858	3506	4668	28

H(28)	10797	2173	5038	25

H(33)	8654	-1173	5289	21

H(34)	7756	-1315	5037	28

H(35)	7523	-689	4375	32

H(36)	8155	133	3998	26

# H(37A)	7577	7068	928	18

# H(37B)	7189	6893	1333	18

H(38A)	7003	2175	1796	17

H(38B)	6728	2566	1366	17

________________________________________________________________________