ANNEXURE I

COMPARISON OF HClO4-SiO2 WITH OTHER REPORTED CATALYSTS

Manuscript No. B304178F

### Manuscript Title:	Perchloric Acid Adsorbed on Silica Gel as a New, Highly Efficient, and Versatile Catalyst for Acetylation of Phenols, Thiols, Alcohols, and Amines.

### Authors:		Asit K. Chakraborti* and Rajesh Gulhane

*Corresponding author:	akchakraborti@niper.ac.in

The examples demonstrating the advantages of HClO4-SiO2 over the reported acetylation catalysts could be analyzed as advantages in terms of  the: (1) amount of catalyst/acylating agent required, necessity to use solvent with the reported catalyst, reaction temperature, and reaction time so as to provide comparable yields with a common substrates, and (2) reaction with sensitive substrates.

1)	Advantages of HClO4-SiO2 over other acetylation catalysts in terms of the amount of catalyst/acylating agent required, necessity to use solvent, reaction temperature, and reaction time:

S. No.	Substrate		Catalyst			Ac2O 		Conditions		Yield

(mol %)			(Equiv)*	(Solv, Temp., Time)	(%)Ref

- Reactions with Phenols/Thiols/Amines:

1	2-Naphthol/Phenol	KSF (20 mg/mmol)		2.0		DCM, 40°C, 2 h	9811

HSZ (20 mg/mmol)		2.0		Neat, 60°C, 1.5 h	10012

Yttria-zirconia (20% wt)	1.5		MeCN, Reflux, 12 h	9714

TaCl5 (10)			1.5		DCM, RT, ?		811

In(OTf)3 (0.1)			1.5		MeCN, RT, 15 min	978

HClO4-SiO2 (1)		1.0		Neat, RT, 5 min	93

2	4-Methoxyphenol	KSF (20 mg/mmol)		2.0		Neat, RT, 4.5 h	9211

HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	94

3	4-Bromophenol	Cu(OTf)2 (2.5)			2.0		DCM, RT, 2 h		937

HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	92

4	4-Hydroxy		Cu(OTf)2 (2.5)			2.0		DCM, RT, 2 h		937

acetophenone		HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	99

5	4-Nitrophenol		Bi(OTf)3 (0.1)			1.5		MeCN, RT, 30 min	909

KSF (20 mg/mmol)		2.0		DCM, 40°C, 2.5 h	9811

HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	91

6	Hydroquinone		Bi(OTf)3 (0.1)			1.5		MeCN, RT, 40 min	889

KSF (20 mg/mmol)		2.0		Neat, RT, 2.0 h	9811

HClO4-SiO2 (1)		1.0		Neat, RT, 5 min	83

7	Catechol		Bi(OTf)3 (0.1)			1.5		MeCN, RT, 15 min	859

KSF (20 mg/mmol)		2.0		Neat, RT, 3.0 h	9811

HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	97

8	Resorcinol		Bi(OTf)3 (0.1)			1.5		MeCN, RT, 15 min	929

KSF (20 mg/mmol)		2.0		CHCl3, 62°C, 3.0 h	7811

HClO4-SiO2 (1)		1.0		Neat, RT, 10 min	91

9	2,4,6-Trimethyl	Bi(OTf)3 (1.0)			10		DCM, RT, 2.5 h	929

phenol			HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	94

10	2,6-Di-tert-butyl-4-	Sc(OTf)3 (1.0)			1.5		MeCN, RT, 1 h	954

methylphenol		HClO4-SiO2 (1)		1.5		Neat, RT, 15 min	100

11	Thiophenol		KSF (20 mg/mmol)		2.0		Neat, RT, 5 h		9211

Nafion-H (15 mg/mmol)	2.0		DCM, RT, 2 h		9913

Yttria-zirconia (20% wt)	1.5		MeCN, Reflux, 10 h	9714

HClO4-SiO2 (1)		1.0		Neat, RT, 5 min	93

12	4-Methylthiophenol	Yttria-zirconia (20% wt)	1.5		MeCN, Reflux, 6 h	9414

HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	92

13	-Toluenethiol	Yttria-zirconia (20% wt)	1.5		MeCN, Reflux, 6 h	9714

HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	90

14	2-Nitroaniline		KSF (20 mg/mmol)		2.0		DCM, 40°C, 3.5 h	8711

HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	83

- Reactions with Alcohols with Ac2O:

1	1-Phenylethanol	TaCl5 (10)			1.5		DCM, RT, ?		801

Cu(OTf)2 (2.5)			2.0		DCM, RT, 1 h		927

TMSOTf (2)			1.5		DCM, 0°C, 5 min	955

Sc(OTf)3 (0.1)			1.5		MeCN, 0°C,1 h	954

Bi(OTf)3 (0.1)			1.5		MeCN, RT, 45 min	929

In(OTf)3 (0.1)			1.5		MeCN, RT, 30 min	988

HClO4-SiO2 (1)		1.0		MeCN, RT, 60 min	87

2	2-Phenylethanol	Bi(OTf)3 (0.5)			1.5		DCM, RT, 4 h		929

HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	90

3	Benzoin		Bi(OTf)3 (0.1)			1.5		MeCN, RT, 3 h 	859

HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	82

4	(-) or (+)-Menthol	HSZ (20 mg/mmol)		2.0		Neat, 60°C, 1 h	10012

Nafion-H (15 mg/mmol)	As solvent	Ac2O, RT, 6 h		9613					Yttria-zirconia (20% wt)	1.5		MeCN, Reflux, 6 h	9614

TaCl5 (10)			1.5		DCM, RT, ?		791

Cu(OTf)2 (2.5)			2.0		DCM, RT, 30 min	987

Sc(OTf)3 (1)			1.5		MeCN, 0°C, 15 min	954

Sc(NTf2)3 (1)			1.2		MeCN, 0°C, 60 min	996

Bi(OTf)3 (0.1)			1.5		MeCN, RT, 45 min	859

In(OTf)3 (0.1)			1.5		MeCN, RT, 30 min	958

HClO4-SiO2 (1)		1.0		Neat, RT, 5 min	90

5	Borneol		Bi(OTf)3 (0.5)			10		THF, RT, 7 h		999

HClO4-SiO2 (1)		1.0		Neat, RT, 45 min	92

6	-D-Glucose		K-10 (500 mg/mmol)		As solvent	Ac2O, RT, 6 h		9411

Nafion-H (15 mg/mmol)	As solvent	Ac2O, RT, 14 h	8113

HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	89

7	Linalool		Bi(OTf)3 (0.5)			10		THF, RT, 12 h		889

Cu(OTf)2 (2.5)			2.0		DCM, 0°C, 12 h	797

# TMSOTf (0.5)			5.0		Ac2O, -10°C, 5 min	Nil5

Sc(OTf)3 (2)			As solvent	Ac2O, -20°C, 2.5 h	684

HClO4-SiO2 (1)		1.0		MeCN, RT, 60 min	80

8	Propargyl alcohol	HSZ (20 mg/mmol)		2.0		Neat, 60°C, 1 h	10012

HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	100

# 9	3-Methyl-1-pentyn-	TMSOTf (2)			2.0		DCM, 0°C, 60 min	805

3-ol			HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	100

10	2-Methyl-3-butyn-	HSZ (20 mg/mmol)		2.0		Neat, 60°C, 1 h	9812		2-ol			HClO4-SiO2 (1)		1.0		Neat, RT, 30 min	100

11	1-Methyl-1-		TMSOTf (5)			5		Ac2O, -10°C, 2 min	1005

cyclohexanol		Sc(OTf)3 (1)			5		MeCN, -20°C,5 h	914

HClO4-SiO2 (1)		1.0		MeCN, RT, 30 min	92

12	1-Ethynylcyclo	Bi(OTf)3 (0.5)			10		MeCN, RT, 4 h	949

hexanol		Sc(OTf)3 (0.5)			10		MeCN, RT, 4 h	889

TMSOTf (10)			10		DCM, RT, 2 h		689

HClO4-SiO2 (1)		1.0		MeCN, RT, 15 min	90

13	1-Adamantanol	Sc(OTf)3 (1.0)			1.5		MeCN, RT, 1 h	954

Bi(OTf)3 (0.01)		10		Ac2O, RT, 6 h		989

Sc(OTf)3 (0.5)			10		MeCN, RT, 8.5 h	999

TMSOTf (10)			10		DCM, RT, 3.5 h	949

HClO4-SiO2 (1)		1.0		Neat, RT, 15 min	90

- Reactions with Alcohols with HOAc: 			HOAc

(Equiv)

1	1-Phenylethanol	Cu(OTf)2 (2.5)			2 mL/mmol	HOAc, 65°C, 14 h	947

Sc(OTf)3 (5)			2 mL/mmol	HOAc, 65°C, 2 h	9813

HClO4-SiO2 (1)		5.0		RT, 6 h		90

65°C, 0.5 h		90

2	2-Phenylethanol	Sc(OTf)3 (5)			2 mL/mmol	HOAc, RT, 24 h	9913					HClO4-SiO2 (1)		5.0		RT, 2 h		90

3	Benzylalcohol		Cu(OTf)2 (2.5)			2 mL/mmol	HOAc, RT, 8 h	947

HClO4-SiO2 (1)		5.0		RT, 6 h		94

4	(-) or (+)-Menthol	Cu(OTf)2 (2.5)			2 mL/mmol	HOAc, 65°C, 12 h	967

Sc(OTf)3 (5)			2 mL/mmol	HOAc, 65°C, 24 h	9913

HClO4-SiO2 (1)		5.0		RT, 6 h		97

65°C, 0.5 h		95

5	1-Adamantanol	Sc(OTf)3 (5.0)			5 mL/mmol	HOAc, 110°C, 0.5 h	7113

HClO4-SiO2 (1)		5 mL/mmol	HOAc, 110°C, 0.5 h	80

*Molar equivalent per OH/SH/NH2 group.

The various catalytic methods may be summarized with respect to the amount of acetylating agent, temperature, need to use solvent, reaction time, and cost of the catalyst as follow:

- Amount of Acetylating Agent: The amounts of Ac2O (equivalent) require for the reported catalysts: Sc(OTf)3 (1.5–as solvent); Sc(NTf2)3 (1.2); clays (2.0), zeolite (2.0); Nafion-H (2.0- as solvent); yttria-zirconia (1.1 – as solvent); TMSOTf (1.5-as solvent); Cu(OTf)2 (2.0); Bi(OTf)3 (1.5–10); HClO4-SiO2 (1).

II)	 Reaction Temperature: High temperature is required for the reported catalysts: clays (40-80 °C); zeolite (60 °C); yttria-zirconia (85°C); HClO4-SiO2 (Room temperature).

Low temperature for acid-sensitive substrates: Cu(OTf)2 (0°C); Sc(NTf2)3 (0 °C); Sc(OTf)3 (-20 to -50 °C); TMSOTf (-10 °C); HClO4-SiO2 (Room temperature).

III) 	Requirement of Solvent: The reported catalysts require solvent for acetylation to take place: Sc(OTf)3 (MeCN or Ac2O); Sc(NTf2)3 (MeCN); clays (DCM or CHCl3); Nafion-H (DCM); yttria-zirconia (dry MeCN); TMSOTf (DCM, MeCN/EtOAc, Ac2O); Cu(OTf)2 (MeCN), Bi(OTf)3 (MeCN, THF, Toluene, DCM); HClO4-SiO2 (No solvent is required in general).

IV)	 Reaction Time: The acetylaion with the reported catalysts require longer time: Sc(OTf)3 (0.5-5 h); Sc(NTf2)3 (1 h for acetylation of menthol); clays (2.5 h); zeolite (1.5-12 h); Nafion-H (2-20 h); yttria-zirconia (4-12 h); Cu(OTf)2 (1-2 h); Bi(OTf)3 (1-8.5 h); HClO4-SiO2 (2 – 60 min).

V) 	Cost of the Catalyst: Aldrich (India) 2000-2001 price (US $): In(OTf)3 (50 g, 362.20); Cu(OTf)2 (50 g, 384.80); Sc(OTf)3 (50 g, 1590.00); estimated price (not being commercially available) (US $): Sc(NTf2)3 (50 g, >4896.00); estimated price (not being commercially available) (US $): Bi(OTf)3.xH2O (50 g, >315.95); HClO4 (50 g, ~2.2).

2)	Advantages of HClO4-SiO2 as acetylation catalyst for acid sensitive substrate:

i)	Acetylation of 1-methyl-1-cyclohexanol requires 5 equiv of Ac2O and low temp (-20°C) when the reaction was catalysed by Sc(OTf)3 to suppress dehydration (even under this condition 9 % of the olefinic product was formed). For similarly reason, the TMSOTf catalysed acetylation of the substrate require 5 equiv of Ac2O and low temp (-10°C). In both of these cases prolonged time (5 h) is required. In comparison to these, HClO4-SiO2 enables the reaction to be carried out at room temperature for 30 min with 1 equiv of Ac2O.

ii)	Acetylation of 1-ethynyl-1-cyclohexanol requires 3 equiv of Ac2O and low temp (-20°C) for the reaction to be carried out in the presence of Sc(OTf)3 to avoid dehydration/rearrangement. The Sc(OTf)3 catalysed acylation of the substrate requires 10 equiv of Ac2O in MeCN and prolonged time (4 h). In comparison, HClO4-SiO2 enables the reaction to be carried out at room temperature for 15 min with 1 equiv of Ac2O .

iii)	Acetylation of 1-adamantanol requires treatment with 10 equiv of Ac2O for 6 h for Bi(OTf)3 catalysed reaction to avoid side reaction. In comparison to these, HClO4-SiO2 enables the reaction to be carried out at room temperature for 15 min with 1 equiv of Ac2O in absence of solvent.

iv)	Acetylation of linalool requires the use of Ac2O as solvent for 2.5 h at –20°C for the Sc(OTf)3 catalyzed affording 68 % of the acetylated derivative and 8 % of the rearranged product. Reaction catalyzed by TMSOTf failed to afford the expected product with Ac2O as solvent at –10°C for in 5 min reflecting the disadvantages of TMSOTf with acid-sensitive substrates. In comparison to these, HClO4-SiO2 enables the reaction to be carried out at room temperature for 60 min with 1 equiv of Ac2O in MeCN to afford 80 % yield of the acetate.