Electronic Supplementary Information

Chemical Synthesis of Turbostratic Carbon Nitride, Containing C-N Crystallites, at Atmosphere Pressure

Yu Qiu and Lian Gao*

Experimental details:

The prepared t-CNx solid sublimate almost completely at 800 °C in N2 and NH3 atmosphere.

Table 1. XPS and CHN elemental analysis of turbostratic carbon nitride

| Gas | XPS analysis (at %) |  |  |  |  | Elemental analysis (wt %) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | N | C | O | N/Csurf |  | N | C | H | N/Cbulk |
| N2 | 13.6 | 83.4 | 3.0 | 0.16 |  | 19.67 | 72.68 | 2.09 | 0.23 |
| NH3 | 25.6 | 70.4 | 3.0 | 0.36 |  | 22.31 | 69.21 | 2.51 | 0.28 |

Note: In N2, the surface underwent more severe nitrogen loss than the interior, thus resulted in a lower N/Csurf (0.16) ratio than overall N/Cbulk ratio (0.23). In more active NH3, the nitrogen loss was depressed (N/Cbulk = 0.28). Meanwhile, the adsorption of NH3 increased the surface N concentration (N/Csurf = 0.36) significantly. Elemental analysis also indicates that there should be trace amount of chlorine residue in the prepared samples.

XPS spectra: C(1s) (left panel) and N(1s) (middle and right panel) core level photoemission spectra for N2-treated (bottom) and NH3-treated (top) sample.

Table 2. Comparison of the transmission electron diffraction data with the predictions in Ref. 16. The lattice constants calculated from our data are: a = 6.568 Å, c = 4.706 Å. Note: s, strong; m, medium; w, weak; vw, very weak.

| Observed |  |  | α-C3N4 (predicted) |  |  |
| --- | --- | --- | --- | --- | --- |
| d (Å) | # I |  | d (Å) | (hkl) | # I |
| 3.62 | s |  | 3.60 | 101 | s |
|  |  |  | 3.23 | 110 | s |
|  |  |  | 2.80 | 200 | m |
| 2.43 | s |  | 2.41 | 201 | s |
|  |  |  | 2.17 | 102 | s |
|  |  |  | 2.12 | 210 | s |
| 1.96 | s |  | 1.90 | 112 | s |
|  |  |  | 1.87 | 300 | s |
| 1.72 | s |  | 1.74 | 301 | m |
| 1.52 | m |  | 1.57 | 212 | vw |
| 1.42 | vw |  | 1.48 | 311 | vw |
| 1.29 | w |  | 1.33 | 222 | m |
| 1.21 | vw |  | 1.24 | 321 | m |
|  |  |  | 1.18 | 004 | w |
| 1.08 | vw |  | 1.13 | 322 | m |