Chiral anilines: development of C2-symmetric, late-transition metal catalysts for isospecific 2-butene polymerization

Anna E. Cherian, Emil B. Lobkovsky and Geoffrey W. Coates*

Department of Chemistry and Chemical Biology, Baker Laboratory, Cornell University, Ithaca, New York, 14853-1301, USA. Tel: 607-255-5447; E-mail: gc39@cornell.edu

# SUPPORTING INFORMATION

Molecular structure of the catalyst precursor (S,S,S,S-1a)NiBr2

Table 1.  Crystal data and structure refinement for (S,S,S,S-1a)NiBr2.

Identification code 	anna6

Empirical formula 	(C58 H52 Br2 N2 Ni)6 * (C4 H8 O)3

Formula weight 	1027.73

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)

Unit cell dimensions	a = 26.236(3) Å	= 90°.

b = 15.3526(16) Å	= 99.863(2)°.

c = 39.579(4) Å	 = 90°.

Volume	15707(3) Å3

Z	2

Density (calculated)	1.304 Mg/m3

Absorption coefficient	1.937 mm-1

F(000)	6338

Crystal size	0.40 x 0.15 x 0.10 mm3

Theta range for data collection	0.79 to 20.82°.

Index ranges	-26<=h<=11, -13<=k<=15, -34<=l<=34

Reflections collected	23732

Independent reflections	22121 [R(int) = 0.0475]

Completeness to theta = 20.82°	86.6 %

Absorption correction	SADABS

Max. and min. transmission	0.8299 and 0.5113

Refinement method	Full-matrix-block least-squares on F2

Data / restraints / parameters	22121 / 3457 / 1663

Goodness-of-fit on F2	1.051

Final R indices [I>2sigma(I)]	R1 = 0.0819, wR2 = 0.1976

R indices (all data)	R1 = 0.1176, wR2 = 0.2151

Absolute structure parameter	0.051(13)

Largest diff. peak and hole	2.141 and -0.494 e.Å-3

Table 2.  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2x 103)

for (S,S,S,S-1a)NiBr2.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Ni(1)	6265(1)	344(2)	5472(1)	34(1)

Br(1)	6988(1)	348(2)	5196(1)	49(1)

Br(2)	5822(1)	1638(2)	5523(1)	59(1)

N(1)	5749(5)	-621(8)	5311(4)	24(4)

N(2)	6456(5)	-468(9)	5886(4)	29(4)

Ni(1D)	6844(1)	5435(2)	1118(1)	38(1)

Br(1D)	6048(1)	5345(2)	1313(1)	60(1)

Br(2D)	7274(1)	6753(2)	1089(1)	51(1)

N(1D)	7400(5)	4522(8)	1299(4)	24(4)

N(2D)	6710(5)	4642(8)	705(4)	25(4)

Ni(1E)	10631(1)	5409(2)	7909(1)	35(1)

Br(1E)	9886(1)	5488(2)	8160(1)	45(1)

Br(2E)	11122(1)	6640(2)	7838(1)	57(1)

N(1E)	11102(5)	4429(8)	8109(4)	22(4)

N(2E)	10509(5)	4588(9)	7505(4)	32(4)

Ni(1C)	4138(1)	202(2)	2239(1)	37(1)

Br(1C)	4084(1)	-974(2)	1864(1)	52(1)

Br(2C)	4089(1)	59(2)	2822(1)	47(1)

N(1C)	4750(5)	1028(10)	2192(4)	41(4)

N(2C)	3672(5)	1200(9)	2019(4)	27(4)

Ni(1A)	7812(1)	207(2)	-1036(1)	37(1)

Br(1A)	7921(1)	-1054(2)	-1349(1)	57(1)

Br(2A)	7545(1)	145(2)	-502(1)	44(1)

N(1A)	8430(5)	979(8)	-1042(4)	27(4)

N(2A)	7416(5)	1184(9)	-1338(4)	31(4)

Ni(1B)	8886(1)	5142(2)	4263(1)	35(1)

Br(1B)	8961(1)	5163(2)	3683(1)	54(1)

Br(2B)	8973(1)	3845(2)	4577(1)	49(1)

N(1B)	9302(5)	6067(9)	4554(4)	29(4)

N(2B)	8292(5)	5950(8)	4324(3)	24(4)

C(1)	5794(6)	-1247(11)	5529(4)	23(5)

C(2)	5522(7)	-2106(13)	5552(5)	41(6)

C(3)	5139(6)	-2520(12)	5320(5)	32(5)

C(4)	4964(7)	-3353(14)	5434(5)	49(6)

C(5)	5168(7)	-3687(13)	5771(5)	42(6)

C(6)	5556(6)	-3239(12)	5989(5)	27(5)

C(7)	5810(7)	-3515(13)	6306(5)	36(5)

C(8)	6171(8)	-3026(14)	6488(6)	56(7)

C(9)	6344(7)	-2185(12)	6382(5)	35(5)

C(10)	6105(7)	-1939(13)	6063(6)	41(6)

C(11)	6146(7)	-1162(13)	5847(5)	40(5)

C(12)	5723(7)	-2437(13)	5866(5)	40(6)

C(13)	5379(6)	-674(12)	4985(5)	30(5)

C(14)	5485(6)	-929(12)	4687(5)	30(5)

C(15)	5080(8)	-1057(15)	4395(6)	61(7)

C(16)	4563(7)	-839(12)	4430(5)	36(5)

C(17)	4467(8)	-513(13)	4743(6)	47(6)

C(18)	4834(7)	-419(12)	5025(5)	36(5)

C(19)	4145(8)	-969(16)	4113(6)	75(8)

C(20)	6041(6)	-1200(12)	4642(5)	30(5)

C(21)	6161(7)	-807(12)	4312(6)	54(6)

C(22)	6217(6)	75(13)	4285(6)	58(6)

C(23)	6340(8)	462(19)	3989(6)	102(10)

C(24)	6408(9)	-72(15)	3722(7)	89(9)

C(25)	6341(9)	-960(16)	3720(7)	97(9)

C(26)	6237(8)	-1285(17)	4026(6)	75(8)

C(27)	6088(7)	-2154(12)	4669(5)	45(6)

C(28)	4747(6)	16(11)	5375(5)	32(5)

C(29)	4643(6)	-616(12)	5651(5)	49(6)

C(30)	4251(6)	-1199(10)	5563(5)	50(6)

C(31)	4121(8)	-1749(13)	5816(5)	63(7)

C(32)	4385(7)	-1656(13)	6148(5)	60(7)

C(33)	4801(8)	-1105(14)	6239(6)	79(8)

C(34)	4915(8)	-574(13)	5982(5)	55(7)

C(35)	4305(7)	681(13)	5281(6)	55(7)

C(36)	6850(7)	-378(13)	6184(6)	39(6)

C(37)	6753(7)	149(14)	6444(5)	43(5)

C(38)	7130(6)	189(13)	6731(5)	36(5)

C(39)	7604(7)	-282(13)	6769(6)	44(6)

C(40)	7677(7)	-762(12)	6487(5)	35(5)

C(41)	7310(7)	-792(12)	6197(5)	32(5)

C(42)	8009(8)	-222(14)	7097(6)	60(7)

C(43)	6236(6)	609(12)	6448(5)	35(5)

C(44)	6352(6)	1569(12)	6580(5)	42(6)

C(45)	6136(7)	1917(14)	6848(5)	67(7)

C(46)	6211(8)	2774(14)	6948(6)	91(9)

C(47)	6514(9)	3244(17)	6764(6)	88(9)

C(48)	6741(9)	2954(14)	6495(6)	76(8)

C(49)	6665(8)	2074(13)	6412(6)	68(7)

C(50)	5929(7)	71(13)	6673(5)	51(6)

C(51)	7416(7)	-1255(13)	5875(6)	46(6)

C(52)	7244(5)	-2199(10)	5825(4)	23(5)

C(53)	6954(5)	-2443(11)	5519(4)	41(6)

C(54)	6787(7)	-3291(11)	5485(5)	68(7)

C(55)	6906(7)	-3883(13)	5745(4)	54(6)

C(56)	7196(7)	-3652(11)	6057(5)	43(6)

C(57)	7370(6)	-2803(10)	6083(5)	35(5)

C(58)	8011(7)	-1176(14)	5839(5)	55(6)

C(1D)	7399(6)	3927(11)	1053(4)	17(4)

C(2D)	7691(7)	3086(12)	1052(5)	33(5)

C(3D)	8032(6)	2651(12)	1279(5)	34(5)

C(4D)	8233(8)	1847(14)	1159(6)	51(6)

C(5D)	8073(6)	1535(12)	842(5)	28(5)

C(6D)	7696(7)	2005(12)	591(5)	39(6)

C(7D)	7486(7)	1714(13)	264(5)	41(5)

C(8D)	7097(8)	2214(13)	73(6)	53(6)

C(9D)	6915(6)	3003(11)	187(5)	24(5)

C(10D)	7115(7)	3293(13)	512(5)	38(5)

C(11D)	7023(6)	4021(12)	729(5)	30(5)

C(12D)	7502(7)	2747(12)	726(5)	33(5)

C(13D)	7781(7)	4441(11)	1608(5)	28(5)

C(14D)	7622(7)	4088(13)	1890(6)	41(6)

C(15D)	7979(7)	3943(12)	2170(5)	35(5)

C(16D)	8508(7)	4098(13)	2180(6)	43(6)

C(17D)	8631(7)	4492(12)	1895(5)	36(5)

C(18D)	8296(8)	4678(14)	1610(6)	51(6)

C(19D)	8899(8)	3977(15)	2492(6)	66(7)

C(20D)	7060(7)	3883(14)	1918(6)	48(6)

C(21D)	6872(7)	4344(12)	2218(6)	54(7)

C(22D)	6808(6)	5233(13)	2199(6)	65(7)

C(23D)	6664(8)	5732(17)	2459(6)	97(10)

C(24D)	6610(8)	5253(15)	2744(6)	79(7)

C(25D)	6661(9)	4362(15)	2782(7)	98(10)

C(26D)	6777(9)	3911(18)	2507(6)	85(8)

C(27D)	6958(7)	2942(13)	1922(6)	51(6)

C(28D)	8433(6)	5185(13)	1301(5)	37(5)

C(29D)	8487(6)	4672(10)	974(5)	38(6)

C(30D)	8846(6)	4010(9)	1006(5)	36(5)

C(31D)	8900(6)	3591(11)	706(4)	38(6)

C(32D)	8598(7)	3833(13)	398(5)	65(7)

C(33D)	8257(7)	4529(12)	372(6)	64(7)

C(34D)	8191(7)	4951(12)	670(4)	48(6)

C(35D)	8953(8)	5710(14)	1429(6)	69(7)

C(36D)	6283(7)	4688(12)	399(5)	32(5)

C(37D)	6337(7)	5290(14)	136(5)	43(5)

C(38D)	5944(6)	5268(13)	-146(5)	41(5)

C(39D)	5550(7)	4684(13)	-196(5)	40(6)

C(40D)	5504(8)	4155(14)	93(6)	55(6)

C(41D)	5872(7)	4144(12)	392(5)	36(5)

C(42D)	5165(7)	4691(13)	-531(5)	49(6)

C(43D)	6767(7)	5963(12)	185(5)	38(5)

C(44D)	6531(6)	6911(10)	166(4)	27(5)

C(45D)	6715(6)	7596(9)	-2(4)	36(5)

C(46D)	6499(6)	8408(11)	7(5)	44(6)

C(47D)	6102(7)	8584(14)	181(5)	63(7)

C(48D)	5906(8)	7885(11)	341(5)	56(7)

C(49D)	6137(6)	7083(11)	354(5)	41(6)

C(50D)	7107(7)	5821(13)	-81(5)	52(6)

C(51D)	5808(7)	3555(12)	696(5)	37(5)

C(52D)	5977(5)	2609(11)	669(4)	27(5)

C(53D)	6304(6)	2297(11)	954(4)	45(6)

C(54D)	6455(7)	1439(11)	934(5)	54(6)

C(55D)	6291(8)	934(16)	654(5)	82(8)

C(56D)	5965(9)	1253(14)	374(6)	82(8)

C(57D)	5802(8)	2098(12)	388(5)	57(7)

C(58D)	5216(7)	3584(12)	760(5)	42(6)

C(1E)	11110(6)	3812(12)	7901(5)	34(5)

C(2E)	11372(7)	2942(12)	7903(5)	37(5)

C(3E)	11741(7)	2540(12)	8125(5)	35(5)

C(4E)	11927(7)	1712(13)	8013(5)	39(5)

C(5E)	11729(7)	1342(13)	7695(5)	43(6)

C(6E)	11363(6)	1756(12)	7474(5)	31(5)

C(7E)	11149(7)	1475(13)	7162(5)	43(6)

C(8E)	10800(7)	1952(13)	6937(6)	44(6)

C(9E)	10608(7)	2778(13)	7040(5)	39(6)

C(10E)	10817(6)	3087(12)	7369(5)	31(5)

C(11E)	10759(5)	3885(10)	7568(4)	11(4)

C(12E)	11182(6)	2578(12)	7578(5)	30(5)

C(13E)	11416(8)	4395(13)	8434(6)	50(6)

C(14E)	11281(6)	4131(11)	8730(5)	23(5)

C(15E)	11618(7)	4012(12)	9048(5)	39(5)

C(16E)	12158(7)	4243(12)	9040(5)	32(5)

C(17E)	12321(8)	4588(13)	8748(6)	45(6)

C(18E)	11990(6)	4660(11)	8449(5)	27(5)

C(19E)	12533(7)	4139(14)	9378(5)	49(6)

C(20E)	10709(5)	3822(10)	8733(4)	14(4)

C(21E)	10530(6)	4151(11)	9043(5)	37(5)

C(22E)	10432(6)	5025(12)	9079(6)	58(6)

C(23E)	10258(7)	5358(17)	9368(6)	81(8)

C(24E)	10195(9)	4765(14)	9616(7)	84(9)

C(25E)	10302(9)	3891(15)	9595(6)	90(9)

C(26E)	10464(8)	3592(15)	9304(5)	63(7)

C(27E)	10667(7)	2847(12)	8674(5)	44(6)

C(28E)	12168(7)	5041(12)	8137(5)	39(5)

C(29E)	12372(6)	4312(10)	7917(4)	32(5)

C(30E)	12764(6)	3766(10)	8051(5)	52(6)

C(31E)	12932(7)	3154(12)	7841(5)	57(7)

C(32E)	12707(6)	3049(12)	7506(5)	46(6)

C(33E)	12328(7)	3629(11)	7370(5)	47(6)

C(34E)	12157(6)	4240(10)	7576(4)	24(5)

C(35E)	12562(8)	5759(15)	8228(6)	71(8)

C(36E)	10144(6)	4653(10)	7210(5)	19(4)

C(37E)	10311(6)	5104(13)	6912(5)	38(5)

C(38E)	9959(6)	5111(13)	6586(5)	44(5)

C(39E)	9466(8)	4738(13)	6560(6)	50(6)

C(40E)	9297(7)	4359(12)	6866(5)	39(6)

C(41E)	9635(6)	4362(11)	7167(5)	27(5)

C(42E)	9087(9)	4790(15)	6231(6)	78(8)

C(43E)	10843(7)	5443(14)	6926(5)	51(6)

C(44E)	10850(7)	6254(13)	6717(5)	56(7)

C(45E)	10976(7)	6272(15)	6389(5)	72(8)

C(46E)	10959(7)	7009(12)	6183(6)	57(7)

C(47E)	10795(8)	7780(15)	6305(6)	79(8)

C(48E)	10684(9)	7786(16)	6634(6)	89(9)

C(49E)	10684(7)	7038(12)	6830(6)	54(7)

C(50E)	11188(8)	4702(13)	6819(6)	60(7)

C(51E)	9458(6)	3924(12)	7489(5)	28(5)

C(52E)	9587(6)	2977(11)	7514(4)	32(5)

C(53E)	9862(5)	2646(12)	7812(5)	48(6)

C(54E)	10013(7)	1790(11)	7846(5)	61(7)

C(55E)	9913(7)	1221(13)	7574(4)	49(6)

C(56E)	9594(6)	1516(11)	7282(5)	42(6)

C(57E)	9458(7)	2379(10)	7255(5)	45(6)

C(58E)	8881(6)	4136(12)	7482(5)	35(5)

C(1C)	4536(7)	1776(13)	2078(5)	37(5)

C(2C)	4795(6)	2586(11)	1953(5)	28(5)

C(3C)	5290(7)	2820(12)	1987(5)	37(5)

C(4C)	5405(7)	3667(12)	1850(5)	35(5)

C(5C)	4970(9)	4141(17)	1698(6)	71(8)

C(6C)	4461(8)	3918(14)	1679(5)	49(6)

C(7C)	3990(7)	4361(12)	1529(5)	34(5)

C(8C)	3523(7)	4025(12)	1539(5)	35(5)

C(9C)	3458(7)	3208(11)	1674(5)	29(5)

C(10C)	3888(6)	2744(11)	1809(5)	22(5)

C(11C)	3978(6)	1885(11)	1958(5)	23(5)

C(12C)	4366(6)	3100(11)	1823(5)	27(5)

C(13C)	5252(6)	916(10)	2314(5)	20(4)

C(14C)	5562(7)	543(12)	2092(5)	35(5)

C(15C)	6098(7)	451(13)	2203(5)	42(5)

C(16C)	6332(8)	700(13)	2520(6)	46(6)

C(17C)	6008(8)	1074(14)	2729(6)	56(7)

C(18C)	5497(7)	1144(11)	2621(5)	27(5)

C(19C)	6901(8)	618(16)	2661(6)	81(8)

C(20C)	5342(6)	257(13)	1721(5)	38(5)

C(21C)	5592(6)	-554(11)	1609(4)	31(5)

C(22C)	5481(7)	-1367(11)	1735(5)	66(7)

C(23C)	5668(7)	-2153(14)	1634(5)	65(7)

C(24C)	5989(7)	-2127(13)	1390(5)	54(6)

C(25C)	6122(8)	-1352(11)	1257(6)	66(7)

C(26C)	5903(6)	-597(12)	1358(5)	35(5)

C(27C)	5381(7)	969(12)	1471(5)	39(6)

C(28C)	5175(7)	1541(12)	2877(5)	33(5)

C(29C)	5065(6)	2528(11)	2821(5)	44(6)

C(30C)	5452(7)	3129(10)	2820(4)	37(5)

C(31C)	5342(7)	3999(11)	2768(4)	56(6)

C(32C)	4837(6)	4281(13)	2709(5)	49(6)

C(33C)	4452(8)	3685(11)	2710(5)	59(7)

C(34C)	4561(6)	2816(11)	2762(5)	44(6)

C(35C)	5369(7)	1353(12)	3251(5)	33(5)

C(36C)	3128(6)	1292(10)	1920(5)	16(4)

C(37C)	2830(6)	1535(10)	2150(4)	17(4)

C(38C)	2302(7)	1666(13)	2031(5)	48(6)

C(39C)	2058(7)	1491(12)	1697(5)	39(6)

C(40C)	2396(7)	1202(12)	1485(6)	42(6)

C(41C)	2908(7)	1064(12)	1592(5)	35(5)

C(42C)	1470(7)	1677(14)	1574(5)	54(6)

C(43C)	3026(7)	1719(12)	2523(5)	34(5)

C(44C)	2688(7)	1310(11)	2760(5)	43(6)

C(45C)	2351(6)	1785(15)	2921(4)	67(7)

C(46C)	2022(7)	1350(12)	3107(5)	60(7)

C(47C)	2042(8)	464(13)	3139(6)	69(7)

C(48C)	2358(8)	-22(15)	2973(5)	77(8)

C(49C)	2687(7)	414(11)	2790(5)	48(6)

C(50C)	3135(8)	2705(13)	2581(6)	54(6)

C(51C)	3283(7)	702(13)	1332(5)	44(6)

C(52C)	3500(5)	1429(10)	1146(4)	32(5)

C(53C)	4018(6)	1383(11)	1116(4)	34(5)

C(54C)	4257(7)	2015(10)	947(4)	46(6)

C(55C)	3956(7)	2710(13)	811(5)	63(7)

C(56C)	3434(7)	2785(13)	834(5)	52(6)

C(57C)	3214(7)	2130(10)	1002(5)	42(6)

C(58C)	2958(6)	45(12)	1075(5)	38(5)

C(1A)	8287(6)	1667(11)	-1213(5)	26(5)

C(2A)	8557(6)	2498(11)	-1308(5)	28(5)

C(3A)	9070(7)	2782(12)	-1250(5)	35(5)

C(4A)	9157(8)	3604(14)	-1397(6)	55(7)

C(5A)	8802(7)	4069(13)	-1585(5)	37(5)

C(6A)	8268(7)	3795(12)	-1654(5)	32(5)

C(7A)	7874(8)	4198(14)	-1865(5)	51(6)

C(8A)	7374(7)	3871(12)	-1907(5)	32(5)

C(9A)	7267(7)	3057(13)	-1756(5)	44(6)

C(10A)	7672(6)	2630(12)	-1559(5)	29(5)

C(11A)	7718(7)	1784(13)	-1373(5)	37(5)

C(12A)	8180(7)	2991(12)	-1510(5)	31(5)

C(13A)	8961(6)	929(11)	-865(5)	20(5)

C(14A)	9318(6)	491(12)	-1036(5)	34(5)

C(15A)	9843(6)	491(12)	-864(5)	31(5)

C(16A)	9993(7)	914(12)	-552(5)	32(5)

C(17A)	9643(7)	1285(13)	-385(5)	43(6)

C(18A)	9121(7)	1301(12)	-538(5)	33(5)

C(19A)	10590(8)	878(14)	-393(6)	61(7)

C(20A)	9205(7)	64(13)	-1389(5)	44(6)

C(21A)	9456(8)	-841(14)	-1394(6)	58(7)

C(22A)	9759(9)	-1010(20)	-1646(7)	145(13)

C(23A)	10021(10)	-1799(19)	-1642(7)	123(12)

C(24A)	9912(10)	-2330(20)	-1385(7)	100(10)

C(25A)	9665(11)	-2278(18)	-1103(8)	126(12)

C(26A)	9440(10)	-1451(16)	-1140(7)	95(10)

C(27A)	9312(8)	631(14)	-1649(6)	63(7)

C(28A)	8688(7)	1669(12)	-351(5)	38(5)

C(29A)	8570(5)	2625(10)	-452(4)	27(5)

C(30A)	8945(7)	3253(9)	-478(4)	43(6)

C(31A)	8835(6)	4126(10)	-546(4)	33(5)

C(32A)	8321(5)	4381(11)	-589(5)	36(5)

C(33A)	7938(6)	3786(8)	-565(4)	24(5)

C(34A)	8057(5)	2918(9)	-499(4)	24(5)

C(35A)	8838(7)	1587(13)	60(5)	42(6)

C(36A)	6879(6)	1218(11)	-1532(5)	23(5)

C(37A)	6500(6)	1563(11)	-1356(5)	25(5)

C(38A)	6027(7)	1718(13)	-1550(5)	38(5)

C(39A)	5925(7)	1459(12)	-1903(5)	39(6)

C(40A)	6322(7)	1114(12)	-2039(5)	34(5)

C(41A)	6810(7)	928(12)	-1859(5)	32(5)

C(42A)	5401(7)	1641(13)	-2109(5)	48(6)

C(43A)	6593(6)	1849(11)	-979(5)	26(5)

C(44A)	6152(6)	1575(10)	-806(4)	38(5)

C(45A)	5749(7)	2148(15)	-773(5)	75(8)

C(46A)	5323(9)	1867(14)	-633(5)	94(9)

C(47A)	5331(8)	1005(12)	-527(5)	61(7)

C(48A)	5710(6)	404(14)	-568(5)	65(7)

C(49A)	6130(6)	722(10)	-699(4)	32(5)

C(50A)	6668(7)	2862(11)	-949(5)	35(5)

C(51A)	7212(7)	529(12)	-2011(5)	41(6)

C(52A)	7517(6)	1160(11)	-2201(5)	38(6)

C(53A)	8051(6)	1093(12)	-2132(5)	60(7)

C(54A)	8339(9)	1605(13)	-2316(5)	83(8)

C(55A)	8119(8)	2160(15)	-2574(6)	88(9)

C(56A)	7584(8)	2221(14)	-2618(6)	67(7)

C(57A)	7271(8)	1727(13)	-2444(5)	72(7)

C(58A)	6988(9)	-183(15)	-2264(6)	79(8)

C(1B)	9038(6)	6677(11)	4646(4)	19(4)

C(2B)	9109(6)	7490(11)	4833(5)	22(5)

C(3B)	9522(7)	7860(12)	5028(5)	33(5)

C(4B)	9468(7)	8686(12)	5208(5)	41(6)

C(5B)	8972(8)	8981(15)	5177(6)	56(6)

C(6B)	8534(7)	8639(12)	4980(5)	34(5)

C(7B)	8006(7)	8926(14)	4946(5)	47(6)

C(8B)	7641(8)	8524(13)	4749(5)	50(6)

C(9B)	7734(7)	7697(13)	4591(5)	45(6)

C(10B)	8221(6)	7400(11)	4621(5)	28(5)

C(11B)	8436(6)	6602(11)	4482(4)	19(4)

C(12B)	8601(7)	7858(12)	4819(5)	35(5)

C(13B)	9846(6)	6084(10)	4721(5)	19(4)

C(14B)	10202(6)	6380(11)	4525(5)	27(5)

C(15B)	10725(8)	6499(13)	4680(5)	46(6)

C(16B)	10887(8)	6232(13)	5021(6)	44(6)

C(17B)	10524(7)	5910(12)	5194(6)	43(6)

C(18B)	9987(7)	5791(12)	5036(5)	35(5)

C(19B)	11427(8)	6400(15)	5197(6)	67(7)

C(20B)	10054(6)	6573(11)	4129(5)	26(5)

C(21B)	10397(8)	6109(14)	3919(6)	61(7)

C(22B)	10362(8)	5221(14)	3899(5)	84(8)

C(23B)	10607(10)	4583(18)	3733(7)	120(12)

C(24B)	10937(10)	5093(19)	3578(7)	112(10)

C(25B)	11060(12)	5967(19)	3558(8)	142(13)

C(26B)	10747(10)	6480(20)	3734(7)	135(13)

C(27B)	10036(8)	7583(14)	4076(6)	62(7)

C(28B)	9632(6)	5400(12)	5250(5)	36(5)

C(29B)	9371(7)	5996(12)	5465(5)	51(6)

C(30B)	9687(8)	6497(11)	5711(5)	62(7)

C(31B)	9475(9)	7036(15)	5934(6)	96(9)

C(32B)	8938(9)	7028(17)	5901(7)	100(10)

C(33B)	8607(9)	6566(15)	5659(6)	81(8)

C(34B)	8837(7)	6030(14)	5443(6)	62(7)

C(35B)	9888(8)	4638(14)	5486(6)	66(7)

C(36B)	7761(7)	5912(12)	4160(5)	31(5)

C(37B)	7439(6)	5403(12)	4343(5)	32(5)

C(38B)	6894(8)	5363(15)	4201(5)	59(6)

C(39B)	6716(8)	5774(13)	3887(6)	48(6)

C(40B)	7049(7)	6224(12)	3727(5)	37(5)

C(41B)	7588(7)	6292(12)	3857(5)	34(5)

C(42B)	6122(8)	5674(15)	3732(6)	66(7)

C(43B)	7611(8)	4969(15)	4698(6)	63(7)

C(44B)	7385(9)	3997(18)	4714(7)	88(9)

C(45B)	7087(10)	3970(30)	4976(7)	160(15)

C(46B)	6879(12)	3160(20)	5027(9)	180(17)

C(47B)	7042(11)	2590(20)	4796(8)	102(10)

C(48B)	7327(14)	2500(20)	4533(9)	185(18)

C(49B)	7504(10)	3359(19)	4492(7)	107(10)

C(50B)	7512(9)	5549(17)	4979(6)	81(8)

C(51B)	7932(7)	6756(12)	3658(5)	30(5)

C(52B)	8060(6)	7675(12)	3775(5)	44(6)

C(53B)	8571(6)	7934(11)	3894(4)	39(6)

C(54B)	8691(8)	8764(11)	4014(5)	60(7)

C(55B)	8299(7)	9350(15)	4017(6)	74(8)

C(56B)	7787(7)	9137(12)	3892(5)	60(7)

C(57B)	7679(8)	8290(11)	3785(5)	59(7)

C(58B)	7734(8)	6759(14)	3255(5)	55(6)

O(1S)	9019	7698	-343	202

O(3S)	9514	-3019	7278	143

O(2S)	6063	7616	2917	182

C(1S)	8119	7780	-265	170

C(2S)	8250	7003	-409	166

C(3S)	8736	6993	-515	198

C(5S)	8655	8337	-293	178

C(6S)	6043	8399	2750	207

C(7S)	5513	8643	2779	174

C(8S)	5234	8243	3033	331

C(10S)	5558	7532	3105	265

C(11S)	9185	-2781	7579	232

C(12S)	9229	-1765	7426	297

C(13S)	8966	-2007	7037	179

C(14S)	9316	-2536	6916	178

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for (S,S,S,S-1a)NiBr2.

_____________________________________________________

Ni(1)-N(1) 	2.035(13)

Ni(1)-N(2) 	2.055(14)

Ni(1)-Br(2) 	2.327(3)

Ni(1)-Br(1) 	2.345(3)

N(1)-C(1) 	1.283(17)

N(1)-C(13) 	1.477(18)

N(2)-C(11) 	1.334(19)

N(2)-C(36) 	1.434(19)

Ni(1D)-N(2D) 	2.020(14)

Ni(1D)-N(1D) 	2.061(13)

Ni(1D)-Br(2D) 	2.330(3)

Ni(1D)-Br(1D) 	2.353(3)

N(1D)-C(1D) 	1.334(17)

N(1D)-C(13D) 	1.445(18)

N(2D)-C(11D) 	1.251(18)

N(2D)-C(36D) 	1.505(18)

Ni(1E)-N(2E) 	2.018(15)

Ni(1E)-N(1E) 	2.021(12)

Ni(1E)-Br(2E) 	2.331(3)

Ni(1E)-Br(1E) 	2.341(3)

N(1E)-C(1E) 	1.258(19)

N(1E)-C(13E) 	1.40(2)

N(2E)-C(11E) 	1.265(15)

N(2E)-C(36E) 	1.382(16)

Ni(1C)-N(2C) 	2.057(13)

Ni(1C)-N(1C) 	2.078(15)

Ni(1C)-Br(1C) 	2.324(3)

Ni(1C)-Br(2C) 	2.346(3)

N(1C)-C(1C) 	1.322(19)

N(1C)-C(13C) 	1.336(16)

N(2C)-C(11C) 	1.369(17)

N(2C)-C(36C) 	1.422(15)

Ni(1A)-N(1A) 	2.012(13)

Ni(1A)-N(2A) 	2.082(14)

Ni(1A)-Br(2A) 	2.338(3)

Ni(1A)-Br(1A) 	2.342(3)

N(1A)-C(1A) 	1.274(17)

N(1A)-C(13A) 	1.452(15)

N(2A)-C(11A) 	1.239(19)

N(2A)-C(36A) 	1.484(16)

Ni(1B)-N(1B) 	2.025(13)

Ni(1B)-N(2B) 	2.038(13)

Ni(1B)-Br(2B) 	2.338(3)

Ni(1B)-Br(1B) 	2.339(3)

N(1B)-C(1B) 	1.257(16)

N(1B)-C(13B) 	1.468(15)

N(2B)-C(11B) 	1.206(16)

N(2B)-C(36B) 	1.433(17)

C(1)-C(11) 	1.44(2)

C(1)-C(2) 	1.51(2)

C(2)-C(12) 	1.36(3)

C(2)-C(3) 	1.39(2)

C(3)-C(4) 	1.46(3)

C(4)-C(5) 	1.44(3)

C(5)-C(6) 	1.40(2)

C(6)-C(7) 	1.38(2)

C(6)-C(12) 	1.42(2)

C(7)-C(8) 	1.32(3)

C(8)-C(9) 	1.45(3)

C(9)-C(10) 	1.36(2)

C(10)-C(12) 	1.39(3)

C(10)-C(11) 	1.48(3)

C(13)-C(14) 	1.32(2)

C(13)-C(18) 	1.52(2)

C(14)-C(15) 	1.44(3)

C(14)-C(20) 	1.56(2)

C(15)-C(16) 	1.43(3)

C(16)-C(17) 	1.40(3)

C(16)-C(19) 	1.53(3)

C(17)-C(18) 	1.35(3)

C(18)-C(28) 	1.59(2)

C(20)-C(27) 	1.47(2)

C(20)-C(21) 	1.52(2)

C(21)-C(22) 	1.369(13)

C(21)-C(26) 	1.392(13)

C(22)-C(23) 	1.399(13)

C(23)-C(24) 	1.372(13)

C(24)-C(25) 	1.373(13)

C(25)-C(26) 	1.380(13)

C(28)-C(29) 	1.52(2)

C(28)-C(35) 	1.54(2)

C(29)-C(30) 	1.363(13)

C(29)-C(34) 	1.382(13)

C(30)-C(31) 	1.398(13)

C(31)-C(32) 	1.384(13)

C(32)-C(33) 	1.380(13)

C(33)-C(34) 	1.377(13)

C(36)-C(41) 	1.36(2)

C(36)-C(37) 	1.37(2)

C(37)-C(38) 	1.37(2)

C(37)-C(43) 	1.53(2)

C(38)-C(39) 	1.42(2)

C(39)-C(40) 	1.38(2)

C(39)-C(42) 	1.53(3)

C(40)-C(41) 	1.37(2)

C(41)-C(51) 	1.53(2)

C(43)-C(50) 	1.54(2)

C(43)-C(44) 	1.58(3)

C(44)-C(49) 	1.381(13)

C(44)-C(45) 	1.393(13)

C(45)-C(46) 	1.378(13)

C(46)-C(47) 	1.373(13)

C(47)-C(48) 	1.379(13)

C(48)-C(49) 	1.397(13)

C(51)-C(52) 	1.52(2)

C(51)-C(58) 	1.59(2)

C(52)-C(53) 	1.367(12)

C(52)-C(57) 	1.379(12)

C(53)-C(54) 	1.372(13)

C(54)-C(55) 	1.366(13)

C(55)-C(56) 	1.382(12)

C(56)-C(57) 	1.379(12)

C(1D)-C(11D) 	1.48(2)

C(1D)-C(2D) 	1.50(2)

C(2D)-C(3D) 	1.33(2)

C(2D)-C(12D) 	1.40(2)

C(3D)-C(4D) 	1.45(3)

C(4D)-C(5D) 	1.34(2)

C(5D)-C(6D) 	1.47(2)

C(6D)-C(7D) 	1.39(2)

C(6D)-C(12D) 	1.39(2)

C(7D)-C(8D) 	1.39(3)

C(8D)-C(9D) 	1.40(3)

C(9D)-C(10D) 	1.38(2)

C(10D)-C(11D) 	1.46(2)

C(10D)-C(12D) 	1.47(2)

C(13D)-C(14D) 	1.37(2)

C(13D)-C(18D) 	1.40(3)

C(14D)-C(15D) 	1.34(2)

C(14D)-C(20D) 	1.53(3)

C(15D)-C(16D) 	1.40(2)

C(16D)-C(17D) 	1.37(2)

C(16D)-C(19D) 	1.48(3)

C(17D)-C(18D) 	1.34(3)

C(18D)-C(28D) 	1.54(3)

C(20D)-C(27D) 	1.47(3)

C(20D)-C(21D) 	1.54(3)

C(21D)-C(22D) 	1.376(13)

C(21D)-C(26D) 	1.381(13)

C(22D)-C(23D) 	1.388(13)

C(23D)-C(24D) 	1.376(13)

C(24D)-C(25D) 	1.380(13)

C(25D)-C(26D) 	1.368(13)

C(28D)-C(29D) 	1.54(2)

C(28D)-C(35D) 	1.59(3)

C(29D)-C(30D) 	1.377(12)

C(29D)-C(34D) 	1.386(12)

C(30D)-C(31D) 	1.377(12)

C(31D)-C(32D) 	1.385(12)

C(32D)-C(33D) 	1.386(13)

C(33D)-C(34D) 	1.382(13)

C(36D)-C(41D) 	1.36(2)

C(36D)-C(37D) 	1.42(2)

C(37D)-C(38D) 	1.38(2)

C(37D)-C(43D) 	1.52(2)

C(38D)-C(39D) 	1.36(2)

C(39D)-C(40D) 	1.42(3)

C(39D)-C(42D) 	1.52(3)

C(40D)-C(41D) 	1.39(2)

C(41D)-C(51D) 	1.54(2)

C(43D)-C(50D) 	1.51(2)

C(43D)-C(44D) 	1.58(2)

C(44D)-C(45D) 	1.375(12)

C(44D)-C(49D) 	1.399(12)

C(45D)-C(46D) 	1.372(12)

C(46D)-C(47D) 	1.369(13)

C(47D)-C(48D) 	1.389(13)

C(48D)-C(49D) 	1.370(12)

C(51D)-C(52D) 	1.53(2)

C(51D)-C(58D) 	1.62(2)

C(52D)-C(57D) 	1.373(12)

C(52D)-C(53D) 	1.381(12)

C(53D)-C(54D) 	1.381(12)

C(54D)-C(55D) 	1.360(13)

C(55D)-C(56D) 	1.370(13)

C(56D)-C(57D) 	1.370(13)

C(1E)-C(11E) 	1.48(2)

C(1E)-C(2E) 	1.50(3)

C(2E)-C(3E) 	1.34(2)

C(2E)-C(12E) 	1.41(2)

C(3E)-C(4E) 	1.46(3)

C(4E)-C(5E) 	1.40(2)

C(5E)-C(6E) 	1.35(2)

C(6E)-C(7E) 	1.34(2)

C(6E)-C(12E) 	1.43(2)

C(7E)-C(8E) 	1.37(2)

C(8E)-C(9E) 	1.45(3)

C(9E)-C(10E) 	1.40(2)

C(10E)-C(12E) 	1.39(2)

C(10E)-C(11E) 	1.48(2)

C(13E)-C(14E) 	1.34(2)

C(13E)-C(18E) 	1.55(3)

C(14E)-C(15E) 	1.42(2)

C(14E)-C(20E) 	1.57(2)

C(15E)-C(16E) 	1.47(2)

C(16E)-C(17E) 	1.40(2)

C(16E)-C(19E) 	1.53(2)

C(17E)-C(18E) 	1.35(2)

C(18E)-C(28E) 	1.51(2)

C(20E)-C(21E) 	1.48(2)

C(20E)-C(27E) 	1.52(2)

C(21E)-C(26E) 	1.376(13)

C(21E)-C(22E) 	1.379(13)

C(22E)-C(23E) 	1.399(13)

C(23E)-C(24E) 	1.370(13)

C(24E)-C(25E) 	1.377(13)

C(25E)-C(26E) 	1.373(13)

C(28E)-C(35E) 	1.51(3)

C(28E)-C(29E) 	1.57(2)

C(29E)-C(30E) 	1.361(12)

C(29E)-C(34E) 	1.378(12)

C(30E)-C(31E) 	1.375(12)

C(31E)-C(32E) 	1.366(13)

C(32E)-C(33E) 	1.373(12)

C(33E)-C(34E) 	1.368(12)

C(36E)-C(41E) 	1.39(2)

C(36E)-C(37E) 	1.50(2)

C(37E)-C(38E) 	1.45(2)

C(37E)-C(43E) 	1.48(2)

C(38E)-C(39E) 	1.40(2)

C(39E)-C(40E) 	1.48(3)

C(39E)-C(42E) 	1.50(3)

C(40E)-C(41E) 	1.36(2)

C(41E)-C(51E) 	1.58(2)

C(43E)-C(44E) 	1.49(3)

C(43E)-C(50E) 	1.56(3)

C(44E)-C(49E) 	1.380(13)

C(44E)-C(45E) 	1.395(13)

C(45E)-C(46E) 	1.390(13)

C(46E)-C(47E) 	1.375(13)

C(47E)-C(48E) 	1.380(13)

C(48E)-C(49E) 	1.386(13)

C(51E)-C(52E) 	1.49(2)

C(51E)-C(58E) 	1.54(2)

C(52E)-C(53E) 	1.371(12)

C(52E)-C(57E) 	1.376(12)

C(53E)-C(54E) 	1.372(13)

C(54E)-C(55E) 	1.376(13)

C(55E)-C(56E) 	1.380(12)

C(56E)-C(57E) 	1.372(12)

C(1C)-C(11C) 	1.47(2)

C(1C)-C(2C) 	1.54(3)

C(2C)-C(3C) 	1.33(2)

C(2C)-C(12C) 	1.40(2)

C(3C)-C(4C) 	1.46(2)

C(4C)-C(5C) 	1.40(3)

C(5C)-C(6C) 	1.37(3)

C(6C)-C(12C) 	1.42(3)

C(6C)-C(7C) 	1.45(2)

C(7C)-C(8C) 	1.34(2)

C(8C)-C(9C) 	1.39(2)

C(9C)-C(10C) 	1.36(2)

C(10C)-C(12C) 	1.36(2)

C(10C)-C(11C) 	1.45(2)

C(13C)-C(18C) 	1.32(2)

C(13C)-C(14C) 	1.42(2)

C(14C)-C(15C) 	1.41(2)

C(14C)-C(20C) 	1.55(2)

C(15C)-C(16C) 	1.35(2)

C(16C)-C(17C) 	1.41(3)

C(16C)-C(19C) 	1.51(3)

C(17C)-C(18C) 	1.34(2)

C(18C)-C(28C) 	1.55(2)

C(20C)-C(27C) 	1.49(2)

C(20C)-C(21C) 	1.51(2)

C(21C)-C(26C) 	1.393(12)

C(21C)-C(22C) 	1.394(13)

C(22C)-C(23C) 	1.388(13)

C(23C)-C(24C) 	1.385(13)

C(24C)-C(25C) 	1.371(13)

C(25C)-C(26C) 	1.381(13)

C(28C)-C(35C) 	1.51(2)

C(28C)-C(29C) 	1.55(2)

C(29C)-C(30C) 	1.372(12)

C(29C)-C(34C) 	1.376(12)

C(30C)-C(31C) 	1.375(13)

C(31C)-C(32C) 	1.374(12)

C(32C)-C(33C) 	1.363(13)

C(33C)-C(34C) 	1.373(13)

C(36C)-C(37C) 	1.35(2)

C(36C)-C(41C) 	1.37(2)

C(37C)-C(38C) 	1.40(2)

C(37C)-C(43C) 	1.50(2)

C(38C)-C(39C) 	1.39(3)

C(39C)-C(40C) 	1.39(2)

C(39C)-C(42C) 	1.56(2)

C(40C)-C(41C) 	1.35(2)

C(41C)-C(51C) 	1.64(3)

C(43C)-C(44C) 	1.53(2)

C(43C)-C(50C) 	1.55(3)

C(44C)-C(49C) 	1.382(13)

C(44C)-C(45C) 	1.384(13)

C(45C)-C(46C) 	1.396(13)

C(46C)-C(47C) 	1.367(13)

C(47C)-C(48C) 	1.365(13)

C(48C)-C(49C) 	1.389(13)

C(51C)-C(52C) 	1.50(2)

C(51C)-C(58C) 	1.58(2)

C(52C)-C(57C) 	1.380(12)

C(52C)-C(53C) 	1.386(12)

C(53C)-C(54C) 	1.387(12)

C(54C)-C(55C) 	1.381(13)

C(55C)-C(56C) 	1.393(13)

C(56C)-C(57C) 	1.385(13)

C(1A)-C(11A) 	1.53(2)

C(1A)-C(2A) 	1.54(2)

C(2A)-C(12A) 	1.38(2)

C(2A)-C(3A) 	1.40(2)

C(3A)-C(4A) 	1.42(3)

C(4A)-C(5A) 	1.30(2)

C(5A)-C(6A) 	1.44(2)

C(6A)-C(7A) 	1.36(2)

C(6A)-C(12A) 	1.40(2)

C(7A)-C(8A) 	1.39(2)

C(8A)-C(9A) 	1.43(3)

C(9A)-C(10A) 	1.37(2)

C(10A)-C(12A) 	1.43(2)

C(10A)-C(11A) 	1.49(3)

C(13A)-C(18A) 	1.41(2)

C(13A)-C(14A) 	1.41(2)

C(14A)-C(15A) 	1.43(2)

C(14A)-C(20A) 	1.53(2)

C(15A)-C(16A) 	1.39(2)

C(16A)-C(17A) 	1.35(2)

C(16A)-C(19A) 	1.59(2)

C(17A)-C(18A) 	1.40(2)

C(18A)-C(28A) 	1.56(2)

C(20A)-C(27A) 	1.41(2)

C(20A)-C(21A) 	1.54(3)

C(21A)-C(26A) 	1.381(13)

C(21A)-C(22A) 	1.400(13)

C(22A)-C(23A) 	1.395(14)

C(23A)-C(24A) 	1.375(14)

C(24A)-C(25A) 	1.386(14)

C(25A)-C(26A) 	1.397(14)

C(28A)-C(29A) 	1.54(2)

C(28A)-C(35A) 	1.61(2)

C(29A)-C(30A) 	1.392(12)

C(29A)-C(34A) 	1.401(12)

C(30A)-C(31A) 	1.387(12)

C(31A)-C(32A) 	1.387(12)

C(32A)-C(33A) 	1.374(12)

C(33A)-C(34A) 	1.384(12)

C(36A)-C(41A) 	1.35(2)

C(36A)-C(37A) 	1.41(2)

C(37A)-C(38A) 	1.36(2)

C(37A)-C(43A) 	1.53(2)

C(38A)-C(39A) 	1.43(2)

C(39A)-C(40A) 	1.36(2)

C(39A)-C(42A) 	1.50(2)

C(40A)-C(41A) 	1.39(2)

C(41A)-C(51A) 	1.44(2)

C(43A)-C(44A) 	1.50(2)

C(43A)-C(50A) 	1.57(2)

C(44A)-C(49A) 	1.380(12)

C(44A)-C(45A) 	1.400(13)

C(45A)-C(46A) 	1.398(13)

C(46A)-C(47A) 	1.388(13)

C(47A)-C(48A) 	1.387(13)

C(48A)-C(49A) 	1.387(12)

C(51A)-C(58A) 	1.53(3)

C(51A)-C(52A) 	1.53(2)

C(52A)-C(57A) 	1.373(13)

C(52A)-C(53A) 	1.383(13)

C(53A)-C(54A) 	1.381(13)

C(54A)-C(55A) 	1.380(13)

C(55A)-C(56A) 	1.387(13)

C(56A)-C(57A) 	1.387(13)

C(1B)-C(2B) 	1.45(2)

C(1B)-C(11B) 	1.60(2)

C(2B)-C(3B) 	1.34(2)

C(2B)-C(12B) 	1.44(2)

C(3B)-C(4B) 	1.47(2)

C(4B)-C(5B) 	1.36(2)

C(5B)-C(6B) 	1.38(2)

C(6B)-C(12B) 	1.38(2)

C(6B)-C(7B) 	1.44(2)

C(7B)-C(8B) 	1.29(2)

C(8B)-C(9B) 	1.45(3)

C(9B)-C(10B) 	1.34(2)

C(10B)-C(12B) 	1.35(2)

C(10B)-C(11B) 	1.49(2)

C(13B)-C(18B) 	1.32(2)

C(13B)-C(14B) 	1.39(2)

C(14B)-C(15B) 	1.42(2)

C(14B)-C(20B) 	1.58(2)

C(15B)-C(16B) 	1.41(3)

C(16B)-C(17B) 	1.36(3)

C(16B)-C(19B) 	1.49(3)

C(17B)-C(18B) 	1.45(2)

C(18B)-C(28B) 	1.49(2)

C(20B)-C(21B) 	1.50(3)

C(20B)-C(27B) 	1.56(3)

C(21B)-C(22B) 	1.368(13)

C(21B)-C(26B) 	1.392(14)

C(22B)-C(23B) 	1.399(13)

C(23B)-C(24B) 	1.387(13)

C(24B)-C(25B) 	1.385(14)

C(25B)-C(26B) 	1.403(14)

C(28B)-C(29B) 	1.49(2)

C(28B)-C(35B) 	1.57(3)

C(29B)-C(34B) 	1.391(13)

C(29B)-C(30B) 	1.395(13)

C(30B)-C(31B) 	1.394(13)

C(31B)-C(32B) 	1.393(13)

C(32B)-C(33B) 	1.374(13)

C(33B)-C(34B) 	1.395(13)

C(36B)-C(41B) 	1.34(2)

C(36B)-C(37B) 	1.43(2)

C(37B)-C(38B) 	1.45(2)

C(37B)-C(43B) 	1.55(3)

C(38B)-C(39B) 	1.40(3)

C(39B)-C(40B) 	1.35(3)

C(39B)-C(42B) 	1.58(3)

C(40B)-C(41B) 	1.42(2)

C(41B)-C(51B) 	1.48(2)

C(43B)-C(50B) 	1.48(3)

C(43B)-C(44B) 	1.61(3)

C(44B)-C(49B) 	1.387(13)

C(44B)-C(45B) 	1.400(14)

C(45B)-C(46B) 	1.395(14)

C(46B)-C(47B) 	1.387(14)

C(47B)-C(48B) 	1.389(14)

C(48B)-C(49B) 	1.414(14)

C(51B)-C(52B) 	1.51(2)

C(51B)-C(58B) 	1.59(2)

C(52B)-C(57B) 	1.381(13)

C(52B)-C(53B) 	1.399(12)

C(53B)-C(54B) 	1.377(13)

C(54B)-C(55B) 	1.369(13)

C(55B)-C(56B) 	1.387(13)

C(56B)-C(57B) 	1.383(13)

O(1S)-C(5S) 	1.4071

O(1S)-C(3S) 	1.4196

O(3S)-C(14S) 	1.6171

O(3S)-C(11S) 	1.6285

O(2S)-C(6S) 	1.3670

O(2S)-C(10S) 	1.6312

C(1S)-C(2S) 	1.3894

C(1S)-C(5S) 	1.6648

C(2S)-C(3S) 	1.4121

C(6S)-C(7S) 	1.4628

C(7S)-C(8S) 	1.4768

C(8S)-C(10S) 	1.3830

C(11S)-C(12S) 	1.6850

C(12S)-C(13S) 	1.6180

C(13S)-C(14S) 	1.3736

N(1)-Ni(1)-N(2)	82.3(5)

N(1)-Ni(1)-Br(2)	109.5(4)

N(2)-Ni(1)-Br(2)	120.4(4)

N(1)-Ni(1)-Br(1)	113.8(4)

N(2)-Ni(1)-Br(1)	105.5(4)

Br(2)-Ni(1)-Br(1)	119.62(13)

C(1)-N(1)-C(13)	121.1(10)

C(1)-N(1)-Ni(1)	110.9(8)

C(13)-N(1)-Ni(1)	127.9(8)

C(11)-N(2)-C(36)	120.8(11)

C(11)-N(2)-Ni(1)	109.4(8)

C(36)-N(2)-Ni(1)	129.8(8)

N(2D)-Ni(1D)-N(1D)	83.5(5)

N(2D)-Ni(1D)-Br(2D)	120.2(4)

N(1D)-Ni(1D)-Br(2D)	106.7(4)

N(2D)-Ni(1D)-Br(1D)	100.8(4)

N(1D)-Ni(1D)-Br(1D)	117.5(4)

Br(2D)-Ni(1D)-Br(1D)	122.13(13)

C(1D)-N(1D)-C(13D)	118.3(10)

C(1D)-N(1D)-Ni(1D)	107.4(7)

C(13D)-N(1D)-Ni(1D)	134.2(8)

C(11D)-N(2D)-C(36D)	119.1(11)

C(11D)-N(2D)-Ni(1D)	112.1(8)

C(36D)-N(2D)-Ni(1D)	128.8(8)

N(2E)-Ni(1E)-N(1E)	81.3(5)

N(2E)-Ni(1E)-Br(2E)	115.3(4)

N(1E)-Ni(1E)-Br(2E)	109.7(4)

N(2E)-Ni(1E)-Br(1E)	109.7(4)

N(1E)-Ni(1E)-Br(1E)	111.8(4)

Br(2E)-Ni(1E)-Br(1E)	121.85(13)

C(1E)-N(1E)-C(13E)	119.9(12)

C(1E)-N(1E)-Ni(1E)	112.5(8)

C(13E)-N(1E)-Ni(1E)	127.6(8)

C(11E)-N(2E)-C(36E)	119.3(11)

C(11E)-N(2E)-Ni(1E)	111.8(9)

C(36E)-N(2E)-Ni(1E)	128.1(9)

N(2C)-Ni(1C)-N(1C)	85.4(5)

N(2C)-Ni(1C)-Br(1C)	110.0(4)

N(1C)-Ni(1C)-Br(1C)	112.4(4)

N(2C)-Ni(1C)-Br(2C)	110.9(4)

N(1C)-Ni(1C)-Br(2C)	108.6(4)

Br(1C)-Ni(1C)-Br(2C)	123.18(13)

C(1C)-N(1C)-C(13C)	124.8(11)

C(1C)-N(1C)-Ni(1C)	105.7(8)

C(13C)-N(1C)-Ni(1C)	128.2(9)

C(11C)-N(2C)-C(36C)	117.8(9)

C(11C)-N(2C)-Ni(1C)	108.8(7)

C(36C)-N(2C)-Ni(1C)	133.3(8)

N(1A)-Ni(1A)-N(2A)	83.7(5)

N(1A)-Ni(1A)-Br(2A)	113.7(4)

N(2A)-Ni(1A)-Br(2A)	110.6(4)

N(1A)-Ni(1A)-Br(1A)	108.0(4)

N(2A)-Ni(1A)-Br(1A)	112.6(4)

Br(2A)-Ni(1A)-Br(1A)	121.80(13)

C(1A)-N(1A)-C(13A)	118.0(9)

C(1A)-N(1A)-Ni(1A)	109.4(8)

C(13A)-N(1A)-Ni(1A)	132.2(8)

C(11A)-N(2A)-C(36A)	119.0(11)

C(11A)-N(2A)-Ni(1A)	109.6(8)

C(36A)-N(2A)-Ni(1A)	131.1(8)

N(1B)-Ni(1B)-N(2B)	81.7(5)

N(1B)-Ni(1B)-Br(2B)	107.5(4)

N(2B)-Ni(1B)-Br(2B)	117.6(4)

N(1B)-Ni(1B)-Br(1B)	114.9(4)

N(2B)-Ni(1B)-Br(1B)	107.6(4)

Br(2B)-Ni(1B)-Br(1B)	121.10(13)

C(1B)-N(1B)-C(13B)	113.5(9)

C(1B)-N(1B)-Ni(1B)	114.6(8)

C(13B)-N(1B)-Ni(1B)	131.1(8)

C(11B)-N(2B)-C(36B)	117.6(10)

C(11B)-N(2B)-Ni(1B)	112.7(8)

C(36B)-N(2B)-Ni(1B)	128.7(8)

N(1)-C(1)-C(11)	119.6(14)

N(1)-C(1)-C(2)	134.8(14)

C(11)-C(1)-C(2)	105.4(15)

C(12)-C(2)-C(3)	123.6(19)

C(12)-C(2)-C(1)	105.5(16)

C(3)-C(2)-C(1)	130.8(18)

C(2)-C(3)-C(4)	115.3(18)

C(5)-C(4)-C(3)	120.8(19)

C(6)-C(5)-C(4)	120.8(19)

C(7)-C(6)-C(5)	126.7(18)

C(7)-C(6)-C(12)	116.6(17)

C(5)-C(6)-C(12)	116.7(18)

C(8)-C(7)-C(6)	121(2)

C(7)-C(8)-C(9)	125(2)

C(10)-C(9)-C(8)	113.3(18)

C(9)-C(10)-C(12)	123(2)

C(9)-C(10)-C(11)	133.6(18)

C(12)-C(10)-C(11)	103.7(18)

N(2)-C(11)-C(1)	117.6(16)

N(2)-C(11)-C(10)	132.8(16)

C(1)-C(11)-C(10)	109.5(16)

C(2)-C(12)-C(10)	116(2)

C(2)-C(12)-C(6)	122.8(18)

C(10)-C(12)-C(6)	121.4(19)

C(14)-C(13)-N(1)	126.2(15)

C(14)-C(13)-C(18)	121.2(17)

N(1)-C(13)-C(18)	112.6(16)

C(13)-C(14)-C(15)	121.3(18)

C(13)-C(14)-C(20)	121.9(16)

C(15)-C(14)-C(20)	116.5(18)

C(16)-C(15)-C(14)	118(2)

C(17)-C(16)-C(15)	119.2(19)

C(17)-C(16)-C(19)	123.9(18)

C(15)-C(16)-C(19)	117(2)

C(18)-C(17)-C(16)	124(2)

C(17)-C(18)-C(13)	116(2)

C(17)-C(18)-C(28)	125.2(18)

C(13)-C(18)-C(28)	118.6(16)

C(27)-C(20)-C(21)	115.4(17)

C(27)-C(20)-C(14)	109.2(15)

C(21)-C(20)-C(14)	109.2(15)

C(22)-C(21)-C(26)	115(2)

C(22)-C(21)-C(20)	120(2)

C(26)-C(21)-C(20)	124.7(19)

C(21)-C(22)-C(23)	122(2)

C(24)-C(23)-C(22)	118(3)

C(23)-C(24)-C(25)	124(3)

C(24)-C(25)-C(26)	113(3)

C(25)-C(26)-C(21)	127(3)

C(29)-C(28)-C(35)	112.0(15)

C(29)-C(28)-C(18)	115.3(15)

C(35)-C(28)-C(18)	106.5(15)

C(30)-C(29)-C(34)	121(2)

C(30)-C(29)-C(28)	117.1(17)

C(34)-C(29)-C(28)	121.7(17)

C(29)-C(30)-C(31)	119(2)

C(32)-C(31)-C(30)	118(2)

C(33)-C(32)-C(31)	124(2)

C(34)-C(33)-C(32)	116(2)

C(33)-C(34)-C(29)	122(2)

C(41)-C(36)-C(37)	121.8(18)

C(41)-C(36)-N(2)	119.8(18)

C(37)-C(36)-N(2)	118.4(15)

C(36)-C(37)-C(38)	116.7(18)

C(36)-C(37)-C(43)	123.9(17)

C(38)-C(37)-C(43)	119.1(19)

C(37)-C(38)-C(39)	124(2)

C(40)-C(39)-C(38)	115.2(18)

C(40)-C(39)-C(42)	123.0(18)

C(38)-C(39)-C(42)	121.7(19)

C(41)-C(40)-C(39)	121.5(18)

C(36)-C(41)-C(40)	121(2)

C(36)-C(41)-C(51)	118.4(17)

C(40)-C(41)-C(51)	120.9(17)

C(37)-C(43)-C(50)	108.0(15)

C(37)-C(43)-C(44)	108.1(14)

C(50)-C(43)-C(44)	113.6(16)

C(49)-C(44)-C(45)	120(2)

C(49)-C(44)-C(43)	117.5(18)

C(45)-C(44)-C(43)	122.1(18)

C(46)-C(45)-C(44)	122(2)

C(47)-C(46)-C(45)	115(3)

C(46)-C(47)-C(48)	127(3)

C(47)-C(48)-C(49)	116(3)

C(44)-C(49)-C(48)	120(2)

C(52)-C(51)-C(41)	117.4(16)

C(52)-C(51)-C(58)	109.5(15)

C(41)-C(51)-C(58)	111.1(15)

C(53)-C(52)-C(57)	120.0(16)

C(53)-C(52)-C(51)	118.9(15)

C(57)-C(52)-C(51)	121.1(15)

C(52)-C(53)-C(54)	117.7(18)

C(55)-C(54)-C(53)	122(2)

C(54)-C(55)-C(56)	121(2)

C(57)-C(56)-C(55)	115.8(18)

C(56)-C(57)-C(52)	123.0(17)

N(1D)-C(1D)-C(11D)	118.8(13)

N(1D)-C(1D)-C(2D)	130.7(14)

C(11D)-C(1D)-C(2D)	110.2(14)

C(3D)-C(2D)-C(12D)	121.7(18)

C(3D)-C(2D)-C(1D)	135.5(18)

C(12D)-C(2D)-C(1D)	102.8(15)

C(2D)-C(3D)-C(4D)	116.4(19)

C(5D)-C(4D)-C(3D)	122(2)

C(4D)-C(5D)-C(6D)	121.6(19)

C(7D)-C(6D)-C(12D)	120.5(18)

C(7D)-C(6D)-C(5D)	125.9(18)

C(12D)-C(6D)-C(5D)	113.0(18)

C(8D)-C(7D)-C(6D)	118(2)

C(7D)-C(8D)-C(9D)	124(2)

C(10D)-C(9D)-C(8D)	119.0(18)

C(9D)-C(10D)-C(11D)	136.5(17)

C(9D)-C(10D)-C(12D)	118.1(18)

C(11D)-C(10D)-C(12D)	105.3(17)

N(2D)-C(11D)-C(10D)	135.4(15)

N(2D)-C(11D)-C(1D)	118.1(15)

C(10D)-C(11D)-C(1D)	106.5(15)

C(6D)-C(12D)-C(2D)	124.2(17)

C(6D)-C(12D)-C(10D)	120.4(18)

C(2D)-C(12D)-C(10D)	115.0(18)

C(14D)-C(13D)-C(18D)	121.8(18)

C(14D)-C(13D)-N(1D)	117.5(14)

C(18D)-C(13D)-N(1D)	120.7(18)

C(15D)-C(14D)-C(13D)	118.1(18)

C(15D)-C(14D)-C(20D)	117(2)

C(13D)-C(14D)-C(20D)	124.8(17)

C(14D)-C(15D)-C(16D)	123(2)

C(17D)-C(16D)-C(15D)	115.1(18)

C(17D)-C(16D)-C(19D)	121.3(19)

C(15D)-C(16D)-C(19D)	123(2)

C(18D)-C(17D)-C(16D)	125(2)

C(17D)-C(18D)-C(13D)	116(2)

C(17D)-C(18D)-C(28D)	124.5(19)

C(13D)-C(18D)-C(28D)	118.9(18)

C(27D)-C(20D)-C(14D)	112.5(17)

C(27D)-C(20D)-C(21D)	111.1(18)

C(14D)-C(20D)-C(21D)	113.7(16)

C(22D)-C(21D)-C(26D)	119(2)

C(22D)-C(21D)-C(20D)	118(2)

C(26D)-C(21D)-C(20D)	123(2)

C(21D)-C(22D)-C(23D)	123(2)

C(24D)-C(23D)-C(22D)	113(3)

C(23D)-C(24D)-C(25D)	127(3)

C(26D)-C(25D)-C(24D)	116(3)

C(25D)-C(26D)-C(21D)	121(3)

C(29D)-C(28D)-C(18D)	118.3(17)

C(29D)-C(28D)-C(35D)	109.2(15)

C(18D)-C(28D)-C(35D)	107.9(16)

C(30D)-C(29D)-C(34D)	125.4(19)

C(30D)-C(29D)-C(28D)	117.5(15)

C(34D)-C(29D)-C(28D)	117.0(15)

C(29D)-C(30D)-C(31D)	115.9(18)

C(30D)-C(31D)-C(32D)	120.3(18)

C(33D)-C(32D)-C(31D)	123(2)

C(34D)-C(33D)-C(32D)	118(2)

C(33D)-C(34D)-C(29D)	117.6(19)

C(41D)-C(36D)-C(37D)	124.4(17)

C(41D)-C(36D)-N(2D)	117.7(16)

C(37D)-C(36D)-N(2D)	117.8(14)

C(38D)-C(37D)-C(36D)	114.9(17)

C(38D)-C(37D)-C(43D)	123.6(19)

C(36D)-C(37D)-C(43D)	121.2(16)

C(39D)-C(38D)-C(37D)	125(2)

C(38D)-C(39D)-C(40D)	115.2(19)

C(38D)-C(39D)-C(42D)	119.9(19)

C(40D)-C(39D)-C(42D)	124.6(18)

C(41D)-C(40D)-C(39D)	123.2(19)

C(36D)-C(41D)-C(40D)	116(2)

C(36D)-C(41D)-C(51D)	122.5(17)

C(40D)-C(41D)-C(51D)	121.3(17)

C(50D)-C(43D)-C(37D)	109.1(16)

C(50D)-C(43D)-C(44D)	111.9(16)

C(37D)-C(43D)-C(44D)	110.3(14)

C(45D)-C(44D)-C(49D)	117.8(16)

C(45D)-C(44D)-C(43D)	124.2(15)

C(49D)-C(44D)-C(43D)	117.9(14)

C(46D)-C(45D)-C(44D)	120.0(18)

C(47D)-C(46D)-C(45D)	123(2)

C(46D)-C(47D)-C(48D)	117(2)

C(49D)-C(48D)-C(47D)	121(2)

C(48D)-C(49D)-C(44D)	120.8(18)

C(52D)-C(51D)-C(41D)	115.6(16)

C(52D)-C(51D)-C(58D)	109.7(14)

C(41D)-C(51D)-C(58D)	110.1(15)

C(57D)-C(52D)-C(53D)	122.6(17)

C(57D)-C(52D)-C(51D)	122.6(16)

C(53D)-C(52D)-C(51D)	114.8(15)

C(52D)-C(53D)-C(54D)	115.3(18)

C(55D)-C(54D)-C(53D)	122(2)

C(54D)-C(55D)-C(56D)	121(2)

C(55D)-C(56D)-C(57D)	118(2)

C(56D)-C(57D)-C(52D)	121(2)

N(1E)-C(1E)-C(11E)	116.6(14)

N(1E)-C(1E)-C(2E)	136.7(16)

C(11E)-C(1E)-C(2E)	106.6(15)

C(3E)-C(2E)-C(12E)	121.2(18)

C(3E)-C(2E)-C(1E)	133.6(19)

C(12E)-C(2E)-C(1E)	105.0(16)

C(2E)-C(3E)-C(4E)	116.3(19)

C(5E)-C(4E)-C(3E)	122.5(18)

C(6E)-C(5E)-C(4E)	120(2)

C(7E)-C(6E)-C(5E)	126(2)

C(7E)-C(6E)-C(12E)	116.2(17)

C(5E)-C(6E)-C(12E)	117.7(18)

C(6E)-C(7E)-C(8E)	124(2)

C(7E)-C(8E)-C(9E)	121(2)

C(10E)-C(9E)-C(8E)	117.1(18)

C(12E)-C(10E)-C(9E)	118.7(18)

C(12E)-C(10E)-C(11E)	105.6(16)

C(9E)-C(10E)-C(11E)	135.6(17)

N(2E)-C(11E)-C(10E)	134.3(14)

N(2E)-C(11E)-C(1E)	117.6(13)

C(10E)-C(11E)-C(1E)	107.9(14)

C(10E)-C(12E)-C(2E)	114.8(17)

C(10E)-C(12E)-C(6E)	123.4(18)

C(2E)-C(12E)-C(6E)	121.8(17)

C(14E)-C(13E)-N(1E)	127.6(17)

C(14E)-C(13E)-C(18E)	116.5(18)

N(1E)-C(13E)-C(18E)	115.9(18)

C(13E)-C(14E)-C(15E)	126.5(17)

C(13E)-C(14E)-C(20E)	119.4(16)

C(15E)-C(14E)-C(20E)	113.8(17)

C(14E)-C(15E)-C(16E)	114.0(18)

C(17E)-C(16E)-C(15E)	122.7(18)

C(17E)-C(16E)-C(19E)	121.3(17)

C(15E)-C(16E)-C(19E)	115.9(18)

C(18E)-C(17E)-C(16E)	120.9(19)

C(17E)-C(18E)-C(28E)	120.4(17)

C(17E)-C(18E)-C(13E)	119(2)

C(28E)-C(18E)-C(13E)	120.5(16)

C(21E)-C(20E)-C(27E)	116.1(15)

C(21E)-C(20E)-C(14E)	110.1(13)

C(27E)-C(20E)-C(14E)	109.9(13)

C(26E)-C(21E)-C(22E)	119(2)

C(26E)-C(21E)-C(20E)	120.6(17)

C(22E)-C(21E)-C(20E)	120.6(18)

C(21E)-C(22E)-C(23E)	122(2)

C(24E)-C(23E)-C(22E)	116(2)

C(23E)-C(24E)-C(25E)	124(3)

C(26E)-C(25E)-C(24E)	118(3)

C(25E)-C(26E)-C(21E)	121(2)

C(18E)-C(28E)-C(35E)	112.6(17)

C(18E)-C(28E)-C(29E)	111.1(15)

C(35E)-C(28E)-C(29E)	111.7(15)

C(30E)-C(29E)-C(34E)	119.1(17)

C(30E)-C(29E)-C(28E)	122.1(15)

C(34E)-C(29E)-C(28E)	118.8(14)

C(29E)-C(30E)-C(31E)	119.1(19)

C(32E)-C(31E)-C(30E)	122(2)

C(31E)-C(32E)-C(33E)	118(2)

C(34E)-C(33E)-C(32E)	120.0(19)

C(33E)-C(34E)-C(29E)	121.2(17)

N(2E)-C(36E)-C(41E)	126.4(16)

N(2E)-C(36E)-C(37E)	116.5(12)

C(41E)-C(36E)-C(37E)	117.1(15)

C(38E)-C(37E)-C(43E)	118.7(18)

C(38E)-C(37E)-C(36E)	118.5(16)

C(43E)-C(37E)-C(36E)	122.3(16)

C(39E)-C(38E)-C(37E)	120(2)

C(38E)-C(39E)-C(40E)	120.3(19)

C(38E)-C(39E)-C(42E)	120(2)

C(40E)-C(39E)-C(42E)	119.1(18)

C(41E)-C(40E)-C(39E)	118.4(18)

C(40E)-C(41E)-C(36E)	125.3(19)

C(40E)-C(41E)-C(51E)	118.0(16)

C(36E)-C(41E)-C(51E)	116.5(15)

C(37E)-C(43E)-C(44E)	111.9(16)

C(37E)-C(43E)-C(50E)	108.7(17)

C(44E)-C(43E)-C(50E)	113.4(18)

C(49E)-C(44E)-C(45E)	115(2)

C(49E)-C(44E)-C(43E)	121(2)

C(45E)-C(44E)-C(43E)	123.9(19)

C(46E)-C(45E)-C(44E)	125(2)

C(47E)-C(46E)-C(45E)	118(2)

C(46E)-C(47E)-C(48E)	118(3)

C(47E)-C(48E)-C(49E)	123(3)

C(44E)-C(49E)-C(48E)	121(2)

C(52E)-C(51E)-C(58E)	114.7(14)

C(52E)-C(51E)-C(41E)	111.9(14)

C(58E)-C(51E)-C(41E)	108.5(14)

C(53E)-C(52E)-C(57E)	114.9(17)

C(53E)-C(52E)-C(51E)	119.9(15)

C(57E)-C(52E)-C(51E)	125.2(15)

C(52E)-C(53E)-C(54E)	122.6(19)

C(53E)-C(54E)-C(55E)	121(2)

C(54E)-C(55E)-C(56E)	117.0(19)

C(57E)-C(56E)-C(55E)	119.6(19)

C(56E)-C(57E)-C(52E)	123.9(18)

N(1C)-C(1C)-C(11C)	123.4(15)

N(1C)-C(1C)-C(2C)	128.8(14)

C(11C)-C(1C)-C(2C)	105.9(15)

C(3C)-C(2C)-C(12C)	126.4(18)

C(3C)-C(2C)-C(1C)	131.5(17)

C(12C)-C(2C)-C(1C)	101.7(15)

C(2C)-C(3C)-C(4C)	117.7(17)

C(5C)-C(4C)-C(3C)	114.6(18)

C(6C)-C(5C)-C(4C)	128(2)

C(5C)-C(6C)-C(12C)	115.9(19)

C(5C)-C(6C)-C(7C)	131(2)

C(12C)-C(6C)-C(7C)	112.7(17)

C(8C)-C(7C)-C(6C)	122(2)

C(7C)-C(8C)-C(9C)	122.4(18)

C(10C)-C(9C)-C(8C)	118.4(17)

C(12C)-C(10C)-C(9C)	120.1(17)

C(12C)-C(10C)-C(11C)	105.4(14)

C(9C)-C(10C)-C(11C)	134.5(16)

N(2C)-C(11C)-C(10C)	135.4(13)

N(2C)-C(11C)-C(1C)	115.9(14)

C(10C)-C(11C)-C(1C)	108.7(14)

C(10C)-C(12C)-C(2C)	117.8(17)

C(10C)-C(12C)-C(6C)	124.4(16)

C(2C)-C(12C)-C(6C)	117.5(16)

C(18C)-C(13C)-N(1C)	126.5(17)

C(18C)-C(13C)-C(14C)	116.0(16)

N(1C)-C(13C)-C(14C)	117.5(14)

C(15C)-C(14C)-C(13C)	119.8(17)

C(15C)-C(14C)-C(20C)	117.2(17)

C(13C)-C(14C)-C(20C)	123.0(15)

C(16C)-C(15C)-C(14C)	122(2)

C(15C)-C(16C)-C(17C)	116(2)

C(15C)-C(16C)-C(19C)	126(2)

C(17C)-C(16C)-C(19C)	118(2)

C(18C)-C(17C)-C(16C)	121(2)

C(13C)-C(18C)-C(17C)	125(2)

C(13C)-C(18C)-C(28C)	118.1(16)

C(17C)-C(18C)-C(28C)	116.7(17)

C(27C)-C(20C)-C(21C)	109.0(15)

C(27C)-C(20C)-C(14C)	111.4(16)

C(21C)-C(20C)-C(14C)	113.8(14)

C(26C)-C(21C)-C(22C)	113.5(18)

C(26C)-C(21C)-C(20C)	126.0(16)

C(22C)-C(21C)-C(20C)	120.3(17)

C(23C)-C(22C)-C(21C)	125(2)

C(24C)-C(23C)-C(22C)	118(2)

C(25C)-C(24C)-C(23C)	121(2)

C(24C)-C(25C)-C(26C)	118(2)

C(25C)-C(26C)-C(21C)	124.6(19)

C(35C)-C(28C)-C(29C)	110.5(15)

C(35C)-C(28C)-C(18C)	115.9(15)

C(29C)-C(28C)-C(18C)	113.5(15)

C(30C)-C(29C)-C(34C)	118.2(17)

C(30C)-C(29C)-C(28C)	122.5(15)

C(34C)-C(29C)-C(28C)	119.2(15)

C(29C)-C(30C)-C(31C)	121.2(18)

C(32C)-C(31C)-C(30C)	120.1(18)

C(33C)-C(32C)-C(31C)	118.8(19)

C(32C)-C(33C)-C(34C)	121(2)

C(33C)-C(34C)-C(29C)	120.5(18)

C(37C)-C(36C)-C(41C)	120.8(16)

C(37C)-C(36C)-N(2C)	120.8(14)

C(41C)-C(36C)-N(2C)	118.3(16)

C(36C)-C(37C)-C(38C)	117.7(17)

C(36C)-C(37C)-C(43C)	125.1(15)

C(38C)-C(37C)-C(43C)	117.2(17)

C(39C)-C(38C)-C(37C)	124(2)

C(40C)-C(39C)-C(38C)	113.3(19)

C(40C)-C(39C)-C(42C)	124.4(19)

C(38C)-C(39C)-C(42C)	122.1(19)

C(41C)-C(40C)-C(39C)	124(2)

C(40C)-C(41C)-C(36C)	119.3(19)

C(40C)-C(41C)-C(51C)	121.9(18)

C(36C)-C(41C)-C(51C)	118.7(16)

C(37C)-C(43C)-C(44C)	112.8(14)

C(37C)-C(43C)-C(50C)	110.6(16)

C(44C)-C(43C)-C(50C)	114.9(16)

C(49C)-C(44C)-C(45C)	118(2)

C(49C)-C(44C)-C(43C)	118.1(17)

C(45C)-C(44C)-C(43C)	123.3(16)

C(44C)-C(45C)-C(46C)	119(2)

C(47C)-C(46C)-C(45C)	121(2)

C(48C)-C(47C)-C(46C)	121(2)

C(47C)-C(48C)-C(49C)	118(2)

C(44C)-C(49C)-C(48C)	122(2)

C(52C)-C(51C)-C(58C)	111.6(16)

C(52C)-C(51C)-C(41C)	112.0(15)

C(58C)-C(51C)-C(41C)	107.8(15)

C(57C)-C(52C)-C(53C)	118.4(17)

C(57C)-C(52C)-C(51C)	123.9(15)

C(53C)-C(52C)-C(51C)	117.7(14)

C(52C)-C(53C)-C(54C)	122.5(17)

C(55C)-C(54C)-C(53C)	117.0(19)

C(54C)-C(55C)-C(56C)	123(2)

C(57C)-C(56C)-C(55C)	117.9(19)

C(52C)-C(57C)-C(56C)	121.5(18)

N(1A)-C(1A)-C(11A)	119.7(14)

N(1A)-C(1A)-C(2A)	135.4(13)

C(11A)-C(1A)-C(2A)	104.9(14)

C(12A)-C(2A)-C(3A)	119.8(18)

C(12A)-C(2A)-C(1A)	106.4(14)

C(3A)-C(2A)-C(1A)	133.7(16)

C(2A)-C(3A)-C(4A)	115.2(17)

C(5A)-C(4A)-C(3A)	125(2)

C(4A)-C(5A)-C(6A)	122(2)

C(7A)-C(6A)-C(12A)	119.4(18)

C(7A)-C(6A)-C(5A)	126.5(19)

C(12A)-C(6A)-C(5A)	113.8(16)

C(6A)-C(7A)-C(8A)	121(2)

C(7A)-C(8A)-C(9A)	120.9(18)

C(10A)-C(9A)-C(8A)	117.9(18)

C(9A)-C(10A)-C(12A)	120.5(18)

C(9A)-C(10A)-C(11A)	133.5(17)

C(12A)-C(10A)-C(11A)	106.0(15)

N(2A)-C(11A)-C(10A)	134.9(15)

N(2A)-C(11A)-C(1A)	117.6(15)

C(10A)-C(11A)-C(1A)	107.5(15)

C(2A)-C(12A)-C(6A)	124.6(16)

C(2A)-C(12A)-C(10A)	115.2(17)

C(6A)-C(12A)-C(10A)	120.2(16)

C(18A)-C(13A)-C(14A)	121.0(16)

C(18A)-C(13A)-N(1A)	122.0(15)

C(14A)-C(13A)-N(1A)	117.0(14)

C(13A)-C(14A)-C(15A)	115.8(17)

C(13A)-C(14A)-C(20A)	126.9(16)

C(15A)-C(14A)-C(20A)	117.2(16)

C(16A)-C(15A)-C(14A)	121.7(17)

C(17A)-C(16A)-C(15A)	121.5(18)

C(17A)-C(16A)-C(19A)	121.9(18)

C(15A)-C(16A)-C(19A)	116.4(17)

C(16A)-C(17A)-C(18A)	120(2)

C(17A)-C(18A)-C(13A)	120.1(18)

C(17A)-C(18A)-C(28A)	122.7(18)

C(13A)-C(18A)-C(28A)	117.1(16)

C(27A)-C(20A)-C(14A)	111.7(18)

C(27A)-C(20A)-C(21A)	114.0(18)

C(14A)-C(20A)-C(21A)	112.6(16)

C(26A)-C(21A)-C(22A)	119(3)

C(26A)-C(21A)-C(20A)	122(2)

C(22A)-C(21A)-C(20A)	118(2)

C(23A)-C(22A)-C(21A)	119(3)

C(24A)-C(23A)-C(22A)	111(3)

C(23A)-C(24A)-C(25A)	138(3)

C(24A)-C(25A)-C(26A)	103(3)

C(21A)-C(26A)-C(25A)	129(3)

C(29A)-C(28A)-C(18A)	110.6(15)

C(29A)-C(28A)-C(35A)	109.8(15)

C(18A)-C(28A)-C(35A)	112.2(15)

C(30A)-C(29A)-C(34A)	116.3(15)

C(30A)-C(29A)-C(28A)	124.5(13)

C(34A)-C(29A)-C(28A)	119.1(13)

C(31A)-C(30A)-C(29A)	123.9(16)

C(30A)-C(31A)-C(32A)	117.5(16)

C(33A)-C(32A)-C(31A)	120.8(16)

C(32A)-C(33A)-C(34A)	120.6(15)

C(33A)-C(34A)-C(29A)	121.0(15)

C(41A)-C(36A)-C(37A)	127.2(16)

C(41A)-C(36A)-N(2A)	116.3(15)

C(37A)-C(36A)-N(2A)	116.5(15)

C(38A)-C(37A)-C(36A)	116.0(18)

C(38A)-C(37A)-C(43A)	118.4(17)

C(36A)-C(37A)-C(43A)	125.3(15)

C(37A)-C(38A)-C(39A)	120.0(19)

C(40A)-C(39A)-C(38A)	117.9(18)

C(40A)-C(39A)-C(42A)	123.4(19)

C(38A)-C(39A)-C(42A)	118.6(17)

C(39A)-C(40A)-C(41A)	125(2)

C(36A)-C(41A)-C(40A)	112.9(18)

C(36A)-C(41A)-C(51A)	123.6(17)

C(40A)-C(41A)-C(51A)	123.4(19)

C(44A)-C(43A)-C(37A)	110.9(14)

C(44A)-C(43A)-C(50A)	109.9(15)

C(37A)-C(43A)-C(50A)	110.6(15)

C(49A)-C(44A)-C(45A)	119.7(18)

C(49A)-C(44A)-C(43A)	118.8(15)

C(45A)-C(44A)-C(43A)	121.4(16)

C(46A)-C(45A)-C(44A)	121(2)

C(47A)-C(46A)-C(45A)	116(2)

C(48A)-C(47A)-C(46A)	125(2)

C(47A)-C(48A)-C(49A)	116(2)

C(44A)-C(49A)-C(48A)	121.8(18)

C(41A)-C(51A)-C(58A)	110.6(17)

C(41A)-C(51A)-C(52A)	114.8(16)

C(58A)-C(51A)-C(52A)	107.7(17)

C(57A)-C(52A)-C(53A)	121.7(19)

C(57A)-C(52A)-C(51A)	121.4(16)

C(53A)-C(52A)-C(51A)	116.8(16)

C(54A)-C(53A)-C(52A)	119(2)

C(55A)-C(54A)-C(53A)	123(2)

C(54A)-C(55A)-C(56A)	115(2)

C(57A)-C(56A)-C(55A)	125(2)

C(52A)-C(57A)-C(56A)	117(2)

N(1B)-C(1B)-C(2B)	139.7(13)

N(1B)-C(1B)-C(11B)	112.5(12)

C(2B)-C(1B)-C(11B)	107.5(13)

C(3B)-C(2B)-C(12B)	120.5(17)

C(3B)-C(2B)-C(1B)	132.8(16)

C(12B)-C(2B)-C(1B)	106.3(14)

C(2B)-C(3B)-C(4B)	120.4(17)

C(5B)-C(4B)-C(3B)	114.4(18)

C(4B)-C(5B)-C(6B)	128(2)

C(5B)-C(6B)-C(12B)	115.6(18)

C(5B)-C(6B)-C(7B)	129(2)

C(12B)-C(6B)-C(7B)	114.8(17)

C(8B)-C(7B)-C(6B)	121(2)

C(7B)-C(8B)-C(9B)	121(2)

C(10B)-C(9B)-C(8B)	119.1(19)

C(9B)-C(10B)-C(12B)	118.1(19)

C(9B)-C(10B)-C(11B)	131.3(17)

C(12B)-C(10B)-C(11B)	110.6(15)

N(2B)-C(11B)-C(10B)	140.0(14)

N(2B)-C(11B)-C(1B)	118.1(13)

C(10B)-C(11B)-C(1B)	101.5(13)

C(10B)-C(12B)-C(6B)	125.2(18)

C(10B)-C(12B)-C(2B)	113.9(18)

C(6B)-C(12B)-C(2B)	120.8(16)

C(18B)-C(13B)-C(14B)	122.4(17)

C(18B)-C(13B)-N(1B)	121.0(16)

C(14B)-C(13B)-N(1B)	116.6(14)

C(13B)-C(14B)-C(15B)	119.5(18)

C(13B)-C(14B)-C(20B)	123.0(15)

C(15B)-C(14B)-C(20B)	117.5(17)

C(16B)-C(15B)-C(14B)	119(2)

C(17B)-C(16B)-C(15B)	118(2)

C(17B)-C(16B)-C(19B)	121(2)

C(15B)-C(16B)-C(19B)	120(2)

C(16B)-C(17B)-C(18B)	123(2)

C(13B)-C(18B)-C(17B)	117.3(19)

C(13B)-C(18B)-C(28B)	125.1(17)

C(17B)-C(18B)-C(28B)	117.5(18)

C(21B)-C(20B)-C(27B)	113.8(17)

C(21B)-C(20B)-C(14B)	113.1(15)

C(27B)-C(20B)-C(14B)	108.4(15)

C(22B)-C(21B)-C(26B)	115(3)

C(22B)-C(21B)-C(20B)	118(2)

C(26B)-C(21B)-C(20B)	128(2)

C(21B)-C(22B)-C(23B)	134(3)

C(24B)-C(23B)-C(22B)	101(3)

C(25B)-C(24B)-C(23B)	138(3)

C(24B)-C(25B)-C(26B)	111(3)

C(21B)-C(26B)-C(25B)	122(3)

C(18B)-C(28B)-C(29B)	117.9(16)

C(18B)-C(28B)-C(35B)	113.0(16)

C(29B)-C(28B)-C(35B)	108.1(16)

C(34B)-C(29B)-C(30B)	120(2)

C(34B)-C(29B)-C(28B)	122.9(17)

C(30B)-C(29B)-C(28B)	117.4(17)

C(31B)-C(30B)-C(29B)	121(2)

C(32B)-C(31B)-C(30B)	116(2)

C(33B)-C(32B)-C(31B)	125(3)

C(32B)-C(33B)-C(34B)	116(2)

C(29B)-C(34B)-C(33B)	121(2)

C(41B)-C(36B)-N(2B)	122.7(17)

C(41B)-C(36B)-C(37B)	123.4(17)

N(2B)-C(36B)-C(37B)	113.9(15)

C(36B)-C(37B)-C(38B)	117.1(17)

C(36B)-C(37B)-C(43B)	125.9(16)

C(38B)-C(37B)-C(43B)	116.7(17)

C(39B)-C(38B)-C(37B)	119(2)

C(40B)-C(39B)-C(38B)	120(2)

C(40B)-C(39B)-C(42B)	122.7(19)

C(38B)-C(39B)-C(42B)	117.2(19)

C(39B)-C(40B)-C(41B)	123(2)

C(36B)-C(41B)-C(40B)	117.0(19)

C(36B)-C(41B)-C(51B)	122.8(17)

C(40B)-C(41B)-C(51B)	120.1(17)

C(50B)-C(43B)-C(37B)	111.1(19)

C(50B)-C(43B)-C(44B)	114(2)

C(37B)-C(43B)-C(44B)	112.5(17)

C(49B)-C(44B)-C(45B)	132(3)

C(49B)-C(44B)-C(43B)	120(3)

C(45B)-C(44B)-C(43B)	108(3)

C(46B)-C(45B)-C(44B)	114(3)

C(47B)-C(46B)-C(45B)	107(3)

C(46B)-C(47B)-C(48B)	145(4)

C(47B)-C(48B)-C(49B)	103(3)

C(44B)-C(49B)-C(48B)	118(3)

C(41B)-C(51B)-C(52B)	114.4(16)

C(41B)-C(51B)-C(58B)	114.3(15)

C(52B)-C(51B)-C(58B)	108.8(15)

C(57B)-C(52B)-C(53B)	116.9(18)

C(57B)-C(52B)-C(51B)	121.6(15)

C(53B)-C(52B)-C(51B)	121.5(15)

C(54B)-C(53B)-C(52B)	122.0(18)

C(55B)-C(54B)-C(53B)	119(2)

C(54B)-C(55B)-C(56B)	122(2)

C(57B)-C(56B)-C(55B)	118(2)

C(52B)-C(57B)-C(56B)	123(2)

C(5S)-O(1S)-C(3S)	106.7

C(14S)-O(3S)-C(11S)	114.5

C(6S)-O(2S)-C(10S)	108.9

C(2S)-C(1S)-C(5S)	98.2

C(1S)-C(2S)-C(3S)	115.6

C(2S)-C(3S)-O(1S)	105.8

O(1S)-C(5S)-C(1S)	104.6

O(2S)-C(6S)-C(7S)	98.4

C(6S)-C(7S)-C(8S)	122.4

C(10S)-C(8S)-C(7S)	96.2

C(8S)-C(10S)-O(2S)	111.3

O(3S)-C(11S)-C(12S)	82.4

C(13S)-C(12S)-C(11S)	94.9

C(14S)-C(13S)-C(12S)	105.4

C(13S)-C(14S)-O(3S)	95.4

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4.   Anisotropic displacement parameters (Å2x 103)for (S,S,S,S-1a)NiBr2.  The anisotropic

displacement factor exponent takes the form: -22[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Ni(1)	44(1) 	23(2)	36(2) 	4(1)	9(1) 	-2(1)

Br(1)	65(1) 	36(1)	54(2) 	7(1)	27(1) 	-1(1)

Br(2)	73(2) 	29(1)	73(2) 	-6(1)	4(1) 	15(1)

Ni(1D)	49(2) 	28(2)	37(2) 	1(1)	11(1) 	4(1)

Br(1D)	61(1) 	47(2)	80(2) 	-2(2)	34(1) 	2(1)

Br(2D)	57(1) 	32(1)	59(2) 	0(1)	-1(1) 	-4(1)

Ni(1E)	52(2) 	22(2)	31(2) 	-1(1)	10(1) 	2(1)

Br(1E)	51(1) 	38(1)	49(2) 	-4(1)	19(1) 	5(1)

Br(2E)	75(2) 	33(1)	62(2) 	5(1)	6(1) 	-13(1)

Ni(1C)	40(1) 	26(2)	46(2) 	5(2)	12(1) 	-2(1)

Br(1C)	45(1) 	36(1)	75(2) 	-16(1)	4(1) 	-2(1)

Br(2C)	44(1) 	46(1)	54(2) 	16(1)	12(1) 	-1(1)

Ni(1A)	35(1) 	23(1)	53(2) 	2(2)	9(1) 	1(1)

Br(1A)	49(1) 	37(1)	82(2) 	-14(1)	3(1) 	4(1)

Br(2A)	37(1) 	43(1)	56(2) 	10(1)	17(1) 	2(1)

Ni(1B)	30(1) 	29(2)	49(2) 	0(2)	13(1) 	2(1)

Br(1B)	81(2) 	37(1)	51(2) 	0(1)	34(1) 	6(1)

Br(2B)	60(1) 	33(1)	55(2) 	8(1)	9(1) 	0(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2x 103) for (S,S,S,S-1a)NiBr2.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(3A)	5002	-2276	5103	39

H(4A)	4712	-3680	5285	59

H(5A)	5036	-4217	5845	51

H(7A)	5725	-4062	6394	43

H(8A)	6329	-3240	6706	68

H(9A)	6599	-1841	6521	42

H(15A)	5156	-1282	4186	74

H(17A)	4122	-347	4759	56

H(19A)	3808	-793	4167	113

H(19B)	4132	-1584	4046	113

H(19C)	4226	-612	3924	113

H(20A)	6288	-943	4837	36

H(22A)	6172	436	4472	69

H(23A)	6375	1076	3973	122

H(24A)	6507	189	3526	107

H(25A)	6365	-1315	3527	116

H(26A)	6214	-1900	4043	90

H(27A)	6431	-2331	4627	68

H(27B)	5821	-2426	4498	68

H(27C)	6045	-2340	4899	68

H(28A)	5068	349	5469	38

H(30A)	4070	-1230	5333	60

H(31A)	3857	-2176	5762	76

H(32A)	4273	-1992	6324	72

H(33A)	4997	-1093	6465	95

H(34A)	5189	-166	6034	66

H(35A)	4236	968	5490	82

H(35B)	3992	379	5169	82

H(35C)	4405	1119	5124	82

H(38A)	7071	552	6915	44

H(40A)	7989	-1080	6494	41

H(42A)	7877	143	7265	89

H(42B)	8328	35	7042	89

H(42C)	8084	-807	7192	89

H(43A)	6037	629	6209	41

H(45A)	5931	1553	6966	81

H(46A)	6064	3020	7130	110

H(47A)	6574	3836	6828	106

H(48A)	6937	3327	6375	91

H(49A)	6828	1822	6238	82

H(50A)	5876	-520	6579	77

H(50B)	5594	347	6676	77

H(50C)	6124	41	6907	77

H(51A)	7218	-926	5676	55

H(53A)	6871	-2040	5335	49

H(54A)	6583	-3472	5275	82

H(55A)	6787	-4466	5710	65

H(56A)	7272	-4053	6241	52

H(57A)	7586	-2626	6289	42

H(58A)	8068	-1473	5630	83

H(58B)	8225	-1448	6038	83

H(58C)	8104	-560	5828	83

H(3DA)	8138	2855	1507	40

H(4DA)	8487	1531	1311	61

H(5DA)	8208	996	779	34

H(7DA)	7604	1191	174	49

H(8DA)	6946	2009	-148	63

H(9DA)	6659	3331	43	29

H(15E)	7869	3725	2370	42

H(17E)	8983	4646	1900	44

H(19M)	9241	4137	2444	99

H(19N)	8902	3366	2564	99

H(19O)	8813	4348	2676	99

H(20E)	6843	4115	1704	57

H(22E)	6865	5520	1996	78

H(23E)	6609	6343	2442	116

H(24E)	6530	5568	2935	94

H(25E)	6617	4076	2988	118

H(26E)	6793	3293	2515	102

H(27M)	6591	2844	1930	77

H(27N)	7169	2680	2125	77

H(27O)	7045	2674	1715	77

H(28E)	8154	5626	1234	44

H(30E)	9044	3851	1221	44

H(31E)	9146	3135	710	45

H(32E)	8838	3949	236	78

H(32F)	8393	3315	311	78

H(33E)	8073	4710	155	77

H(34E)	7950	5415	666	57

H(35M)	8916	6054	1632	103

H(35N)	9023	6100	1246	103

H(35O)	9241	5299	1487	103

H(38E)	5951	5697	-318	49

H(40E)	5208	3792	81	66

H(42M)	4907	4232	-526	73

H(42N)	5349	4587	-723	73

H(42O)	4992	5259	-561	73

H(43E)	6981	5879	417	46

H(45E)	6992	7507	-125	44

H(46E)	6631	8870	-112	53

H(47E)	5968	9156	191	76

H(48E)	5606	7965	442	67

H(49E)	6028	6638	492	49

H(50M)	7249	5229	-59	78

H(50N)	7391	6243	-46	78

H(50O)	6902	5898	-311	78

H(51E)	6027	3807	904	44

H(53E)	6416	2647	1150	54

H(54E)	6681	1193	1123	65

H(55E)	6406	348	652	99

H(56E)	5855	901	178	98

H(57E)	5565	2333	201	68

H(58M)	5182	3222	959	64

H(58N)	4987	3362	557	64

H(58O)	5122	4186	803	64

H(3EA)	11874	2782	8343	42

H(4EA)	12192	1412	8162	47

H(5EA)	11855	793	7635	51

H(7EA)	11243	915	7092	51

H(8EA)	10684	1738	6712	53

H(9EA)	10352	3098	6891	47

H(15F)	11503	3801	9248	47

H(17F)	12669	4772	8761	54

H(19P)	12876	4347	9349	74

H(19C)	12554	3524	9444	74

H(19R)	12409	4481	9557	74

H(20F)	10488	4104	8532	17

H(22F)	10485	5414	8901	69

H(23F)	10188	5961	9390	97

H(24F)	10071	4969	9813	101

H(25F)	10264	3505	9777	109

H(26F)	10532	2988	9282	75

H(27P)	10310	2661	8673	66

H(27C)	10897	2545	8859	66

H(27R)	10768	2705	8454	66

H(28F)	11858	5308	7992	47

H(30F)	12920	3808	8285	62

H(31F)	13215	2790	7933	68

H(32G)	12810	2590	7371	55

H(33F)	12185	3605	7133	57

H(34F)	11885	4622	7481	29

H(35P)	12427	6193	8372	106

H(35C)	12631	6038	8018	106

H(35R)	12884	5512	8354	106

H(38F)	10063	5367	6390	52

H(40F)	8961	4119	6853	46

H(42P)	8761	4518	6262	117

H(42C)	9228	4485	6050	117

H(42R)	9026	5402	6167	117

H(43F)	10982	5596	7170	61

H(45F)	11083	5741	6300	86

H(46F)	11058	6980	5964	69

H(47F)	10759	8291	6168	95

H(48F)	10604	8326	6730	106

H(49F)	10569	7066	7045	65

H(50P)	11153	4181	6956	90

H(50C)	11550	4891	6858	90

H(50R)	11077	4567	6575	90

H(51F)	9657	4211	7698	34

H(53F)	9952	3025	8003	57

H(54F)	10190	1587	8061	73

H(55F)	10056	652	7586	59

H(56F)	9471	1123	7101	50

H(57F)	9263	2576	7044	54

H(58P)	8768	3882	7684	53

H(58C)	8675	3892	7273	53

H(58R)	8834	4769	7484	53

H(3CA)	5558	2449	2095	45

H(4CA)	5748	3880	1864	42

H(5CA)	5036	4679	1595	86

H(7CA)	4014	4907	1419	41

H(8CA)	3225	4357	1449	42

H(9CA)	3122	2977	1674	34

H(15D)	6303	206	2050	50

H(17D)	6154	1280	2951	67

H(19J)	7080	375	2484	122

H(19K)	6949	232	2861	122

H(19L)	7043	1195	2729	122

H(20D)	4966	126	1711	46

H(22D)	5262	-1384	1903	79

H(23D)	5579	-2690	1728	78

H(24D)	6120	-2656	1314	65

H(25D)	6358	-1334	1100	80

H(26D)	5970	-69	1248	43

H(27J)	5232	772	1240	59

H(27K)	5745	1122	1479	59

H(27L)	5191	1480	1530	59

H(28D)	4829	1252	2824	40

H(30D)	5802	2940	2857	44

H(31D)	5616	4407	2772	68

H(32D)	4758	4880	2669	59

H(33D)	4103	3875	2673	70

H(34D)	4286	2411	2757	53

H(35J)	5417	724	3283	50

H(35K)	5115	1561	3388	50

H(35L)	5699	1652	3324	50

H(38D)	2098	1887	2188	57

H(40D)	2258	1096	1251	50

H(42J)	1310	1840	1771	81

H(42K)	1302	1153	1466	81

H(42L)	1430	2154	1407	81

H(43D)	3370	1423	2579	41

H(45D)	2343	2403	2906	80

H(46D)	1783	1673	3213	71

H(47D)	1831	182	3279	83

H(48D)	2353	-640	2982	92

H(49D)	2919	83	2682	57

H(50J)	3364	2907	2426	80

H(50K)	3302	2803	2819	80

H(50L)	2808	3027	2535	80

H(51D)	3577	377	1471	53

H(53D)	4217	901	1214	41

H(54D)	4612	1972	927	55

H(55D)	4112	3155	697	76

H(56D)	3236	3269	738	63

H(57D)	2857	2164	1018	50

H(58J)	3178	-201	923	57

H(58K)	2666	353	939	57

H(58L)	2827	-425	1205	57

H(3AA)	9342	2450	-1122	42

H(4AA)	9499	3830	-1354	66

H(5AA)	8897	4602	-1680	44

H(7AA)	7942	4709	-1986	62

H(8AA)	7098	4192	-2037	38

H(9AA)	6928	2821	-1791	53

H(15B)	10097	194	-965	37

H(17B)	9750	1535	-165	52

H(19D)	10649	1184	-173	92

H(19E)	10790	1158	-550	92

H(19F)	10698	269	-358	92

H(20B)	8823	-38	-1437	53

H(22B)	9786	-585	-1817	174

H(23B)	10246	-1949	-1797	148

H(24B)	10042	-2904	-1408	120

H(25B)	9653	-2697	-928	151

H(26B)	9251	-1286	-966	115

H(27D)	9140	1191	-1630	94

H(27E)	9185	372	-1874	94

H(27F)	9687	723	-1623	94

H(28B)	8366	1321	-427	45

H(30B)	9296	3072	-447	51

H(31B)	9103	4533	-562	40

H(32B)	8233	4974	-636	44

H(33B)	7588	3972	-594	28

H(34B)	7787	2514	-486	28

H(35D)	8555	1818	167	63

H(35E)	9154	1921	141	63

H(35F)	8896	974	124	63

H(38B)	5765	1999	-1451	46

H(40B)	6259	990	-2278	41

H(42D)	5176	1882	-1959	72

H(42E)	5252	1098	-2212	72

H(42F)	5434	2061	-2290	72

H(43B)	6916	1561	-859	31

H(45B)	5764	2735	-847	90

H(46B)	5043	2245	-612	113

H(47B)	5055	812	-418	73

H(48B)	5683	-193	-510	78

H(49B)	6411	343	-716	39

H(50D)	6735	3031	-707	53

H(50E)	6354	3154	-1065	53

H(50F)	6962	3035	-1057	53

H(51B)	7461	248	-1823	49

H(53B)	8215	704	-1961	72

H(54B)	8705	1574	-2262	100

H(55B)	8318	2476	-2711	105

H(56B)	7419	2632	-2781	80

H(57B)	6904	1778	-2490	87

H(58D)	6799	-606	-2147	119

H(58E)	7269	-478	-2351	119

H(58F)	6751	80	-2455	119

H(3BA)	9851	7586	5051	40

H(4BA)	9755	8988	5334	49

H(5BA)	8923	9484	5308	67

H(7BA)	7926	9419	5072	57

H(8BA)	7304	8773	4705	60

H(9BA)	7454	7371	4469	54

H(15C)	10964	6757	4555	56

H(17C)	10625	5755	5428	52

H(19G)	11628	6645	5033	100

H(19H)	11585	5852	5289	100

H(19I)	11423	6813	5386	100

H(20C)	9695	6349	4053	31

H(22C)	10117	4987	4026	101

H(23C)	10561	3969	3727	144

H(24C)	11135	4746	3449	134

H(25C)	11320	6189	3442	170

H(26C)	10775	7095	3725	162

H(27G)	9944	7714	3831	93

H(27H)	10376	7832	4166	93

H(27I)	9777	7834	4199	93

H(28C)	9347	5124	5085	43

H(30C)	10051	6472	5726	74

H(31C)	9685	7387	6100	115

H(32C)	8788	7371	6058	120

H(33C)	8242	6608	5640	97

H(34C)	8624	5680	5278	75

H(35G)	9631	4376	5607	99

H(35H)	10176	4868	5653	99

H(35I)	10019	4195	5344	99

H(38C)	6660	5062	4318	71

H(40C)	6917	6509	3517	44

H(42G)	6048	5976	3511	99

H(42H)	5914	5928	3890	99

H(42I)	6037	5055	3698	99

H(43C)	7995	4905	4727	75

H(45C)	7031	4470	5108	192

H(46C)	6665	3018	5191	216

H(47C)	6903	2029	4833	122

H(48C)	7388	1991	4410	222

H(49C)	7699	3494	4318	129

H(50G)	7675	6116	4957	121

H(50H)	7657	5288	5200	121

H(50I)	7138	5628	4965	121

H(51C)	8266	6429	3696	36

H(53C)	8842	7527	3892	47

H(54C)	9040	8926	4094	72

H(55C)	8379	9918	4106	89

H(56C)	7520	9560	3881	72

H(57C)	7328	8124	3715	71

H(58G)	7978	7088	3142	83

H(58H)	7392	7032	3204	83

H(58I)	7712	6159	3169	83

________________________________________________________________________________