# First liquid crystalline, expanded porphyrin

Jonathan L. Sessler*a, Wyeth Callaway, a Stephen P. Dudek, a Richard W. Date, b Vincent Lynch a and Duncan W. Bruce*b

a Department of Chemistry and Biochemistry, Institute for Cellular and Molecular Biology, The University of Texas at Austin, Austin, TX 78712-0165, USA. Fax: 1-512-471-7550; E-mail: sessler@mail.utexas.edu

b School of Chemistry, University of Exeter, Stocker Road, Exeter EX4 4QD, UK. Fax:44 1392263434; E-mail: d.bruce@exeter.ac.uk

# Supplemental Information

Appendix A: Experimental.

Appendix B: Crystallographic data and tables relating to the structure of 1a.

## Appendix A

All solvents and chemicals were obtained commercially and used as received.  Proton and 13C-NMR spectra were measured at 25 ºC on a Varian Unity Innova Spectrometer at 300 MHz. UV-vis spectra were recorded on a BECKMAN DU 640B spectrophotometer. High resolution CI mass spectra were obtained on a VG ZAB2-E mass spectrometer.

3,4-Dimethoxypyrrole  (2a) was synthesized in accord with a standard literature procedure.1

The diformylpyrrole precursors for hydrazinophyrin are air and light sensitive. Therefore, the alkoxy pyrrole derivatives are stored as the more stable -free species. When needed for a condensation, the -free species is first diformylated as described below and condensed then reacted with hydrazine immediately after work-up.

Formylation of 3,4-alkoxypyrroles: General procedure.

2,5-Diformyl-3,4-dimethoxypyrrole (3a)  3,4-dimethoxypyrrole (2) (0.632 g, 4.97 mmol) was added to a 3-neck RBF, equipped with a dropping funnel, evacuated, and protected from light.  The flask was placed under argon and cooled in an ice bath. Trifluoroacetic acid (20 ml) was then added, followed by the dropwise addition of triethyl orthoformate (20 ml) over 15 minutes.  After the addition was complete, the reaction was removed from the ice bath and stirred for one hour.  The reaction mixture was then poured slowly and carefully into 150 ml sat. aqueous NaHCO3.  Dichloromethane was added (200 ml) and the resulting organic layer was washed with sat. NaHCO3 (3 x 50 ml).  The organic layer was dried over Na2SO4, filtered through a plug of silica gel which was then washed with methanol (50 ml).  The filtrate and washings were combined and the solvents were then removed under reduced pressure.  The resulting oil was purified by chromatography over alumina using argon pressure with EtOAc as the eluant.  This gave (3) as a white solid (0.557 g, 61.2%).  1H NMR (300 MHZ, CDCl3):  ( 4.06 (s, 6H, CH3), 9.17 (broad, 1H, NH-pyrrole), 9.85 (s, 2H, CHO); 13C NMR (75.5 MHZ, CDCl3): ( 62.5, 123.3, 143.8, 178.9; MS (CI+): 184.12.

(1a) The diformyl pyrrole (3a) (0.260g, 1.45 mmol) was added to a 500 ml RBF, followed by a mixture of toluene/methanol (1:1, 450 ml).  Stirring was then commenced and hydrazine (0.056 g, 1.74 mmol) was added to the solution followed by conc. HCl (0.336 ml).  Within 15 minutes the solution became dark red and a precipitate formed.  The reaction mixture was heated at reflux for 2 hours.  The mix was neutralized via the addition of triethylamine (1 ml).  The solvents were removed under reduced pressure.  Chromatography over silica gel was performed using a gradient of 0-2% MeOH/CHCl3 as the eluent.  The recovered material was recrystallized from acetone, filtered and washed with cold ether to yield (1a) as a black solid (0.161g, 58.1%).  1H NMR (300 MHZ, CDCl3): ( 3.846 (s, 3H, CH3), 3.851 (s, 3H, CH3), 3.858 (s, 3H, CH3), 3.88 (s, 3H, CH3), 7.33 (s, 2H, CH=N-N), 8.02 (s, 2H, CH=N-N ), 8.11 (s, 2H, CH=N-N), 9.79 (s, 2H, CH=N-N), 12.03 (s, 2H, NH-pyrrole), 13.15 (s, 2H, NH-pyrrole); 13C NMR (75.5 MHZ, CDCl3): ( 59.81, 60.00, 60.61, 60.67, 116.00, 118.06, 119.42, 119.70, 136.67, 140.24, 140.40, 140.88, 141.65, 146.66, 148.48, 152.95;  HRMS (CI+) m/e calc’d for C32H36N12O8: 717.2857 found: 717.2860; UV-Vis (DCM), (max  419 (( = 2.8 x 105 L-1 M-1).

(1b) 1H NMR (300 MHZ, CDCl3): ( 0.87 (m, OCH2CH2(CH2)3CH3), 1.2-1.5 (m, OCH2CH2(CH2)3CH3), 1.66 (m, OCH2CH2(CH2)3CH3), 3.95 (m, OCH2CH2(CH2)3CH3), 7.23 (s, 2H, CH=N-N), 7.90 (s, 2H, CH=N-N), 8.10 (s, 2H, CH=N-N), 9.75 (s, 2H, CH=N-N), 12.15 (s, 2H, NH-pyrrole), 13.37 (s, 2H, NH-pyrrole).

(1c) 1H NMR (300 MHZ, CDCl3): ( 0.90 (m, OCH2CH2(CH2)7CH3), 1.2-1.5 (m, OCH2CH2(CH2)7CH3), 1.70 (m, OCH2CH2(CH2)7CH3), 3.98 (m, OCH2CH2(CH2)7CH3), 7.31 (s, 2H, CH=N-N), 8.0 (s, 2H, CH=N-N), 8.18 (s, 2H, CH=N-N), 9.8 (s, 2H, CH=N-N), 12.14 (s, 2H, NH-pyrrole), 13.41 (s, 2H, NH-pyrrole).

(1d) 1H NMR (300 MHZ, CDCl3): ( 0.86 (m, OCH2CH2(CH2)11CH3), 1.0-1.6 (m, OCH2CH2(CH2)11CH3), 1.64 (m, OCH2CH2(CH2)11CH3), 3.95 (m, OCH2CH2(CH2)11CH3),7.25 (s, 2H, CH=N-N), 7.93 (s, 2H, CH=N-N), 8.11 (s, 2H, CH=N-N), 9.73 (s, 2H, CH=N-N), 12.12 (s, 2H, NH-pyrrole), 13.23 (s, 2H, NH-pyrrole).

Dimethyl 1-benzyl-3,4-dihydroxypyrrole-2,5-dicarboxylate (4) was synthesized in accord with a standard literature procedure.1

Alkylation of dihydroxypyrrole (4 ( 5b-5d): General procedure.

Dimethyl-1-benzyl-3,4-didecyloxypyrrole-2,5-dicarboxylate (5c)  The dihydroxy pyrrole (4) (11.0 g, 36 mmol) was dissolved in acetonitrile (250 ml). Solid K2CO3 (24.8 g, 180 mmol) was then added, followed by 1-bromodecane (15.94 g, 72 mmol).  The resulting mixture was heated at reflux for 2 days and filtered to remove unreacted K2CO3.  The solvent was removed under reduced pressure and the residue was subjected to kugelrohr distillation to remove left over bromodecane.  Column chromotography over silica gel using 4% EtOAc/hexanes as the eluent yielded product (5c) as a brown oil (12.63 g, 60%).  1H NMR (300 MHZ, CDCl3): (  0.86 (t, 6H, OCH2CH2(CH2)7CH3), 1.2-1.4 (m, 28H, OCH2CH2(CH2)7CH3), 1.71 (p, 4H, OCH2CH2(CH2)7CH3), 3.78 (s, 6H, CO2CH3), 4.01 (t, 4H, OCH2CH2(CH2)7CH3),  5.97 (s, 2H, CH2C6H5), 6.8-7.2 (m, 5H, CH2C6H5); 13C NMR (75.5 MHZ, CDCl3): ( 14.06, 22.65, 26.00, 29.31, 29.45, 29.58, 29.64, 30.03, 31.87, 48.73, 51.53, 75.10, 116.49, 125.83, 126.77, 128.31, 139.04, 142.70, 160.78; MS (CI+): 586.42.

Debenzylation of dimethyl 1-benzyl-3,4-dialkoxypyrrole-2,5-dicarboxylates 5b-5d ( 6b-6d: General procedure.

Dimethyl 3,4-didecyloxypyrrole-2,5-dicarboxylate (6c) The N-benzyl pyrrole (12.63 g, 21.56 mmol) (5c) was dissolved in trifluoroacetic acid (100 ml), and then anisole (3.03 g, 28.02 mmol) and H2SO4 (0.81 ml) were added.  The resulting solution was heated at reflux for 30 minutes.  The solvent was then removed under reduced pressure and aqueous sat. NaHCO3 was added to neutralize the residue.  The ensuing mixture was extracted with dichloromethane (3 x 150 ml) and dried over Na2SO4. The solvents were removed under reduced pressure and purification was effected by column chromatography over silica gel using 1-2% EtOAc/hexanes to elute first remaining starting material, then 10% EtOAc/hexanes to afford the product as a brown oil (8.24 g, 77%). 1H NMR (300 MHZ, CDCl3): ( 0.86 (t, 6H, OCH2CH2(CH2)7CH3), 1.25-1.44 (m, 28H, OCH2CH2(CH2)7CH3), 1.72 (p, 4H, OCH2CH2(CH2)7CH3), 3.87 (s, 6H, CO2CH3), 4.06 (t, 4H, OCH2CH2(CH2)7CH3), 8.83 (s, 1H, NH-pyrrole); 13C NMR (75.5 MHZ, CDCl3): ( 14.34, 22.92, 26.138, 29.59, 29.68, 29.84, 29.90, 30.19, 32.15, 52.09, 75.31, 113.56, 142.03, 160.47.

Saponification and decraboxylation of dimethyl-3,4-dialkoxypyrrole-2,5-dicarboxylate 6b-d ( 2b-d: General procedure.

3,4-Didecyloxypyrrole (2c) The pyrrole dicarboxylate (6c) (8.24 g, 16.62 mmol) was added to ethylene glycol (150 ml) and degassed for 2 hours under reduced pressure (0.5 mm Hg).  KOH was added (3.73 g, 66.47 mmol) and the mixture degassed an additional hour.  The mixture was placed under argon and added to a preheated oil bath at 180oC and heated for 3 hours.  The reaction mixture was cooled and water was added (250 ml); the mixture was then extracted with EtOAc (3 x 150 ml).  The extracts were dried over Na2SO4, and the solvent was then removed under reduced pressure.  Column chromatography over silica gel using a gradient of 10-20% EtOAc/hexanes as the eluent gave the product as a flaky lustrous tan solid (3.6 g, 57%).1H NMR (300 MHZ, CDCl3): ( 0.87 (t, 6H, OCH2CH2(CH2)7CH3), 1.2-1.45 (m, 28H, OCH2CH2(CH2)7CH3), 1.74 (p, 4H, OCH2CH2(CH2)7CH3), 3.84 (t, 4H, OCH2CH2(CH2)7CH3), 6.18 (d, 2H, (-H-pyrrole), 7.06 (s, 1H, NH-pyrrole); 13C NMR (75.5 MHZ, CDCl3): ( 13.96, 22.54, 25.89, 29.21, 29.33, 29.46, 29.49, 31.77, 71.50, 100.60, 137.27; MS (CI+): 380.34.

References

1. A. Merz, R. Schropp, E. Dotterl, Synthesis, 1995, 795-800.

## Appendix B

Crystallographic Data for “Hydrazinophyrin” (1a)

# X-ray Experimental

Table 1.  Crystallographic Data for 1a.

Table 2. Fractional coordinates and equivalent isotropic thermal parameters (Å2) for the non-hydrogen atoms of 1a.

Table 3.  Bond Lengths (Å) and Angles (o) for the non-hydrogen atoms of 1a.

Table  4.   Anisotropic thermal parameters for the non-hydrogen atoms of 1a.

Table 5. Fractional coordinates and isotropic thermal parameters (Å2) for the hydrogen atoms of 1a.

Table 6.  Torsion Angles (o) for the non-hydrogen atoms of 1a.

Figure 1.  View of 1a showing the atom labeling scheme.  Displacement ellipsoids are scaled to the 50% probability level.  Some of the hydrogen atoms have been removed for clarity.  The macrocycle lies around a crystallographic inversion center at ½, ½, ½.  Atoms with labels appended by ‘ are related by 1-x, 1-y, 1-z.  Dashed lines are indicative of H-bonding interactions with geometry:  N11-H11…O1a’, N…O 2.763(3)Å, H…O 1.86(3)Å, N-H…O 171(3)°; O1a-H1a…N7, O…N 2.698(3)Å, H…N 1.86(3)Å, O-H…N 166(3)°.

Figure 2.  Unit cell packing diagram for 1a.  The view is approximately down the a axis.

X-ray Experimental for C32H36N12O8 - 2 CH3OH:  Crystals grew as very long, thin needles by layering THF and MeOH over water in a small tube.  The data crystal was a cut from a larger crystal and had approximate dimensions; 0.41x0.11x0.09 mm.  The data were collected on a Nonius Kappa CCD diffractometer using a graphite monochromator with MoK radiation ( = 0.71073Å).  A total of 433 frames of data were collected using -scans with a scan range of 1.1( and a counting time of 136 seconds per frame.  The data were collected at 153 K using an Oxford Cryostream low temperature device.  Details of crystal data, data collection and structure refinement are listed in Table 1.  Data reduction were performed using DENZO-SMN.1  The structure was solved by direct methods using SIR922 and refined by full-matrix least-squares on F2 with anisotropic displacement parameters for the non-H atoms using SHELXL-97.3  The hydrogen atoms on carbon were calculated in ideal positions with isotropic displacement parameters set to 1.2xUeq of the attached atom (1.5xUeq for methyl hydrogen atoms).  The hydrogen atoms bound to nitrogen and oxygen were observed in a (F map and refined with isotropic displacement parameters.  The function, (w(|Fo|2 - |Fc|2)2, was minimized, where w = 1/[((Fo))2 + (0.0407*P)2 + (1.0354*P)] and P = (|Fo|2 + 2|Fc|2)/3.  Rw(F2) refined to 0.153, with R(F) equal to 0.0654 and a goodness of fit, S, = 1.333.  Definitions used for calculating R(F),Rw(F2) and the goodness of fit, S, are given below.4  The data were corrected for secondary extinction effects.  The correction takes the form:  Fcorr = kFc/[1 + (1.0(2)x10-5)* Fc2 3/(sin2)]0.25 where k is the overall scale factor.  Neutral atom scattering factors and values used to calculate the linear absorption coefficient are from the International Tables for X-ray Crystallography (1992).5  All figures were generated using SHELXTL/PC.6  Tables of positional and thermal parameters, bond lengths and angles, torsion angles, figures and lists of observed and calculated structure factors are located in tables 1 through 7.

References

- DENZO-SMN.  (1997).  Z. Otwinowski and W. Minor, Methods in Enzymology, 276: Macromolecular Crystallography, part A, 307 – 326, C. W. Carter, Jr. and R. M. Sweets, Editors, Academic Press.

2)	SIR92.  (1993).  A program for crystal structure solution. Altomare, A., Cascarano, G., Giacovazzo, C. & Guagliardi, A.   J. Appl. Cryst. 26, 343-350.

3)	Sheldrick, G. M. (1994).  SHELXL97.  Program for the Refinement of Crystal Structures.  University of Gottingen, Germany.

4)	Rw(F2) =  {w(|Fo|2 - |Fc|2)2/w(|Fo|)4}1/2 where w is the weight given each reflection.

R(F) =  (|Fo| - |Fc|)/|Fo|} for reflections with Fo > 4((Fo)).

S =  [w(|Fo|2 - |Fc|2)2/(n - p)]1/2, where n is the number of reflections and p is the number of refined parameters.

- International Tables for X-ray Crystallography (1992). Vol. C, Tables 4.2.6.8 and 6.1.1.4, A. J. C. Wilson, editor, Boston: Kluwer Academic Press.

6)	Sheldrick, G. M. (1994).  SHELXTL/PC (Version 5.03).  Siemens Analytical X-ray Instruments, Inc., Madison, Wisconsin, USA.

Table 1.  Crystal data and structure refinement for 1a.

Empirical formula 	C17 H22 N6 O5

Formula weight 	390.41

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 7.4409(1) Å	= 90°.

b = 13.4669(2) Å	= 90.1340(8)°.

c = 19.1745(4) Å	 = 90°.

Volume	1921.39(6) Å3

Z	4

Density (calculated)	1.350 Mg/m3

Absorption coefficient	0.102 mm-1

F(000)	824

Crystal size	0.41 x 0.11 x 0.09 mm

Theta range for data collection	2.93 to 27.47°.

Index ranges	-9<=h<=9, -17<=k<=17, -24<=l<=24

Reflections collected	8262

Independent reflections	4363 [R(int) = 0.0264]

Completeness to theta = 27.47°	99.3 %

Absorption correction	None

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4363 / 0 / 266

Goodness-of-fit on F2	1.333

Final R indices [I>2sigma(I)]	R1 = 0.0654, wR2 = 0.1412

R indices (all data)	R1 = 0.1008, wR2 = 0.1528

Extinction coefficient	1.01(16)x10-5

Largest diff. peak and hole	0.64 and -0.46 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103)

for 1a.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

N1	2719(3)	6218(2)	7336(1)	32(1)

C2	2834(3)	6697(2)	7961(1)	33(1)

C3	1324(3)	6429(2)	8352(1)	33(1)

C4	292(3)	5785(2)	7946(1)	33(1)

C5	1179(3)	5658(2)	7309(1)	31(1)

C6	627(3)	5044(2)	6748(1)	32(1)

N7	1555(3)	4939(1)	6183(1)	31(1)

N8	778(3)	4260(2)	5718(1)	32(1)

C9	1758(3)	4114(2)	5176(1)	31(1)

C10	1295(3)	3408(2)	4644(1)	29(1)

N11	2373(3)	3324(2)	4073(1)	33(1)

C12	1766(3)	2584(2)	3651(1)	35(1)

C13	248(3)	2165(2)	3969(1)	34(1)

C14	-45(3)	2675(2)	4589(1)	29(1)

C15	2550(4)	2310(2)	3002(1)	42(1)

N16	4024(3)	2713(2)	2747(1)	38(1)

N17	4368(3)	2294(2)	2101(1)	50(1)

C18	5806(4)	2620(2)	1815(2)	43(1)

O19	977(2)	6786(1)	9010(1)	43(1)

C20	1788(4)	6211(2)	9556(1)	55(1)

O21	-1261(2)	5289(2)	8082(1)	51(1)

C22	-2304(4)	5587(3)	8659(2)	56(1)

O23	-1310(2)	2425(1)	5078(1)	34(1)

C24	-2750(3)	3132(2)	5150(1)	42(1)

O25	-615(2)	1351(1)	3713(1)	49(1)

C26	-2509(4)	1423(2)	3677(2)	67(1)

O1A	5151(3)	5197(1)	6198(1)	41(1)

C2A	5585(4)	4460(2)	6710(2)	49(1)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for  1a.

_____________________________________________________

N1-C2 	1.363(3)

N1-C5 	1.372(3)

N1-H1 	0.80(3)

C2-C3 	1.400(3)

C2-C18#1 	1.433(3)

C3-O19 	1.374(3)

C3-C4 	1.395(3)

C4-O21 	1.360(3)

C4-C5 	1.401(3)

C5-C6 	1.417(3)

C6-N7 	1.293(3)

C6-H6 	0.96

N7-N8 	1.402(3)

N8-C9 	1.286(3)

C9-C10 	1.436(3)

C9-H9 	0.96

C10-N11 	1.364(3)

C10-C14 	1.406(3)

N11-C12 	1.360(3)

N11-H11 	0.91(3)

C12-C13 	1.403(3)

C12-C15 	1.425(3)

C13-O25 	1.361(3)

C13-C14 	1.391(3)

C14-O23 	1.372(3)

C15-N16 	1.318(3)

C15-H15 	0.96

N16-N17 	1.386(3)

N17-C18 	1.281(3)

C18-C2#1 	1.433(3)

C18-H18 	0.96

O19-C20 	1.434(3)

C20-H20A 	0.96

C20-H20B 	0.96

C20-H20C 	0.96

O21-C22 	1.410(3)

C22-H22A 	0.96

C22-H22B 	0.96

C22-H22C 	0.96

O23-C24 	1.441(3)

C24-H24A 	0.96

C24-H24B 	0.96

C24-H24C 	0.96

O25-C26 	1.414(4)

C26-H26C 	0.96

C26-H26A 	0.96

C26-H26B 	0.96

O1A-C2A 	1.433(3)

O1A-H1A 	0.86(3)

C2A-H2AC 	0.96

C2A-H2AA 	0.96

C2A-H2AB 	0.96

C2-N1-C5	110.1(2)

C2-N1-H1	127(2)

C5-N1-H1	123(2)

N1-C2-C3	107.5(2)

N1-C2-C18#1	127.6(2)

C3-C2-C18#1	124.9(2)

O19-C3-C4	128.7(2)

O19-C3-C2	123.7(2)

C4-C3-C2	107.6(2)

O21-C4-C3	131.7(2)

O21-C4-C5	120.6(2)

C3-C4-C5	107.6(2)

N1-C5-C4	107.2(2)

N1-C5-C6	126.2(2)

C4-C5-C6	126.6(2)

N7-C6-C5	123.0(2)

N7-C6-H6	118.5

C5-C6-H6	118.5

C6-N7-N8	112.57(19)

C9-N8-N7	112.39(19)

N8-C9-C10	122.7(2)

N8-C9-H9	118.5

C10-C9-H9	118.8

N11-C10-C14	107.5(2)

N11-C10-C9	118.9(2)

C14-C10-C9	133.4(2)

C12-N11-C10	110.0(2)

C12-N11-H11	126.3(17)

C10-N11-H11	123.3(17)

N11-C12-C13	107.7(2)

N11-C12-C15	124.9(2)

C13-C12-C15	127.4(2)

O25-C13-C14	129.1(2)

O25-C13-C12	123.1(2)

C14-C13-C12	107.5(2)

O23-C14-C13	124.9(2)

O23-C14-C10	127.5(2)

C13-C14-C10	107.3(2)

N16-C15-C12	124.1(2)

N16-C15-H15	117.8

C12-C15-H15	118.1

C15-N16-N17	108.7(2)

C18-N17-N16	113.5(2)

N17-C18-C2#1	133.0(3)

N17-C18-H18	113.5

C2#1-C18-H18	113.6

C3-O19-C20	113.7(2)

O19-C20-H20A	109.6

O19-C20-H20B	110.0

H20A-C20-H20B	109.5

O19-C20-H20C	108.8

H20A-C20-H20C	109.5

H20B-C20-H20C	109.5

C4-O21-C22	118.7(2)

O21-C22-H22A	109.2

O21-C22-H22B	109.4

H22A-C22-H22B	109.5

O21-C22-H22C	109.8

H22A-C22-H22C	109.5

H22B-C22-H22C	109.5

C14-O23-C24	114.49(17)

O23-C24-H24A	109.6

O23-C24-H24B	109.4

H24A-C24-H24B	109.5

O23-C24-H24C	109.4

H24A-C24-H24C	109.5

H24B-C24-H24C	109.5

C13-O25-C26	115.7(2)

O25-C26-H26C	112.1

O25-C26-H26A	107.0

H26C-C26-H26A	111.8

O25-C26-H26B	107.0

H26C-C26-H26B	111.8

H26A-C26-H26B	106.8

C2A-O1A-H1A	108(2)

O1A-C2A-H2AC	108.4

O1A-C2A-H2AA	111.3

H2AC-C2A-H2AA	108.4

O1A-C2A-H2AB	111.2

H2AC-C2A-H2AB	108.4

H2AA-C2A-H2AB	109.1

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:   #1 -x+1,-y+1,-z+1

Table 4.   Anisotropic displacement parameters  (Å2x 103) for 1a.  The anisotropic

displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

N1	31(1) 	32(1)	32(1) 	-2(1)	7(1) 	-1(1)

C2	34(1) 	29(1)	37(1) 	-5(1)	4(1) 	1(1)

C3	35(1) 	28(1)	36(1) 	-4(1)	5(1) 	3(1)

C4	30(1) 	32(1)	39(1) 	1(1)	4(1) 	0(1)

C5	29(1) 	29(1)	35(1) 	2(1)	-1(1) 	0(1)

C6	29(1) 	33(1)	33(1) 	3(1)	-3(1) 	-1(1)

N7	33(1) 	30(1)	31(1) 	-1(1)	-8(1) 	-2(1)

N8	35(1) 	35(1)	27(1) 	2(1)	-5(1) 	-4(1)

C9	31(1) 	28(1)	33(1) 	6(1)	-8(1) 	-2(1)

C10	27(1) 	32(1)	27(1) 	4(1)	-2(1) 	0(1)

N11	29(1) 	36(1)	33(1) 	2(1)	1(1) 	-4(1)

C12	32(1) 	40(1)	34(1) 	-1(1)	5(1) 	0(1)

C13	35(1) 	33(1)	34(1) 	-3(1)	1(1) 	-3(1)

C14	29(1) 	30(1)	28(1) 	4(1)	2(1) 	0(1)

C15	43(2) 	43(2)	40(1) 	-9(1)	5(1) 	-5(1)

N16	38(1) 	38(1)	38(1) 	-12(1)	1(1) 	-6(1)

N17	52(1) 	55(2)	42(1) 	-18(1)	10(1) 	-12(1)

C18	43(2) 	43(2)	44(2) 	-9(1)	8(1) 	-9(1)

O19	48(1) 	44(1)	37(1) 	-11(1)	12(1) 	0(1)

C20	63(2) 	66(2)	36(2) 	-7(1)	-2(1) 	-9(2)

O21	40(1) 	55(1)	59(1) 	-14(1)	17(1) 	-17(1)

C22	36(2) 	80(2)	53(2) 	-5(2)	16(1) 	-9(2)

O23	37(1) 	34(1)	31(1) 	5(1)	9(1) 	-4(1)

C24	36(1) 	43(2)	46(2) 	1(1)	12(1) 	-4(1)

O25	48(1) 	43(1)	55(1) 	-18(1)	4(1) 	-12(1)

C26	60(2) 	48(2)	91(3) 	-7(2)	-26(2) 	-17(2)

O1A	33(1) 	49(1)	40(1) 	3(1)	-1(1) 	-12(1)

C2A	39(2) 	56(2)	50(2) 	7(1)	-3(1) 	7(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for 1a.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H6	-491	4692	6787	38

H9	2842	4494	5126	37

H15	1965	1805	2731	51

H18	6009	2357	1356	52

H20A	1491	6495	10000	82

H20B	1362	5539	9536	82

H20C	3068	6219	9495	82

H22A	-3354	5175	8687	85

H22B	-1607	5517	9078	85

H22C	-2660	6268	8604	85

H24A	-3574	2908	5500	63

H24B	-2264	3765	5283	63

H24C	-3370	3196	4712	63

H26C	-2930	2072	3801	100

H26A	-2985	919	3979	100

H26B	-2853	1246	3210	100

H2AC	4752	4521	7090	73

H2AA	6779	4552	6890	73

H2AB	5483	3803	6520	73

H11	3270(40)	3760(20)	3972(14)	44(8)

H1	3450(40)	6220(20)	7026(14)	41(8)

H1A	4000(40)	5200(20)	6143(16)	61(10)

________________________________________________________________________________

Table 6.  Torsion angles [°] for 1a.

________________________________________________________________

C5-N1-C2-C3	0.5(3)

C5-N1-C2-C18#1	-177.5(2)

N1-C2-C3-O19	-178.9(2)

C18#1-C2-C3-O19	-0.8(4)

N1-C2-C3-C4	-0.5(3)

C18#1-C2-C3-C4	177.6(2)

O19-C3-C4-O21	-3.9(4)

C2-C3-C4-O21	177.8(3)

O19-C3-C4-C5	178.6(2)

C2-C3-C4-C5	0.2(3)

C2-N1-C5-C4	-0.4(3)

C2-N1-C5-C6	-178.6(2)

O21-C4-C5-N1	-177.8(2)

C3-C4-C5-N1	0.1(3)

O21-C4-C5-C6	0.4(4)

C3-C4-C5-C6	178.3(2)

N1-C5-C6-N7	0.4(4)

C4-C5-C6-N7	-177.5(2)

C5-C6-N7-N8	177.3(2)

C6-N7-N8-C9	-176.2(2)

N7-N8-C9-C10	176.33(19)

N8-C9-C10-N11	177.6(2)

N8-C9-C10-C14	-8.0(4)

C14-C10-N11-C12	1.0(3)

C9-C10-N11-C12	176.8(2)

C10-N11-C12-C13	-0.9(3)

C10-N11-C12-C15	178.5(2)

N11-C12-C13-O25	-174.7(2)

C15-C12-C13-O25	5.9(4)

N11-C12-C13-C14	0.4(3)

C15-C12-C13-C14	-179.0(2)

O25-C13-C14-O23	0.8(4)

C12-C13-C14-O23	-173.9(2)

O25-C13-C14-C10	175.0(2)

C12-C13-C14-C10	0.3(3)

N11-C10-C14-O23	173.2(2)

C9-C10-C14-O23	-1.7(4)

N11-C10-C14-C13	-0.8(3)

C9-C10-C14-C13	-175.6(2)

N11-C12-C15-N16	3.6(4)

C13-C12-C15-N16	-177.2(3)

C12-C15-N16-N17	-178.2(3)

C15-N16-N17-C18	-178.4(3)

N16-N17-C18-C2#1	2.7(5)

C4-C3-O19-C20	94.1(3)

C2-C3-O19-C20	-87.8(3)

C3-C4-O21-C22	15.8(4)

C5-C4-O21-C22	-166.9(2)

C13-C14-O23-C24	-112.9(3)

C10-C14-O23-C24	74.2(3)

C14-C13-O25-C26	52.8(4)

C12-C13-O25-C26	-133.3(3)

________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y+1,-z+1

Figure 1.  View of 1a showing the atom labeling scheme.  Displacement ellipsoids are scaled to the 50% probability level.  Some of the hydrogen atoms have been removed for clarity.  The macrocycle lies around a crystallographic inversion center at ½, ½, ½.  Atoms with labels appended by ‘ are related by 1-x, 1-y, 1-z.  Dashed lines are indicative of H-bonding interactions with geometry:  N11-H11…O1a’, N…O 2.763(3)Å, H…O 1.86(3)Å, N-H…O 171(3)°; O1a-H1a…N7, O…N 2.698(3)Å, H…N 1.86(3)Å, O-H…N 166(3)°.

Figure 2.  Unit cell packing diagram for a1.  The view is approximately down the a axis.