General procedure for the synthesis of PAP. 4-[N-methyl-N-(p-vinylbenzyl)amino]pyridine was prepared starting from 4-(methylamino)pyridine sodium salt and p-(chloromethyl)styrene, and was copolymerised with styrene (1 eq.) and divinylbenzene (0.02 eq.) to give the polymer-bound 4-(N-benzyl-N-methylamino)pyridine (PAP). A more detailed experimental procedure can be found in: Polymer-supported bases. 1. Synthesis and catalytic activity of polymer-bound 4-(N-benzyl-N-methylamino)pyridine. Tomoi, M.; Akada, Y.; Kakiuchi, H. Makromolekulare Chemie, Rapid Commun. (1982), 3(8), 537-542.