Al-Free Zr-Zeolite Beta as a Regioselective Catalyst in the Meerwein-Ponndorf-Verley Reaction

Yongzhong Zhu, Gaikhuan Chuah and Stephan Jaenicke*

Department of Chemistry, National University of Singapore,Kent Ridge, Singapore 119260, Singapore. Fax: 65 6779 1691; Tel: 65 6874 2918; E-mail: chmsj@nus.edu.sg

29Si MAS NMR

29Si MAS NMR spectra were recorded on a Bruker DRX-400 spectrometer at a 29Si frequency of 79.46 MHz with a spinning rate of 12kHz and a recycle time of 20 s. The 29Si chemical shifts are reported relative to TMS.

| Sample | Si/Zr |
| --- | --- |
| Si-beta | - |
| Zr75 | 84 |
| Zr100 | 107 |
| Zr200 | 194 |