# Supporting Information

Encapsulation of paramagnetic 3d1- vanadium(IV) in an antiferromagnetically coupled dodecanuclear copper(II) cage

Arindam Mukherjee, Munirathinam Nethaji and Akhil R. Chakravarty*

Department of Inorganic and Physical Chemistry, Indian Institute of Science, Bangalore-560012, India. E-mail: arc@ipc.iisc.ernet.in

Table S1. Magnetic susceptibility data MT (per molecule) vs. T for 1 in the temperature range 17-450 K

| T MT (per molecule) | T MT (per molecule) |
| --- | --- |
| 17.10732 0.39007 17.23532 0.39182 17.2671 0.39056 17.43589 0.38953 17.88187 0.38628 18.14078 0.38709 18.59374 0.39078 19.4253 0.39577 22.22069 0.41303 25.3262 0.38915 28.38827 0.39288 30.76574 0.40816 32.78494 0.39471 34.46818 0.40091 36.15567 0.40721 37.49759 0.41388 38.78122 0.41941 39.54474 0.42049 58.42094 0.49978 59.97241 0.50861 62.08413 0.52023 64.45443 0.53349 67.34189 0.55446 70.22934 0.57312 72.55655 0.59142 75.18542 0.60983 77.29714 0.62634 79.62435 0.64696 81.99465 0.66803 84.10637 0.68971 86.17499 0.71128 87.76956 0.72929 90.09676 0.75341 92.14951 0.77599 93.9804 0.7827 95.78516 0.8095 97.5748 0.83226 99.30109 0.84445 101.0181 0.86515 102.7293 0.87862 104.3724 0.89703 106.0089 0.92385 107.5992 0.94008 109.1388 0.95229 110.7318 0.96559 112.2934 0.98382 113.8277 1.00586 115.3502 1.04592 116.8758 1.04351 118.3934 1.06575 119.8804 1.08445 167.7492 1.69574 169.2184 1.71303 170.7291 1.73682 172.2443 1.75896 173.7818 1.74963 175.2694 1.77387 176.7747 1.78944 178.3107 1.81885 179.8129 1.83605 181.3081 1.85108 182.8486 1.84553 184.3473 1.8865 185.8372 1.91096 187.3398 1.92896 188.853 1.95404 190.3261 1.94539 191.8294 1.9766 193.346 1.99745 194.8492 1.9986 196.3354 2.02926 197.826 2.0399 199.2889 2.05124 200.7393 2.08286 202.2394 2.09278 203.7369 2.12214 205.2863 2.12522 206.7711 2.12642 208.2187 2.14722 209.7052 2.16807 211.1668 2.20255 212.6412 2.20031 214.1243 2.22996 215.5788 2.22475 263.1419 2.70676 264.4649 2.72532 265.6823 2.73304 267.0478 2.72761 268.308 2.77245 269.586 2.76676 270.812 2.78015 272.0907 2.77119 273.3454 2.79434 274.5659 2.76805 275.7698 2.81696 277.0951 2.83156 277.55556 2.84701 279.5197 2.85364 280.7536 2.86237 281.9608 2.84624 283.1586 2.87702 284.3437 2.87354 284.83796 2.90468 286.5911 2.92898 287.26543 2.91619 288.5496 2.88687 289.50617 2.93955 290.5789 2.93563 291.6414 2.96306 292.6382 2.94528 293.6703 2.96847 294.6739 2.95916 295.6625 3.0008 296.6196 2.99605 297.5387 3.02238 298.4398 3.00663 299.2866 3.02564 320.515 3.2109 321.208 3.21764 322.36 3.22655 322.751 3.22778 323.161 3.2329 323.552 3.23427 324.03 3.2374 324.919 3.24601 325.401 3.25031 325.881 3.25379 326.367 3.25565 326.856 3.25923 327.415 3.26485 327.915 3.26716 328.492 3.27225 329.07 3.2745 329.656 3.28181 330.238 3.28568 330.814 3.28991 331.487 3.29531 332.16 3.30066 332.814 3.30375 333.498 3.31035 334.163 3.31295 334.836 3.32078 335.605 3.32471 335.989 3.3272 336.462 3.33122 337.261 3.33747 338.181 3.34308 338.938 3.35021 339.899 3.35453 340.657 3.36332 383.515 3.67104 384.948 3.6835 386.389 3.69148 387.816 3.70156 389.435 3.71374 390.861 3.71909 392.466 3.73202 394.071 3.7422 395.711 3.75212 397.444 3.76337 399.213 3.77642 401.035 3.7889 402.929 3.80083 404.862 3.8143 406.972 3.8283 409.063 3.84484 411.175 3.8604 413.315 3.87583 415.541 3.8909 | 40.62215 0.4253 41.65646 0.42936 42.94935 0.4341 44.8025 0.44391 45.83681 0.44795 46.91422 0.45236 47.68995 0.45376 48.46569 0.45938 49.5 0.46404 50.01716 0.46567 50.83599 0.47144 51.61172 0.47367 52.64603 0.47641 53.72344 0.48062 54.49918 0.48399 55.27491 0.4856 57.12805 0.49432 57.64521 0.49689 121.3662 1.1218 122.8424 1.12756 124.2985 1.15199 125.7764 1.17734 127.1692 1.18244 128.6199 1.2092 130.0629 1.2132 131.4691 1.23599 132.9164 1.25213 134.3513 1.27967 135.7559 1.28296 137.1569 1.30391 138.5545 1.32816 139.8845 1.33269 141.2684 1.35281 142.6494 1.38296 144.0226 1.3945 145.3856 1.41786 146.7586 1.43549 148.1441 1.44232 149.4849 1.45827 150.826 1.47519 152.1724 1.49982 153.5239 1.49928 154.8636 1.5365 156.2036 1.54459 157.539 1.55141 158.901 1.58189 160.2939 1.59094 161.7383 1.603 163.2802 1.63296 164.7569 1.66491 166.2366 1.65528 217.0342 2.26274 218.5063 2.27227 219.9655 2.2774 221.4198 2.303 222.8828 2.32383 224.339 2.34212 225.798 2.33159 227.2445 2.36798 228.69 2.36829 230.0889 2.38216 231.5251 2.4137 232.9642 2.41612 234.3459 2.42155 235.7985 2.44953 237.1938 2.48212 238.5924 2.46541 240.0461 2.48216 241.4061 2.49684 242.8397 2.51202 244.3179 2.52665 245.5868 2.54073 246.9926 2.56036 248.3358 2.56891 249.7442 2.58541 251.0975 2.57955 252.5049 2.61383 253.8575 2.62006 255.14815 2.63999 256.5691 2.66522 257.9066 2.67573 259.2011 2.68146 260.5385 2.69468 261.833 2.70417 300.119 3.00368 300.8841 3.04591 301.6484 3.02681 302.57716 3.06162 303.1248 3.06057 303.7448 3.09122 304.3446 3.06634 305.00463 3.08555 307.3056 3.12268 308.599 3.11965 308.807 3.12145 308.966 3.12379 309.402 3.12427 309.799 3.12927 309.998 3.13117 310.077 3.12847 310.891 3.13805 311.089 3.13812 311.982 3.14679 312.18 3.147 312.974 3.15463 313.267 3.15485 313.853 3.15835 314.049 3.16389 314.942 3.16983 315.334 3.171 316.018 3.17712 316.95 3.18453 317.205 3.18557 318.279 3.19613 318.865 3.20077 319.158 3.20293 319.841 3.20708 341.604 3.36969 342.55 3.37453 343.496 3.38401 344.443 3.38877 345.389 3.39757 346.405 3.40372 347.456 3.41002 348.591 3.42075 349.53 3.42733 350.648 3.43365 351.778 3.4423 352.9 3.45045 354.186 3.4599 355.324 3.46827 356.628 3.48119 357.736 3.48716 359.055 3.4956 360.336 3.50608 361.631 3.51455 363.106 3.5256 364.391 3.53429 365.817 3.53946 367.158 3.55133 368.614 3.56434 370.083 3.57357 371.544 3.58329 373.006 3.5961 374.479 3.60687 376.079 3.62049 377.544 3.63104 378.992 3.63772 380.439 3.64933 381.887 3.65946 417.8 3.90815 419.892 3.92287 422.144 3.9415 424.211 3.95126 426.457 3.96755 428.522 3.98711 430.63 4.00465 432.651 4.02049 434.701 4.0405 436.752 4.06248 438.734 4.07944 440.682 4.10389 444.286 4.11585 445.013 4.13696 447.637 4.1405 448.05556 4.1528 449.673 4.14395 450.51111 4.16279 |