The structure of [1] consists of clusters of three octahedrally coordinated cobalt atoms bridged by succinate molecules into 1D chains (Figure 1). The cobalt – oxygen clusters contain two crystallographically independent cobalt atoms. Co[2] lies on an inversion center, and coordinates through edge sharing with two Co[1] octahedra. The coordination sphere of Co[2] is composed entirely of carboxylate oxygen atoms, while that of Co[1] consists of three carboxylate oxygen atoms and three water molecules. There are two crystallographically unique succinate molecules in the asymmetric unit. The first, containing C[1] through C[4], is bidentate with Co[2] binding with an oxygen atom from both carboxylate groups, O[2] and O[4] (Figure 2). Similar binding is seen in MIL-9 and -16. O[2] and O[4] also coordinate with Co[1], resulting in edge-sharing polyhedra. O[1] and O[3] are terminal, but are hydrogen bonded to coordinated water molecules in the trimetallic unit. The second distinct succinate molecule bridges two clusters by coordinating to Co[1] and Co[2] with both (crystallographically identical) carboxylate groups. The water molecules coordinated to Co[1] are stabilized by extensive hydrogen bonding to water molecules on adjacent clusters and to the terminal oxygen atoms on one of the carboxylate groups.

Figure 1:  View of the trimeric Co(II) clusters with the atomic numbering scheme shown.  Co(II) atoms are in blue, oxygen atoms red, carbon atoms grey, and hydrogen atoms white.

Figure 2:  Graphical summary of cobalt succinate structures that form at the different temperatures studied.  Purple polyhedra are drawn around cobalt centers, and oxygen atoms are colored red, carbon atoms grey, and hydrogen atoms white.

Crystallographic summary: A purple single crystal of [1], approx. 1 x 0.1 x 0.1 mm, was selected under a polarizing microscope, glued to a glass fiber, and mounted on a Siemens SMART CCD diffractometer with MoKα radiation (0.71073 Å). The structure was solved using direct methods, and the data were refined against |F2|. All non-hydrogen atoms were refined anisotropically. Hydrogen atoms on the succinate molecules were placed in calculated positions with isotropic U values 20 % higher than the carbon to which they were bound. At the end of the refinement of [1], the six highest peaks in the Fourier map all occurred in chemically reasonable positions for the six hydrogen atoms of the water molecules. These were assigned isotropic U values 20 % higher than the oxygen to which they were bound, and refined into chemically reasonable positions without constraint.  Crystal Data for [1]: orthorhombic, Pbca, a = 9.9608(18)  Å, b = 14.688(3) Å c = 14.925(3) Å, V = 2183.7(7) Å3, c = 1.926 g/cm3,  = 0.71073, Z = 12, R1 = 0.0307 for 2628 reflections with I > 2, GOF = 0.833, 175 refined parameters. Crystallographic data (excluding structure factors) have been deposited with the Cambridge Crystallographic Data Centre as number 221317. Copies of the data can be obtained free of charge on application to the CCDC, 12 Union Rd., Cambridge CB21EZ, UK (fax: (+44)1223-336-033; email : deposit@ccdc.cam.ac.uk).

Table 1.  Crystal data and structure refinement for cobalt succinate dihydrate.

Identification code 	cobalt succinate dihydrate

Empirical formula 	C4 H8 Co O6

Formula weight 	211.03

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 9.9608(18) Å	α= 90°.

b = 14.688(3) Å	β= 90°.

c = 14.925(3) Å	γ = 90°.

Volume	2183.7(7) Å3

Z	12

Density (calculated)	1.926 Mg/m3

Absorption coefficient	2.339 mm-1

F(000)	1284

Crystal size	1.0 x 0.1 x 0.1 mm3

Theta range for data collection	2.73 to 28.30°.

Index ranges	-11<=h<=13, -18<=k<=19, -19<=l<=17

Reflections collected	12404

Independent reflections	2628 [R(int) = 0.0841]

Completeness to theta = 28.30°	97.0 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2628 / 0 / 175

Goodness-of-fit on F2	0.833

Final R indices [I>2sigma(I)]	R1 = 0.0307, wR2 = 0.0792

R indices (all data)	R1 = 0.0379, wR2 = 0.0837

Largest diff. peak and hole	0.358 and -0.984 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103)

for cobalt succinate dihydrate.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	1455(1)	1842(1)	5561(1)	17(1)

Co(2)	0	0	5000	14(1)

O(1)	-842(2)	1514(1)	7161(1)	52(1)

O(2)	359(2)	766(1)	6161(1)	21(1)

O(3)	1208(2)	2160(1)	3329(1)	51(1)

O(4)	466(2)	1272(1)	4418(1)	21(1)

O(5)	3032(1)	972(1)	5315(1)	25(1)

O(6)	-2032(1)	340(1)	5056(1)	24(1)

WA1	2389(2)	2811(1)	4770(1)	25(1)

WA2	-101(2)	2745(1)	5927(1)	26(1)

WA3	2364(2)	2294(1)	6724(1)	32(1)

C(1)	-393(2)	801(2)	6857(1)	28(1)

C(2)	-704(4)	-68(2)	7339(2)	60(1)

C(3)	-150(3)	904(2)	2911(2)	42(1)

C(4)	552(2)	1495(1)	3591(2)	25(1)

C(5)	3052(2)	160(1)	5073(1)	20(1)

C(6)	4402(2)	-305(2)	4945(2)	30(1)

________________________________________________________________________________

Table 4. Bond lengths and angles for cobalt succinate dihydrate.

_____________________________________________________

Co(1)-O(5) 	2.0577(14)

Co(1)-WA3 	2.0674(17)

Co(1)-WA1 	2.0695(16)

Co(1)-WA2 	2.1109(15)

Co(1)-O(2) 	2.1193(14)

Co(1)-O(4) 	2.1404(14)

Co(2)-O(6)#1 	2.0863(15)

Co(2)-O(6) 	2.0863(15)

Co(2)-O(2) 	2.0965(14)

Co(2)-O(2)#1 	2.0965(14)

Co(2)-O(4)#1 	2.1125(14)

Co(2)-O(4) 	2.1125(14)

O(1)-C(1) 	1.226(3)

O(2)-C(1) 	1.282(3)

O(3)-C(4) 	1.239(3)

O(4)-C(4) 	1.280(3)

O(5)-C(5) 	1.247(2)

O(6)-C(5)#1 	1.269(2)

C(1)-C(2) 	1.498(3)

C(2)-C(3)#1 	1.540(4)

C(3)-C(4) 	1.507(3)

C(3)-C(2)#1 	1.540(4)

C(5)-O(6)#1 	1.269(2)

C(5)-C(6) 	1.520(3)

C(6)-C(6)#2 	1.500(4)

O(5)-Co(1)-WA3	90.84(7)

O(5)-Co(1)-WA1	88.96(6)

WA3-Co(1)-WA1	93.54(8)

O(5)-Co(1)-WA2	175.08(7)

WA3-Co(1)-WA2	84.41(8)

WA1-Co(1)-WA2	92.64(7)

O(5)-Co(1)-O(2)	90.31(6)

WA3-Co(1)-O(2)	96.30(7)

WA1-Co(1)-O(2)	170.14(7)

WA2-Co(1)-O(2)	88.91(7)

O(5)-Co(1)-O(4)	88.08(6)

WA3-Co(1)-O(4)	175.09(7)

WA1-Co(1)-O(4)	91.23(7)

WA2-Co(1)-O(4)	96.54(7)

O(2)-Co(1)-O(4)	78.92(5)

O(6)#1-Co(2)-O(6)	180.0

O(6)#1-Co(2)-O(2)	89.78(6)

O(6)-Co(2)-O(2)	90.22(6)

O(6)#1-Co(2)-O(2)#1	90.22(6)

O(6)-Co(2)-O(2)#1	89.78(6)

O(2)-Co(2)-O(2)#1	180.0

O(6)#1-Co(2)-O(4)#1	91.02(6)

O(6)-Co(2)-O(4)#1	88.98(6)

O(2)-Co(2)-O(4)#1	99.94(5)

O(2)#1-Co(2)-O(4)#1	80.06(5)

O(6)#1-Co(2)-O(4)	88.98(6)

O(6)-Co(2)-O(4)	91.02(6)

O(2)-Co(2)-O(4)	80.06(5)

O(2)#1-Co(2)-O(4)	99.94(5)

O(4)#1-Co(2)-O(4)	180.00(7)

C(1)-O(2)-Co(2)	126.27(14)

C(1)-O(2)-Co(1)	127.84(13)

Co(2)-O(2)-Co(1)	98.00(6)

C(4)-O(4)-Co(2)	129.56(13)

C(4)-O(4)-Co(1)	129.66(13)

Co(2)-O(4)-Co(1)	96.86(6)

C(5)-O(5)-Co(1)	131.18(13)

C(5)#1-O(6)-Co(2)	129.24(13)

O(1)-C(1)-O(2)	123.2(2)

O(1)-C(1)-C(2)	118.3(2)

O(2)-C(1)-C(2)	118.5(2)

C(1)-C(2)-C(3)#1	116.7(2)

C(4)-C(3)-C(2)#1	111.5(3)

O(3)-C(4)-O(4)	122.7(2)

O(3)-C(4)-C(3)	119.1(2)

O(4)-C(4)-C(3)	118.17(19)

O(5)-C(5)-O(6)#1	125.78(18)

O(5)-C(5)-C(6)	118.75(18)

O(6)#1-C(5)-C(6)	115.43(17)

C(6)#2-C(6)-C(5)	114.8(2)

_____________________________________________________________

Table 5.   Anisotropic displacement parameters  (Å2x 103) for cobalt succinate dihydrate.  The anisotropic

displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	14(1) 	15(1)	21(1) 	-2(1)	1(1) 	0(1)

Co(2)	11(1) 	13(1)	19(1) 	-1(1)	2(1) 	-1(1)

O(1)	68(1) 	39(1)	47(1) 	-1(1)	38(1) 	10(1)

O(2)	23(1) 	21(1)	19(1) 	-3(1)	4(1) 	-4(1)

O(3)	74(1) 	52(1)	28(1) 	11(1)	-5(1) 	-38(1)

O(4)	23(1) 	19(1)	20(1) 	2(1)	-1(1) 	-4(1)

O(5)	14(1) 	18(1)	43(1) 	-8(1)	1(1) 	1(1)

O(6)	12(1) 	19(1)	40(1) 	-4(1)	1(1) 	1(1)

WA1	27(1) 	18(1)	31(1) 	-2(1)	4(1) 	-5(1)

WA2	20(1) 	26(1)	33(1) 	-1(1)	0(1) 	2(1)

WA3	32(1) 	39(1)	27(1) 	-10(1)	-12(1) 	12(1)

C(1)	31(1) 	30(1)	22(1) 	-3(1)	4(1) 	-6(1)

C(2)	111(3) 	35(1)	35(2) 	-7(1)	38(2) 	-25(2)

C(3)	74(2) 	28(1)	25(1) 	7(1)	-18(1) 	-15(1)

C(4)	29(1) 	23(1)	24(1) 	3(1)	-3(1) 	-3(1)

C(5)	14(1) 	18(1)	27(1) 	-1(1)	1(1) 	1(1)

C(6)	15(1) 	20(1)	55(2) 	-7(1)	3(1) 	2(1)

______________________________________________________________________________

Table 6.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for cobalt succinate dihydrate.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

HW1A	2600(40)	3370(30)	4890(20)	38

HW1B	2050(40)	2690(30)	4290(30)	38

HW2A	-730(40)	2800(30)	5540(20)	39

HW2B	-340(30)	2480(20)	6340(30)	39

HW3A	2990(40)	2000(20)	6980(20)	49

HW3B	2010(40)	2510(20)	7130(30)	49

H(2A)	-1639	-216	7232	72

H(2B)	-604	40	7977	72

H(3A)	-330	1259	2376	51

H(3B)	-1003	703	3153	51

H(6A)	4473	-800	5374	36

H(6B)	4427	-570	4350	36

__________________________________________________________________________