20

30

40

50

60

70

80

90

100

0

100

200

300

400

500

600

Temperature (°C)

Weight loss (%)

12.1%

7.7%

9.1%

40.5%

Water molecules

DMF

free terephthalic acid

Terephthalate linkers

S1 : TG curve of MIL-68

S2 : N2 sorption and desorption isotherms measured at 77 K for MIL-68.

0

50

100

150

200

250

0

0.2

0.4

0.6

0.8

1

P/Po

N2

/ cm

3

.g

-1

(STP)

Adsorption

Desorption

S3 : I.R spectrum of MIL-68.

Table S1 :  Crystal data and structure refinement for MIL-68.

Empirical formula                	 C16 H8 O10 V2

Formula weight                  	 462.10

Temperature                       	293(2) K

Wavelength                       	 0.71073 Å

Crystal system, space group       	Orthorhombic,  Cmcm

Unit cell dimensions              	a = 21.211(2) Å

b = 36.721(4) Å

c = 6.8606(6) Å

Volume                            		5343.5(9) Å3

Z, Calculated density             	6,  0.862 g/cm3

Absorption coefficient            	0.552 mm-1

F(000)                            		1380

Crystal size                      		0.04 x 0.02 x 0.01 mm

 range for data collection   	1.11 to 23.27 °

Limiting indices                  	-19 ≤ h ≤ 23, -38 ≤ k ≤ 40, -7 ≤ l ≤7

Reflections collected / unique    	7810 / 2133 [R(int) = 0.1131]

Completeness to  = 23.27     	97.4 %

Absorption correction             	Semi-empirical from equivalents

Max. and min. transmission        	0.9945 and 0.9783

Refinement method                 	Full-matrix least-squares on F2

Data / restraints / parameters    	2133 / 0 / 111

Goodness-of-fit on F2            	0.948

Final R indices [I > 2(I)]     	R1 = 0.0975, wR2 = 0.2635

R indices (all data)              	R1 = 0.1662, wR2 = 0.2867

Largest diff. peak and hole       1.227 and -1.025 e.Å-3

Table S2 : Atomic coordinates (x 104) and equivalent isotropic displacement parameters (Å2 x 103) for MIL-68.

U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

atoms          x            y          z       U(eq)

V(1)            0             0          5000          40(1)

V(2)         2500          2500          5000          43(1)

O(1)         3367(1)       2383(1)       5904(2)       34(1)

O(2)          626(1)        372(1)       5841(2)       48(1)

O(3)         2231(1)       2007(1)       5849(2)       42(1)

O(4)            0           176(1)       2500         127(3)

O(5)         2700(2)       2287(1)       2500          77(1)

C(1)         4358(2)       2327(1)       7500          25(1)

C(2)         4689(1)       2318(1)       5786(4)       47(1)

C(3)         2072(2)       1882(1)       7500          40(1)

C(4)         3601(2)       2376(1)       7500          21(1)

C(5)         1688(1)       1318(1)       9208(4)       44(1)

C(6)         1834(2)       1484(1)       7500          38(1)

C(7)          803(2)        496(1)       7500          37(1)

C(8)         1209(2)        848(1)       7500          39(1)

C(9)         1369(1)        999(1)       9233(4)       50(1)

H(2)         4472          2313          4607          56

H(5)         1809          1425         10378          53

H(9)         1263           886         10402          60

________________________________________________________________

Table S3 :  Anisotropic displacement parameters (Å2 x 103) for MIL-68.

The anisotropic displacement factor exponent takes the form:

-2 2.[h2.a*2.U11 + ... + 2.h.k.a*.b*.U12]

atoms    U11       U22       U33       U23       U13       U12

V(1)     47(1)      15(1)      58(1)      -7(1)       0          0

V(2)     25(1)      39(1)      64(1)      24(1)      -8(1)     -14(1)

O(1)     19(1)      63(1)      22(1)       9(1)     -14(1)      -2(1)

O(2)     73(1)      34(1)      36(1)       6(1)      -3(1)     -30(1)

O(3)     51(1)      40(1)      36(1)      14(1)     -10(1)     -17(1)

O(4)    303(8)      70(3)       9(2)       0          0          0

O(5)     78(2)     105(2)      49(2)       0          0        -31(2)

C(1)     15(2)      41(2)      18(2)       0          0        -16(2)

C(2)     24(1)      95(2)      22(1)     -11(2)       4(1)       2(2)

C(3)     46(3)      57(2)      16(2)       0          0        -21(2)

C(4)     37(2)      25(2)       2(2)       0          0        -13(2)

C(5)     67(2)      37(1)      28(2)      -1(1)      -4(2)     -23(2)

C(6)     38(2)      33(2)      43(2)       0          0         -8(2)

C(7)     48(3)      24(2)      39(2)       0          0          7(2)

C(8)     50(3)      26(2)      41(2)       0          0        -10(2)

C(9)     68(2)      49(2)      32(2)      -4(1)     -10(2)     -29(2)

_______________________________________________________________________

Table S4 : Bond lengths [Å] and angles [°] for MIL-68.

V(1)-O(4)#1 : 1.8323(17)

V(1)-O(4) : 1.8323(17)

V(1)-O(2) : 1.9900(18)

V(1)-O(2)#1 : 1.9900(18)

V(1)-O(2)#2 : 1.9900(18)

V(1)-O(2)#3 : 1.9900(18)

V(2)-O(5)#4 : 1.9329(16)

V(2)-O(5) : 1.9329(16)

V(2)-O(3)#4 : 1.9837(17)

V(2)-O(3) : 1.9837(17)

V(2)-O(1)#4 : 1.9868(16)

V(2)-O(1) : 1.9868(16)

O(1)-C(4) : 1.203(2)

O(2)-C(7) : 1.282(2)

O(3)-C(3) : 1.269(2)

O(4)-V(1)#5 : 1.8323(17)

O(5)-V(2)#6 : 1.9329(16)

C(1)-C(2)#7 : 1.370(3)

C(1)-C(2) : 1.370(3)

C(1)-C(4) : 1.615(5)

C(2)-C(2)#8 : 1.321(5)

C(2)-H(2) : 0.9300

C(3)-O(3)#7 : 1.269(2)

C(3)-C(6) : 1.546(5)

C(4)-O(1)#7 : 1.203(2)

C(5)-C(9) : 1.354(4)

C(5)-C(6) : 1.356(3)

C(5)-H(5) : 0.9300

C(6)-C(5)#7 : 1.356(3)

C(7)-O(2)#7 : 1.282(2)

C(7)-C(8) : 1.553(5)

C(8)-C(9) : 1.354(3)

C(8)-C(9)#7 : 1.354(3)

C(9)-H(9) : 0.9300

O(4)#1-V(1)-O(4) : 180.0(3)

O(4)#1-V(1)-O(2) : 88.28(11)

O(4)-V(1)-O(2) : 91.72(11)

O(4)#1-V(1)-O(2)#1 : 91.72(11)

O(4)-V(1)-O(2)#1 : 88.28(11)

O(2)-V(1)-O(2)#1 :180.00(11)

O(4)#1-V(1)-O(2)#2 : 91.72(11)

O(4)-V(1)-O(2)#2 : 88.28(11)

O(2)-V(1)-O(2)#2 : 96.34(11)

O(2)#1-V(1)-O(2)#2 : 83.66(11)

O(4)#1-V(1)-O(2)#3 : 88.28(11)

O(4)-V(1)-O(2)#3 : 91.72(11)

O(2)-V(1)-O(2)#3 : 83.66(11)

O(2)#1-V(1)-O(2)#3 : 96.34(11)

O(2)#2-V(1)-O(2)#3 : 180.00(11)

O(5)#4-V(2)-O(5) : 180.00(18)

O(5)#4-V(2)-O(3)#4 : 87.38(11)

O(5)-V(2)-O(3)#4 : 92.62(11)

O(5)#4-V(2)-O(3) : 92.62(11)

O(5)-V(2)-O(3) : 87.38(11)

O(3)#4-V(2)-O(3) : 180.00(4)

O(5)#4-V(2)-O(1)#4 : 89.20(11)

O(5)-V(2)-O(1)#4 : 90.80(11)

O(3)#4-V(2)-O(1)#4 : 88.70(7)

O(3)-V(2)-O(1)#4 : 91.30(7)

O(5)#4-V(2)-O(1) : 90.80(11)

O(5)-V(2)-O(1) : 89.20(11)

O(3)#4-V(2)-O(1) : 91.30(7)

O(3)-V(2)-O(1) : 88.70(7)

O(1)#4-V(2)-O(1) : 180.00(10)

C(4)-O(1)-V(2) : 132.18(19)

C(7)-O(2)-V(1) : 134.19(19)

C(3)-O(3)-V(2) : 132.1(2)

V(1)#5-O(4)-V(1) : 138.8(3)

V(2)-O(5)-V(2)#6 : 125.08(18)

C(2)#7-C(1)-C(2) : 118.3(3)

C(2)#7-C(1)-C(4) : 120.76(16)

C(2)-C(1)-C(4) : 120.76(16)

C(2)#8-C(2)-C(1) : 120.81(16)

C(2)#8-C(2)-H(2) : 119.6

C(1)-C(2)-H(2) : 119.6

O(3)-C(3)-O(3)#7 : 126.4(4)

O(3)-C(3)-C(6) : 115.55(18)

O(3)#7-C(3)-C(6) : 115.55(18)

O(1)-C(4)-O(1)#7 : 131.1(3)

O(1)-C(4)-C(1) : 114.42(17)

O(1)#7-C(4)-C(1) : 114.42(17)

C(9)-C(5)-C(6) : 120.9(3)

C(9)-C(5)-H(5) : 119.6

C(6)-C(5)-H(5) : 119.6

C(5)#7-C(6)-C(5) : 119.6(3)

C(5)#7-C(6)-C(3) : 119.88(17)

C(5)-C(6)-C(3) : 119.88(17)

O(2)-C(7)-O(2)#7 : 125.1(3)

O(2)-C(7)-C(8) : 117.31(16)

O(2)#7-C(7)-C(8) : 117.31(16)

C(9)-C(8)-C(9)#7 : 122.7(4)

C(9)-C(8)-C(7) : 118.60(18)

C(9)#7-C(8)-C(7) : 118.60(18)

C(5)-C(9)-C(8) : 117.9(3)

C(5)-C(9)-H(9) : 121.0

C(8)-C(9)-H(9) : 121.0

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y,-z+1    #2 x,-y,-z+1    #3 -x,y,z

#4 -x+1/2,-y+1/2,-z+1    #5 -x,-y,z-1/2

#6 -x+1/2,-y+1/2,z-1/2    #7 x,y,-z+3/2

#8 -x+1,y,z