Supplementary Information

Fig. S1 and fig. S2 show the raw and corrected kinetic data of Pol396 and Pol397 with substrate 3.

General methodology for polymer preparation and kinetic assays

In a typical preparation the arginine (2eq.) and the tyrosine (1eq) monomers are dissolved in the appropriate volume of DMSO followed by addition of the template (1eq.). After a few minutes acrylamide, N,N’-ethylene bisacrylamide and the initiator azoisobutyronitrile (1.5%) are added. The reaction mixture is flushed with nitrogen and sealed in WhetmanTM bottles and is heated at 80ºC for 4 days. Subsequently the polymer is precipitated by the addition of diethylether, filtered and resuspended  in a solution of 5% triethylamine in methanol (v/v) to extract the template. The solution is gently stirred overnight. Polymer is isolated by extensive dialysis against water followed by freezedrying that gives the polymer as a fine white poweder. Non imprinted polymers follow the same procedure.

Hydrolysis of carbonate 2 was performed in a 9:1 solution of DMSO and Tris-HCl buffer (0.05M, pH 8.0) at 25°C. The catalytic activity of the microgels was investigated by monitoring the release of 4-nitrophenolate, at =425nm (=9473 M-1s-1) or 2-nitrophenolate at = 441(=1957 M-1s-1).