# Supplementary Information

Schematic of MOCVD rig

Fig 1c SEM image of sintered specimen at low magnification

Fig 2 SEM image of unsintered specimen at low magnification

Fig 1a SEM image of unsintered specimen at low magnification

Fig 2 SEM image of unsintered specimen at low magnification

Fig. 1b SEM image of unsintered specimen at high magnification (x1000)

Fig. 3 SEM image of unsintered specimen at high magnification (x1000)

Fig. 1d SEM image of sintered specimen at high magnification (x1000)

Table 1 FT-Raman  peaks for sintered specimen, human femur, calcium carbonate and carbonated apatite

| Peak Assignment (cm-1) | Sintered Ca/P specimen | Human Femur | Synthetic Hydroxyapatite | Synthetic Carbonated Apatite | Calcium Carbonate (standard spectra) |
| --- | --- | --- | --- | --- | --- |
| CH stretch Amide Band I CO32- CO32- C-H (bend) Amide Band II C-O CO32- CO32- (bend) PO43- (symmetric stretch) PO43- (asymmetric stretch) CO32- (bend) PO43- (bend) PO43- (bend) | 3000 - 2800 - - - - - - - - 953 786 702 - 444 | 3000 – 2900 1636 - - 1450 1262 1242 1062 1036 952 - - 584 429 | - - - 1578 - 1507 - - - - - 952 774, 690 - - 436 | - - - - - - - 1078 - 946 - - 595 438, 454 | - - 1747 1434 - - - 1084 - - - 710 - - |

a Footnote text.

Table 2 FTIR peaks for sintered specimen, carbonated apatite (IRC) and commercial HA

| Peak Assignment HA (cm-1) | Sintered Ca/P specimen | Commercial HA Merck | Carbonated apatite |
| --- | --- | --- | --- |
| Hydroxyl stretch Carbonate v3 - (m) - (m) - (m) - (w) Phosphate v3 - (vs) - (vs) Phosphate v1 (m) Carbonate v2 (m) Phosphate v4 (m) - (m) - (vs) - (vs) Phosphate v2 (w) | 3538 - - - 1417 - 1200 - 966 1096 1044 982 860 - - 605 555 - | 3570 1650 – 1300 1648 1455 1417 - 1190 – 976 1091 1042 962 877 660 - 520 632 602 566 472 | 3571 1650 – 1300 1650 1454 1417 1321 1190 – 976 - 1041 961 873 660 - 520 629 603 567 469 |

a Footnote text.

Fig.2 Raman spectrum for (a) sintered CVD coating, (b) deproteinated human bone mineral and (c) commercial HA (Plasma Biotol P120)

Fig 2 SEM image of unsintered specimen at low magnification

Fig. 3 FTIR spectrum of (a) sintered CVD coating, (b) deproteinated human bone mineral and  (c) commercial HA (Plasma Biotol P120).

Fig 2 SEM image of unsintered specimen at low magnification

.

# Comments

General comments

I explained to Ven that we must use the standard FTIR and FT-raman spectra of HA to provide comparison. A couple of figure on overlayed spectra will be very useful

# Text boxes

c

Mixer

- Bubblers

Sample

- Flow regulator

Exhaust

TBP

Ca(hffpd)2

Heated Zone

Cold wall reactor

Argon

b

c

b

a

a