Supporting Information

Poly(ethylene glycol) as Solvent for Transition Metal Mediated Living Radical Polymerisation: Towards the Design of Green Polymerisation Processes

Sébastien Perrier,* Hesna Gemici and Song Li

Department of Colour and Polymer Chemistry, The University of Leeds, Leeds, LS2 9JT. Fax: +44 113 343 2947; Tel: +44 113 343 2947; E-mail: S.perrier@leeds.ac.uk

| Solvent | Time (min) | Conversion (%) | ln(1/(1-X)) | Mn, th | Mn, SEC | PDI |
| --- | --- | --- | --- | --- | --- | --- |
| PEG400 | 20 | 20.3 | 0.23 | 2,000 | 2,300 | 1.06 |
|  | 40 | 46.2 | 0.62 | 4,600 | 5,200 | 1.19 |
|  | 54 | 57.2 | 0.85 | 5,700 | 6,300 | 1.20 |
|  | 71 | 65.6 | 1.07 | 6,600 | 6,500 | 1.24 |
|  | 87 | 69.0 | 1.17 | 6,900 | 7,100 | 1.26 |
|  | 108 | 75.8 | 1.42 | 7,600 | 7,900 | 1.28 |
| Toluene | 60 | 30.0 | 0.36 | 3,000 | 5,200 | 1.11 |
|  | 120 | 49.3 | 0.68 | 5,000 | 6,600 | 1.16 |
|  | 160 | 59.8 | 0.91 | 6,000 | 7,600 | 1.17 |
|  | 190 | 68.1 | 1.14 | 6,800 | 8,000 | 1.16 |
|  | 1,032 | 99.1 | 4.71 | 10,000 | 11,700 | 1.10 |

Table 1. Data for the polymerisation of MMA at 90oC initiated by 2-EIBr and mediated by Cu / N-(n-pentyl)-2-pyridylmethanimine in PEG400 ([M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:0.97:0.03:2) and toluene ([M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:1:0:2).

| Solvent | Time (min) | Conversion (%) | ln(1/(1-X)) | Mn, th | Mn, SEC | PDI |
| --- | --- | --- | --- | --- | --- | --- |
| PEG400 | 300 | 6.1 | 0.06 | 600 | 1,000 | 1.22 |
|  | 1,380 | 10.6 | 0.11 | 1,100 | 1,500 | 1.24 |
|  | 2,815 | 15.6 | 0.17 | 1,600 | 1,600 | 1.24 |
|  | 3,165 | 21.4 | 0.24 | 2,200 | 1,600 | 1.24 |
|  | 4,620 | 22.6 | 0.26 | 2,400 | 1,800 | 1.24 |
| Xylene | 50 | 11.9 | 0.13 | 1,200 | 1,500 | 1.64 |
|  | 100 | 20.2 | 0.23 | 2,100 | 2,800 | 1.43 |
|  | 150 | 28.5 | 0.34 | 3,000 | 3,400 | 1.43 |
|  | 200 | 37.9 | 0.48 | 4,000 | 4,000 | 1.41 |
|  | 250 | 45.0 | 0.60 | 4,700 | 4,800 | 1.35 |
|  | 300 | 51.2 | 0.72 | 5,300 | 5,600 | 1.30 |
|  | 4,200 | 97.0 | 3.51 | 10,100 | 9,800 | 1.21 |

Table 2. Data for the polymerisation of Styrene at 110oC initiated by 2-EIBr and mediated by Cu / N-(n-pentyl)-2-pyridylmethanimine in PEG400 ([M]:[I]:[Cu(I)]:[L] = 100:1:1:2) and xylene ([M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:1:2).

Fig. 1. Pseudo first order rate plot for the polymerisation of MMA at 90oC initiated by 2-EIBr and mediated by Cu / N-(n-pentyl)-2-pyridylmethanimine in PEG 400 (■; [M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:0.97:0.03:2), (□; [M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:1:0:2) and toluene (●; [M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:1:0:2) (Note: The datapoint for the polymerisation in PEG 400 (□; [M]:[I]:[Cu(I)]:[L] = 100:1:1:2) corresponding to 98.7% conversion after 18.3h has not been included for the clarity of the graph).

Figure 2. Evolution of molecular weight and PDI with monomer conversion for the polymerisation of MMA at 90oC initiated by 2-EIBr and mediated by Cu / N-(n-pentyl)-2-pyridylmethanimine in PEG 400 (■; [M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:0.97:0.03:2), (□; [M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:1:0:2) and toluene (●; [M]:[I]:[Cu(I)]:[Cu(II)]:[L] = 100:1:1:0:2). The theoretical Mn is indicated by a straight line.