Supporting materials

(1) Chemical preparations:

All chemicals were reagent grade and were used without further purification.

Compound 1: An aqueous solution (10ml) of 1,1’-dimethyl-4,4’-bipyridinium dichloride hydrate (0.155g, 0.5mmol) was slowly added to a solution of KSCN (0.291g, 3mmol) and 3CdSO4(8H2O (0.085g, 0.111mmol) in distilled water (15ml), the resulting solution was allowed to stand for 72 hours. The resulting yellow crystalline precipitate was filtered and dried for the crystallographic study. Compound 2 was obtained by following a similar process but with a more amount of 3CdSO4(8H2O (0.256g, 0.333mmol) as colorless crystals.

(2) Crystal data and details of determinations

Crystal data for 1 (0.5 x 0.4 x 0.25 mm), monoclinic, P21/c, a=11.728(1), b=13.294(1), c=13.240(1)Å, (=93.79(1) V=2059.9(2)Å3, Z=4, ρcalcd=1.712 mg/m3, R1= 0.043, wR2= 0.126 (17230 reflections total, 3620 unique, 3350 (I>2((I)), goodness-of-fit =1.07. Crystal data for 2 (0.3 x 0.26 x 0.1 mm), triclinic, P-1 (no. 2), a=11.4079(8), b=12.7469(10), c=15.7543(10) Å, V=2167.67(30) Å3, =86.74(1)°, =71.98(1)°, =84.51(1)°, Z=1, ρcalcd=1.948 mg/m3, R1= 0.025, wR2= 0.068 (37635 reflections total, 9553 unique, 7993 (I>2((I)), goodness-of-fit =1.06. The data collections were performed for 1 at 173 K on a Bruker SMART diffractometer and for 2 at 210K on a STOE IPDS diffractometer, using MoK( ((=0.71073), by (-scan method, within limits 1.74(<θ<25.00( for 1 and 3.03(<θ<25.68( for 2. An empirical adsorption correction was applied using the SADABS program. The structure was solved by direct method and refined using full-matrix least squares on F2 (SHELXL). In 1 all H-atoms were placed in calculated positions but in 2 some of H-atoms were placed in calculated positions and others were allowed to ride on their respective parent atoms. CCDC-201155-201156 in the Cambridge Crystallographic Data Centre contains supplementary crystallographic data for the structures of this paper. Copies of the data can be obtained free of charge on application to CCDC, 12 Union Road, Cambridge CB21EZ, UK (e-mail:deposit@ccdc.cam.ac.uk).

(3) The structure of compound [MV](NCS)2

Table S1 Crystallographic Data for [MV](NCS)2

____________________________________________________________

T (K) 	173(2)

Empirical formula 	C14 H14 N4 S2

Formula weight 	302.41

a, Å            	           				5.5395(5)

b, Å				                     	7.5164(6)

c, Å				                     	9.3414(8)

alpha				                 	91.154(2)

beta              				 	102.372(2)

gamma				                 	105.0000(10)

V Å3						365.79(5)

Symmetry	triclinic

Space group 	P-1 (no. 2)

wavelength           				0.7107

no. of unique reflections			1870

Z			1

Density, calculated			1.373 g/cm3

R 						0.0359

Rw 						0.1028

____________________________________________________________

(4)  IR spectra for compound 1, compound 2 and Methylviologen dichloride

(5)   EPR spectra for compound 1 and compound 2 at room temperature