Supplemental Figures

C1 Coupling via Bromine Activation and Tandem Catalytic Condensation and Neutralization over CaO/Zeolite Composites.

Ivan Lorkovic,a* Maria Noy,a Mike Weiss,b Jeff Sherman,b Eric McFarland, b,c Galen D. Stucky,a and Peter C. Forda

a.Department of Chemistry and Biochemistry, University of California, Santa Barbara, CA  93106.

Fax:  805 893 4120; Tel:  805 893 5239; E-mail:  lorkovic@chem.ucsb.edu

bGas Reaction Technogies, Inc., 301B S. Wimbrow Dr.  Sebastian, FL  32958

cDepartment of Chemical Engineering, University of California, Santa Barbara, CA  93106

Figure S1.   Continued methane bromination and condensation over the same Ca/ZSM-5 bed (5.0 g) used in Figure 1 past the HBr saturation limit (reached at ~100 min) of the bed.  Feed:  CH4:Br2 (5:0.5 cc/min).  First Stage:  Plug flow reactor (1 x 100 mm glass tube, 500o C.  space time = 0.3 s.  Br2 conversion = 100%, CH4 conversion = 8.2%).  Second Stage:  Fixed bed:  (10 x 100 mm plug of 5 g. Ca-ZSM-5, 400 C, space time = 20 s, WHSV = 0.04 h-1).

Figure S2.  CH3Br condensation to olefins over a 10 x 100 mm plug of CaO/ZSM-5 (5 g) at 400 C.  Feed, CH4:CH3Br (5:0.6 cc/min); space time = 20 s, WHSV = 0.025 h-1.  Selectivity to C2-C5 is >70%.

.