Supplementary Information

Preparation of metal sulfide-polymer composite microspheres

with patterned surface structures

Yu Fang*, Chaoliang Bai and Ying Zhang

School of Chemistry and Materials Science, Shaanxi Normal University, Xi’an 710062, P. R. China. Fax: 0086 29 5307025; Tel: 0086 29 5307534(L); E-mail: yfang@snnu.edu.cn.

- Formation of the patterned surface structures of the composite microspheres is a gradual process. As an example, Fig.1 shows the SEM image of the CuS-PNIPAM-MAA composite microspheres and their enlarged surface structure. In this case, the precipitation was lasted for only 5 min.

- The metal sulfides in the composites have been confirmed by (-ray diffraction analysis. The XRD patterns of the composites are shown in Fig. 2.

- The IR spectra of the two templates are shown in Fig. 3.

- The contents of metal sulfides in the composites have been analyzed by TG analysis. The results are very close to the theoretical values.

# Text boxes

b

a

Fig. 1 SEM images of CuS-PNIPAM-MAA composite microspheres (a, b) and high magnification image of part of the surface of the microspheres (c). The precipitation was lasted for 5 min.

c

2θ

Fig. 2 XRD patterns of P(NIPAM-co-MAA) microgels (red) and its composite micro-spheres with Ag2S

a

b

Fig. 3 Infrared spectra of (a) PNIPAM and (b) P(NIPAM-co-MAA)