The Kinetics of Propene and Hexene Polymerization with [(SBI)ZrR]+X-: Evidence for Monomer-Dependent Early or Late Transition States

Fuquan Song, Roderick D. Cannon and Manfred Bochmann*

Wolfson Materials and Catalysis Centre, School of Chemical Sciences, University of East Anglia, Norwich NR4 7TJ, UK.

Supporting Information

1. Propene polymerizations with pre-formed [(SBI)ZrCH2SiMe3+·· MeB(C6F5)3 -]:

Fig. S1. Propene polymerisation with [(SBI)ZrCH2SiMe3···MeB(C6F5)3]: polymer mass vs. initial catalyst concentration. Conditions: Batch reaction, toluene, T = 20 ºC, V = 100 mL, [M] = 0.71 mol L-1, t = 1 min.

Fig. S2. Propene polymerisation with [(SBI)ZrCH2SiMe3···MeB(C6F5)3]: Polymer mass vs. polymerization time. Conditions: batch reaction, toluene, T = 20 ºC, V = 100 mL, [M] = 0.71 mol L-1, Cm0 = 10 mol. Average productivity = (3.1 ± 0.1) x 106g·PP (mol Zr)-1·h-1·[C3H6]-1 .

With [M] = monomer concentration, Cm0 = amount of initially added catalyst:

Slope in Fig S2 = 0.1102 = 42⋅[M]⋅Cmo⋅kpo

kpo = 6.2 L mol-1s-1

Taking account of catalyst deactivation from Fig. S1, Cm = 10-6.9 = 3.1 mol, hence

kp = kpo(Cmo/ Cm) = (19.9 ± 1.1) L mol-1s-1

Alternatively, kp can be calculated from Fig. S1: Slope = 42×10−6[M]⋅t⋅kp

kp=0.035942⋅10−6[M]⋅t=20.0L mol-1L-1

2. Propene polymerizations with pre-formed [(SBI)ZrCH2SiMe3+·· B(C6F5)4 -]:

Propene polymerisation with [(SBI)ZrCH2SiMe3···B(C6F5)4]. Catalyst solution was prepared by combining (SBI)Zr(Me)CH2SiMe3 with trityl salt in toluene +10 vol-% difluorobenzene.

Table S1. Results from batch reactions of 0.5 min duration.

| Run | Zr. mol | B(C6F5)4-, mol | time (min) | PP yield, g | Productivitya |
| --- | --- | --- | --- | --- | --- |
| 18 | 10 | 10 | 0.5 | 3.813 | 207.9 |
| 19 | 10 | 10 | 0.5 | 3.703 | 201.8 |
| 20 | 10 | 10 | 0.5 | 3.781 | 206.2 |

a In 106 g PP (mol Zr)-1h-1[C3H6]-1.

Conditions: T = 20°C, V = 100 mL, toluene; [C3H6] = 0.71 mol/L.

kp = (1358 ± 12) L mol-1s-1.

3. Hexene polymerizations with pre-formed [(SBI)ZrCH2SiMe3+·· MeB(C6F5)3 -]:

Fig. S3. Mass of polyhexene mass vs. Cm0. Catalyst [(SBI)ZrCH2SiMe3···MeB(C6F5)3]. Conditions: T = 20 ºC, 100 mL,  toluene, [hexene]0 = 0.80 mol L-1, t = 1 min.  Cmo- Cm =  3.4 µmol

Fig. S4. Mass of polyhexene vs. time. [(SBI)ZrCH2SiMe3···MeB(C6F5)3], T = 20 ºC, 100 mL, toluene. [hexene]0 = 0.80 mol L-1, Cmo =  10 µmol.

Calculation:		Y=84.16⋅[M]⋅Cmo⋅kpo⋅t

kpo from Fig. S4:      kpo = 2.9 L mol-1s-1

Alternatively, using rate law

ln([M]0/[M]) = kpo[Cmo] t

kpo = 3.2 L mol-1s-1

From Fig. S3 it can be seen that 3.4 µmole of precursor added at t = 0 has been deactivated, hence kp = (4.8 ± 0.1) L mol-1s-1.

kp from Fig.S3, slope 0.0184:

kp=0.018484.16⋅10−6[M]⋅t=4.6L mol-1L-1

4. Hexene polymerizations with pre-formed [(SBI)ZrCH2SiMe3+·· B(C6F5)4-]:

Fig. S5. Mass of polyhexene mass as a function of [(SBI)ZrCH2SiMe3···B(C6F5)4] concentration. Cmo - Cm = 2.3 µmol. Conditions: T = 20°C, 100 mL, toluene, [hexene]0 = 0.80 mol L-1, t = 1 min.

Fig. S6. Mass of polyhexene as function of t. Catalyst [(SBI)ZrCH2SiMe3···B(C6F5)4]. catalyst system. Conditions: T = 20 ºC, 100 mL, toluene. [hexene]0 = 0.80 mol L-1, Cmo =  10 µmol.

kpo = (11.6 ± 0.9) L mol-1s-1

kp = kpo(Cm0/Cm) = (15.1 ± 1.1) L mol-1s-1

5. Hexene polymerizations with (SBI)ZrMe(R) /CPh3[B(C6F5)4] in the presence of  TIBA scavenger:

Table S2. 1-Hexene polymerization catalyzed by (SBI)ZrMe(R) / TIBA / [Ph3C][B(C6F5)4]

| run | Zr (mol) | Ph3C/µmol | 1-hexene/g | t/min | Yield/g | kp Lmol-1s-1 |
| --- | --- | --- | --- | --- | --- | --- |
| 2252 | R = Me (5.0) | 5.0 | 2.02 | 2.5 | 0.55 | 21.2 |
| 2262 | R = CH2SiMe3 (5.0) | 5.0 | 2.1 | 2.5 | 0.518 | 18.9 |

Toluene, 50 mL, 23°C.

Fig. S7. 1H NMR spectra of [(SBI)ZrCH2SiMe3][B(C6F5)4] at 20 ˚C and  –20 ˚C in d8-tol with 20% 1,2-F2C6H4.

19F NMR (20 °C):  (-132.48 (o-F), -163.18 (p-F), -167.03 (m-F).

Fig. S8. 1H NMR spectrum of [(SBI)ZrCH2SiMe3···MeB(C6F5)3] in toluene-d8 at 20 ˚C.