Supporting information:

A powder X-Ray pattern of crystals homogenous sample (giving below) showed that all reflections are indexed in the monoclinic cell of [Cu(O2C-(CH2)3-NH3)2]PbBr4 given above. 1 melts at 194 °C and rapidly decomposes in two steps up to 570 °C. Single crystals EDX microanalysis (SEM) give the following average Cu, Pb, Br atomic ratio (theoretical values appear in brackets) : Cu 16.1 (16.7), Pb 16.7 (16.7); Br 67.5 (66.7)

Powder X-Ray pattern of blue-green sample of [Cu(O2C-(CH2)3-NH3]PbBr4

(0 0 2)

(0 1 1)

(1 0 -1)

(1 1 1)

(1 1 0)

(0 0 4)

(1 0 1)

(2 0 0)

(0 1 4)

(0 2 0)

(1 1 4)

(0 0 6)

(0 1 6)

indexation of the twelve first peaks together with the highest one in the monoclinic cell a =8.4581, b=8.3703, c=26.9075, =98.62

(2 2 -2)