# Supplementary data

#### Preparation and Structure Characterization:

1Er: The pH value of an aqueous solution (10 ml) of Er(ClO4)36H2O (0.574g, 1mmol) and glycine (0.150g, 2mmol) was adjusted to about 7.0 by slow addition of 0.1 M NaOH solution. After two hours of being heated and stirred at 60C, Cu(ClO4)26H2O (0.741g, 2mmol) was added. Then the pH value of the solution was again adjusted to about 6.6. After two hours of stirring, the solution was filtrated and placed in a desiccator filled with phosphorus pentaoxide. Blue crystals were obtained several weeks later. Yield: 0.31g, 23%. Element analysis (%) calcd for C40H210Cl24Cu27Er6N20Na2O216: C 5.97, H 2.63, N 3.48; found: C 5.74, H 2.49, N 3.79.

Crystal data of 1Er: Na2[Er6Cu27(Gly)20(3-OH)30 (H2O)22(ClO4)] (ClO4)23 (H2O)28, Mr = 8044.20, triclinic, P-1, a = 17.3348(3), b = 18.0854(2), c = 20.76920(10) Å,  = 106.9130(10),  = 100.5850(10), = 105.8490(10), V= 5742.67(12) Å3, Z= 1,  = 2.326 g cm-3, 2qmax = 50.12°, (-20  h 10, -21  k  21, -24  l  24), T = 293(2)K, 29441 measured reflections. R1= 0.0735 for 15070 reflections (I>2s(I)), R2 = 14.80 for 19927 independent reflections (all data) and 1527 parameters. Gof = 1.146. Several oxygen atoms from ClO4- were treated to be isotropic. Hydrogen atoms on carbon and nitrogen atoms were added geometrically and not refined, no attempt was made to locate the hydrogen atoms of water.

Intensity data were collected on a Siemens Smart/CCD area-detector diffractometer with Mo-K radiation (=0.71073Å). Data reductions and cell refinements were performed with Smart-CCD software [1]. The structures were solved by direct methods using SHELXS-97[2] and were refined by full-matrix least squares methods using SHELXL-97.

[1] XSCANS (Version 2.1), Siemens Analytical X-Ray Instruments Inc., Madison, WI, 1994.

[2] G. M. Sheldrick, SHELXL-97, Program for X-ray Crystal Structure Refinement; University of Göttingen: Göttingen, (Germany), 1997.

Structure Figures:

Figure S1. Coordination polyhedron of Er3+ ion.

(a)                                      (b)

, Er;, Cu; , O

Figure S2. (a) The metal-hydroxide framework of the Er6Cu24 node of 1Er; (b) the structure of one of the faces of the octahedron.

, Er;, Cu; , C; , N; , O

Figure S3. The structure of the cation of 1Er (the captured ClO4- ion is omitted for clarity).

Figure S4. The structure of one of vertices (Er1) of the octahedron of 1Er. (ellipsoids at 25% probability).

Figure S5. The structure of one of vertices (Er2) of the octahedron of 1Er. (ellipsoids at 25% probability).

Figure S6. The structure of one of vertices (Er3) of the octahedron of 1Er. (ellipsoids at 25% probability).

Physical Properties

Figure S7. Temperature dependence of the electrical conductivity of 1Er.

Figure S8. Temperature dependence of magnetic susceptibility of 1Er. : 2-300K at 5000G : 2-300K at 2000G.