SUPPLEMENTARY MATERIAL

XRD pattern of trumpet-shaped structure:

The pattern corresponds to the calcite phase of calcium carbonate.  The sample was measured at room temperature on a STOE Powder Diffraction System with monochromated Co radiation.