Paper B403213F

Supplementary Material for Chemical Reactions for Catalyst Preparation

Au101(PPh3)21Cl5

b NaHB4

c

a

HAuCl4 + 2PPh3 + H2O              AuCl(PPh3) + O=PPh3 + 3HCl

Scheme 1. Reaction pathway to nanoparticles c. a: Toluene, water, tetraoctylammonium bromide, 5 min, room temperature. b: 10 equiv of sodium borohydride, 3 h, room temperature. c: average empirical formula from ref 12. (All operations are carried out in a fume hood under ambient conditions.)