The proton NMR spectra (a) and (b) are zirconium isopropoxide with 0.5 and 1 mol equivalent of acetylacetone. Spectra (c) was obtained from Zr(OiPr)(acac)3 crystals. Mixed ligand precursor after 15 minutes (d) and 16 hours (e) after addition of 2 mol equivalent mol acetylacetone.

The signals corresponding to Zr(OiPr)3(acac) are marked with (), to Zr(OiPr)(acac)3 – with (), and to Zr(OiPr)3(iPrOH) – with (),  Zr(acac)4 – with ().