Monoreduced [M(R,R'timdt)2]– Dithiolenes (M = Ni, Pd, Pt; R,R'timdt = disubstituted imidazolidine-2,4,5-trithione): Solid State Photoconducting Properties in the Third Optical Fiber Window

M. Carla Aragoni,a Massimiliano Arca,a,* Mario Caironi,c Carla Denotti,a Francesco A. Devillanova,a Emanuela Grigiotti,b Francesco Isaia,a Franco Laschi,b Vito Lippolis,a Dario Natali,c Luca Pala,a Marco Sampietro,c Piero Zanellob

a Dipartimento di Chimica Inorganica ed Analitica,Università degli Studi di Cagliari, S.S. 554 bivio per Sestu, 09042 Monserrato – Cagliari, Italy. E-mail: marca@unica.it; Fax: +39 070 675 4456; Tel: +39 070 675 4483

b Dipartimento di Chimica, Università degli Studi di Siena, Via A. Moro, 53100 Siena, Italy

c Dipartimento di Elettronica e Informazione, Politecnico di Milano, P.za L. da Vinci 32, 20133, Milano, Italy and INFN, sez. di Milano, Via Celoria 16, 20133 Milano, Italy

Electronic Supplementary Information (ESI)

Device Specifications

Devices were prepared by casting a CH2Cl2 solution of the active material on a hot 500m thick SiO2 substrate where a chromium micro-lithography was previously provided: a low capacitive planar metal-semiconductor-metal configuration was obtained (Fig. S1) with interelectrode spacings of 12 m and an effective width of 15mm. We irradiated our prototype photodetectors with a set of light emitting diodes. Device responsivity (Fig. 2 in the paper) was measured by biasing with a voltage source and connecting the device to a transimpedance amplifier, as shown in Fig. S1; light pulses lasted 500s. In order to measure the time response to an impinging train of light pulses (Fig. 3 in the paper), the amplifying chain was enhanced by connecting a band pass filter to the output of the transimpedance amplifier in order to increase the signal-to-noise ratio.

Fig. S1 Schematic representation of the planar configuration adopted for the photodetector, biased and connected to a transimpedance amplifier (left); top view of the interdigitated geometry adopted (right).

SiO2

Band Pass Filter

Fig. S2 Frontier KS-molecular orbital diagram and symmetry representations of the molecular orbitals involved in the NIR transition for [Pt(H2timdt)2]0/–