Definition of each states of porous coordination polymers.

We define each porous coordination polymers with or without guests in the pore as follows.

CPL-1 : host framework without guests.

CPL-1 nH2O : as synthesized compound which contains water molecules as guests.

CPL-1 nCH3OH : porous compound contains methanol molecules as guests.

Simulated lineshapes of 2H NMR.

The quadrupole coupling constant Q, the angle β between the principal axis of the quadrupolar tensor and that of the dipole tensor, the paramagnetic shift parameter νP, and relative intensity for each component RI (i = 1~3) obtained from the simulation are collected in Table below.

Table  Fit parameters of the 2H NMR spectra of CPL-1 nCH3OH at various temperatures

| i | βi /deg | νPi /kHz |  | 293 K |  |  |  | 253 K |  |  |  | 223 K |  |  |  | 173 K |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Qi /kHz | RIa | θ/degb |  | Qi /kHz | RI | θ/deg |  | Qi /kHz | RI | θ/deg |  | Qi /kHz | RI | θ/deg |
| 1 | 40 | 2.0 |  | 16.2 | 0.50 | 41.4 |  | 18.0 | 0.20 | 39.9 |  | 18.0 | 0.06 | 39.9 |  | 21.8 | 0.03 | 36.7 |
| 2 | 40 | 3.0 |  | 28.0 | 0.25 | 31.3 |  | 28.0 | 0.38 | 31.3 |  | 29.4 | 0.17 | 30.0 |  | 31.6 | 0.10 | 27.9 |
| 3 | 80 | 2.0 |  | 36.8 | 0.25 | 22.4 |  | 38.2 | 0.42 | 20.7 |  | 38.6 | 0.77 | 20.2 |  | 41.4 | 0.87 | 16.4 |

a The relative intensity of the spectral component at each temperature.  b The angle for the rotation of  CD3OH obtained by equation 1 with Q0 = 47 kHz.