Proton transfer and N(+)–HS(–) hydrogen bonds in the crystal structure of 4-aminothiophenol

Ram K. R. Jetti,a Roland Boese,a* Tejender S. Thakur,b Venu R. Vangala,b and Gautam R. Desirajub*

aInstitut für Anorganische Chemie, Universität Duisburg-Essen, Universitätsstrasse 57, 45177 Essen, Germany.

bSchool of Chemistry, University of Hyderabad, Hyderabad 500 046, India,

Email:  desiraju@uohyd.ernet.in

# Supplementary Material (ESI)

- (16 pages)

- (i) ORTEP plot drawn at 50 % probability level for nonH atoms.

- (ii) Difference Fourier map for the H-atom positions around the N-atom.

- (iii) Pertinent intermolecular interactions for compound 1.

- (iv) A CSD search on NHS interactions.

- (v) Computational details.

- (vi) Structure refinement parameters.

- (vii) Computation related references.

- (viii) IR spectra recorded at variable temperatures.

(i) ORTEP plot of compound 1 drawn at 50% probability level for nonH atoms.

(ii) Difference Fourier map for the H-atom positions around the N-atom.

Given below is the difference Fourier for the H-atom positions calculated only in the plane of idealised and normalised (1.009 Ǻ) H-atoms at the nitrogen. The contour spacing is 0.05 e Å–3. The maximum contour line is 0.35 e Å–3.

(iii) Table 1. Pertinent intermolecular interactions for compound 1.

| Compound | Interaction | d (Å) | D (Å) |   |
| --- | --- | --- | --- | --- |
| 1 | NHS | 2.2175(5) | 3.1913(13) | 161.72(8) |
|  | NHS | 2.2256(5) | 3.2032(13) | 162.75(8) |
|  | NHS | 2.1362(7) | 3.1428(17) | 175.24(8) |

(iv) A CSD search on NHS interactions.

A search of the CSD (Version 5.25, November 2003) for error free NHS organic, non polymeric structures with R<0.10 were carried out. ‘No co-ordinates present’ structures were excluded from the search. Of the 1932 hits with NHS (neutral and ionic) interactions in the subset, 59 hits with the N(+)HS()  [distance (D) and angle () range: 2.84.3 Å, 120180] were found.

| a | b |
| --- | --- |

Fig. 1 Histogram of (a) NS distance (D) plot for both neutral and ionic NHS interactions and (b) N(+)S() distance (D) plot for only ionic interactions.

Refcodes for aromatic amine thiolates.

CETPAS, GETQEB, HOXYOI, HUZHEP, POXKIW, POXKOC, PUJDUT, REGPIC, WADQUO, WIRPIW, ZIKSIV.

(V) Computational details.

Table 2. Spartan1 RHF/6-31G** computations for the SHN interaction.

| S.No. | Complex | E (kcal mol1) | d (Å) | D (Å) |   |
| --- | --- | --- | --- | --- | --- |
| 1 | HSHNH3 | 3.532 | 2.30 | 3.633 | 178.5 |
| 2 | HSHNH2CH3 | 3.475 | 2.30 | 3.636 | 177.0 |
| 3 | HSHNH(CH3)2 | 3.218 | 2.30 | 3.633 | 180.0 |
| 4 | HSHN(CH3)3 | 3.105 | 2.31 | 3.639 | 176.0 |
| 5 | HSHNH2C6H5 | 2.594 | 2.43 | 3.764 | 179.3 |
| 6 | CH3SHNH2CH3 | 2.666 | 2.39 | 3.716 | 178.4 |
| 7 | CH3SHNH(CH3)2 | 2.245 | 2.23 | 3.560 | 179.0 |
| 8 | CH3SHN(CH3)3 | 2.366 | 2.40 | 3.726 | 177.3 |
| 9 | CH3SHNH2C6H5 | 2.227 | 2.59 | 3.895 | 166.5 |
| 10 | NH2C6H4SHNH3 | 2.667 | 2.39 | 3.637 | 155.2 |
| 11 | NH2C6H4SHNH2CH3 | 2.572 | 2.35 | 3.680 | 173.9 |
| 12 | NH2C6H4SHNH(CH3)2 | 2.461 | 2.37 | 3.694 | 174.5 |
| 13 | NH2C6H4SHNH(CH3)3 | 2.494 | 2.38 | 3.701 | 170.4 |
| 14 | NH2C6H4SH NH2C6H5 | 1.603 | 2.55 | 3.848 | 164.4 |

Table 3. GAMESS022 RHF/6-311G** level calculations on the IBM-AIX 32 processor machine.

| S.No. | Complex | EHF (a. u.) | E kcal mol1 | d (Å) | D (Å) |   |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | HS+NH4 | 454.375602 | 194.8630 | 1.726 | 2.8490 | 156.45 |
| 2 | HS +NH3CH3 | 493.920791 | 345.1748 | 1.702 | 2.9384 | 172.45 |
| 3 | HS +NH2(CH3)2 | 532.961667 | 113.1820 | 1.844 | 2.9699 | 174.36 |
| 4 | HS +NH (CH3)3 | 572.002205 | 108.6301 | 1.899 | 2.9151 | 176.33 |
| 5 | CH3S +NH (CH3)3 | 611.030973 | 109.6422 | 1.671 | 2.9093 | 172.91 |
| 6 | HS +NH3C6H5 | 684.463195 | 111.0391 | 1.746 | 2.9025 | 157.60 |
| 7 | C6H5S +NH3C6H5 | 914.046990 | 102.8249 | 1.671 | 2.9302 | 168.24 |
| 8 | NH2C6H4S+NH3C6H4SH | 1366.628377 | 107.7434 | 1.662 | 2.9346 | 168.76 |
| 9 | HSHNH3 | 454.919126 | 3.4989; 2.84# | 2.374 | 3.7095 | 176.38 |
| 10 | HSHNH2CH3 | 493.951284 | 3.4826; 2.67# | 2.383 | 3.7198 | 179.59 |
| 11 | HSHNH(CH3)2 | 532.986793 | 3.2888; 2.45# | 2.387 | 3.7211 | 175.06 |
| 12 | HSHN(CH3)3 | 572.023759 | 3.0566; 2.24# | 2.389 | 3.7238 | 175.77 |
| 13 | CH3SHN(CH3)3 | 611.061897 | 3.8887; 1.55# | 2.478 | 3.8099 | 176.48 |
| 14 | HSHNH2C6H5 | 684.507949 | 2.4862 | 2.501 | 3.8331 | 133.41 |
| 15 | C6H5S HNH2C6H5 | 914.092488 | 2.5460 | 2.652 | 3.8771 | 152.09 |
| 16 | NH2C6H4SHNH2C6H4SH | 1366.677061 | 2.7002 | 2.979 | 3.8850 | 151.99 |

# BSSE corrected interaction energies calculated at 6-31G** level.

Table 4. Infrared spectra of 4-aminothiophenol at room temperature vs simulated spectra performed on Gaussian033 at RHF/6-31++G(d, p) level of theory.

| S.No. | Mode of vibration | Experimental | Simulated spectra at RHF/631++G(d, p) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Neutral monomer | Zwitterionic monomer | Zwitterionic dimer |
| 1 | NH asymmetric stretch | 3430 | 3918.4 | 3747.7 | 3756, 3749 |
| 2 | NH symmetric stretch | 3371 | 3809.3 | 3708.5 | 3689, 3681 |
| 3 | NH stretch | 3211 |  |  | 3292 |
| 4 | CH aromatic stretch | 3026 | 3340.5 | 3305.6 | 3423-3324 |
| 5 | SH stretch | 2553 | 2863 |  |  |
| 6 | NH bend(scissoring) | 1886 | 1816.3 | 1809 | 1805-1782 |
| 7 | NH3+ bending (deformation) | 1598 |  | 1628.4 | 1670,1624 |
| 8 | C=C aromatic stretch | 1626, 1499, 1423 | 1757, 1664, 1573 | 1733, 1616, 1562 | 1748-1729, 1617-1553, 1313-1311 |
| 9 | CN stretch | 1289 | 1392.8 | 1238 | 1245,1228 |
| 10 | CH in plane bending | 1178, 1089 | 1202, 1296.4 | 1215, 1287.5 | 1279 |
| 11 | CH out of plane bending | 830 | 920 | 886 | 887 |
| 12 | CS stretch | 696 | 770 | 677 | 738 |
| 13 | NH out of plane bending (wagging) | 636 | 433 |  |  |
| 14 | C=C out of plane bending | 522 | 464 | 455 | 509-452 |

Table 5. Corresponding coordinates for calculation2 of the energy of the N(+)HS() interaction (See Table 1 in the main paper).

| complex | X(+)HA(-) at  = 157.6 | X(+)HA(-) at  ~ 90 |
| --- | --- | --- |
| HS +NH3C6H5 | N 3.600614 0.258273 3.349317 S 1.151276 -1.277719 3.091997 H 0.093259 -0.545145 2.725532 H 2.511241 -0.183507 3.057793 H 3.949030 -0.521328 3.880713 H 3.434481 1.005042 3.994803 C 4.548599 0.644957 2.327553 C 5.566283 1.521848 2.678976 C 6.516605 1.879801 1.741832 C 6.446577 1.349196 0.464412 C 5.434112 0.468430 0.123967 C 4.469060 0.107494 1.051846 H 5.608418 1.901341 3.684315 H 7.306001 2.564515 1.975640 H 7.166550 1.634119 -0.273962 H 5.406245 0.079115 -0.876073 H 3.686907 -0.570376 0.788957 | C 4.702568 0.209781 0.744631 C 4.574470 0.669802 2.060673 C 5.556802 1.502509 2.609874 C 6.667233 1.875195 1.843031 C 6.795331 1.415175 0.526989 C 5.812999 0.582468 -0.022212 N 3.432315 0.286467 2.849426 S 0.969099 -0.787790 3.946364 H -0.068012 -1.231952 4.443856 H 2.482138 0.296546 2.359193 H 3.381633 -0.698292 3.179520 H 3.203996 0.763363 3.688847 H 5.457160 1.860338 3.633568 H 7.431345 2.522922 2.270230 H 7.659085 1.705071 -0.069506 H 5.912641 0.224638 -1.045906 H 3.938456 -0.437946 0.317431 |

| complex | X(+)HA(-) at  = 168.2 | X(+)HA(-) at  ~ 90 |
| --- | --- | --- |
| C6H5S +NH3C6H5 | N 3.342102 0.194168 3.848806 S 0.971128 -1.246126 2.905376 C -0.399909 -1.583249 3.994079 H 2.296395 -0.482510 3.577392 H 3.854595 -0.290673 4.564368 H 2.984139 1.042890 4.259568 C 4.211150 0.512677 2.721973 C 5.246350 1.409957 2.915947 C 6.090231 1.728435 1.867686 C 5.887837 1.156326 0.624437 C 4.858081 0.253719 0.440137 C 4.008593 -0.076482 1.487112 H 5.378056 1.851370 3.887575 H 6.901249 2.418476 2.027740 H 6.525478 1.418471 -0.204051 H 4.704028 -0.201304 -0.526134 H 3.205158 -0.772161 1.329500 C -1.515931 -2.234011 3.454423 C -2.609089 -2.555287 4.235965 C -2.634925 -2.237204 5.585905 C -1.544433 -1.570574 6.130877 C -0.446364 -1.248887 5.343617 H -1.522562 -2.488738 2.406871 H -3.450719 -3.050330 3.785189 H -3.487234 -2.477240 6.193763 H -1.547166 -1.288475 7.163336 H 0.379194 -0.731810 5.797230 | C -1.228777 -1.448725 6.227806 C -0.976216 -1.624886 4.862090 C -1.901197 -2.305351 4.061235 C -3.078741 -2.809656 4.626091 C -3.331303 -2.633496 5.991807 C -2.406319 -1.953030 6.792665 S 0.462071 -1.008915 4.172157 N 2.948751 0.075576 3.064769 C 4.090908 0.458910 2.276017 C 5.073239 1.291618 2.825217 C 6.183669 1.664304 2.058374 C 6.311767 1.204284 0.742332 C 5.329436 0.371576 0.193131 C 4.219005 -0.001111 0.959974 H 1.998575 0.085655 2.574537 H 2.898070 -0.909183 3.394863 H 2.720433 0.552471 3.904190 H 4.973597 1.649447 3.848911 H 6.947783 2.312031 2.485573 H 7.175522 1.494180 0.145837 H 5.429078 0.013746 -0.830562 H 3.454892 -0.648838 0.532774 H -1.704740 -2.442379 2.998903 H -3.798246 -3.338962 4.003140 H -4.247263 -3.025773 6.431187 H -2.602776 -1.816003 7.854995 H -0.509272 -0.919422 6.850759 |

| complex | X(+)HA (-) at  = 168.8 | X(+)HA(-) at  ~ 90 |
| --- | --- | --- |
| NH2C6H4S+NH3C6H4SH | N 2.984795 0.729827 3.745493 S 0.959789 -1.188725 2.834162 C -0.398401 -1.593262 3.921758 H 2.471924 1.592564 3.774310 H 2.063925 -0.129172 3.483152 H 3.332946 0.540485 4.667967 C 4.060162 0.782960 2.776378 C 5.199785 1.530514 3.019570 C 6.198300 1.602664 2.064534 C 6.071279 0.925289 0.856803 C 4.944713 0.153874 0.630843 C 3.944364 0.086209 1.584909 H 5.312791 2.064474 3.944830 H 7.081676 2.190057 2.266118 S 7.389981 1.061340 -0.328817 H 4.839158 -0.405931 -0.271873 H 3.071998 -0.520612 1.398840 C -1.488921 -2.293647 3.397559 C -2.545022 -2.679703 4.194100 C -2.569715 -2.383472 5.552021 C -1.499295 -1.678024 6.081799 C -0.428711 -1.302806 5.275923 H -1.490152 -2.567188 2.358182 H -3.355475 -3.255381 3.769642 N -3.613122 -2.879562 6.356549 H -1.472074 -1.452885 7.135409 H 0.409690 -0.803156 5.733888 H -3.676325 -2.443938 7.249005 H -4.500667 -2.866040 5.907101 H 6.770219 0.483955 -1.350373 | N 3.295983 0.217862 2.875637 H 3.162797 0.750938 3.721369 S 0.740945 -0.709420 4.260459 C -0.705497 -1.198494 5.156998 C -0.832362 -0.961955 6.521939 C -1.966601 -1.332399 7.224706 C -3.028129 -1.957057 6.584708 C -2.908092 -2.210645 5.224619 C -1.772415 -1.834596 4.529540 H -1.712152 -2.030696 3.474434 H -3.710113 -2.705396 4.702077 N -4.174920 -2.365043 7.296730 H -5.001832 -2.333342 6.740040 H -4.315985 -1.837375 8.130965 H -2.023777 -1.130262 8.281784 H -0.029597 -0.470436 7.041167 H 3.292920 -0.750771 3.184588 H 2.403381 0.299824 2.393453 C 4.459655 0.624064 2.104625 C 4.605360 0.177531 0.807311 C 5.716623 0.563291 0.082040 C 6.677862 1.390522 0.649739 C 6.512943 1.827907 1.957176 C 5.403748 1.444702 2.685498 H 5.283968 1.788851 3.697548 H 7.248096 2.468786 2.407638 H 5.827238 0.217288 -0.927897 H 3.865594 -0.462379 0.359084 S 8.127574 1.928492 -0.220606 H 7.890529 1.307528 -1.370515 |

Calculation of the energy of herringbone interaction of 4-aminothiophenol with its nearest neighbours.

4-Aminothiophenol has been taken for calculating the stabilization of herringbone interactions. In the crystal structure of 1, three different herringbone interactions are present. Using the crystal geometry at these ring plane distances and corresponding ring plane angles, the herringbone energies were calculated at the RHF/6-311G (2d, 2p)3 level taking into account BSSE with the counterpoise correction.

Fig. 2 Showing the three different herringbone interactions

Table 7. Herringbone energy between three different phenyl planes.

|  | r (Å) |   | E (a. u.) |  |  | E (kcal mol1) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | RHF | MP2 |  | RHF | MP2 |
| monomer |  |  | 683.260152 | 684.462967 |  |  |  |
| dimer1 | 4.876 | 60.8 | 1366.522229 | 1368.935332 |  | 0.8776 | 5.8972 |
| dimer2 | 5.851 | 0.0 | 1366.521431 | 1368.934861 |  | 0.3769 | 5.6016 |
| dimer3 | 4.839 | 60.8 | 1366.522499 | 1368.981251 |  | 1.0471 | 3.3363 |
|  |  |  |  | Total |  | 2.3016 | 14.8351 |

Total herringbone stabilization per molecule = 2 x 14.8351 = 29.6702 kcal mol1. Hence the estimated potential energy barrier for one proton transfer could be around 14.83 kcal mol1.

(vi) Structure Refinement Parameters: Atomic co-ordinates, Bond lengths, angles and  Anisotropic displacement parameters for compound 1.

Table 1.  Crystal data and structure refinement for compound 1.

Identification code              1

Empirical formula                C6 H7 N S

Formula weight                   125.19

Temperature                      203(2) K

Wavelength                       0.71073 Å

Crystal system, space group      Monoclinic,  Pc

Unit cell dimensions             a = 7.2305(12) Å   alpha = 90

b = 5.8513(10) Å   beta =107.364(3)

c = 7.7552(13) Å   gamma = 90.

Volume                            313.15(9) Å3

Z, Calculated density             2,  1.328 Mg/m3

Absorption coefficient            0.399 mm-1

F(000)                            132

Crystal size                      0.24 x 0.18 x 0.05 mm

Theta range for data collection   3.48 to 28.31.

Limiting indices                  -9<=h<=9, -7<=k<=7, -10<=l<=10

Reflections collected / unique    3386 / 1518 [R(int) = 0.0201]

Completeness to theta = 28.31     99.2 %

Absorption correction             Bruker AXS SADABS program

multiscan v2.03 R.H. Blessing,

Acta Cryst. (1995) A51 33-38)

Max. and min. transmission        1.00 and 0.87

Refinement method                 Full-matrix least-squares on F2

Data / restraints / parameters    1518 / 2 / 86

Goodness-of-fit on F^2            1.072

Final R indices [I>2sigma(I)]     R1 = 0.0277, wR2 = 0.0757

R indices (all data)              R1 = 0.0283, wR2 = 0.0767

Absolute structure parameter      0.02(8)

Largest diff. peak and hole       0.237 and -0.164 e.A-3

Table 2.  Atomic coordinates ( x 104) and equivalent isotropic

displacement parameters (A2 x 103) for compound 1.  U(eq) is defined

as one third of the trace of the orthogonalized Uij tensor.

______________________________________________________________

x             y             z           U(eq)

______________________________________________________________

S(1)         8044(1)       2598(1)       8716(1)       37(1)

N(1)         -591(2)       2413(2)       5232(2)       33(1)

C(1)         5529(2)       2564(2)       7645(2)       26(1)

C(2)         4341(2)       4324(2)       7939(2)       33(1)

C(3)         2354(2)       4285(2)       7125(2)       34(1)

C(4)         1518(2)       2471(2)       5996(2)       28(1)

C(5)         2662(2)        728(2)       5663(2)       33(1)

C(6)         4659(2)        784(2)       6483(2)       33(1)

______________________________________________________________

Table 3.  Bond lengths [A] and angles [deg] for compound 1.

___________________________________________________________

S(1)-C(1)                     1.7598(17)

N(1)-C(4)                     1.462(2)

N(1)-H(1A)                    1.05(3)

N(1)-H(1B)                    1.00(3)

N(1)-H(1C)                    0.91(3)

C(1)-C(6)                     1.3977(18)

C(1)-C(2)                     1.4031(19)

C(2)-C(3)                     1.3860(19)

C(2)-H(2)                     0.9400

C(3)-C(4)                     1.3937(19)

C(3)-H(3)                     0.9400

C(4)-C(5)                     1.385(2)

C(5)-C(6)                     1.3934(18)

C(5)-H(5)                     0.9400

C(6)-H(6)                     0.9400

C(4)-N(1)-H(1A)             112(2)

C(4)-N(1)-H(1B)             112.4(17)

H(1A)-N(1)-H(1B)            111(3)

C(4)-N(1)-H(1C)             105(2)

H(1A)-N(1)-H(1C)            109(3)

H(1B)-N(1)-H(1C)            108(2)

C(6)-C(1)-C(2)              118.18(15)

C(6)-C(1)-S(1)              121.06(10)

C(2)-C(1)-S(1)              120.77(11)

C(3)-C(2)-C(1)              121.01(13)

C(3)-C(2)-H(2)              119.5

C(1)-C(2)-H(2)              119.5

C(2)-C(3)-C(4)              119.67(13)

C(2)-C(3)-H(3)              120.2

C(4)-C(3)-H(3)              120.2

C(5)-C(4)-C(3)              120.45(16)

C(5)-C(4)-N(1)              121.06(12)

C(3)-C(4)-N(1)              118.44(12)

C(4)-C(5)-C(6)              119.50(13)

C(4)-C(5)-H(5)              120.2

C(6)-C(5)-H(5)              120.3

C(5)-C(6)-C(1)              121.17(12)

C(5)-C(6)-H(6)              119.4

C(1)-C(6)-H(6)              119.4

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4.  Anisotropic displacement parameters (A2 x 103) for compound 1.

The anisotropic displacement factor exponent takes the form:

-2 pi2 [ h2 a*2 U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________

U11        U22        U33        U23        U13      U12

______________________________________________________________________

S(1)     22(1)      31(1)      51(1)      -1(1)       2(1)       0(1)

N(1)     21(1)      28(1)      46(1)       1(1)       3(1)       2(1)

C(1)     21(1)      25(1)      31(1)       2(1)       6(1)       0(1)

C(2)     31(1)      26(1)      42(1)      -7(1)       8(1)      -1(1)

C(3)     30(1)      29(1)      44(1)      -6(1)       9(1)       2(1)

C(4)     22(1)      25(1)      34(1)       2(1)       4(1)       1(1)

C(5)     29(1)      29(1)      39(1)      -6(1)       5(1)      -1(1)

C(6)     29(1)      27(1)      42(1)      -5(1)      111(1)       2(1)   _______________________________________________________________________

Table 5.  Hydrogen coordinates ( x 104) and isotropic displacement parameters (A2 x 103) for compound 1.

____________________________________________________________________

x             y             z           U(eq)

____________________________________________________________________

H(1A)       -1110(50)      3870(60)      4460(40)      83(9)

H(1B)       -1050(40)      1000(50)      4510(30)      60(7)

H(1C)       -1040(50)      2410(30)      6210(40)      58(9)

H(2)         4900          5549          8701          40

H(3)         1575          5475          7333          41

H(5)         2095          -484          4890          40

H(6)         5434          -396          6251          40

____________________________________________________________________

(vii) Computation related references.

- Spartan Pro 1.0.1, Wave Function Inc., 18401 von Karman Avenue, Suite 370, Irvine, CA 92612.

- M.W. Schmidt, K. K. Balridge, J. A. Boatz, S. T. Elbert, M. S. Gordon, J. H. Jensen, S. Koseki, N. Matsunaga, K. A. Nguyen, S. J. Su, T. L. Wndus, M. Dupuis and J. A. Montgomery, J. Comput. Chem., 1993, 14,1347.

- M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria, M. A. Robb, J. R. Cheeseman, J. A. Montgomery, Jr., T. Vreven, K. N. Kudin, J. C. Burant, J. M. Millam, S. S. Iyengar, J. Tomasi, V. Barone, B. Mennucci, M. Cossi, G. Scalmani, N. Rega, G. A. Petersson, H. Nakatsuji, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, M. Klene, X. Li, J. E. Knox, H. P. Hratchian, J. B. Cross, C. Adamo, J. Jaramillo, R. Gomperts, R. E. Stratmann, O. Yazyev, A. J. Austin, R. Cammi, C. Pomelli, J. W. Ochterski, P. Y. Ayala, K. Morokuma, G. A. Voth, P. Salvador, J. J. Dannenberg, V. G. Zakrzewski, S. Dapprich, A. D. Daniels, M. C. Strain, O. Farkas, D. K. Malick, A. D. Rabuck, K. Raghavachari, J. B. Foresman, J. V. Ortiz, Q. Cui, A. G. Baboul, S. Clifford, J. Cioslowski, B. B. Stefanov, G. Liu, A. Liashenko, P. Piskorz, I. Komaromi, R. L. Martin, D. J. Fox, T. Keith, M. A. Al-Laham, C. Y. Peng, A. Nanayakkara, M. Challacombe, P. M. W. Gill, B. Johnson, W. Chen, M. W. Wong, C. Gonzalez, and J. A. Pople, Gaussian, Inc., Pittsburgh PA, 2003.

(viii) IR spectra recorded at variable temperatures (63, 38, 25 and 33C).