# Supplementary Material (ESI) for Chemical Communications

# This journal is © The Royal Society of Chemistry 2004

Electronic supporting information file (ESI)

Towards mesomorphism in tetrahedral luminescent zinc complexes

Raquel Giménez, Ana Belén Manrique, Santiago Uriel, Joaquín Barberá and José Luis Serrano.

Characterization data of the novel complexes:

L2m: Elemental analysis (%) calcd. for C71H104N4O4: C, 79.13; H, 9.73; N, 5.20. Found: C, 79.17; H, 9.68; N: 5.16. MS (FAB-LSIMS): 1078 [M+1+]+. 1H NMR (300 MHz, CDCl3)  = 0.89 (t, 12H), 1.29-1.49 (m, 56 H), 1.77-1.85 (m, 8H), 3.98 (t, J = 6.6 Hz, 4H), 4.02 (t, J = 6.6 Hz, 4H), 6.17 (s, 2H), 6.51 (s,2H), 6.91 (d, J = 8.8 Hz, 4H), 7.02 (d, J = 8.8 Hz, 4H), 7.73 (d, J = 8.8 Hz, 4H), 7.87 (d, J = 8.8 Hz, 4H).

L2e: Elemental analysis (%) calcd. for C72H106N4O4: C, 79.22; H, 9.79; N, 5.13. Found: C, 79.22; H, 9.75; N, 5.07. MS (FAB-LSIMS): 1092 [M]+. 1H NMR (300 MHz, CDCl3)  = 0.91 (t, 12H), 1.22-1.49 (m, 56 H), 1.67-1.81 (m, 8H), 3.69 (t, J = 6.6 Hz, 4H), 3.97 (t, J = 6.6 Hz, 4H), 4.56 (s, 4H), 6.31 (s,2H), 6.65 (d, J = 8.8 Hz, 4H), 6.86 (d, J = 8.8 Hz, 4H), 6.89 (d, J = 8.8 Hz, 4H), 7.59 (d, J = 8.8 Hz, 4H).

[ZnL2Cl2]: Elemental analysis (%) calcd. for C70H104Cl2N4O4Zn: C, 69.95; H, 8.72; N, 4.66. Found: C, 69.87; H, 8.70; N, 4.60. MS (LSIMS): 1164 [M-Cl]+. 1H NMR (300 MHz, DMSO-d6)  = 0.86 (t, 12H), 1.20-1.42 (m, 56 H), 1.68-1.76 (m, 8H), 3.98 (t, J = 6.3 Hz, 4H), 4.00 (t, J = 6.3 Hz, 4H), 6.95 (s, 2H), 6.96 (d, J = 8.6 Hz, 4H), 7.01 (d, J = 8.6 Hz, 4H), 7.69 (d, J = 8.6 Hz, 4H), 7.75 (d, J = 8.6 Hz, 4H).

[Zn(L2m)Cl2]: Elemental analysis (%) calcd. for C71H104Cl2N4O4Zn: C, 70.25; H, 8.64; N, 4.62. Found: C, 70.24; H, 8.65; N, 4.58. MS (LSIMS): 1175 [M-Cl]+. 1H NMR (300 MHz, CDCl3)  = 0.85-0.90 (m, 12H), 1.25-1.49 (m, 56 H), 1.70-1.85 (m, 8H), 3.93 (t, J = 6.2 Hz, 4H), 3.94 (t, J = 6.2 Hz, 4H), 6.45 (s, 4H), 6.74 (d, J = 8.8 Hz, 4H), 6.94 (d, J = 8.8 Hz, 4H), 7.01 (d, J = 8.8 Hz, 4H), 7.73 (d, J = 8.8 Hz, 4H).

[Zn(L2e)Cl2]: Elemental analysis (%) calcd. for C72H106Cl2N4O4Zn: C, 70.42; H, 8.70; N, 4.56. Found: C, 70.45; H, 8.76; N, 4.58. MS (Electrospray): 1250 [M+Na]+. 1H NMR (300 MHz, CDCl3)  = 0.86-0.90 (m, 12H), 1.28-1.44 (m, 56 H), 1.75-1.85 (m, 8H), 3.86 (t, J = 6.3 Hz, 4H), 3.96 (t, J = 6.3 Hz, 4H), 4.69 (s, 4H), 6.35 (s, 2H), 6.84 (d, J = 8.6 Hz, 4H), 6.91 (d, J = 8.6 Hz, 4H), 7.07 (d, J = 8.6 Hz, 4H), 7.67 (d, J = 8.6 Hz, 4H).

Microphotograph under polarised light of the texture displayed by compound [Zn(L2e)Cl2] at 152ºC (SmA).

Microphotograph under polarised light of the texture displayed by compound [Zn(L2e)Cl2] at 132ºC (SmC).