Supplementary Information.

Figure 1s. Graphical representation for TiPc/TiO2 (a) LUMO and (b) HOMO orbitals determined from semi-empirical calculations using ZINDO/1 in Hyperchem 7.0.

Figure 2S. Excitation (em= 775 nm) and emission (ex= 650 nm) spectra of the TiPC dye in dichloromethane measured at room temperature under ambient conditions.

Figure 3S. Cyclic Voltametry of TiPc dye (concentration 1 x 10-4 M) in nitrogen degassed CH2Cl2 containing 0.1 M tetrabutylammonium hexafluorophosphate salt at a scan rate of 50mV s-1 employing a Pt wire counter electrode and Ag/AgCL reference electrode.

# (4-Carboxycatecholato)-2,(3)-(tetra-tert-butylphthalocyaninato)titanium(IV) (TiPc): 2,(3)-(Tetra-tert-butylphthalocyaninato)titanium(IV) oxide (30 mg, 0.037 mmol) and 3,4-dihydroxybenzoic acid (14 mg, 0.091 mmol) were dissolved in CHCl3 (3 mL) and heated for 2 h under reflux. After cooling to room temperature, the solvent was removed in vacuo and the crude product washed with methanol. The dark green precipitate was filtered and dried. Yield: 60%. m.p. > 250ºC. 1H NMR (CDCl3): = 1.8-1.9 (br s, 36H, C(CH3)3), 4.42 (d, J = 8.6 Hz, 1H, catechol), 5.00 (s, 1H, catechol), 6.23 (d, J = 8.6 Hz, 1H, catechol), 8.3-8.5 (m, 4H, phthalocyanine), 9.3-9.6 ppm (m, 8H, phthalocyanine). MALFI-TOF (TCNQ): m/z = 936.5 (M+). IR spectrum (in KBr) of TiPc: 3425 (w), 2962, 2922 (w), 2862 (w), 1715, 1668 (s), 1609, 1458, 1435, 1400, 1366, 1327, 1263, 1146, 1068, 831 cm-1.

Transient optical studies were performed as reported previously ,. Control data on unsensitised films gave negligible transient signals under the experimental conditions employed. Dye sensitised photoelectrochemical solar cells were fabricated as reported before, employing a non-scattering TiO2 film.

M. Barthel, D. Dini, S. Vagin,  M. Hanack, Eur. J. Org. Chem., 2002, 3756.

John N. Clifford, E. Palomares, Md. K. Nazeeruddin, M. Gratzel, J. Nelson, X. Li, Nicholas J. Long, James R. Durrant. J. Am. Chem. Soc., 2004, 126, 5225.

N. Hirata, J.-J. Lagref, Emilio J. Palomares, James R. Durrant, M. K. Nazeeruddin, M. Gratzel, D. di Censo., Chem. Eur. J., 2004, 10, 595.

E. Palomares, John N. Clifford, Saif A. Haque, T. Lutz, James R. Durrant., J. Am. Chem. Soc., 2003, 125, 475.