Electronic Supplementary Information

Self-assembly of a 1D heterotrimetallic Cu(II)-Sr(II)-Na(I) propeller-like chiral coordination polymer with ferromagnetic interactions

Wenlong Liu, You Song, Yizhi Li, Yang Zou, Dongbin Dang, Chunlin Ni, and Qingjin Meng*

Figure S1.  Packing of 1 along c axis showing the O(5)-H…O(2) hydrogen bonds and the Br…Br interactions

( dBr…Br =  3.5735(15) Å ; dO(5)…O(2) = 2.729(11) Å)

Thermalgravimetric analyses of complex 1 exhibits that water of crystallization is lost at lower temperature(<63 ℃). The weight loss from 170 to 230℃ corresponds with the lose of three water. The higher dehydration temperature suggests that three water molecules are coordinated to the metal ions. The decomposition temperature of complex 1 is 299℃.

Figure S2. Thermogravimetric (TG) curve of complex 1, heating from 20-400℃ at 10 ℃/min, in air.

Circular dichroism spectra were measured with a Jasco model J-810 spectropolarimeter. Measurements were made on the resulting complex as dispersions of 2 mg in 100 mg of oven-dried KBr. 13-mm diameter disks were made in a standard disk press. The baseline correction was performed with the spectrum of a pure KBr disk, prepared in the same conditions. The displayed absorption spectra result from subtraction of spectrum of a standard KBr disk. Spectra were recorded for the wavelength range 750-200nm for all the disks.

Figure S3. Circular dichroism spectra of the coordination polymer ground crystals in KBr pellet.