Equivalent circuit used to fit the impedance spectra presented in Figure 2-d.

where Rs is the uncompensated solution resistance; Rct denotes the charge-transfer resistance; and CPE  is an constant phase element.

Mathematically, a CPE's impedance is given by:

ZCPE=

If  CPE_P equals one, then the CPE is considered a capacitor.

Table S1  The values for the parameters Rct, CPE_T, CPE_P and their associated error % computed by fitting of the experimental EIS data (Fig 2-d).a

|  | Rct (Ω cm2) CPE_T (mF cm-2) CPE_P |
| --- | --- |
| Electrode | Value Error% Value Error% Value Error% |
| Pt wire 7178 3.15 0.14 2.49 0.83 0.46 S1 1525 5.88 0.57 4.15 0.93 1.07 S2 275 5.77 1.83 5.29 0.95 1.42 |  |

aExperiment data were measured in 0.5 M H2SO4 + 0.1 M CH3OH solutions at an electrode potential of 300 mV.