Supporting Information

A High Spin Molecular Square Based on Square Pyramidal CoII

and Tetrahedral MnII Centers: [{MnIICl2}2{CoII(triphos)(CN)2}2]

Ferdi Karadas, Eric J. Schelter, Andrey V. Prosvirin, John Bacsa  and Kim R. Dunbar

T (emuK/mol)

1/ (mol/emu)

0

0.05

0.1

0.15

0.2

0.25

0.3

0.35

0.4

0.45

0

50

100

150

200

250

300

0

100

200

300

400

500

600

700

800

Temperature (K)

Figure S1. Temperature dependence of the T product () and the inverse susceptibility (o) for Co(triphos)(CN)2. Solid line corresponds to the best fit obtained with Curie-Weiss law ( = -0.06 K, TIP = 14010-6 emumol-1 and C = 0.425 emuKmol-1, which correspond S=1/2 and g = 2.13).

M (B)

0

0.2

0.4

0.6

0.8

1

1.2

0

1

2

3

4

5

6

7

H (T)

Figure S2. Field dependent magnetization data for Co(triphos)(CN)2 collected at 1.8 K. The solid line shows the Brillouin function for an S = 1/2 paramagnet.