Supporting Information

A High Spin Molecular Square Based on Square Pyramidal CoII

and Tetrahedral MnII Centers: [{MnIICl2}2{CoII(triphos)(CN)2}2]

Ferdi Karadas, Eric J. Schelter, Andrey V. Prosvirin, John Bacsa  and Kim R. Dunbar

Temperature (K)

Figure S1. Temperature dependence of the (T product (() and the inverse susceptibility (o) for Co(triphos)(CN)2. Solid line corresponds to the best fit obtained with Curie-Weiss law (( = -0.06 K, TIP = 140(10-6 emu(mol-1 and C = 0.425 emu(K(mol-1, which correspond S=1/2 and g = 2.13).

H (T)

Figure S2. Field dependent magnetization data for Co(triphos)(CN)2 collected at 1.8 K. The solid line shows the Brillouin function for an S = 1/2 paramagnet.

# Text boxes

M ((B)

100

50

0

0.45

0.4

0.35

0.3

0.25

0.2

0.15

0.1

0.05

0

1/( (mol/emu)

(T (emu(K/mol)

5

4

3

2

1

0

1.2

1

0.8

0.6

0.4

0.2

0

800

700

600

500

400

300

200

100

0

300

250

200

150

6

7