This journal is © The Royal Society of Chemistry 2006

Magnetic Fe Nanoparticle Functionalized Water-soluble Multi-Walled Carbon Nanotubles toward the Preparation of Sorbent for Aromatic Compounds Removal

Jin Jun, Rong Li, Huangling Wang, Hangling Chen, Kun Liang and Jiantai Ma*

* College of Chemistry and Chemical Engineering, Lanzhou University, Lanzhou, 730000, P. R. China. Fax: +86-931-891-2582.; Tel: +86-931-891-2311; E-mail: majiantai@lzu.edu.cn

MWNTs generated via chemical vapor deposition (CVD) method were purchased from Shenzhen nanoport (Shenzhen. China), and their purity was over 90%. Other reagents including Fe(NO3)3·9H2O , AIBN, toluene, sodium hydroxide, methanol and four model aromatic compounds were A. R. grade and were used as supplied.

Preparation of magnetic Fe nanoparticle functionalized multi-wall carbon nanotubes (Fe-MWNTs-CH2COONa)

1) Preparation of Fe-MWNTs

200 mg MWNTs were dispersed in 20 wt.% Fe(NO3)3·9H2O solution with the help of an ultrasonic bath. After draining the excess of water on a rotary evaporator with a vacuum pump and calcined for 0.5 h, the samples were reduced using H2 at 560 oC for 1.5 h and at 900 oC for 1 h successively in the flow of H2 and Ar (the ratio of which was 1: 10 with 5 oC·min-1) . Thus, Fe-MWNTs were obtained.

2) Preparation of Fe-MWNTs-CN

180 mg Fe-MWNTs were dispersed in 180 mL toluene by strong stirring for 30 min. Then, under continuous stirring, 36 mL toluene solution containing 11.52 g AIBN was added to the dispersion. Subsequently, in a Ar atmosphere, the resulting dispersion was heated at 75 oC for 4h. The product was washed with toluene repeatedly and dried in vacuum at 40 oC overnight, thus, Fe-MWNTs-cyano (Fe-MWNTs-CN) were produced.

3) Preparation of Fe-MWNTs-CH2COONa

To prepare Fe-MWNTs-CH2COONa, 100 mg Fe-MWNTs-CN were dispersed in a mixture of methanol and 10 M sodium hydroxide, the resulting materials were subjected to refluxing at 60 oC for 48 h. The product was washed with distilled water for several times. Finally, the purified Fe-MWNTs-CH2COONa was dried in vacuum at 40 oC overnight.

FT-IR Characterization

The FT-IR spectra of raw MWNTs, Fe-MWNTs, Fe-MWNTs-CN and Fe-MWNTs-CH2COONa were shown in Figure S1. Compared with the spectra of raw MWNTs (Figure S1a), the intensity of most of peaks became weak and a few peaks (Figure S1b) disappeared because a few organic groups decomposed in high temperature. Compared with the spectra of Fe-MWNTs in Figure S1b, there appeared a characteristic peak of cyano groups at ca. 2234 cm-1 in Figure S1c, which proved that carbon radicals originated from AIBN were efficiently grafted onto Fe-MWNTs. As shown in Figure S1d, the disappearance of the peak of -CN groups and the appearance of peak at 1637 nm-1 confirmed that carboxylic sodium were produced via hydrolysis of -CN groups on Fe-MWNTs. The water solubility of Fe-MWNTs-CH2COONa was highly improved, because of the grafting of carboxylic sodium groups on Fe-MWNTs.

XRD Characterization

The XRD pattern of Fe-MWNTs-CH2COONa was represented in Figure S2. The peaks appearing at 2θ= 26.2 o, 43.6o and 50.7 o  are characteristic of the graphite of carbon nanotubes, and the peaks appearing at 44.6 o, 64.9 o, 82.2 o and 98.8 o are characteristic of the presence of the Fe metal. Obviously, the diffraction peaks of Fe inside Fe-MWNTs-CH2COONa were quite wide, indicating that Fe particles were very small. To evaluate the grain size of powder, Scherrer equation was applied. This equation was written as where ( was the wavelength of X-ray (1.5418Å) for CuK( radiation, θwas the Bragg angle, and

(1)

is full width at half the maximum intensity of peak. According to equation 1, the grains size of Fe inside Fe-MWNTs-CH2COONa was around 11.25 nm.

# Text boxes

Figure S2 XRD pattern of Fe-MWNTs-CH2COONa

a

d

c

b

Figure S1 FT-IR spectra of raw MWNTs (a), Fe-MWNTs (b), Fe-MWNTs-CN (c), Fe-MWNTs-CH2COONa (d).

20              40              60               80

2-theta(degrees)

（110）

(

（200）

(

（211）

(

（220）

(

（002）

(

(（100）

（102）

(

( MWNTs

( Fe