Supplementary Material (ESI) for CrystEngComm

This journal is © The Royal Society of Chemistry 2003


Supporting information
Materials: ZnTPP and Prz were purchased from Aldrich. C60 of 99.98 % purity was used from MTR Ltd.. Toluene and benzonitrile was doubly distilled over Na/benzophenon in the argon atmosphere. 

General: UV-visible-NIR spectra were measured on Shimadzu-3100 spectrometer in 240-2600 nm range. FT-IR spectra were measured in KBr pellets with a Perkin-Elmer 1000 Series spectrometer (400-7800 cm-1). 

Elemental analyse [(ZnTPP)2Prz](C60(5.34C7H8(0.66C6H5CN: C190.5H98.02N10.66Zn2
	Elements
	Found
	Calculated

	C (%)
	87.35
	85.81

	H (%)
	3.15
	3.68

	N (%)
	5.43
	5.60

	Zn (%)
	4.13
	4.91


IR spectrum of the complex 1 and starting compounds (cm-1)
	Compaunds
	ZnTPP
	Prz
	C6H5CH3
	C6H5CN
	C60
	1

	ZnTPP
	433w

670m

675m

702s

717m

752s

797s

833w

993s

1001s

1068m

1109w

1176m

1203m

1339s

1385w

1439m

1485m

1522m

1595m

1653s

2924w

3024w

3053w

3103w
	
	
	
	
	432m

660m

670w

700s

716m

752s

794s

832w

992s

1002s

1068m

1176w

1202m

1338m

1438m

1482m

1522m

1596m

1654m

2922w

3014w

3050w

3116w

	Prz
	
	680m

700w

1040m

1350m

1530m

1600m

2335s

2365s

2880w

2933m
	
	
	
	684w

1560m

1606w

2344m

2362m

2922w

	C6H5CH3
	
	
	464m

694s

728s

1029w

1081w

1495m

1604w

3026m
	
	
	466w

696w

728m

1035m

	C6H5CN
	
	
	
	554m

686m

754s

1445w

1490m

2235w

3090m
	
	548m

684m

755s



	C60
	
	
	
	
	526s

576m

1182m

1429s
	527s

578m

1181m

1427m

	w - weak, m - middle, and s - strong intensity.


X-ray Crystallography


Crystallographic data and parameters of the X-ray analysis for 1 are listed in Table 1. X-ray diffraction data were collected at 90K on a Bruker 1K SMART CCD diffractometer equipped with the rotating anode (MoK( radiation, (=0.71073 Å). The data were collected by a rotation method with 0.3( frame width (( scan). Data collection nominally covered full reciprocal space by a combination of six ω scans (600 frames in each set), with different φ angle. Reflection intensities were integrated using SAINT program.1

The solution and the refinement of the structures were performed with SHELXTL program package.2 The structure was refined by full-matrix least squares against F2 of all the data. Non‑hydrogen atoms were refined in an anisotropic approximation. Hydrogen atoms were revealed from the difference Fourier maps and refined using the ‘riding’ model (Uiso=1.5Ueq of the preceding carbon atom for CH3 hydrogens and Uiso=1.2Ueq for the rest H-atoms). 


The asymmetric unit contains toluene and benzonitrile solvent molecules (six in total) with partial occupancies. This makes stoicheometry of the crystal as follows: [(ZnTPP)2Prz](C60(5.34Toluene(0.66Benzonitrile. Only two of the toluene molecules are ordered, the rest solvent molecules are disordered. The other toluene molecules are disordered through the non-crystallographic inversion center, which almost resides at the center of the toluene benzene ring. Two more toluene and two benzonitrile molecules occupy two sites, each site has fully overlapped toluene and benzonitrile molecules. Although these two sites are 100% occupied, each molecule in each site has partial occupancy. At the first site toluene/benzonitrile ratio is 0.54/0.44, while at the other one 0.78/0.22. The last two toluene molecules (C43S…C46S and C47S…C51S) occupy one site (50/50) and reside in a special position at the inversion center, each of them being disordered through it, making this site occupied by one toluene molecule in each unit cell.

Several restraints were used to bring geometries of some fullerene bonds and disordered solvent molecules to reasonable values. Some 5-6 and 6-6 bonds of the fullerene molecule were restrained to their ideal values 1.450(3)Å and 1.380(3)Å, respectively. Benzene rings of toluene and benzonitrile solvent molecules were constrained to be perfect hexagons, with C-C bonds of 1.390Å. All CH3-CAr bonds of the solvents were restrained to be 1.450(3)Å, while all N(CAr bonds of the disordered benzonitrile molecules were restrained to be 1.210(3)Å. Carbon atoms of toluene molecules C43S…C46S and C47S…C51S were refined in an isotropic approximation due to severe disorder. Their bond lengths were restrained to be 1.390(2)Å (CAr-CAr) and 1.450(3)Å (CMe-CAr).

References
1 SMART and SAINT, Area detector control and integration software, Ver. 6.01., Bruker Analytical X‑ray Systems, Madison, Wisconsin, U.S.A, 1999.

2 SHELXTL, An integrated system for solving, refining and displaying crystal structures from diffraction data, Ver. 5.10. Bruker Analytical X-ray Systems, Madison, Wisconsin, U.S.A, 1997.








PAGE  
2



