for CrystEngComm

Host-guest and network structures of some tetraphenylmethane derivatives

Srinivas Basavoju, Srinivasulu Aitipamula, Gautam R. Desiraju*

School of Chemistry, University of Hyderabad, Hyderabad 500 046, India.

E-mail: desiraju@uohyd.ernet.in

Supplementary Information

(3 pages)

(Atom-labelling schemes of the compounds in this study, details of structure solution and refinement for (TCTPM).(MeCN)0.5)

| DNTPM | (DNTPM)3.(H2O)2 |
| --- | --- |
| (DNTPM).(THF) | TCTPM |
| (TCTPM).(MeCN)0.5 (before SQUEEZE) | (TCTPM).(MeCN)0.5 (after SQUEEZE) |

ORTEP diagrams of the compounds in this study. Displacement ellipsoids are drawn at the 50% probability level for non-H atoms.

Structure solution and refinement details for (TCTPM).(MeCN)0.5:

The structure was solved by direct methods (SHELXS97). The disordered solvent molecules (located in the voids of the channels of the lattice) were incorporated in the model with the PLATON/SQUEEZE procedure (P. V. Sluis and A. L. Spek, Acta Crystallogr., Sect. A, 1990, 46, 194). This shows a smooth convergence of the Squeeze interation with a significant improvement of R-value. The residual agreement factor for all data before SQUEEZE are R1 = 0.0925, wR2 = 0.2372, and after R1 = 0.0687, wR2 = 0.1550.  Additionally, the number of residual electrons (18, which is half of electrons in MeCN) reported to be found in a void is close to that expected for the assumed MeCN solvent. The final formulation of the compound, in agreement with the residual volume is (TCTPM).(MeCN)0.5.