Supplementary Material

Figure 1s - SAXS patterns from equimolar mixtures of CnH2n+2:C36D74 for i) n = 31, ii) n = 30, iii) n = 27 and iv) n = 26, immediately on quenching (dotted line) and aged for between three and four weeks (continuous line).

Figure 3s - SANS from n = 28 quenched to i) 10˚C and ii) 20˚C and iii) n = 30 quenched to 20˚C. Normalised patterns are shown in the insets to i and ii.

Figure 5s - A comparison of SANS in the low Q region after long-time aging for 24 ≤ n ≤ 30. C24H50:C36D74, C26H54:C36D74 and C28H58:C36D74 aged for five months and C30H62:C36D74 after aging for greater than four years.

Figure 7s - Porod plot for aged 24 ≤ n ≤ 30 mixtures. The slope in the low Q region for these systems is less steep than for C20H42:C36D74 and is modified to varying extents by microphase scattering.

Figure 8s - Heating curves for selected 20 ≤ n ≤ 34 mixtures. i) n = 30; ii) n = 29 and iii) n = 27, freshly quenched from the melt, aged for ca. 70 days, and after heating aged sample. A magnification of the additional endotherm is shown in the insets. Individual heating scans have been shifted for clarity.

Figure 1s

Figure 1s continued

Figure 3s

Figure 3s continued

Figure 5s

Figure 7s

Figure 8s

Figure 8s continued

Table 1s

|  |  | Manufacturer's Specifications |  |  | Structure |
| --- | --- | --- | --- | --- | --- |
| Alkane | Formula | Source | Purity / % | Tmelt / ˚C |  |
| Eicosane | C20H42 | Fluka | > 97 | 36-38 | T |
| Tetracosane | C24H50 | Fluka | > 99 | 49-51 | T |
| Hexacosane | C26H54 | Aldrich | 99 | 56-58 | T / M |
| Heptacosane | C27H56 | Aldrich | 99 | 59-61 | O |
| Octacosane | C28H58 | Aldrich | 99 | 61-63 | M |
| Nonacosane | C29H60 | Aldrich | 99 | 65-67 | O |
| Triacontane | C30H62 | Aldrich | 99 | 65-67 | M |
| Hentriacontane | C31H64 | TCI | 97 | 66 | O |
| Dotriacontane | C32H66 | Aldrich | 97 | 68-70 | M |
| Tritriacontane | C33H68 | Aldrich | 98 | 71-73 | O |
| Tetratriacontane | C34H70 | Sigma | ca. 98 | - | M |
| Hexatriacontane | C36H74 | Aldrich | 98 | 74-76 | M / O |
| Hexatriacontane-D74 | C36D74 | CIL | 98 | - | M / O |

Table 1s - Alkanes used in the present study. Manufacturers, their specification of purity and melting point, and low temperature crystal structure. T, M and O refer to triclinic, monoclinic and orthorhombic structures respectively.