10/6/99 Final version submitted to PCCP - Supplementary material.

Table 1S 29Si NMR isotropic chemical shifts for methyl modified alkoxy silanes under different solution conditionsa

| Silanec | Neatb | 2.24 Mb | Rw = 3.0b |
| --- | --- | --- | --- |
| TEOS | -82.22 | -81.97 | -81.82 |
| MTES | -44.06 | -43.27 | -42.14 |
| DMDES | -5.57 | -4.14 | -3.85 |
| TMES | +14.66 | +16.71 | +17.78 |
| TMOS | -78.81 | -78.55 | -78.29 |
| MTMS | -40.11 | -39.46 | -38.24 |
| DMDMS | -1.98 | +0.41 | +1.25 |
| TMMS | +17.32 | +19.52 | +20.72 |

a All chemical shifts referenced to internal TMS (0.1%), with high frequency corresponding to positive  values.

bSolution composition: Neat = silane plus reference TMS (0.1%), 2.24 M = silane concentration in parent alcohol, Rw = 3.0 is 2.24 M solution plus 3 molar equivalents of distilled H2O added.

c TEOS, tetraethoxysilane; MTES, methyltriethoxysilane; DMDES, dimethyldimethoxysilane; TMES, trimethylethoxysilane; TMOS, tetramethoxysilane; MTMS, methyltrimethoxysilane; DMDMS, dimethyldimethoxysilane; TMMS, trimethyltrimethoxysilane.

Table 2S Predicted PCM populations of silicon outer-valence orbitals for the reference compounds.

| Compound | Ps | Pxx | Pyy | Pzz | Pa | Pub |
| --- | --- | --- | --- | --- | --- | --- |
| Si(CH3)4 | 1.32852 | 0.85032 | 0.85032 | 0.85032 | 0.00000 | 0.97760 |
| SiF4 | 0.97020 | 0.57321 | 0.57321 | 0.57321 | 0.00000 | 0.81785 |
| SiH4 | 1.35414 | 0.88502 | 0.88502 | 0.88502 | 0.00000 | 0.98678 |
| SiCl4 | 1.06214 | 0.76977 | 0.76977 | 0.76977 | 0.00000 | 0.94699 |
| SiO2 (quartz) | 1.27571 | 0.57679 | 0.57679 | 0.57679 | 0.00000 | 0.82089 |
| Si(OH)4 | 1.11167 | 0.65689 | 0.65684 | 0.65727 | 0.00041 | 0.88235 |
| Si(OCH3)4 | 1.24914 | 0.64468 | 0.64468 | 0.64468 | 0.00000 | 0.87375 |
| Si(OC2H5)4 | 1.28161 | 0.63562 | 0.63487 | 0.63977 | 0.00453 | 0.86805 |

a . b Pu defined by eqn. (6).

Table 3S 29Si NMR shielding constants and corresponding parameters for reference compounds.

| Compound | exp (ppm) | iso (ppm) | dia (ppm) | q(Si) |  (eV) |
| --- | --- | --- | --- | --- | --- |
| Si(CH3)4 | 368.50 | 368.51 (+0.01) | 1008.13 | 0.121 | 8.10 |
| SiF4 | 482.00 | 481.68 (-0.32) | 1094.56 | 1.310 | 14.33 |
| SiH4 | 475.30 | 475.18 (-0.12) | 913.33 | -0.009 | 10.60 |
| SiCl4 | 384.15 | 384.30 (+0.15) | 1195.34 | 0.629 | 8.90 |
| SiO2 (quartz) | 475.90 | 476.31 (+0.41) | 1072.28 | 0.994 | 12.80 |
| Si(OH)4 | 440.82 | 440.64 (-0.18) | 1066.87 | 0.917 | 12.60 |
| Si(OCH3)4 | 447.31 | 447.20 (-0.11) | 1067.98 | 0.817 | 11.94 |
| Si(OC2H5)4 | 450.72 | 450.82 (+0.10) | 1068.28 | 0.808 | 11.87 |

Table 4S Predicted PCM silicon outer valence gross population for the methyl alkoxy series MexSi(OR)y(OH)4-x-y (OR = OMe, OEt)

| Compound | Ps | Pxx | Pyy | Pzz | P | Pu |
| --- | --- | --- | --- | --- | --- | --- |
| Si(OEt)4 | 1.28161 | 0.63487 | 0.63562 | 0.63977 | 0.00453 | 0.86805 |
| Si(OEt)3(OH) | 1.25959 | 0.63625 | 0.63880 | 0.65151 | 0.01399 | 0.87199 |
| Si(OEt)2(OH)2 | 1.23096 | 0.64229 | 0.64423 | 0.65252 | 0.00926 | 0.87494 |
| Si(OEt)(OH)3 | 1.18855 | 0.64780 | 0.64894 | 0.65291 | 0.00454 | 0.87742 |
| Si(OH)4 | 1.11167 | 0.65684 | 0.65689 | 0.65727 | 0.00041 | 0.88235 |
| MeSi(OEt)3 | 1.29062 | 0.63039 | 0.66989 | 0.76864 | 0.11850 | 0.90537 |
| MeSi(OEt)2(OH) | 1.26435 | 0.63632 | 0.67676 | 0.78021 | 0.12367 | 0.91049 |
| MeSi(OEt)(OH)2 | 1.23506 | 0.63875 | 0.67962 | 0.78246 | 0.12327 | 0.91199 |
| MeSi(OH)3 | 1.19168 | 0.63272 | 0.67579 | 0.78347 | 0.12921 | 0.91040 |
| Me2Si(OEt)2 | 1.29475 | 0.63220 | 0.71041 | 0.90664 | 0.23534 | 0.94404 |
| Me2Si(OEt)(OH) | 1.27490 | 0.63123 | 0.71065 | 0.91622 | 0.24528 | 0.94605 |
| Me2Si(OH)2 | 1.24441 | 0.62382 | 0.70807 | 0.91936 | 0.25342 | 0.94544 |
| Me3Si(OEt) | 1.30834 | 0.74273 | 0.74349 | 0.91885 | 0.17574 | 0.96411 |
| Me3Si(OH) | 1.29209 | 0.73207 | 0.73215 | 0.92441 | 0.19231 | 0.96258 |
| Si(OMe)4 | 1.24914 | 0.64468 | 0.64468 | 0.64468 | 0.00000 | 0.87375 |
| Si(OMe)3(OH) | 1.22700 | 0.64479 | 0.64614 | 0.65147 | 0.00601 | 0.87572 |
| Si(OMe)2(OH)2 | 1.19741 | 0.65042 | 0.65090 | 0.65217 | 0.00151 | 0.87831 |
| Si(OMe)(OH)3 | 1.16670 | 0.65011 | 0.65142 | 0.65549 | 0.00472 | 0.87914 |
| MeSi(OMe)3 | 1.26228 | 0.63836 | 0.67785 | 0.78441 | 0.12630 | 0.91203 |
| MeSi(OMe)2(OH) | 1.24268 | 0.63876 | 0.68100 | 0.78841 | 0.12854 | 0.91361 |
| MeSi(OMe)(OH)2 | 1.22737 | 0.62933 | 0.67436 | 0.78694 | 0.13510 | 0.91031 |
| Me2Si(OMe)2 | 1.27707 | 0.63823 | 0.71782 | 0.91679 | 0.23877 | 0.94811 |
| Me2Si(OMe)(OH) | 1.25994 | 0.63639 | 0.71570 | 0.92427 | 0.24823 | 0.94919 |
| Me3Si(OMe) | 1.29719 | 0.74733 | 0.74813 | 0.91863 | 0.17090 | 0.96510 |
| Me4Si | 1.32852 | 0.85032 | 0.85032 | 0.85032 | 0.00000 | 0.97760 |