Table 1  Changes in the molar concentrations (CAl)L of aluminium, (CSi)L of silicon and their ratios (CSi/CAl)L in the liquid phase as well as amounts (in mol/kg) (CAl)s of aluminium, (CSi)s of silicon, and their ratios (CSi/CAl)s in the solid phase during dissolution of the solid NaA (sodium form of zeolite A) in 2 M NaOH solution at 70 C. td is time of dissolution.

td (CSi)L (CAl)L (CSi/CAl)L (CSi)S (CAl)S (CSi/CAl)S (min) (mol/dm-3) (mol/dm-3) (mol/kg) (mol/kg)

1 0.0015 0.0016 0.937 5.335 5.326 1.002

3 0.0029 0.0028 1.028 5.389 5.338 1.010

4 0.0031 0.0032 0.968 5.383 5.350 1.006

6 0.0036 0.0039 0.933 5.385 5.357 1.005

8 0.0050 0.0051 0.972 5.386 5.367 1.004

11 0.0053 0.0056 0.953 5.386 5.395 0.988

14 0.0070 0.0069 1.014 5.378 5.406 0.995

20 0.0096 0.0089 1.083 ------- ------- -------

30 0.0098 0.0097 1.010 5.390 5.423 0.994

45 0.0110 0.0112 0.982 5.400 5.422 0.996

60 0.0126 0.0124 1.016 5.410 5.429 0.996

90 0.0139 0.0135 1.030 5.410 5.420 0.998

120 0.0147 0.0143 1.030 5.420 5.436 0.997

180 0.0177 0.0167 1.060 ------- ------- -------

Table 2  Changes in the molar concentrations (CAl)L of aluminium, (CSi)L of silicon and their ratios (CSi/CAl)L in the liquid phase as well as amounts (in mol/kg) (CAl)s of aluminium, (CSi)s of silicon, and their ratios (CSi/CAl)s in the solid phase during dissolution of the solid KA (potassium-exchanged zeolite A) in 2 M NaOH solution at 70 C. td is time of dissolution.

td (CSi)L (CAl)L (CSi/CAl)L (CSi)S (CAl)S (CSi/CAl)S (min) (mol/dm-3) (mol/dm-3) (mol/kg) (mol/kg)

1 0.00449 0.00468 0.960 5.099 5.115 0.997

3 0.00479 0.00478 1.002 5.085 5.107 0.996

5 0.00718 0.00674 1.065 5.090 5.100 0.996

8 0.00715 0.00704 1.011 5.100 5.116 0.997

10 0.00802 0.00810 0.990 5.110 5.117 0.999

15 0.00859 0.00870 0.997 5.135 5.119 1.003

20 0.00979 0.00950 1.030 5.134 5.121 1.002

25 0.01059 0.01028 1.030 ------- ------- ------

30 0.01086 0.01090 1.000 ------- ------- ------

45 0.01311 0.01350 0.970 5.140 5.127 1.002

60 0.01623 0.01530 1.060 5.139 5.126 1.002

90 0.02360 0.02340 1.000 5.142 5.129 1.002

120 0.02740 0.02710 1.010 5.140 5.127 1.002

Table 3  Changes in the molar concentrations (CAl)L of aluminium, (CSi)L of silicon and (CK)L of potassium and their ratios (CSi/CAl)L and (CK/CAl)L in the liquid phase as well as amounts (in mol/kg) (CAl)s of aluminium, (CSi)s of silicon, and  (CK)s  and their ratios (CSi/CAl)s and (CK/CAl)s in the solid phase during dissolution of the solid K-as (amorphous aluminosilicate obtained by heating of the solid KA at 762 C for 30 min) in 2 M NaOH solution at 70 C. td is time of dissolution.

td (CSi )L (CAl)L (CK)L (CSi/CAl )L (CK/CAl)L (CSi )S (CAl)S (CK)S (CSi/CAl )S (CK/CAl)S (min) (mol/dm-3) (mol/dm-3) (mol/dm-3) (mol/kg) (mol/kg) (mol/kg)

1 0.00798 0.00715 --------- 1.116 ------ 6.162 6.240 5.900 0.988 0.946

3 0.01078 0.0118 0.0105 0.913 0.890 6.127 6.239 6.020 0.987 0.965

5 0.01279 0.0141 0.0126 0.907 0.894 6.157 6.242 5.900 0.986 0.945

10 0.01973 0.0195 0.0171 1.012 0.877 6.159 6.244 5.900 0.986 0.945

15 0.02470 0.0227 0.0236 1.088 1.040 6.162 6.244 6.144 0.987 0.984

20 0.02710 0.0279 0.0287 0.970 1.030 6.165 6.247 5.900 0.987 0.944

25 0.0289 0.0297 0.0290 0.973 0.976 6.166 6.247 5.900 0.987 0.944

30 0.0314 0.0317 0.0310 0.991 0.979 6.168 6.249 6.020 0.987 0.963

45 0.0388 0.0389 0.0366 0.997 0.941 6.171 6.254 6.144 0.987 0.982

60 0.0437 0.0428 0.0434 1.021 1.014 6.170 6.251 6.020 0.987 0.963

90 0.0549 0.0557 0.0535 0.986 0.960 6.172 6.257 6.144 0.986 0.982

120 0.0662 0.0680 0.0907 0.974 1.334 6.175 6.258 6.020 0.987 0.962

195 0.1040 0.1060 0.2020 0.981 1.906 --- --- --- --- ---

Table 4  Changes in the molar concentrations (CAl)L of aluminium, (CSi)L of silicon and (CK)L  and their ratios (CSi/CAl)L and (CK/CAl)L, in the liquid phase as well as amounts (in mol/kg) (CAl)s of aluminium, (CSi)s of silicon, and (CK)s and their ratios  (CSi/CAl )L and (CK/CAl)L, in the solid phase during dissolution of the solid kk (a mixture of kalsilite and kaliophilite obtained by heating of the solid KA at 762 C for 180 min) in 2 M NaOH solution at 70 C. td is time of dissolution.

td (CSi )L (CAl)L (CK)L (CSi/CAl )L (CK/CAl)L (CSi )S (CAl)S (CK)S (CSi/CAl )S (CK/CAl)S (min) (mol/dm-3) (mol/dm-3) (mol/dm-3) (mol/kg) (mol/kg) (mol/kg)

1 0.00580 0.00612 -------- 0.948 ------- 6.279 6.183 5.636 1.016 0.912

3 0.00790 0.00700 0.00691 1.129 0.987 6.285 6.185 5.871 1.016 0.949

5 0.01160 0.01203 0.01012 0.963 0.841 6.280 6.187 6.106 1.015 0.987

8 0.01442 0.01410 0.01250 1.023 0.887 6.286 6.181 6.106 1.015 0.988

10 0.01648 0.01589 0.01427 1.037 0.898 6.288 6.192 6.106 1.016 0.986

20 0.02378 0.02304 0.02060 1.032 0.894 6.285 6.192 5.753 1.015 0.929

30 0.02825 0.02686 0.02660 1.052 0.990 6.288 6.185 5.753 1.017 0.930

45 0.03196 0.03328 0.03270 0.960 0.983 6.287 6.180 5.988 1.017 0.969

60 0.03827 0.03879 0.04140 0.987 1.067 --- --- --- --- ---

90 0.05662 0.05475 0.04620 1.034 0.844 6.288 6.182 5.871 1.017 0.950

120 0.0682 0.06750 0.07460 1.010 1.105 6.290 6.186 5.988 1.017 0.968

180 --- --- --- --- 6.288 6.189 5.988 1.016 0.968