# Supplementary Information

# Spectroscopic behaviour of lanthanide(III) coordination compounds with Schiff base ligands

Koen Binnemans(*), Rik Van Deun, Christiane Görller-Walrand, Simon R. Collinson, Françoise Martin, Duncan W. Bruce, and Claudia Wickleder

Supplementary Table I. Intensity calculations on the Ho(III) Schiff base complex [Ho(L1H)3(NO3)3]

| Transition (a) | Wave number (cm-1) | Dexp (10-6 Debye2) | Dcalc (b) (10-6 Debye2) | Dexp-Dcalc | Dcalc/Dexp |
| --- | --- | --- | --- | --- | --- |
| 5I5 | 11250 | 103 | 33 | +70 | 0.32 |
| 5F5 | 15550 | 584 | 607 | -23 | 1.04 |
| 5F4,5S2 | 18550 | 783 | 730 | +53 | 0.93 |
| 5F3 | 20620 | 270 | 219 | +51 | 0.81 |
| 3K8, 5F2 | 21140 | 154 | 323 | -169 | 2.10 |
| 5G6 | 21950 | 6590 | 6587 | +3 | 1.00 |

- All the transitions start from the 5I8 ground state.

- The set of Judd-Ofelt intensity parameters used to calculate the dipole strength Dcalc is: (2 = (22.65 ( 1.21)(10-20 cm2, (4 = (3.34 ( 2.18)(10-20 cm2, (6 = (3.62 ( 0.88)(10-20 cm2. The rms value is 115(10-6 Debye2.

Supplementary Table II. Intensity calculations on the Er(III) Schiff base complex [Er(L1H)3(NO3)3]

| Transition (a) | Wave number (cm-1) | Dexp (10-6 Debye2) | Dcalc (b) (10-6 Debye2) | Dexp-Dcalc | Dcalc/Dexp |
| --- | --- | --- | --- | --- | --- |
| 4I11/2 | 10240 | 225 | 278 | -53 | 1.24 |
| 4I9/2 | 12560 | 21 | 43 | -22 | 2.05 |
| 4F9/2 | 15270 | 358 | 347 | +11 | 0.97 |
| 4S3/2 | 18450 | 89 | 110 | -21 | 1.24 |
| 2H11/2 | 19120 | 2324 | 2184 | +140 | 0.94 |
| 4F7/2 | 20460 | 428 | 344 | +84 | 0.80 |

- All the transitions start from the 5I15/2 ground state.

- The set of Judd-Ofelt intensity parameters used to calculate the dipole strength Dcalc is: (2 = (16.47 ( 0.58)(10-20 cm2, (4 = (1.26 ( 0.71)(10-20 cm2, (6 = (2.85 ( 0.46)(10-20 cm2. The rms value is 101(10-6 Debye2.

Supplementary Figure I. Absorption spectrum of the Ho(III) complex [Ho(L1H)3(NO3)3] in chloroform (conc. 0.005 M, ambient temperature). All the transitions start from the 5I8 ground state.

Supplementary Figure II. Luminescence decay curve of the Eu(III) complex (Eu(L1H)3(NO3)3( at 20 K, excited at 579 nm.