 

Supplemental Material

Molecular Dynamics Simulations of the Lithium Coordination Environment in Phosphate Glasses

Todd M. Alama, Jian-Jie Liangb and Randall T. Cyganb

a Organic Materials Department, Sandia National Laboratories, MS-1407, Albuquerque, NM, 87185-1407, USA E-mail:tmalam@sandia.gov

b Geochemistry Department, Sandia National Laboratories, MS-0750, Albuquerque, NM, 87185-0750, USA

Table 1S:  Number of atoms and cell dimensions of the

Li-ultraphosphate glasses, x Li2O  (1-x) P2O5.

| x | Number of atoms | Simulation cell dimensions (Å) |
| --- | --- | --- |
| 0.0 | 336 | 16.8 x 16.8 x 12.6 |
| 0.1 | 396 | 23.3 x 15.6 x 15.6 |
| 0.2 | 372 | 22.9 x 15.4 x 15.4 |
| 0.3 | 348 | 22.7 x 15.2 x 15.2 |
| 0.4 | 324 | 22.3 x 14.9 x 14.9 |
| 0.5 | 360 | 21.4 x 16.0 x 16.0 |

Fig. 1S: A comparison of the experimental G(r) for a lithium metaphosphate glass (x = 0.5) obtained from neutron diffraction46 (solid line), X-ray diffraction47 (upper offset solid line) and the MD simulation G(r) (dashed line). It should be noted that natural lithium has a negative neutron scattering length, such that the pair distribution correlations between Li-O and Li-P produce a negative peak in the G(r) [ See Eqn. 1 of Ref. 46]. These negative peaks have been included in the MD simulated G(r) for direct comparison to the neutron diffraction results.

Fig. 2S: Pair distribution function  for the Li-O atomic pair for the xLi2O·(1-x)P2O5 glass at 300 K from MD simulations as a function of Li2O concentration.

Fig. 3S: Pair distribution function  for the Li-P atomic pair for the xLi2O·(1-x)P2O5 glass at 300 K from MD simulations as a function of Li2O concentration.

Fig. 4S: Pair distribution function  for the Li-Li atomic pair for the xLi2O·(1-x)P2O5 glass at 300 K from MD simulations as a function of Li2O concentration.