- Table Captions

- Table S2 (ESI): Optimized parameters of the equilibrium geometry of 4-cyanopyridine

- Table S3 (ESI): Internal valence coordinates and scale factors used in the present work.

Table S4: Frequency vibration calculated by SFC, DFT, MP2 and SQM, Ir and Raman intensity of 4-CP, compared to the calculated and experimental results [13] and Topacli and Bayari[25].

- Table S5 (ESI): Calculated vibrational frequencies of Au-NCPyr and Au-pyrCNmolecule (a) with and without electric field (b) and 4-CP (c).

- Table S6 (ESI): Charge distribution in Au28/pyrCN and Au28/Ncpyr clusters (on-top configuration), compared to Au-pyrCN and Au-CNpyr molecules.

- Table S7 (ESI): Bond indices in 4-CP, Au-Ncpyr, Au-Cnpyr, Au28/pyrCN and Au28/Ncpyr.

Name Definition SCF DFT MP2 [1, 2] exp [3]

r1 R(2,1) 1.137} 1.164 1.188} 1.157 1.137

r2 R(3,2) 1.448} 1.435 1.444} 1.463 1.439

r3 R(4,3) 1.388} 1.401 1.409} 1.393 1.381

r4 R(6,4) 1.387} 1.394 1.403} 1.387 1.383

r5 R(8,6) 1.322} 1.337 1.350} 1.354 1.331

r6 R(9,4) 1.079} 1.090 1.094} 1.082 0.99

r7 R(11,6) 1.082} 1.095 1.096} 1.087 1.01

3’ A(2,3,4) 120.44} 120.68 120.74} 120.77 120.0}

3 A(4,3,5) 119.12} 118.63 118.53} 118.46 120.0}

4 A(3,4,6) 117.78} 118.05 118.16} 118.72 117.5}

6 A(4,6,8) 123.67} 124.07 124.32} 124.20 123.9}

8 A(6,8,7) 117.96} 117.13 116.52} 115.71 117.3}

4 A(3,4,9) 121.22} 120.84 120.77} 120.80 119.5}

4’ A(6,4,9) 120.99} 121.11 121.07} 120.5 123.0}

 6 A(4,6,11) 119.96} 119.84 119.81} 119.8 121.1}

 6’ A(8,6,11) 116.36} 116.08 115.88} 116.0 115.0}

- W. J. Savich, Thesis, University of Guelph, Canada, 1996.

- S. Akiyama, S. Yamauci, N. Hirota, S. Nagaoka, J. Phys. Chem. 97(1993) 40.

- M. Laing, N. Sparrow, P. Sommerville, Acta Crystallogr. B27 (1986).

table S2 : Optimized parameters of the equilibrium geometry of 4-CP

S definition type SF

In plane deformation 1 r6 C-H stretching 0.980171a

2 r’6b C-H stretching 0.980171a

3 r7 C-H stretching 0.980171a

4 r’7b C-H stretching 0.980171a

5 r3 C-C stretching 0.940373a

6 r’3b C-C stretching 0.940373a

7 r4 C-C stretching 0.940373a

8 r’4b C-C stretching 0.940373a

r5 C-N stretching 0.940373a

10 r’7b C-N stretching 0.940373a

11 r1 C-N stretching 1.035393c

12 r2 C-(CN) stretching 0.988191c

13 13d C-(CN) rocking 1.012131a

14 14d C-H rocking 1.012131a

15 16d C-H rocking 1.012131a

16 17d C-H rocking 1.012131a

17 15d C-H rocking 1.012131a

18 1e b1u in plane ring deformation 1.010073a

19 2f e2g in plane ring deformation 1.010073a

20 3g e2g in plane ring deformation 1.010073a

21 i in plane linear bending (ILB) 1.425218c

out of plane deformation 22 0 out of plane linear bending (OLB) 1.425218c

23 4h C-H wagging 1.016871a

24 5h C-H wagging 1.016871a

25 6h C-H wagging 1.016871a

26 7h C-H wagging 1.016871a

27 8h C-(CN) wagging 1.016871a

28 1i b2g out of plane ring deformation 1.017724b

29 2j e2u out of plane ring deformation 1.017724a

30 3k e2gout of plane ring deformation 1.017724a

a from benzene

b r3',r4'...r7' are the symmetric elements of r3,r4...r7.

c From CH3-CN.

d With 13=2-1/2[3-3’]where 3 is the symmetric element of 3’ and similar definitions for 14,15, 16, 17, and 5,5’,7, 7’, the symmetric elements of 4,4’,6, 6’.

e  1= 6-1/2[3-4-5+6+7-8].

f  2= 12-1/2[23-4-5-6-7+28].

g  3= 2-1[4-5-6+7].

h  4=D(H9C4C3C6), 5=D(H10C6C6C6),6=D(H11C6C4N8),7=D(H12C7C(N8), ),8=D(C2C3C4C5).

i1=6-1/2[3-4-5+6+7-_ with 3=D(C5C3C4C6), 4=D(C3C4C6N8) 5=D(C4C3C5C7), 6=D(C4C6N8C7), 7=D(N8C7C5C3), 8=D(C5C7C6N8).

j2=6-1[-3+4+5-

k 1=12-1/2[3+24-5-6+7-.

- Table S3

Internal valence coordinates and scales factors used in the present work.

SCFa DFTa MP2a SQMa IIRb IRAb PED [13] exp[25] calc.[25] ass.a

a1 modes

1 487 456 450 450 0.6 4.5 S19(61) S12(20) 455 461 449 5

2 828 782 775 766 22.2 6.6 S1930) S12(24)S1(15)S2(15) 775 777 767 10

3 1089 1010 1002 970 5.2 25.5 S18(27)S5(22)S6(22) 987-991 992 1003 15

4 1171 1090 1085 1055 2.4 2.6 S18(35)S17(14)S17(14) 1065-1080 1084 1085 16

5 1303 1226 1222 1213 0.3 32. S18(24)S12(18)S14(14)S1è(14) 1192-1200 1194 1175 18

6 1333 1248 1246 1218 3.8 5.0 S15(19)S16(19)S3(13)S4(13) 1226-1235 1236 1246 19

7 1658 1522 1513 1503 8.1 3.4 S15(24)S16(24)S17(10) 1487-1494 1493 1491 23

8 1804 1654 1643 1585 54.6 31.1 S3(20)S4(20) 1588-1592 1593 1593 25

9 2604 2356 2170 2231 17.5 213 S11(74)S12(25) 2237-2244 26

10 3352 3177 3218 3154 7.8 89.4 S19(46)S10(46) 3040-3052 3045 3047 28

11 3390 3227 3252 3187 0.6 199 S7(48)S8(48) 3065-3076 3067 3074 29

a2 modes

1 432 376 375 381 0.0 0.0 S26(58)S28(37) 368 381 3

2 972 887 886 901 0.0 0.8 S22(42)S25(42) 871 858 12

3 1120 1006 988 1004 0.0 1.0 S23(37)S24(37)S22(10)S25(10) 965-980 974 965 14

b1 modes

1 185 166 158 185 8.7 3.6 S13(56)S30(41) 170-190 2

2 617 564 538 641 0.7 4.0 S30(54)S13(28) 368-376d 350d 6

3 734 680 674 685 0.0 5.4 S20(78) 660-669 663 654 8

4 1155 1106 1101 1068 20.0 7.9 S3(21)S4(21)S14(17)S17(17) 1102-1108 1113 1126 17

5 1241 1315 1336 1323 12.9 9.6 S14(24)S17(24)S15(11)S16(11) 1208 1206 1220 20

6 1450 1338 1395 1348 0.1 2.9 S5(31)S6(31)S15(10)S16(10) 1323-1335 1336 1325 21

7 1551 1439 1456 1430 31.5 1.6 S3(23)S4(23)S15(20)S16(20) 1407-1412 1412 1402 22

8 1761 1613 1597 1533 30.7 2.3 S1(26)S2(37)S5(12)S6(12) 1542-1552 1545 1559 23

9 3350 3175 3216 3152 22.4 109 S9(48)S10(48) 3022-3033 3029 3045 27

10 3389 3227 3252 3187 4.4 9.4 S7(48)S10(48) 3082-3091 3085 3065 30

b2 modes

1 163 145 140 153 8.9 0.1 S21(42)S28(26)S29(16)S26(10) 144-149 149 1

2 434 389 370 419 0.4 1.5 S28(47)S29(230S26(18) 4

3 638 585 615 659 29.6 5.6 S21(42)S29(43)S27(34)S21(26) 560-563 559 556 7

4 816 754 725 749 0.0 0.1 S21(42)S27(79)S26(16) 711-726 731 761 9

5 927 841 826 852 38.9 1.0 S21(42)S22(28)S25(28)S23(19) 822-829 827 840 11 S24(19)S21(14)

6 1088 986 965 981 0.9 0.7 S23(24)S24(24)S22(17)S25(17) 911 912 936 13 S27(12)

a our work

b  from our SCF calculations

c  from SQM calculations; the weight of the S internal coordinate is in parentheses

d  it seems to us that it concerns the second b2 vibrational frequency}

- Table S4: Vibrational frequencies of 4-cyanopyridine (cm-1}

|  4-CP Au-Ncpyr Au-pyrCN |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fz=0 Fz<0 Fz>0 |  | Fz=0 Fz<0 Fz>0 |  | Fz=0 Fz<0 Fz>0 |  |  |
| a1 modes |  |  |  |  |  |  |  |
| 5 487.7 486.2 485.9 489.6 490.9 491.4 489.1 488.8 490.9 |  |  |  |  |  |  |  |
| 10 828.7 827.8 823.6 830.3 825.6 828.3 829.4 826.3 837.8 |  |  |  |  |  |  |  |
| 15 1089.0 1085.3 1088.6 1090.0 1088.7 1091.9 1092.1 1093.5 1087.6 |  |  |  |  |  |  |  |
| 16 1171.1 1168.0 1169.5 1176.9 1176.0 1177.7 1174.0 1173.9 1174.2 |  |  |  |  |  |  |  |
| 18 1303.3 1299.2 1300.4 1307.2 1306.4 1314.8 1309.9 1308.8 1312.1 |  |  |  |  |  |  |  |
| 19 1333.3 1341.7 1320.1 1334.7 1334.3 1331.2 1334.2 1336.6 1331.8 |  |  |  |  |  |  |  |
| 23 1657.9 1660.6 1651.0 1659.9 1658.1 1660.6 1658.8 1658.5 1659.2 |  |  |  |  |  |  |  |
| 25 1804.8 1800.7 1800.5 1809.1 1805.6 1812.5 1807.0 1803.8 1811.8 |  |  |  |  |  |  |  |
| 26 2604.5 2597.8 2600.6 2611.7 2606.0 2618.1 2612.1 2607.4 2616.4 |  |  |  |  |  |  |  |
| 28 3353.0 3354.9 3350.2 3359.4 3360.5 3357.8 3354.8 3354.0 3353.2 |  |  |  |  |  |  |  |
| 29 3390.0 3388.0 3391.2 3380.8 3382.5 3377.7 3380.5 3380.9 3381.9 |  |  |  |  |  |  |  |
| a2 modes |  |  |  |  |  |  |  |
| 3 431.8 420.9 431.5 444.2 455.0 444.9 445.2 443.7 445.6 |  |  |  |  |  |  |  |
| 12 972.4 967.7 971.8 971.3 968.3 974.4 972.4 969.5 974.5 |  |  |  |  |  |  |  |
| 14 1120.2 1128.8 1107.7 1124.7 1127.4 1123.0 1122.7 1124.6 1121.3 |  |  |  |  |  |  |  |
| b1 modes |  |  |  |  |  |  |  |
| 2 185.3 175.9 144.6 191.5 194.0 188.9 196.4 196.1 196.0 |  |  |  |  |  |  |  |
| 6 616.9 611.8 602.6 620.8 623.0 619.2 618.8 620.8 616.2 |  |  |  |  |  |  |  |
| 8 734.0 734.1 729.3 736.6 736.4 736.7 735.0 735.3 735.4 |  |  |  |  |  |  |  |
| 17 1154.9 1143.3 1157.0 1173.2 1171.4 1176.3 1174.5 1173.0 1175.7 |  |  |  |  |  |  |  |
| 20 1240.8 1230.4 1244.8 1252.5 1253.9 1252.2 1250.9 1253.8 1248.2 |  |  |  |  |  |  |  |
| 21 1450.1 1453.3 1442.0 1456.0 1455.7 1455.8 1455.9 1455.8 1456.3 |  |  |  |  |  |  |  |
| 22 1551.2 1560.0 1539.5 1563.9 1563.4 1563.6 1560.6 1559.0 1563.4 |  |  |  |  |  |  |  |
| 24 1760.8 1756.1 1758.4 1758.9 1759.2 1758.9 1755.1 1757.6 1754.0 |  |  |  |  |  |  |  |
| 27 3350.6 3352.9 3347.6 3360.7 3362.0 3358.5 3356.2 3355.7 3354.5 |  |  |  |  |  |  |  |
| 30 3389.3 3387.3 3390.6 3388.2 3388.9 3387.3 3385.7 3385.2 3387.1 |  |  |  |  |  |  |  |

b2 modes

1 162.8 150.6 131.4 167.5 174.2 164.6 174.8 173.3 173.2

4 433.6 430.5 415.6 438.8 443.7 435.4 438.3 440.2 435.0

7 638.4 632.9 629.9 637.9 640.8 636.9 639.2 640.1 638.6

9 816.1 806.8 816.8 815.8 816.6 816.6 816.5 815.3 817.0

11 927.1 927.1 922.6 936.3 940.9 936.3 938.6 937.3 940.3

13 1087.8 1090.2 1081.2 1090.3 1089.7 1089.1 1088.9 1089.3 1088.9

a without the 3 modes related to the Au-bond

b with ¦F_z¦ = 0.002 au ~ 109 V/m

c from our SCF calculations

- Table S5 : Vibrational frequencies (cm-1) of Au-NCpyr and Au-pyrCN moleculesa with and

without electric fieldb compared to  4-cyanopyridinec

Atom free 4-CP Au-Ncpyr Au-pyrCN Au28/pyrCNa Au28/NCpyrb

Au -0.104 -1.08c

N1 -0.140 -0.250 -0.123 -0.125 -0.282

C2 +0.011 +0.200 +0.017 +0.019 +0.256

C3 -0.026 -0.046 -0.016 -0.003 -0.016

C4 -0.059 -0.059 -0.041 -0.045 -0.058

C6 +0.201 +0.205 +0.265 0.278} +0.204

N8 -0.324 -0.315 -0.475 -0.498 0.315

H9 +0.046 +0.054 +0.058 +0.059 +0.060

H11 +0.050 +0.057 +0.085 +0.035 +0.057

Au -0.136 -1.01c

a the charge distribution reported in this table has been

obtained}in the a-top configuration with a link via pyridine ring in the

optimized geometry.

b the charge distribution reported in this table has been

obtained in the a-top configuration with a link via cyano group in the

optimized geometry.

c charge of the central Au atom of the Au28

- Table S6: Charge distribution in free 4-CP, Au-NCpyr, Au-pyrCN, Au28/pyrCN, Au28/Ncpyr

Bond free 4-CP Au-Ncpyr Au-pyrCN Au28/pyrCNa Au28/NCpyrb

Au-N1 0.21 0.14

N1-C2 3.1 2.88 3.17 3.17 3.02

C2-C3 1.01 1.04 1.02 1.02 1.03

C3-C4 1.41 1.41 1.41 1.41 1.41

C4-C6 1.44 1.44 1.47 1.48 1.44

C6-N8 1.50 1.50 1.37 1.40 1.50

C4-H9 0.97 0.97 0.97 0.97 0.97

C6-H11 0.98 0.98 0.97 0.94 0.98

Au-N8 0.24 0.19}

a the bond indices reported in this table have been obtained

in the a-top configuration with a link via pyridine ring in the

optimized geometry.

b the bond indices reported in this table have been obtained

in the a-top configuration with a link via cyano group in the

optimized geometry}.

- Table S7: Bond indices in free 4-CP, Au-NCpyr, Au-pyrCN, Au28/pyrCN, Au28/Ncpyr