Table S1-S4. Electronic supplementary material

Table S1.

Ionic charges, bond lengths and angles in MgO clusters within the

B3LYP approximation for three different basis sets. The results are grouped in rhombic, hexagonal and octagonal ring based stacks. Two interlayer distances are given in case of three-layer stacks. The shorter distance corresponds to an O atom in the terminal ring.

__________________________________________________________________________________________

STO-3G basis set

__________________________________________________________________________________________

inter-layer

(MgO)n		structure		Ionic charge	Bond lengthsa (Å) 	spacing (Å)	(MgOMg)

__________________________________________________________________________________________

MgO		monomer	0.47		a=1.662b

(MgO)2		rhombic ring	0.39		a=1.90					=73

(MgO)4		2-ring stack	±0.60		a=1.88			1.88		=82.1

(MgO)6		3-ring stack	0.57<q<0.63	a=c=1.87		1.83/1.89	==81°

-0.63<q<0.60	b=1.97					=85°

(MgO)3		hexagonal ring	0.55		a=1.78					=93

(MgO)6		2-ring stack	0.60		a=b=1.83		1.89		==106

(MgO)9		3-ring stack	0.58<q<0.62	a=c=1.83		1.85/1.91	==102

-0.64<q<-0.58	b=1.91					=118

(MgO)4		octagonal ring	0.54		a=1.77					=99

(MgO)8		2-ring stack	0.60		a=b=1.81		1.89		==121

(MgO)12		3-ring stack	0.59<q<0.62	a=c=1.82		1.85/1.92	==111

-0.65<q<-0.58	b=1.90					=138

__________________________________________________________________________________________

6-311G basis set

__________________________________________________________________________________________

MgO		monomer	0.73		a=1.777

(MgO)2		rhombic	ring	0.66		a=1.97					=81

(MgO)4		2-ring stack	±0.85		a=b=1.98		1.98		==86°

(MgO)6		3-ring stack	0.97<q<1.13	a=c=1.97		1.98/1.93	==85°

-1.14<q<-1.04	b=2.17					=89°

(MgO)3		hexagonal ring	1.05		a=1.84					=109

(MgO)6		2-ring stack	1.10		a=b=1.92		2.01		==115

(MgO)9		3-ring stack	0.94<q<1.24	a=c=1.92		1.96/2.01	==114

-1.21<q<-1.09	b=2.06					=119

(MgO)4		octagonal ring	1.10		a=1.82					=125

(MgO)8		2-ring stack	1.13		a=b=1.90		2.03		==131

(MgO)12		3-ring stack	0.90<q<1.20	a=c=1.90		1.97/2.03	==131

-1.20<q<-1.10	b=2.02					=134

Table S1 continues.

__________________________________________________________________________________________

6-311G(d) basis set

__________________________________________________________________________________________

MgO		monomer	0.62		a=1.756b	 		(exp. 1.749 Å [12])

(MgO)2		rhombic ring	0.52		a=1.96					=80.0

(MgO)4		2-ring stack	±0.86		a=1.97			1.97		=85°

(MgO)6		3-ring stack	0.87<q<0.91	a=c=1.96		1.97/1.93	==84°

-0.94<q<-0.85	b=2.16					=87°

(MgO)3		hexagonal ring	0.83		a=1.84					=105

(MgO)6		2-ring stack	0.90		a=b=1.92		2.01		==115

(MgO)9		3-ring stack	0.89<q<0.98	a=c=1.92		1.96/2.01	==112

-1.00<q<-0.87	b=2.06					=117

(MgO)4		octagonal ring	0.83		a=1.83					=119

(MgO)8		2-ring stack	0.90		a=b=1.90		2.03		==128

(MgO)12		3-ring stack          0.94<q<1.00	a=c=1.90		1.97/2.02	==130

-1.07<q<-0.91	b=2.04

Table S2.

Computed B3LYP total energies and binding energies in (MgO)n clusters for three basis sets. The results are grouped in 1-4 ring stacks for each of the rhombic hexagonal and octagonal ring structures. Only 1-3 layer stacks are considered for the STO-3G basis set.

STO-3G basis set

__________________________________________________________________________________________

(MgO)n		structure		Total energy (Hartree)		Binding energy (eV)

___________________________________________________________________________

MgO			monomer		-271.585547			2.35

(MgO)2			rhombic ring		-543.46603			6.36

(MgO)4			2-ring stack		-1087.35886			9.27

(MgO)6			3-ring stack		-1631.23302			10.15

(MgO)3			hexagonal ring		-815.354136			7.77

(MgO)6			2-ring stack		-1631.21475			10.07

(MgO)9			3-ring stack		-2447.07077			10.82

(MgO)4			octagonal ring		-1087.18979			8.12

(MgO)8			2-ring stack		-2174.98595			10.18

(MgO)12			3-ring stack		-3262.79761			10.90

__________________________________________________________________________________________

6-311G basis set

__________________________________________________________________________________________

MgO			monomer		-275.24108			1.73

(MgO)2			rhombic	 ring		-550.68422			4.48

(MgO)4			2-ring stack		-1101.64797			6.35

(MgO)6			3-ring stack		-1652.61528			7.03

(MgO)8			4-ring stack		-2203.57932			7.31

(MgO)3			hexagonal ring		-826.161978			5.71

(MgO)6 			2-ring stack		-1652.62865			7.09

(MgO)9			3-ring stack		-2479.10977			7.59

(MgO)12			4-ring stack		-3305.58667			7.81

(MgO)4			octagonal  ring		-1101.61086			6.13

(MgO)8			2-ring stack		-2203.57575			7.33

(MgO)12			3-ring stack		-3305.55939			7.78

(MgO)16			4-ring stack		-4407.53980			7.99

Table S2 continues.

__________________________________________________________________________________________

6-311G(d) basis set

__________________________________________________________________________________________

MgO			monomer		-275.25310		         2.03 (exp. 3.56 eV [12])

(MgO)2			rhombic ring		-550.72047			4.95

(MgO)4			2-ring stack		-1101.70391			6.73

(MgO)6			3-ring stack		-1652.68627			7.32

(MgO)8			4-ring stack		-2203.66319			7.60

(MgO)3			hexagonal ring		-826.21097			6.12

(MgO)6			2-ring stack		-1652.6969			7.37

(MgO)9			3-ring stack		-2479.19943			7.83

(MgO)12			4-ring stack		-3305.69680			8.06

(MgO)4			octagonal ring		-1101.67017			6.50

(MgO)8			2-ring stack		-2203.66151			7.59

(MgO)12			3-ring stack		-3305.66584			7.99

(MgO)16			4-ring stack		-4407.67473			8.19

Table S3.

Ionic charges, bond lengths and angles in CaO clusters within the B3LYP approximation for four different basis sets. The results are arranged in groups comprising rhombic, hexagonal and octagonal ring based stacks. Two interlayer distances are given in case of three-layer stacks. The shorter distance corresponds to an O atom in the terminal ring.

STO-3G basis set

__________________________________________________________________________________________

Inter-layer

(CaO)n		structure		Ionic charge	Bond lengthsa (Å) 	spacing (Å)	(CaOCa)

__________________________________________________________________________________________

CaO		monomer	0.23		a=2.00

(CaO)2		rhombic ring	0.22		a=2.34					=83

(CaO)4		2-ring stack	±0.33		a=b=2.34		2.34		=90

(CaO)6		3-ring stack	0.30<q<0.34	a=c=2.33		2.34/2.31	==91°

-0.34<q<-0.32	b=2.37					=96°

(CaO)3		hexagonal ring	0.26		a=2.31					=97

(CaO)6 		2-ring stack	0.32		a=b=2.29		2.32		==111

(CaO)9 		3-ring stack	0.32<q<0.35	a=c=2.30		2.31/2.34	==111

-.0.37<q<-0.31	b=2.33					=126

(CaO)4		octagonal ring	0.26		a=2.29					=101

(CaO)8		2-ring stack	0.32		a=b=2.28		2.32		==121

(CaO)12		3-ring stack         0.31<q<0.36	a=c=2.30		2.32/2.34	==116

-.38<q<-.30	b=2.33					=149

_________________________________________________________________________________________________________________

6-311G basis set

__________________________________________________________________________________________

CaO		monomer	0.90		a=2.04

(CaO)2		rhombic	ring	0.81		a=2.13					=94

(CaO)4		2-ring stack	±0.95		a=b=2.22		2.22		=92

(CaO)6		3-ring stack	1.12<q<1.36	a=c=2.16		2.23/2.22	==92°

-1.32<q<-1.26	c=2.34					=93°

(CaO)3		hexagonal ring	1.29		a=2.09					=125

(CaO)6		2-ring stack	1.30		a=b=2.17		2.21		==122

(CaO)9		3-ring stack	1.02<q<1.46	a=c=2.18		2.26/2.26	==123

-1.36<q<-1.28	b=2.32					=123

(CaO)4		octagonal ring	1.31		a=2.08					=141

(CaO)8		2-ring stack	1.32		a=b=2.17		2.28		==138

(CaO)12		3-ring stack	1.12<q<1.54	a=c=2.17		2.29/2.27	==140

-1.35<q<-1.28	b=2.30					=137

Table S3 continues.

__________________________________________________________________________________________

6-311G(d) basis set

__________________________________________________________________________________________

CaO		monomer	0.73		a=1.826

(CaO)2		rhombic ring	0.90		a=2.03					=93

(CaO)4		2-ring stack	±0.95		a=b=2.18		2.18		=92

(CaO)6		3-ring stack	0.93<q<1.00	a=c=2.16		2.23/2.22	==92°

-1.01<q<-0.95	b=2.34					=93°

(CaO)3		hexagonal ring	0.94		a=2.04					=123

(CaO)6		2-ring stack	0.97		a=b=2.16		2.21		==122

(CaO)9		3-ring stack	0.84<q<1.07	a=c=2.15		2.26/2.25	==123

-1.04<q<-0.96	b=2.31					=122

(CaO)4		octagonal ring	0.96		a=2.05					=139

(CaO)8		2-ring stack	0.99		a=b=2.16		2.21		==137

(CaO)12		3-ring stack	0.77<q<1.13	a=c=2.16		2.25/2.26	==139

-1.05<q<-0.99	b=2.31					=136

__________________________________________________________________________________________

6-311G(2d) basis set

__________________________________________________________________________________________

CaO		monomer	0.77		a=1.803			(exp. 1.82 Å [12])

(CaO)2		rhombic ring	0.92		a=2.03					=93

(CaO)4		2-ring stack	±0.97		a=b=2.17		2.17		=92

(CaO)6		3-ring stack	0.97<q<1.00	a=c=2.15		2.23/2.22	==93°

-1.00<q<-0.97	b=2.34					=93°

(CaO)3		hexagonal ring	0.95		a=2.04					=123

(CaO)6		2-ring stack	0.99		a=b=2.16		2.20		==122

(CaO)9		3-ring stack	0.96<q<1.03	a=c=2.15		2.25/2.25	==123

-1.03<q<-0.99	b=2.31					=122

(CaO)4		octagonal ring	0.95		a=2.05					=140

(CaO)8		2-ring stack	0.99		a=b=2.17		2.21		==137

(CaO)12		3-ring stack	0.94<q<1.04	a=c=2.16		2.25/2.26	==139

-1.04<q<-0.99	b=2.31					=136

Table S4.

Computed B3LYP total energies and binding energies in (CaO)n clusters for four basis sets. The results are grouped in results for 1-3 ring stacks for each of the rhombic hexagonal and octagonal ring structures.

STO-3G basis set

__________________________________________________________________________________________

(CaO)n		structure			Total energy (Hartree)	    Binding energy (eV)

__________________________________________________________________________________________

CaO		monomer		-744.732030			-0.75

(CaO)2		rhombic	ring		-1489.65478			2.10

(CaO)4		2-ring stack   		-2979.65411			4.19

(CaO)4		3-ring stack   		-4469.66055			4.95

(CaO)3		hexagonal ring		-2234.58447			2.76

(CaO)6		2-ring stack		-4469.61990			4.81

(CaO)9		3-ring stack		-6704.63893			5.44

(CaO)4		octagonal ring		-2979.49309			3.08

(CaO)8		2-ring stack		-5959.53740			4.96

(CaO)12		3-ring stack		-8939.55044			5.51

__________________________________________________________________________________________

6-311G basis set

__________________________________________________________________________________________

CaO		monomer		-752.722700			1.69

(CaO)2		rhombic ring		-1505.64680			4.40

(CaO)4		2-ring stack		-3011.58939			6.42

(CaO)6		3-ring stack		-4517.51958			7.06

(CaO)3		hexagonal ring		-2258.58330			5.46

(CaO)6		2- ring stack		-4517.51747			7.05

(CaO)9		3-ring-stack		-6776.44019			7.55

(CaO)4		octagonal ring		-3011.49033			5.77

(CaO)8		2-ring stack		-6023.40430			7.21

(CaO)12		3-ring stack		-9035.30709			7.67

Table S4 continues

__________________________________________________________________________________________

6-311G(d) basis set

__________________________________________________________________________________________

CaO		monomer		-752.799507			3.75

(CaO)2		rhombic ring		-1505.79640			6.44

(CaO)4		2-ring stack		-3011.83206			7.52

(CaO)6		3-ring stack		-4517.83816			8.45

(CaO)3		hexagonal ring		-2258.76105			7.04

(CaO)6		2-ring stack		-4517.82706			8.42

(CaO)9		3-ring stack		-6776.85874			8.78

(CaO)4		octagonal ring		-3011.69865			7.16

(CaO)8		2-ring stack		-6023.78614			8.48

(CaO)12		3-ring stack		-9035.83147			8.83

__________________________________________________________________________________________

6-311G(2d) basis set

__________________________________________________________________________________________

CaO		monomer		-752.81876			4.28     (exp. 4.76 eV [12])

(CaO)2		rhombic ring		-1505.82485			6.82

(CaO)4		2-ring stack		-3011.86621			7.75

(CaO)6		3-ring stack		-4517.88195			8.67

(CaO)3		hexagonal ring		-2258.80184			7.41

(CaO)6		2-ring stack		-4517.87406			8.64

(CaO)9		3-ring stack		-6776.91901			8.96

(CaO)4		octagonal ring		-3011.75285			7.55

(CaO)8		2-ring stack		-6023.84931			8.70

(CaO)12		3-ring stack		-9035.91172			9.01