Supplementary material

TABLE 1. Physical properties at T = 298.15 K of methyl benzoate

| Compound | M g·mol-1 | ( g·cm-3 | ((V/(T)p·10-7 dm3·g-1·K-1 | cp J·K-1·g-1 |
| --- | --- | --- | --- | --- |
| Polyethylene | 13.6422 | 0.91871 | 0.2481 | 2.01 |
| Mylar | 192.1681 | 1.382 | 0.95982 | 1.322 |
| Cotton | 27.700 | 1.5 | 9.693 | 1.48 |
| Methyl benzoate | 136.1479 | 1.08884 | (3.354) | 1.635 |

Value in parentheses was estimated

# References

1.	Properties are those given by the supplier.

2.	J. D. Cox,  H. A. Gundry, A. J. Head,  Trans. Faraday Soc. 1964, 60, 653.

3.	S. Inagaki, S. Murata,  M. Sakiyama,  Bull. Chem. Soc. Jpn.1982, 55, 2808.

4.	CRC Handbook of Chemistry and Physics. R.C. Weast, M.J. Astle, W.H.          Beyer: editors. CRC Press: Boca Raton. 65th edn. 1985.

5.	R. Fuchs, J. Chem. Thermodynamics 1989, 11, 959.