Supplementary Data

Systematic analysis of calcium-oxygen coordination environment by calcium K-edge XANES.

F.E. Sowreya*, L.J. Skippera, D.M. Pickupa, K.O. Drakeb, Z. Linb, M.E. Smithb and R.J. Newporta.

aSchool of Physical Sciences, University of Kent, Canterbury, CT2 7NR, UK. bDepartment of Physics, University of Warwick, Coventry, CV4 7AL, UK.

The following represent X-ray crystallographic data found in the ISCD database for calcium minerals. The chemical formula, mineral name (where relevant) and space group are followed by a reference to the original paper. All Ca-X distances below 4 Å are then presented.

CaMoO4, Powellite, [I41/aS]

# Aleksandrov 1968

Kristallografiya 13 (1968) P. 512-513

Ca1

3.871 Ca 1	3.871 Ca 1	3.871 Ca 1	3.871 Ca 1

3.694 Mo1	3.694 Mo1	3.694 Mo1	3.694 Mo1

3.871 Mo1	3.871 Mo1	3.871 Mo1	3.871 Mo1

2.454 O1		2.454 O1		2.454 O1		2.454 O1

2.478 O1		2.478 O1		2.478 O1		2.478 O1

3.749 O1		3.749 O1		3.749 O1		3.749 O1

# Hazen 1985

Journal of Physics and Chemistry of Solids 46 2 (1985) P. 253-263

Ca1

3.870 Ca1	3.870 Ca1	3.870 Ca1	3.870 Ca1

3.693 Mo1	3.693 Mo1	3.693 Mo1	3.693 Mo1

3.870 Mo1	3.870 Mo1	3.870 Mo1	3.870 Mo1

2.451 O1		2.451 O1		2.451 O1		2.451 O1

2.465 O1		2.465 O1		2.465 O1		2.465 O1

3.769 O1		3.769 O1		3.769 O1		3.769 O1

Ca4(Si3O9)(OH)2 Foshagite, [P-1]

Gard (1960)

Acta Crystallographica 13 (1960) P. 785-793

Ca 1

3.480 Ca1	3.480 Ca2	3.680 Ca2	3.680 Ca2

3.690 Ca3	3.690 Ca4

2.339 O4		2.407 O2		2.434 O2		2.434 O1

2.474 O5		2.474 O6		2.747 O11	3.797 O10

3.910 O9		3.910 O10

3.117 Si2	3.117 Si3	3.668 Si1

Ca 2

3.480 Ca1	3.480 Ca2	3.680 Ca1	3.680 Ca 1

3.690 Ca4	3.690 Ca3

2.339 O3		2.407 O1		2.434 O1		2.434 O2

2.474 O6		2.474 O5		3.399 O10	3.399 O9

3.797 O9

3.263 Si1	3.392 Si3	3.392 Si2	3.668 Si1

3.972 Si1

Ca 3

3.680 Ca4	3.680 Ca4	3.690 Ca2	3.690 Ca1

2.209 O5		2.367 O7		2.367 O8		2.550 O4

2.550 O3		2.561 O9		3.480 O7		3.817 O11

3.114 Si1	3.505 Si2	3.572 Si2	3.702 Si 2

3.702 Si3

Ca 4

3.680 Ca3	3.680 Ca3	3.690 Ca2	3.690 Ca1

2.209 O6		2.367 O8		2.367 O7		2.550 O3

2.550 O4		2.561 O10	3.173 O11	3.480 O8

3.817 O11

3.114 Si1	3.452 Si3	3.452 Si2	3.505 Si3

3.572 Si3

Ca6(Si6O17)(OH)2, Xonotlite, [P12/a1]

# Mamedov 1956

Doklady Akademii Nauk SSSR,104,(1955),P. 615-618

Ca 1

3.665 Ca2	3.665 Ca2	3.685 Ca3	3.685 Ca4

3.685 Ca3	3.685 Ca4

2.328 O10	2.328 O10	2.358 O4		2.358 O3

2.358 O3		2.358 O4		3.215 O2		3.215 O2

3.377 Si2	3.377 Si1	3.377 Si1	3.377 Si2

Ca 2

3.665 Ca1	3.665 Ca1	3.685 Ca4	3.685 Ca3

3.685 Ca3	3.685 Ca4

2.328 O9		2.328 O9		2.358 O3		2.358 O3

2.358 O4		2.358 O4		3.520 O1		3.520 O1

3.470 Si3	3.470 Si3	3.718 Si2	3.718 Si1

3.718 Si1	3.718 Si2

Ca 3

3.665 Ca 4	3.665 Ca 4	3.685 Ca2	3.685 Ca1

3.693 Ca4	3.693 Ca3

2.275 O9		2.275 O10	2.372 O7		2.372 O8

2.456 O8		2.616 O4		2.832 O5		3.849 O2

3.924 O6		3.924 O5

3.081 Si3	3.119 Si1	3.721 Si2	3.721 Si1

Ca 4

3.665 Ca3	3.665 Ca3	3.685 Ca1	3.685 Ca2

3.693 Ca3	3.693 Ca4

2.275 O10	2.275 O9		2.372 O8		2.372 O7

2.456 O7		2.616 O3		2.832 O6		3.115 O2

3.849 O2

3.081 Si3	3.119 Si2	3.381 Si1	3.381 Si2

CaSiO3, Wollastonite [P-1]

Mamedov 1956

Doklady Akademii Nauk SSSR 107 (1956) P. 463-466

Ca 1

3.576 Ca 2	3.576 Ca 3	3.579 Ca 2	3.579 Ca 3

3.642 Ca 1	3.643 Ca 1

2.325 O  4	2.325 O  3	2.352 O  4	2.352 O  3

2.531 O  1	2.531 O  2	2.781 O  9	3.458 O  8

3.459 O  7	3.979 O  7	3.980 O  8

3.155 Si 1	3.159 Si 3	3.159 Si 2	3.513 Si 2

3.517 Si 1

Ca 2

3.576 Ca 1	3.579 Ca 1	3.642 Ca 3	3.643 Ca 3

2.322 O  6	2.323 O  5	2.414 O  2	2.417 O  3

2.419 O  7	2.423 O  1	2.983 O  9	3.722 O  5

3.906 O  8	3.943 O  9

3.064 Si 3	3.335 Si 1	3.337 Si 2	3.512 Si 1

3.606 Si 1	3.669 Si 3

Ca 3

3.576 Ca 1	3.579 Ca 1	3.642 Ca 2	3.643 Ca 2

2.322 O  5	2.323 O  6	2.414 O  1	2.417 O  4

2.418 O  8	2.423 O  2	3.722 O  6	3.902 O  7

3.943 O  9

3.058 Si 3	3.512 Si 2	3.606 Si 2	3.670 Si 3

3.676 Si 2	3.678 Si 1

Ito 1969

Proceedings of the Japan Academy 45 (1969) P. 913-918

Ca 1

3.516 Ca 3	3.520 Ca 2	3.678 Ca 1	3.678 Ca 1

3.708 Ca 2	3.708 Ca 3

2.312 O  4	2.317 O  3	2.386 O  1	2.427 O  3

2.432 O  4	2.476 O  2	2.641 O  9	3.626 O  8

3.630 O  7	3.807 O  7	3.813 O  8

3.106 Si 1	3.111 Si 2	3.329 Si 3	3.564 Si 2

3.570 Si 1	3.921 Si 3

Ca 2

3.520 Ca 1	3.660 Ca 3	3.660 Ca 3	3.708 Ca 1

2.294 O  6	2.319 O  5	2.355 O  3	2.404 O  7

2.417 O  1	2.514 O  2	3.164 O  9	3.697 O  5

3.824 O  9	3.969 O  8

3.067 Si 3	3.355 Si 2	3.360 Si 1	3.487 Si 1

3.606 Si 1	3.714 Si 3

Ca 3

3.516 Ca 1	3.660 Ca 2	3.660 Ca 2	3.708 Ca 1

2.288 O  6	2.304 O  5	2.342 O  4	2.425 O  8

2.425 O  1	2.531 O  2	3.728 O  6	3.844 O  9

3.979 O  7

3.083 Si 3	3.466 Si 2	3.614 Si 1	3.620 Si 2

3.625 Si 2	3.738 Si 3

Ohashi 1984

Physics and Chemistry of Minerals (Germany) 10 (1984) P. 217-229

Ca 1

3.517 Ca 3	3.620 Ca 2	3.686 Ca 3	3.701 Ca 2

2.266 O  5	2.295 O  4	2.326 O  1	2.422 O  9

2.445 O  6	2.550 O  3	3.728 O  4	3.749 O  7

3.934 O  8

3.079 Si 3	3.477 Si 1	3.588 Si 2	3.606 Si 1

3.613 Si 1	3.733 Si 3

Ca 2

3.518 Ca 3	3.620 Ca 1	3.675 Ca 3	3.701 Ca 1

2.311 O  5	2.321 O  2	2.358 O  4	2.407 O  8

2.422 O  6	2.502 O  3	3.251 O  7	3.712 O  7

3.769 O  5	3.949 O  9

3.068 Si 3	3.361 Si 2	3.380 Si 1	3.493 Si 2

3.590 Si 2	3.696 Si 3

Ca 3

3.517 Ca 1	3.518 Ca 2	3.673 Ca 3	3.675 Ca 2

3.686 Ca 1	3.686 Ca 3

2.345 O  1	2.345 O  6	2.356 O  2	2.417 O  1

2.422 O  3	2.435 O  2	2.639 O  7	3.639 O  9

3.640 O  8	3.843 O  9	3.859 O  8

3.118 Si 1	3.118 Si 2	3.350 Si 3	3.577 Si 1

3.582 Si 2	3.901 Si 3

Buerger 1961

Proceedings of the National Academy of Sciences, U.S.A. 47 (1961) P. 1884-1888

Ca 1

3.518 Ca 3	3.620 Ca 2	3.698 Ca 3	3.700 Ca 2

2.272 O  6	2.302 O  5	2.324 O  3	2.411 O  7

2.437 O  2	2.548 O  1	3.724 O  5	3.733 O  9

3.942 O  8

3.075 Si 3	3.479 Si 1	3.593 Si 2	3.610 Si 1

3.621 Si 1	3.736 Si 3

Ca 2

3.520 Ca 3	3.620 Ca 1	3.683 Ca 3	3.700 Ca 1

2.315 O  6	2.316 O  4	2.368 O  5	2.406 O  8

2.421 O  2	2.501 O  1	3.266 O  9	3.697 O  9

3.768 O  6	3.948 O  7

3.066 Si 3	3.366 Si 2	3.384 Si 1	3.495 Si 2

3.594 Si 2	3.697 Si 3

Ca 3

3.518 Ca 1	3.520 Ca 2	3.676 Ca 3	3.683 Ca 2

3.687 Ca 3	3.698 Ca 1

2.334 O  3	2.349 O  4	2.349 O  2	2.429 O  3

2.438 O  1	2.441 O  4	2.642 O  9	3.647 O  8

3.655 O  7	3.841 O  7	3.846 O  8

3.112 Si 1	3.114 Si 2	3.359 Si 3	3.582 Si 1

3.587 Si 2	3.899 Si 3

NaCa16(AlSi23O60)O, Gyrolite, [P-1]

Merlino 1988

Mineralogical Magazine 52 (1988) P. 377-387

Ca 1

3.616 Ca 6	3.632 Ca 7	3.638 Ca 5	3.668 Ca 3

3.669 Ca 2	3.673 Ca 4

2.344 O  5	2.350 O  4	2.356 O  6	2.402 O  12

2.405 O  11	2.419 O  10	3.789 O  34	3.865 O  33

3.937 O  32

3.629 Si 7	3.656 Si 6	3.672 Si 5

Ca 2

3.647 Ca 6	3.669 Ca 1	3.694 Ca 5	3.743 Ca 3

3.753 Ca 4	3.794 Ca 7

2.301 O  4	2.389 O  13	2.424 O  1	2.470 O  9

2.471 O  10	2.571 O  3	2.861 O  16	3.449 O  24

3.322 Si 3	3.446 Si 5	3.466 Si 10	3.699 Si 1

3.994 Si 2

Ca 3

3.640 Ca 7	3.668 Ca 1	3.696 Ca 6	3.743 Ca 2

3.757 Ca 4	3.787 Ca 5

2.338 O  5	2.357 O  132.398 O  2	2.483 O  11

2.511 O  7	2.544 O  1	2.853 O  173.457 O  25

3.327 Si 1	3.475 Si 8	3.476 Si 6	3.715 Si 2

3.993 Si 3

Ca 4

3.643 Ca 5	3.673 Ca 1	3.691 Ca 7	3.753 Ca 2

3.757 Ca 3	3.796 Ca 6

2.313 O  6	2.358 O  13	2.407 O  3	2.447 O  8

2.447 O  12	2.550 O  2	2.837 O  15	3.424 O  26

3.316 Si 2	3.442 Si 7	3.461 Si 9	3.712 Si 3

3.999 Si 1

Ca 5

3.638 Ca 1	3.643 Ca 4	3.694 Ca 2	3.732 Ca 7

3.739 Ca 6	3.787 Ca 3

2.317 O  6	2.393 O  14	2.404 O  8	2.409 O  1

2.411 O  7	2.417 O  10	3.351 O  21	3.359 O  18

3.765 O  30

3.375 Si 8	3.398 Si 5	3.422 Si 1	3.423 Si 4

3.592 Si 9

Ca 6

3.616 Ca 1	3.647 Ca 2	3.696 Ca 3	3.739 Ca 7

3.739 Ca 5	3.796 Ca 4

2.305 O  4	2.377 O  11	2.400 O  9	2.407 O  14

2.414 O  8	2.458 O  2	3.335 O  22	3.337 O  19

3.711 O  31

3.362 Si 9	3.365 Si 6	3.423 Si 4	3.435 Si 2

3.581 Si 10

Ca 7

3.632 Ca 1	3.640 Ca 3	3.691 Ca 4	3.732 Ca 5

3.739 Ca 6	3.794 Ca 2

2.283 O  5	2.389 O  9	2.404 O  14	2.412 O  3

2.415 O  7	2.428 O  12	3.268 O  23	3.351 O  20

3.820 O  29

3.337 Si 10	3.380 Si 7	3.413 Si 4	3.416 Si 3

3.639 Si 8

Ca10 Si18 O46 (H2O)18, Okenite, [P-1]

Merlino 1983

American Mineralogist 68 (1983) P. 614-622

Ca 1

3.526 Ca 2	3.646 Ca 4	3.669 Ca 4	3.678 Ca 3

2.321 O  3	2.337 O  6	2.382 O  4	2.386 O  2

2.410 O  5	2.413 O  1	3.526 O  18	3.691 O  25

3.811 O  13	3.821 O  13	3.869 O  9

3.296 Si 7	3.493 Si 4	3.537 Si 2	3.567 Si 1

3.579 Si 6

Ca 2

3.526 Ca 1	3.636 Ca 3	3.646 Ca 3	3.703 Ca 4

2.244 O  10	2.267 O  9	2.372 O  2	2.395 O  1

2.420 O  11	2.478 O  7	3.322 O  16	3.363 O  17

3.380 O  16

3.338 Si 2	3.385 Si 5	3.395 Si 3	3.414 Si 4

3.415 Si 3

Ca 3

3.636 Ca 2	3.646 Ca 2	3.678 Ca 1	3.683 Ca 4

2.299 O  10	2.306 O  9	2.334 O  12	2.445 O  1

2.490 O  5	2.528 O  7	3.385 O  15	3.482 O  15

3.669 O  19	3.820 O  20

3.364 Si 9	3.386 Si 1	3.422 Si 3	3.441 Si 3

3.581 Si 4	3.792 Si 5

Ca 4

3.646 Ca 1	3.669 Ca 1	3.683 Ca 3	3.703 Ca 2

2.278 O  8	2.313 O  4	2.378 O  6	2.405 O  7

2.440 O  2	2.464 O  5	3.622 O  21	3.764 O  14

3.990 O  24

3.458 Si 5	3.511 Si 6	3.563 Si 1	3.602 Si 2

3.718 Si 7

CaZrO3, [PM3-M]

Rabenau 1956

Zeitschrift fuer Anorganische und Allgemeine Chemie 288 (1956) P. 221-234

Ca 1

2.843 O  1	2.843 O  1	2.843 O  1	2.843 O  1

2.843 O  1	2.843 O  1	2.843 O  1	2.843 O  1

2.843 O  1	2.843 O  1	2.843 O  1	2.843 O  1

3.481 Zr 1	3.481 Zr 1	3.481 Zr 1	3.481 Zr 1

3.481 Zr 1	3.481 Zr 1	3.481 Zr 1	3.481 Zr 1

[PCMN]

Koopmans 1983

Acta Crystallographica C (1983) P. 1323-1325

Ca 1

3.921 Ca 1	3.921 Ca 1

2.341 O  1	2.362 O  2	2.362 O  2	2.461 O  1

2.680 O  2	2.680 O  2	2.844 O  2	2.844 O  2

3.343 O  1	3.447 O  1	3.625 O  2	3.625 O  2

3.280 Zr 1	3.280 Zr 1	3.397 Zr 1	3.397 Zr 1

3.507 Zr 1	3.507 Zr 1	3.748 Zr 1	3.748 Zr 1

CaAl4O7, Grossite, [C12/C1]

Ponomarev 1970

Kristallografiya 15 (1970) P. 1140-1143

Ca 1

3.206 Al 1	3.206 Al 1	3.275 Al 1	3.275 Al 1

3.477 Al 2	3.477 Al 2	3.618 Al 2	3.618 Al 2

3.774 Al 1	3.774 Al 1

2.332 O  3	2.332 O  3	2.370 O  2	2.370 O  2

2.457 O  1	2.872 O  2	2.872 O  2	3.653 O  4

3.653 O  4

Ca 1

3.205 Al 1	3.205 Al 1	3.275 Al 1	3.275 Al 1

3.477 Al 2	3.477 Al 2	3.618 Al 2	3.618 Al 2

3.773 Al 1	3.773 Al 1

2.331 O  3	2.331 O  3	2.370 O  2	2.370 O  2

2.457 O  1	2.872 O  2	2.872 O  2	3.653 O  4

3.653 O  4

Goodwin 1970

Acta Crystallographica B 26 (1970) P. 1230-1235

Ca 1

3.197 Al 1	3.197 Al 1	3.263 Al 1	3.263 Al 1

3.464 Al 2	3.464 Al 2	3.616 Al 2	3.616 Al 2

3.761 Al 1	3.761 Al 1

2.330 O  3	2.330 O  3	2.364 O  2	2.364 O  2

2.535 O  1	2.876 O  2	2.876 O  2	3.646 O  4

3.646 O  4

CaTiO3, Pervoskite, [Pcmn]

Kay 1957

Acta Crystallographica 10 (1957) P. 219-226

Ca 1

3.822 Ca 1	3.822 Ca 1	3.822 Ca 1	3.822 Ca 1

3.836 Ca 1	3.836 Ca 1

2.469 O  1	2.499 O  1	2.553 O  2	2.553 O  2

2.584 O  2	2.584 O  2	2.685 O  2	2.685 O  2

2.894 O  1	2.990 O  1	3.025 O  2	3.025 O  2

3.193 Ti 1	3.193 Ti 1	3.298 Ti 1	3.298 Ti 1

3.298 Ti 1	3.298 Ti 1	3.461 Ti 1	3.461 Ti 1

Koopmanns 1983

Acta Crystallographica C 39 (1983) P. 1323-1325

Ca 1

3.766 Ca 1	3.766 Ca 1	3.844 Ca 1	3.844 Ca 1

3.892 Ca 1	3.892 Ca 1

2.363 O  1	2.379 O  2	2.379 O  2	2.471 O  1

2.614 O  2	2.614 O  2	2.667 O  2	2.667 O  2

3.044 O  1	3.051 O  1	3.240 O  2	3.240 O  2

3.169 Ti 1	3.169 Ti 1	3.271 Ti 1	3.271 Ti 1

3.343 Ti 1	3.343 Ti 1	3.489 Ti 1	3.489 Ti 1

[Pbmn]

Sasaki 1987

Acta Crystallographica C 43 (1987) P. 1668-1674

Ca 1

3.775 Ca 1	3.775 Ca 1	3.841 Ca 1	3.841 Ca 1

3.878 Ca 1	3.878 Ca 1

2.359 O  1	2.379 O  2	2.379 O  2	2.473 O  1

2.617 O  2	2.617 O  2	2.663 O  2	2.663 O  2

3.035 O  1	3.051 O  1	3.236 O  2	3.236 O  2

3.166 Ti 1	3.166 Ti 1	3.275 Ti 1	3.275 Ti 1

3.334 Ti 1	3.334 Ti 1	3.487 Ti 1	3.487 Ti 1

CaHPO4, Monetite, [P-1]

Catti 1977

Acta Crystallographica B 33 (1977) P. 1223-1229

Ca 1

3.767 Ca 1	3.838 Ca 2	3.897 Ca 2	3.986 Ca 2

2.882 H  2	2.893 H  3	3.399 H  2	3.404 H  3

3.656 H  1

2.292 O  4	2.370 O  8	2.419 O  1	2.424 O  2

2.447 O  2	2.447 O  6	2.764 O  7	3.359 O  3

3.411 O  5	3.750 O  1	3.782 O  4	3.801 O  8

3.918 O  5

3.240 P  2	3.397 P  1	3.447 P  2	3.659 P  1

3.673 P  1	3.737 P  1

Ca 2

3.749 Ca 2	3.838 Ca 1	3.897 Ca 1	3.986 Ca 1

2.484 H  3	2.967 H  1	3.314 H  2	3.586 H  2

3.710 H  3

2.373 O  3	2.434 O  5	2.478 O  8	2.481 O  4

2.485 O  3	2.502 O  7	2.518 O  6	2.575 O  2

3.586 O  4	3.646 O  1	3.790 O  7	3.903 O  7

3.965 O  8

3.097 P  1	3.513 P  1	3.576 P  1	3.645 P  2

3.674 P  2	3.782 P  2	3.835 P  2

Dickens 1972

Acta Crystallographica B 28 (1972) P. 797-806

Ca 1

3.762 Ca 1	3.836 Ca 2	3.897 Ca 2	3.979 Ca 2

2.297 O  4	2.363 O  8	2.414 O  1	2.449 O  6

2.460 O  2	2.530 O  2	2.764 O  7	3.347 O  3

3.427 O  5	3.762 O  1	3.790 O  4	3.799 O  8

3.910 O  5

3.238 P  2	3.395 P  1	3.450 P  2	3.664 P  1

3.674 P  1	3.737 P  1

Ca 2

3.742 Ca 2	3.836 Ca 1	3.897 Ca 1	3.979 Ca 1

2.375 O  3	2.433 O  5	2.478 O  3	2.479 O  4

2.483 O  8	2.510 O  7	2.518 O  6	2.520 O  2

3.586 O  4	3.650 O  1	3.796 O  7	3.890 O  7

3.973 O  8

3.101 P  1	3.513 P  1	3.575 P  1	3.633 P  2

3.682 P  2	3.787 P  2	3.838 P  2

Jones 1961

Zeitschrift fuer Kristallographie, Kristallgeometrie, Kristallphysik, Kristallchemie 116 (1961) P. 101-125

Acta Crystallographica 8 (1955) P. 579-583

Ca 1

3.765 Ca 1	3.847 Ca 2	3.873 Ca 2	3.994 Ca 2

2.281 O  4	2.359 O  8	2.415 O  2	2.425 O  1

2.456 O  2	2.458 O  6	2.771 O  7	3.357 O  3

3.405 O  5	3.732 O  1	3.787 O  4	3.819 O  8

3.918 O  5

3.238 P  2	3.388 P  1	3.470 P  2	3.664 P  1

3.665 P  1	3.743 P  1

Ca 2

3.771 Ca 2	3.847 Ca 1	3.873 Ca 1	3.994 Ca 1

2.408 O  3	2.421 O  5	2.463 O  3	2.476 O  4

2.487 O  7	2.504 O  8	2.515 O  6	2.584 O  2

3.573 O  4	3.679 O  1	3.801 O  7	3.906 O  7

3.985 O  1	3.993 O  8

3.097 P  1	3.496 P  1	3.598 P  1	3.644 P  2

3.683 P  2	3.786 P  2	3.823 P  2

CaH2PO4(H2O), [P-1]

Schroeder 1975

Acta Crystallographica B 31 (1975) P. 9-12

Ca 1

3.934 Ca 1	3.968 Ca 1

2.897 H  6	3.182 H  5	3.259 H  1	3.360 H  2

3.428 H  1	3.489 H  2

2.317 O  1	2.327 O  2	2.397 O  5	2.480 O  9

2.523 O  2	2.540 O  1	2.621 O  3	2.633 O  4

3.773 O  7

3.235 P  1	3.240 P  1	3.649 P  2	3.661 P  1

3.671 P  1

Dickens 1973

Acta Crystallographica B 29 (1973) P. 2057-2070

Ca 1

3.771 Ca 1	3.853 Ca 1

3.221 H  3	3.415 H  2	3.572 H  2	3.710 H  3

3.994 H  5

2.346 O  2	2.379 O  1	2.426 O  5	2.429 O  7

2.433 O  1	2.483 O  5	2.671 O  4	2.831 O  6

3.609 O  6	3.771 O  1	3.956 O  5	3.981 O  7

3.204 P  1	3.521 P  1	3.536 P  2	3.576 P  2

3.618 P  2	3.653 P  1

Jones 1961

Zeitschrift fuer Kristallographie, Kristallgeometrie, Kristallphysik, Kristallchemie 116 (1961) P. 101-125

Acta Crystallographica 11 (1958) P. 273-277

Acta Crystallographica 9 (1956) P. 187-190

Ca 1

3.910 Ca 1	3.978 Ca 1

2.230 O  1	2.343 O  2	2.407 O  5	2.494 O  1

2.520 O  2	2.536 O  9	2.695 O  4	2.757 O  3

3.759 O  7

3.224 P  1	3.260 P  1	3.651 P  2	3.658 P  1

3.674 P  1

CaWO4, Scheelite, [I41/AZ]

Zalkin 1964

Journal of Chemical Physics 40 (1964) P. 501-504

Ca 1

3.868 Ca 1	3.868 Ca 1	3.868 Ca 1	3.868 Ca 1

2.436 O  1	2.436 O  1	2.436 O  1	2.436 O  1

2.481 O  1	2.481 O  1	2.481 O  1	2.481 O  1

3.798 O  1	3.798 O  1	3.798 O  1	3.798 O  1

3.707 W  1	3.707 W  1	3.707 W  1	3.707 W  1

3.868 W  1	3.868 W  1	3.868 W  1	3.868 W  1

Kay 1964

Journal of Chemical Physics 40 (1964) P. 504-506

Ca 1

3.868 Ca 1	3.868 Ca 1	3.868 Ca 1	3.868 Ca 1

2.438 O  1	2.438 O  1	2.438 O  1	2.438 O  1

2.479 O  1	2.479 O  1	2.479 O  1	2.479 O  1

3.802 O  1	3.802 O  1	3.802 O  1	3.802 O  1

3.707 W  1	3.707 W  1	3.707 W  1	3.707 W  1

3.868 W  1	3.868 W  1	3.868 W  1	3.868 W  1

Burbank 1965

Acta Crystallographica 18 (1965) P. 88-97

Ca 1

3.867 Ca 1	3.867 Ca 1	3.867 Ca 1	3.867 Ca 1

2.449 O  1	2.449 O  1	2.449 O  1	2.449 O  1

2.480 O  1	2.480 O  1	2.480 O  1	2.480 O  1

3.792 O  1	3.792 O  1	3.792 O  1	3.792 O  1

3.707 W  1	3.707 W  1	3.707 W  1	3.707 W  1

3.867 W  1	3.867 W  1	3.867 W  1	3.867 W  1

CaSiO3, Pseudowollastonite, [C-1]

Yamanaka 1981

Acta Crystallographica B 37 (1981) P. 1010-1017

Ca 1

3.876 Ca 2	3.876 Ca 2	3.994 Ca 2	3.994 Ca 2

2.407 O  2	2.407 O  2	2.572 O  1	2.572 O  1

2.603 O  14	2.603 O  14	2.678 O  3	2.678 O  3

3.222 Si 1	3.222 Si 1	3.282 Si 3	3.282 Si 3

3.669 Si 2	3.669 Si 2

Ca 2

3.853 Ca 2	3.876 Ca 1	3.912 Ca 2	3.994 Ca 1

2.279 O  3	2.279 O  1	2.572 O  13	2.593 O  3

2.597 O  15	2.636 O  1	2.677 O  2	2.715 O  2

3.223 Si 2	3.234 Si 3	3.238 Si 1	3.248 Si 2

3.678 Si 1	3.723 Si 3

Ca 3

3.856 Ca 5	3.877 Ca 4	3.880 Ca 4

2.299 O  5	2.308 O  9	2.566 O  8	2.569 O  16

2.572 O  14	2.578 O  4	2.634 O  7	2.640 O  6

3.196 Si 5	3.206 Si 1	3.231 Si 4	3.243 Si 3

3.726 Si 2	3.733 Si 6

Ca 4

3.877 Ca 3	3.880 Ca 3	3.909 Ca 5	3.986 Ca 5

3.988 Ca 5

2.271 O  4	2.276 O  8	2.592 O  15	2.595 O  17

2.613 O  6	2.617 O  7	2.661 O  9	2.675 O  5

3.231 Si 3	3.238 Si 4	3.271 Si 2	3.271 Si 6

3.672 Si 5	3.678 Si 1

Ca 5

3.856 Ca 3	3.909 Ca 4	3.986 Ca 4	3.988 Ca 4

2.310 O  7	2.319 O  6	2.589 O  9	2.595 O  18

2.604 O  5	2.610 O  13	2.663 O  4	2.667 O  8

3.241 Si 6	3.245 Si 2	3.259 Si 1	3.265 Si 5

3.658 Si 4	3.670 Si 3

Ca 6

3.877 Ca 7	3.877 Ca 7	3.994 Ca 7	3.994 Ca 7

2.312 O  12	2.312 O  12	2.592 O  11	2.592 O  11

2.602 O  16	2.602 O  16	2.699 O  10	2.699 O  10

3.226 Si 5	3.226 Si 5	3.292 Si 4	3.292 Si 4

3.664 Si 6	3.664 Si 6

Ca 7

3.854 Ca 7	3.877 Ca 6	3.912 Ca 7	3.994 Ca 6

2.296 O  11	2.300 O  10	2.585 O  17	2.586 O  18

2.599 O  10	2.617 O  12	2.642 O  11	2.650 O  12

3.226 Si 6	3.231 Si 4	3.238 Si 5	3.247 Si 6

3.687 Si 5	3.724 Si 4

[C12/C1]

Yang 1999

American Mineralogist 84 (1999) P. 1902-1905

Ca 1

3.851 Ca 1	3.876 Ca 2	3.892 Ca 1	3.992 Ca 2

3.992 Ca 2

2.282 O  2	2.282 O  4	2.573 O  3	2.577 O  5

2.609 O  4	2.619 O  2	2.621 O  1	2.622 O  1

3.214 Si 2	3.231 Si 1	3.232 Si 1	3.237 Si 1

3.677 Si 2	3.720 Si 1

Ca 2

3.876 Ca 1	3.876 Ca 1	3.992 Ca 1	3.992 Ca 1

3.992 Ca 1	3.992 Ca 1

2.308 O  1	2.308 O  1	2.591 O  4	2.591 O  4

2.598 O  3	2.598 O  3	2.660 O  2	2.660 O  2

3.228 Si 2	3.228 Si 2	3.265 Si 1	3.265 Si 1

3.655 Si 1	3.655 Si 1

CaCO3, Aragonite, [R-3C]

Maslen 1995

Acta Crystallographica B 51 (1995) P. 929-939

Ca 1

3.212 C  1	3.212 C  1	3.212 C  1	3.212 C  1

3.212 C  1	3.212 C  1

2.359 O  1	2.359 O  1	2.359 O  1	2.359 O  1

2.359 O  1	2.359 O  1	3.458 O  1	3.458 O  1

3.458 O  1	3.458 O  1	3.458 O  1	3.458 O  1

Wartchow 1989

Zeitschrift fuer Kristallographie 186 (1989) P. 300-302

Ca 1

3.212 C  1	3.212 C  1	3.212 C  1	3.212 C  1

3.212 C  1	3.212 C  1

2.359 O  1	2.359 O  1	2.359 O  1	2.359 O  1

2.359 O  1	2.359 O  1	3.458 O  1	3.458 O  1

3.458 O  1	3.458 O  1	3.458 O  1	3.458 O  1

[C121]

Smyth 1997

Geophysical Research Letters 24 ISSUE 13 (1997) P. 1595-1598

American Mineralogist 79 (1994) P. 15-23

Ca 1

3.073 C  2	3.073 C  2	3.112 C  2	3.112 C  2

3.220 C  2	3.220 C  2

3.755 Ca 2	3.755 Ca 2	3.853 Ca 2	3.853 Ca 2

2.263 O  3	2.263 O  3	2.379 O  5	2.379 O  5

2.435 O  4	2.435 O  4	3.142 O  5	3.142 O  5

3.259 O  4	3.259 O  4	3.474 O  3	3.474 O  3

Ca 2

3.072 C  1	3.100 C  2	3.132 C  2	3.150 C  1

3.160 C  2	3.174 C  1

3.755 Ca 1	3.853 Ca 1	3.859 Ca 2	3.859 Ca 2

2.180 O  3	2.185 O  5	2.192 O  4	2.286 O  1

2.291 O  2	2.295 O  2	3.236 O  2	3.386 O  3

3.439 O  1	3.460 O  2	3.546 O  4	3.571 O  5

CaO, Lime, [FM-3M]

Huang 1994

Physica C 227 (1994) P. 1-9

Ca 1

3.398 Ca 1	3.398 Ca 1	3.398 Ca 1	3.398 Ca 1

3.398 Ca 1	3.398 Ca 1	3.398 Ca 1	3.398 Ca 1

3.398 Ca 1	3.398 Ca 1	3.398 Ca 1	3.398 Ca 1

2.402 O  1	2.402 O  1	2.402 O  1	2.402 O  1

2.402 O  1	2.402 O  1

Jay 1946

Nature 154 (1944) P. 116-116

Ca 1

3.400 Ca 1	3.400 Ca 1	3.400 Ca 1	3.400 Ca 1

3.400 Ca 1	3.400 Ca 1	3.400 Ca 1	3.400 Ca 1

3.400 Ca 1	3.400 Ca 1	3.400 Ca 1	3.400 Ca 1

2.404 O  1	2.404 O  1	2.404 O  1	2.404 O  1

2.404 O  1	2.404 O  1

Primak 1948

Journal of the American Chemical Society 70 (1948) P. 2043-2046

Ca 1

3.393 Ca 1	3.393 Ca 1	3.393 Ca 1	3.393 Ca 1

3.393 Ca 1	3.393 Ca 1	3.393 Ca 1	3.393 Ca 1

3.393 Ca 1	3.393 Ca 1	3.393 Ca 1	3.393 Ca 1

2.399 O  1	2.399 O  1	2.399 O  1	2.399 O  1

2.399 O  1	2.399 O  1

Ca(OH)2, Portlandite, [P-3M1]

Henderson 1962

American Mineralogist 47 (1962) P. 1231-1251

Ca 1

3.585 Ca 1	3.585 Ca 1	3.585 Ca 1	3.585 Ca 1

3.585 Ca 1	3.585 Ca 1

2.361 O  1	2.361 O  1	2.361 O  1	2.361 O  1

2.361 O  1	2.361 O  1

Desgranges 1993

Acta Crystallographica B 49 (1993) P. 812-817

Ca 1

3.589 Ca 1	3.589 Ca 1	3.589 Ca 1	3.589 Ca 1

3.589 Ca 1	3.589 Ca 1

2.369 O  1	2.369 O  1	2.369 O  1	2.369 O  1

2.369 O  1	2.369 O  1

Greaves 1986

Acta Crystallographica B 42 (1986) P. 51-55

Journal of Chemical Physics 26 (1957) P. 563-568

Ca 1

3.592 Ca 1	3.592 Ca 1	3.592 Ca 1	3.592 Ca 1

3.592 Ca 1	3.592 Ca 1

2.370 O  1	2.370 O  1	2.371 O  1	2.371 O  1

2.371 O  1	2.371 O  1

CaAl12O19, [P63/MMC]

Utsunomiya 1988

Journal of Solid State Chemistry 75 (1988) P. 197-200

Ca 1

3.213 Al 2	3.213 Al 2	3.214 Al 2	3.214 Al 2

3.214 Al 2	3.214 Al 2	3.459 Al 4	3.459 Al 4

3.459 Al 4	3.459 Al 4	3.460 Al 4	3.460 Al 4

3.468 Al 5	3.468 Al 5	3.468 Al 5	3.468 Al 5

3.468 Al 5	3.468 Al 5

2.712 O  5	2.712 O  5	2.712 O  5	2.712 O  5

2.712 O  5	2.712 O  5	2.783 O  3	2.783 O  3

2.783 O  3	2.783 O  3	2.783 O  3	2.783 O  3

3.896 O  1	3.896 O  1	3.897 O  1	3.897 O  1

3.897 O  1	3.897 O  1

Hydroxylapatite

[P63/M]

Ca10(PO4)6(OH)2

Posner 1958

Acta Crystallographica 11 (1958) P. 308-309

Ca 1

3.427 Ca 1	3.454 Ca 1	3.952 Ca 2	3.953 Ca 2

3.953 Ca 2

2.415 O  1	2.416 O  1	2.416 O  1	2.450 O  2

2.450 O  2	2.450 O  2	2.770 O  3	2.771 O  3

2.771 O  3	3.947 O  3	3.947 O  3	3.948 O  3

3.204 P  1	3.204 P  1	3.205 P  1	3.602 P  1

3.603 P  1	3.603 P  1

Ca 2

3.952 Ca 1	3.952 Ca 1

2.354 O  4	2.356 O  2	2.377 O  3	2.377 O  3

2.508 O  3	2.508 O  3	2.712 O  1	3.413 O  3

3.413 O  3	3.463 O  1	3.973 O  1	3.973 O  1

3.992 O  2

3.088 P  1	3.299 P  1	3.466 P  1	3.674 P  1

3.674 P  1

Ca5(PO4)3(OH)

Kay 1964

Nature 204 (1964) P. 1050-1052

Ca 1

3.421 Ca 1	3.460 Ca 1	3.948 Ca 2	3.949 Ca 2

3.949 Ca 2

2.407 O  1	2.407 O  1	2.408 O  1	2.454 O  2

2.454 O  2	2.455 O  2	2.807 O  3	2.808 O  3

2.808 O  3	3.932 O  3	3.932 O  3	3.933 O  3

3.216 P  1	3.216 P  1	3.217 P  1	3.598 P  1

3.598 P  1	3.599 P  1

Ca 2

3.948 Ca 1	3.948 Ca 1

2.692 H  1	2.692 H  1	3.188 H  1	3.188 H  1

2.346 O  3	2.346 O  3	2.358 O  2	2.383 O  4

2.383 O  4	2.513 O  3	2.513 O  3	2.708 O  1

3.386 O  3	3.386 O  3	3.462 O  1	3.897 O  4

3.897 O  4	3.974 O  1	3.974 O  1	3.981 O  2

3.083 P  1	3.286 P  1	3.472 P  1	3.667 P  1

3.667 P  1

Hughes 1989

American Mineralogist 74 (1989) P. 870-876

Ca 1

3.417 Ca 1	3.457 Ca 1	3.943 Ca 2	3.943 Ca 2

3.943 Ca 2

2.403 O  1	2.403 O  1	2.404 O  1	2.452 O  2

2.452 O  2	2.452 O  2	2.801 O  3	2.802 O  3

2.802 O  3	3.925 O  3	3.926 O  3	3.926 O  3

3.210 P  1	3.210 P  1	3.211 P  1	3.592 P  1

3.592 P  1	3.592 P  1

Ca 2

3.943 Ca 1	3.943 Ca 1

2.765 H  1	2.765 H  1	3.088 H  1	3.088 H  1

2.343 O  3	2.343 O  3	2.353 O  2	2.385 O  4

2.385 O  4	2.509 O  3	2.509 O  3	2.710 O  1

3.386 O  3	3.386 O  3	3.450 O  1	3.878 O  4

3.878 O  4	3.968 O  2	3.969 O  1	3.969 O  1

3.078 P  1	3.287 P  1	3.460 P  1	3.664 P  1

3.664 P  1

Calcium Acetate Monohydrate, [P-1]

Klop 1984

Acta Cryst. C 1984, 40, 51

Ca1

2.270 O  5	2.321 O  4	2.396 O  1	2.399 O  8

2.477 O  1	2.496 O  2	2.728 O  2	2.933 O  2

Ca2

2.301 O  8	2.348 O  7	2.360 O  9	2.368 O  10

2.490 O  3	2.503 O  2	2.460 O  4

Ca1

3.905 Ca 1	3.950 Ca 2	3.958 Ca 2

Ca(NO3)2.4H2O Nitrocalcite, [P121/n1]

Leclaire A

Acta Crystallographica B  33 (1977) P. 1861-1866

Ca 1

2.673 H  4	2.823 H  7	2.854 H  1	2.859 H  3

2.882 H  8	2.904 H  6	2.911 H  5	2.971 H  2

2.975 H  9	3.590 H  5	3.896 H  2	3.921 H  4

2.946 N  1	3.111 N  2	3.501 N  2

2.426 O  8	2.436 O  7	2.443 O  9	2.460 O  10

2.490 O  1	2.514 O  4	2.520 O  4	2.580 O  2

2.838 O  6	3.732 O  5

Ribar B

Acta Crystallographica B 29 (1973) P. 1546-1548

Ca 1

2.950 N  2	3.109 N  1	3.513 N  1

2.413 O  8	2.441 O  9	2.448 O  7	2.474 O  10

2.478 O  6	2.520 O  2	2.525 O  2	2.562 O  4

2.852 O  1	3.743 O  3

Ribar (Neutron Study)

Ca 1

2.951 H  6	2.963 H  1	3.004 H  3	3.014 H  8

3.041 H  4	3.054 H  2	3.093 H  7	3.113 H  5

3.621 H  4	3.758 H  2

2.984 N  2	3.082 N  1	3.516 N  1

2.444 O  8	2.473 O  7	2.477 O  9	2.479 O  2

2.499 O  10	2.514 O  2	2.518 O  6	2.599 O  4

2.826 O  1	3.751 O  3